Original Research Article

Advances and Future Perspectives of Zeolite Materials: Bridging Structure–Function Relationships for Environmental and Industrial Applications

ABSTRACT

Zeolites, owing to their unique microporous structures, high thermal stability, and remarkable ion-exchange capabilities, have long served as versatile materials across environmental, catalytic, and industrial sectors. However, the current research landscape remains fragmented, often isolating structure–function relationships within narrow application domains. This review offers a critical and integrative synthesis of recent advances in zeolite science, focusing on how structural engineering strategies—such as hierarchical pore design, surface functionalization, and ion-exchange tuning—enhance application-specific performance. Emphasis is placed on the role of structural modifications in overcoming mass transport limitations, improving adsorption selectivity, and facilitating catalytic activity for sustainable technologies. Applications discussed include heavy metal removal, ammonium recovery, volatile organic compound (VOC) mitigation, and carbon dioxide capture, with additional insights into emerging areas such as solid waste stabilization and resource recovery. By bridging structural features with multifunctional applications, this review not only identifies current gaps in the literature but also maps future directions for the rational design of next-generation zeolitic materials. The findings highlight the pivotal role of engineered zeolites in addressing global challenges in environmental protection, energy transition, and sustainable development

Keyword: Zeolite, Structure–Function Relationship, Hierarchical Pore Engineering, Environmental Applications, Catalysis

- INTODUCTION

Zeolites are a unique class of crystalline aluminosilicates characterized by their well-defined microporous structures, high thermal stability, and remarkable ion-exchange and adsorption capacities (Kordala & Wyszkowski, 2024). Naturally occurring and synthetic zeolites have attracted substantial scientific and industrial interest due to their versatile functionalities across a wide range of applications, including environmental remediation, catalysis, energy storage, and water purification. The intrinsic properties of zeolites—such as their large surface areas, tunable pore sizes, framework flexibility, and chemical robustness—render them highly suitable for addressing pressing global challenges related to sustainable development and green technologies  (Y. Li & Yu, 2021a; Ristanović et al., 2013; Wu et al., 2019). In recent decades, the strategic utilization of zeolitic materials has expanded beyond traditional uses, finding novel roles in emerging fields such as carbon capture, biomedical applications, and smart catalysis systems (Valencia, 2021; Weckhuysen & Yu, 2015; Xu & Wu, 2022). This evolving landscape underlines the critical importance of zeolites as multifunctional materials that can bridge gaps between material science innovations and practical environmental and industrial solutions (Bacakova et al., 2018; Lü et al., 2024; Yu & Zhao, 2022a).

Despite the remarkable progress in zeolite research, the current literature remains notably fragmented, with most reviews concentrating narrowly on isolated application domains such as heavy metal adsorption, petrochemical catalysis, or wastewater treatment. While such compartmentalized approaches have yielded important insights into specific functionalities, they fail to present a holistic view of how the fundamental structure–property relationships in zeolites govern their multifunctional performance across diverse sectors (Kordala & Wyszkowski, 2024). Moreover, significant advancements in zeolite engineering—encompassing hierarchical porosity design, ion-exchange optimization, surface functionalization, and hybrid composite development—have yet to be critically synthesized within an integrated framework. The lack of comprehensive analysis connecting these structural innovations to emerging applications, particularly those aligned with sustainability imperatives, leaves a substantial gap in the scientific understanding necessary to propel zeolite-based technologies forward. Addressing this gap is essential not only for maximizing the potential of zeolitic materials but also for strategically guiding future research and industrial deployment (Huang et al., 2024).

In contrast to previous reviews that have predominantly emphasized either the traditional roles or isolated applications of zeolites, the present work offers a critical and integrative perspective that bridges structural characteristics with multifunctional applications across environmental, energy, and industrial sectors(Xue & Yang, 2021). By systematically synthesizing recent developments in zeolite modification strategies—such as hierarchical pore engineering, ion-exchange optimization, and hybrid material formation—this review highlights how structural tailoring directly influences application-specific performance. Furthermore, the article contextualizes these advances within the framework of sustainable development, mapping out the emerging roles of zeolites in carbon capture, green catalysis, and resource recovery initiatives (Y. Li & Yu, 2021a). Such a holistic approach not only deepens the understanding of structure–function–application relationships but also identifies new frontiers where zeolitic materials can be strategically positioned to address global sustainability challenges (Kumari et al., 2024).

This review aims to provide a comprehensive and critical synthesis of recent advancements in zeolite research, with a particular focus on elucidating the relationships between structural modifications and multifunctional applications. By integrating insights across environmental remediation, catalysis, energy storage, and industrial processes, the article seeks to bridge the existing disciplinary divides and offer a unified framework for understanding zeolite functionality. Additionally, this review endeavors to identify current challenges, emerging trends, and prospective research directions that could guide the rational design of next-generation zeolitic materials. Through this systematic approach, the review aspires to serve not only as a reference point for researchers and practitioners but also as a strategic roadmap for advancing the sustainable and innovative deployment of zeolite-based technologies.

Given the accelerating demand for sustainable technologies and advanced functional materials, a comprehensive and integrative understanding of zeolite systems has become increasingly critical. Zeolites, with their tunable structures and exceptional physicochemical properties, are poised to address a spectrum of global challenges ranging from environmental pollution to renewable energy production. However, the fragmented nature of existing research impedes the optimization and large-scale application of zeolitic materials. By offering a critical synthesis that links structure, property, and application, this review fills a significant gap in the current literature and provides essential insights for both academic research and industrial innovation. Furthermore, aligning the discussion with the imperatives of the Sustainable Development Goals (SDGs) enhances the relevance of zeolite research in contributing to a greener and more resilient future. Thus, this review is not only timely but also strategically positioned to catalyze future advancements in material science, environmental engineering, and sustainable technology development.

- Fundamentals of Zeolite Structures

Zeolites are crystalline aluminosilicates distinguished by their highly ordered three-dimensional frameworks composed of SiO₄ and AlO₄ tetrahedra linked through shared oxygen atoms (Boer et al., 2023; J. Li et al., 2022)(dina,23). This intricate framework generates a system of uniform micropores and interconnected channels, imparting zeolites with exceptionally high surface areas, tunable pore sizes, and remarkable selective adsorption properties. The substitution of Si⁴⁺ by Al³⁺ within the framework introduces a net negative charge, which is compensated by the presence of exchangeable extra-framework cations such as Na⁺, K⁺, or Ca²⁺ (Kordala & Wyszkowski, 2024; J. Li et al., 2022). These unique features underpin the diverse range of functional applications for zeolites, spanning from catalysis and adsorption to ion-exchange and separation processes. A thorough understanding of their chemical composition, pore topology, and cation distribution is fundamental for the rational design and optimization of zeolite-based materials for targeted applications (Bacakova et al., 2018; Tang et al., 2008).

- Chemical Composition of Zeolites

The chemical composition of zeolites primarily consists of silicon and aluminum atoms tetrahedrally coordinated by oxygen atoms, forming an extensive three-dimensional network. Variations in the Si/Al ratio significantly affect the physicochemical properties of zeolites, including hydrophobicity, acidity, thermal stability, and ion-exchange capacity (J. Li et al., 2022; Rajaei et al., 2021). Zeolites with high silica content (Si/Al > 10) exhibit enhanced hydrophobicity and thermal resistance, making them ideal for hydrocarbon processing and organic pollutant adsorption under harsh conditions. Conversely, low-silica zeolites (Si/Al ~1) possess higher ion-exchange capacities, favoring their use in water softening, heavy metal removal, and other aqueous applications (S. Lee et al., 2024; Y. Li & Yu, 2021a; Xu & Wu, 2022). Furthermore, the presence and type of extra-framework cations not only stabilize the structure but also influence the electronic environment of the framework, thereby affecting catalytic activity. Understanding these compositional nuances enables the strategic selection or modification of zeolites to enhance their performance in specific environmental and industrial settings.

- Pore Topology and Structural Frameworks

The pore topology of zeolites—defined by the size, shape, and connectivity of the internal cavities and channels—plays a critical role in determining their functional properties. Zeolite frameworks are classified into distinct types such as MFI, FAU, LTA, MOR, and BEA, each characterized by unique pore systems cataloged by the International Zeolite Association (IZA). Pore sizes typically fall within the microporous range (<2 nm), although hierarchical zeolites exhibiting mesoporous features (2–50 nm) have been engineered to overcome diffusion limitations (Y. Li & Yu, 2021a; Moller & Bein, 2013). Three-dimensional channel systems, as seen in FAU and MFI types, facilitate high molecular accessibility and are advantageous for catalytic and adsorption processes involving bulky molecules. In contrast, one-dimensional channels, such as those in mordenite (MOR), offer enhanced shape-selectivity but may suffer from diffusion constraints (Pérez-Ramírez et al., 2008). Tailoring the pore structure through synthetic strategies, such as templating or post-synthetic modification, allows for fine-tuning zeolite performance toward specific separation and catalytic applications. Table 1 summarizes key zeolite frameworks, their characteristic pore sizes, channel dimensionalities, and typical application domains (Davis, 1993; Jiang et al., 2010; Z. Liu et al., 2020; Paillaud et al., 2004; Tang et al., 2008).

Table 1. Zeolite Frameworks: Pore Size, Channel System, and Applications

| Framework Type | Pore Size (Å) | Channel System | Typical Applications |
| --- | --- | --- | --- |
| LTA (Zeolite A) | ~4.1 | 3D | Water softening, gas separation (CO₂, O₂/N₂) |
| FAU (Zeolite X/Y) | ~7.4 | 3D | Catalysis (FCC), adsorption of large organics |
| MFI (ZSM-5) | ~5.5–5.6 | 3D | Shape-selective catalysis, hydrocarbon isomerization |
| MOR (Mordenite) | ~6.5 × 7.0 and 2.6 × 5.7 | 1D | Aromatic adsorption, alcohol dehydration |
| BEA (Beta Zeolite) | ~6.6 × 6.7 | 3D | Biomass conversion, fine chemical synthesis |
| FER (Ferrierite) | ~4.2 × 5.4 and 3.5 × 4.8 | 2D | Olefin skeletal isomerization, gas separations |

- Cation Distribution and Ion-Exchange Properties

Beyond their framework architecture, the location and nature of extra-framework cations critically influence the functional behavior of zeolites, particularly in ion-exchange and catalytic applications (Lü et al., 2024). Cations are positioned within the channels and cages of the zeolite structure, often situated close to the AlO₄ units that create localized negative charges. The accessibility, mobility, and exchangeability of these cations depend heavily on the framework topology, the Si/Al ratio, and the degree of hydration. Ion-exchange processes, where native cations are replaced with desired target ions, underpin key applications such as water decontamination, heavy metal capture, and selective separation of ions in industrial processes. Furthermore, the nature of these cations can modulate the Brønsted and Lewis acidity of zeolites, significantly affecting their catalytic activity in acid-catalyzed reactions (S. Lee et al., 2024). Optimizing cation distribution through tailored synthesis or post-synthetic ion-exchange treatments is thus vital for maximizing zeolite efficiency in specific functional roles (Yu & Zhao, 2022b).

- Engineering Zeolite Structures for Advanced Applications

The remarkable performance of zeolites in various technological fields stems not only from their intrinsic crystalline structures but also from deliberate engineering strategies that modify and enhance their physicochemical properties (Huang et al., 2024; Yue et al., 2020). Recent advancements in zeolite science have focused on tailoring the pore architecture, surface chemistry, and compositional characteristics to overcome inherent limitations such as restricted mass transport, limited active site accessibility, and structural rigidity (Blay et al., 2017; Grifasi et al., 2024; Masoumifard et al., 2018). These engineering approaches aim to extend the functional versatility of zeolites, enabling their deployment in more complex and demanding environmental, catalytic, and energy-related applications (Ding et al., 2015; F. Yang et al., 2023). In this section, we discuss key strategies for engineering zeolite structures, namely hierarchical pore design, surface functionalization, and ion-exchange tuning, with an emphasis on their impact on application-specific performance (X. Liu et al., 2024).

- Hierarchical Pore Engineering

The intrinsic microporosity of conventional zeolites offers excellent molecular selectivity and stability; however, it also imposes significant diffusion limitations, particularly for larger molecules (Sun et al., 2022). Restricted mass transport through narrow micropores can lead to inefficient reactant accessibility, product evacuation delays, and overall reduced catalytic efficiency, especially in reactions involving bulky substrates. Addressing these intrinsic limitations has become a major focus of modern zeolite research, leading to the development of hierarchical zeolite structures that integrate multiple levels of porosity (Rhodes, 2011).

Hierarchical zeolites are characterized by the coexistence of micropores (<2 nm), mesopores (2–50 nm), and occasionally macropores (>50 nm) within a single material (Qiu et al., 2024). This multiscale porosity dramatically enhances mass transport properties while preserving the intrinsic catalytic or adsorption functionalities of the microporous framework. Various synthetic strategies have been devised to create hierarchical structures, including bottom-up templating methods and top-down post-synthetic modifications. Hard templating approaches utilize pre-formed templates, such as carbon particles or polymer beads, around which zeolitic frameworks are crystallized (Schrettl et al., 2016; Serrano et al., 2013). After template removal, well-defined mesoporous networks remain embedded within the microporous matrix. Soft templating, on the other hand, relies on surfactant micelles or other organic agents to direct mesopore formation during synthesis (Qin et al., 2015). Alternatively, post-synthetic treatments such as desilication (selective removal of Si atoms) or dealumination (removal of Al atoms) create mesopores by introducing controlled defects into existing frameworks (Valtchev et al., 2013).

Each hierarchical engineering method imparts distinct structural and functional characteristics. Templated synthesis typically results in uniform and ordered mesoporosity, offering highly accessible active sites and reduced diffusion path lengths (Khan et al., 2019). In contrast, post-synthetic treatments often produce a broader distribution of pore sizes but are simpler and more versatile for industrial-scale modifications (Qu et al., 2020). Regardless of the technique employed, hierarchical zeolites consistently demonstrate superior performance in catalytic processes where diffusion limitations are critical (Samart, 2022). For instance, in biomass valorization reactions, the increased accessibility provided by hierarchical porosity enables the effective conversion of bulky, oxygen-rich molecules that are otherwise inaccessible to conventional microporous catalysts (Bai et al., 2019).

Moreover, the introduction of mesoporosity in zeolites also mitigates deactivation issues such as coke deposition, which typically occurs near external surfaces or at pore entrances in traditional microporous materials (Qiu et al., 2024). By facilitating faster mass transport and providing alternative pathways, hierarchical structures extend catalyst lifetimes and enhance turnover frequencies. Hierarchical zeolites have also shown enhanced adsorption capacities and kinetics in environmental applications, particularly for the removal of large organic contaminants and complex pollutant mixtures from water and air matrices (Wu et al., 2019; Xia et al., 2011)(karen, 11). A schematic comparison of mass transport pathways in conventional microporous zeolites and hierarchically structured zeolites is illustrated in Figure 1. The introduction of mesopores effectively mitigates diffusion

Figure 1 Microporous vs Hierarchical Zeolite Mass Transport

limitations, enhancing reactant accessibility and product evacuation.

In summary, hierarchical pore engineering represents a transformative strategy in zeolite design, bridging the gap between microporous precision and mesoporous accessibility. The creation of multiscale porosity enables zeolites to overcome longstanding transport barriers, broadening their applicability to reactions and separations that demand both molecular selectivity and rapid mass transfer. Future advancements in hierarchical zeolite synthesis are expected to further refine pore architectures, achieving optimized trade-offs between structural order, surface area, and functional performance for next-generation catalytic, environmental, and energy-related technologies (Bai et al., 2019)

- Surface Functionalization Strategies

While intrinsic zeolitic properties such as high surface area, ion-exchange capacity, and shape selectivity have made zeolites indispensable materials in catalysis and separations, their natural surface chemistry often requires further modification to meet the demands of advanced and highly specific applications (Bein & Mintova, 2005; Lang et al., 2024). Surface functionalization strategies offer a versatile route to tailor the chemical, physical, and catalytic properties of zeolites without compromising their underlying framework stability (Mancinelli & Martucci, 2025). By selectively modifying the external surface and internal pore environment, functionalization expands the range of interactions zeolites can engage in, thereby enabling new or enhanced functionalities for environmental remediation, chemical synthesis, and energy storage applications (Chaudhary, 2017).

Surface functionalization typically involves post-synthetic treatments that graft organic groups, metal species, or other functional moieties onto the zeolite surface. One widely used approach is the anchoring of organosilanes bearing amino, thiol, carboxyl, or phosphonate groups (Rao et al., 2019). These organic functionalities introduce new binding sites, alter surface polarity, and facilitate selective adsorption of target molecules such as heavy metals, dyes, or greenhouse gases like CO₂ (Barquist, 2009; S. Y. Lee et al., 2021). For instance, amine-functionalized zeolites have demonstrated high CO₂ capture capacities under ambient conditions due to strong chemisorption interactions between amine groups and carbon dioxide molecules (Kwon et al., 2022; L. Yang et al., 2024). Similarly, thiol-functionalized zeolites exhibit excellent affinity toward soft heavy metal ions like Hg²⁺, enabling efficient removal from contaminated waters.

Beyond organic modifications, surface functionalization through metal incorporation presents another powerful strategy to introduce catalytic activities. Methods such as ion-exchange, impregnation, and deposition–precipitation allow for the controlled insertion of metal nanoparticles (e.g., Pd, Pt, Ag) or single atoms (e.g., Cu⁺, Fe³⁺) onto the zeolite matrix (Farrusseng & Tuel, 2016; Matveeva & Bronstein, 2023). These metal-loaded zeolites exhibit bifunctional properties, combining the intrinsic acidity or adsorption capability of the zeolite with the redox or hydrogenation abilities of the metal species. For example, Pd-functionalized zeolites are highly effective in tandem catalytic processes, such as hydrodeoxygenation reactions vital for biofuel upgrading, while Fe- or Cu-modified zeolites show promise in Fenton-like oxidative degradation of organic pollutants (Dai et al., 2020; Kanan & Moyet, 2021).

The choice of functionalization strategy significantly impacts the resulting material’s performance by altering surface hydrophilicity/hydrophobicity balance, charge distribution, and accessibility of active sites. Hydrophobic surface modifications can enhance zeolite selectivity toward nonpolar molecules and improve stability in humid environments, which is critical for gas separation membranes and catalytic reactions under aqueous conditions (S. Y. Lee et al., 2021; Sonoda et al., 2010). Meanwhile, selective introduction of acid or base functional groups can fine-tune reaction pathways in acid–base bifunctional catalysis, enabling higher product selectivity and conversion rates in complex organic transformations (Cavuoto et al., 2020).

Importantly, functionalization processes must preserve the integrity of the original zeolitic framework. Excessive blocking of micropores, aggregation of metal species, or collapse of the crystalline structure during post-treatment can severely diminish material performance (Y. Li & Yu, 2021b). Thus, precise control over functionalization parameters—such as reagent concentration, reaction time, temperature, and pH—is essential to achieve homogeneous modification without sacrificing porosity or crystallinity (Rajaei et al., 2021; Valtchev et al., 2013).

In conclusion, surface functionalization provides a powerful toolkit for extending the utility of zeolitic materials beyond their natural capabilities. By judiciously introducing organic groups, metal centers, or hydrophobic coatings, the surface properties of zeolites can be finely tuned to meet the increasingly complex requirements of modern environmental, catalytic, and energy-related applications. Future innovations in functionalization chemistry, particularly at the single-atom level and under green synthesis conditions, are expected to open even broader horizons for zeolite-based technologies

- Ion-Exchange Tunning and Compositional Modification

Ion-exchange tuning represents one of the most powerful and versatile strategies for modifying the physicochemical properties of zeolites, allowing for precise control over acidity, charge distribution, redox behavior, and adsorption selectivity (Chukanov et al., 2020; Karge & Beyer, 2002). Unlike structural modifications that alter the framework itself, ion-exchange processes preserve the crystalline integrity of the zeolite while significantly altering its functional characteristics. Through selective substitution of extra-framework cations, zeolites can be tailored to meet highly specific catalytic, separation, and environmental remediation demands (Rodríguez-Iznaga et al., 2022).

The ion-exchange process typically involves replacing the native cations—commonly Na⁺, K⁺, or Ca²⁺—that balance the negative framework charge with alternative cations introduced through solution-mediated methods. Proton exchange (H⁺-form zeolites) is among the most widely utilized transformations, imparting strong Brønsted acidity to the material (Wang, 2011). This acid character is critical for numerous catalytic processes, including hydrocarbon cracking, isomerization, and alkylation reactions, where proton donation mechanisms govern reaction pathways. High-acidity zeolites such as H-ZSM-5 and H-Y have demonstrated outstanding performance in refining and petrochemical industries, underscoring the significance of controlled protonation (Dyer, 2005; Rhodes, 2011).

Beyond simple protonation, ion-exchange with transition metal cations introduces redox activity and expands the catalytic versatility of zeolites. Incorporating species such as Fe³⁺, Cu²⁺, Co²⁺, or Mn²⁺ into zeolitic matrices generates active sites capable of facilitating oxidation, reduction, and Fenton-like processes (Rhoda et al., 2022; Sazama et al., 2016). For instance, Cu-exchanged zeolites have been extensively studied for selective catalytic reduction (SCR) of NOₓ emissions in automotive exhaust treatment, while Fe-exchanged zeolites have been applied in the catalytic degradation of organic pollutants in advanced oxidation processes (AOPs) (Wichtelová et al., 2003). The dispersion and speciation of these metal ions within the zeolite framework are critical, as they influence the accessibility, reactivity, and stability of the catalytic centers (Sánchez-López et al., 2021).

Moreover, ion-exchange tuning enables the development of multifunctional zeolites by incorporating combinations of cations that impart complementary functionalities. For example, the simultaneous introduction of acid (H⁺) and redox (Cu⁺ or Fe³⁺) centers creates bifunctional catalysts capable of complex reaction sequences, such as tandem oxidation–isomerization processes (Moliner & Corma, 2018; Xu & Wu, 2022). Such multifunctionality is particularly advantageous in biomass conversion, fine chemical synthesis, and emerging sustainable technologies that demand integrated catalytic systems (Lang et al., 2024).

The impact of ion-exchange also extends to adsorption properties. Selective cation replacement can enhance zeolite affinity for specific ions or molecules based on electrostatic interactions, hydration energy differences, and pore accessibility. Zeolites exchanged with Ag⁺, for example, show high selectivity for halogenated organic compounds and microbial inactivation, making them attractive for water purification and disinfection technologies (Dyer, 2005; El-Nabarawy & Samra, 1994).

Nevertheless, achieving optimal ion-exchange outcomes requires meticulous control over experimental parameters, including ion concentration, pH, temperature, and contact time (Uchida et al., 2010). Over-exchange or excessive metal loading may lead to pore blockage, framework distortion, or the formation of undesirable extraframework metal clusters that compromise material performance. Therefore, careful optimization of ion-exchange protocols is essential to balance ion dispersion, framework preservation, and functional enhancement (Pabalan & Bertetti, 2001).

In summary, ion-exchange tuning offers a highly effective means of tailoring zeolitic materials to meet diverse functional requirements. By modulating acidity, redox behavior, and adsorption specificity through controlled cation substitution, researchers can strategically engineer zeolites for advanced catalytic, environmental, and separation applications. Future developments are expected to explore novel ion-exchange methodologies, including single-atom ion-exchange and in situ dynamic ion-exchange systems, to furtherr expand the frontiers of zeolite functionality in next-generation technologies

- Environmental Applications

The unique physicochemical properties of zeolites—including high surface area, tunable pore architecture, selective adsorption capabilities, and ion-exchange potential—render them highly attractive for a wide range of environmental applications (Senila & Cadar, 2024). Their ability to selectively interact with contaminants at the molecular level enables zeolites to address critical challenges in water purification, air pollution control, and waste remediation. In recent decades, engineered zeolitic materials have been increasingly deployed in technologies targeting heavy metal removal, ammonium elimination, volatile organic compound (VOC) adsorption, and greenhouse gas mitigation, thereby contributing significantly to sustainable environmental management (Abdelwahab & Thabet, 2023; Kordala & Wyszkowski, 2024).

One of the most extensively studied environmental applications of zeolites is the removal of heavy metals from aqueous systems. The negative charge framework and ion-exchange capabilities of zeolites facilitate the selective uptake of toxic metal ions such as Pb²⁺, Cd²⁺, Hg²⁺, and Cu²⁺ (Dai et al., 2020; Mardiana & Rusli, 2023). Both natural and synthetic zeolites have been demonstrated to efficiently reduce heavy metal concentrations in industrial effluents, mining runoff, and municipal wastewater. The performance of zeolites in metal adsorption is governed by several factors, including cation selectivity sequences, pore size compatibility, and the Si/Al ratio, which modulates surface charge density. Modified or functionalized zeolites, such as thiol- or amine-grafted variants, further enhance adsorption capacity and selectivity, expanding their applicability even to trace-level contaminant removal under complex environmental conditions (Mudaber & Batur, 2023; Vishnu et al., 2021; Zhao, 2016).

In addition to heavy metals, zeolites exhibit high affinity for ammonium ions (NH₄⁺), making them valuable materials for nutrient recovery and wastewater treatment. Ammonium contamination is a major environmental concern due to its contribution to eutrophication in aquatic ecosystems (Godifredo et al., 2023; Rahmani et al., 2004; Wasielewski et al., 2018). Natural zeolites such as clinoptilolite have been widely applied for ammonium adsorption, offering high capacity, regenerability, and cost-effectiveness. Emerging applications also explore zeolite-based systems integrated with biological processes, such as coupled ion-exchange–nitrification reactors, to achieve more efficient and sustainable nitrogen management in wastewater treatment plants (Godifredo et al., 2023; Kumari et al., 2024).

Zeolites also play a vital role in air pollution control, particularly in the adsorption and catalytic oxidation of volatile organic compounds (VOCs) and gaseous pollutants. The microporous network and hydrophobic characteristics of high-silica zeolites enable the effective capture of VOCs, including benzene, toluene, and formaldehyde, even at low concentrations (Qiu et al., 2024; Xue & Yang, 2021). Furthermore, metal-exchanged zeolites, such as Cu- and Fe-zeolites, serve as active catalysts for the selective catalytic reduction (SCR) of nitrogen oxides (NOₓ), a major contributor to air pollution and acid rain. These catalysts offer high efficiency, thermal stability, and resistance to poisoning, rendering them integral components in automotive exhaust after-treatment systems and industrial emission control technologies (Xue & Yang, 2021; Zaitan et al., 2016).

Another rapidly growing area of environmental application is the use of zeolites for greenhouse gas mitigation, particularly carbon dioxide (CO₂) capture. Zeolites exhibit competitive CO₂ adsorption capacities due to their high surface area, tunable pore sizes, and adjustable framework polarity (Boer et al., 2023; Xia et al., 2011). Amine-functionalized zeolites, in particular, display enhanced CO₂ capture performance under both dry and humid conditions, overcoming limitations typically faced by purely physical adsorbents. Their potential integration into carbon capture and storage (CCS) systems offers promising pathways to reduce anthropogenic CO₂ emissions and combat climate change (Bahmanzadegan & Ghaemi, 2023; Kwon et al., 2022; Nguyen et al., 2016).

In solid waste management, zeolites are increasingly being utilized for the immobilization and stabilization of hazardous materials. Their ion-exchange ability and structural robustness enable zeolites to sequester radioactive isotopes (e.g., Cs⁺, Sr²⁺) and heavy metals within stable matrices, reducing leachability and environmental risks (Lang et al., 2024; Senila & Cadar, 2024; Zhang et al., 2024). Additionally, zeolites derived from industrial by-products (e.g., fly ash, slags) represent a sustainable approach to valorize waste streams while addressing environmental contamination (Pabalan & Bertetti, 2001; Rhodes, 2010).

In summary, the versatility, tunability, and sustainability of zeolitic materials underpin their broad applicability in environmental technologies. Advances in zeolite engineering—such as hierarchical structuring, functionalization, and hybrid material development—have significantly expanded their capabilities beyond traditional uses. As environmental regulations tighten and the demand for greener, more efficient remediation technologies grows, zeolites are poised to play an increasingly central role in ensuring environmental protection and resource recovery for a sustainable future

- REFERENCES

Abdelwahab, O., & Thabet, W. M. (2023). Natural zeolites and zeolite composites for heavy metal removal from contaminated water and their applications in aquaculture Systems: A review. The Egyptian Journal of Aquatic Research. https://doi.org/10.1016/j.ejar.2023.11.004

Bacakova, L., Vandrovcová, M., Kopova, I., & Jirka, I. (2018). Applications of zeolites in biotechnology and medicine – a review. Biomaterials Science, 6(5), 974–989. https://doi.org/10.1039/C8BM00028J

Bahmanzadegan, F., & Ghaemi, A. (2023). Modification and functionalization of zeolites to improve the efficiency of CO2 adsorption: A review. In Case Studies in Chemical and Environmental Engineering. https://doi.org/10.1016/j.cscee.2023.100564

Bai, R., Song, Y., Li, Y., & Yu, J. (2019). Creating Hierarchical Pores in Zeolite Catalysts (Vol. 1, Issue 6, pp. 601–611). https://doi.org/10.1016/J.TRECHM.2019.05.010

Barquist, K. N. (2009). Synthesis and environmental adsorption applications of functionalized zeolites and iron oxide/zeolite composites. https://doi.org/10.17077/ETD.XZTD7S2G

Bein, T., & Mintova, S. (2005). Advanced applications of zeolites (Vol. 157). Elsevier. https://doi.org/10.1016/S0167-2991(05)80015-1

Blay, V., Louis, B., Miravalles, R., Yokoi, T., Peccatiello, K. A., Clough, M., & Yilmaz, B. (2017). Engineering Zeolites for Catalytic Cracking to Light Olefins. ACS Catalysis, 7(10), 6542–6566. https://doi.org/10.1021/ACSCATAL.7B02011

Boer, D. G., Langerak, J., & Pescarmona, P. P. (2023). Zeolites as Selective Adsorbents for CO2 Separation. ACS Applied Energy Materials, 6(5), 2634–2656. https://doi.org/10.1021/acsaem.2c03605

Cavuoto, D., Zaccheria, F., & Ravasio, N. (2020). Some Critical Insights into the Synthesis and Applications of Hydrophobic Solid Catalysts. Catalysts, 10(11), 1337. https://doi.org/10.3390/CATAL10111337

Chaudhary, A. (2017). Zeolites: The Aluminosilicate Framework with Promising Scenarios (Vol. 2, Issue 5). https://doi.org/10.19080/RAPSCI.2017.02.555598

Chukanov, N. V., Kazheva, O. N., Chervonnaya, N. A., Varlamov, D. A., Ermolaeva, V. N., Pekov, I. V., & Shilov, G. V. (2020). Ion-exchange properties of the natural zeolite amicite. Macedonian Journal of Chemistry and Chemical Engineering, 39(2), 207–216. https://doi.org/10.20450/MJCCE.2020.1984

Dai, H., Wu, J., Zhang, H., Chen, Y., Ma, L., Huang, H., & Zhang, Y. (2020). Recent advances on cellulose nanocrystals for Pickering emulsions: Development and challenge, Trends Food Sci. Technol, 102, 16–29.

Davis, M. E. (1993). New vistas in zeolite and molecular sieve catalysis. Accounts of Chemical Research, 26(3), 111–115. https://doi.org/10.1021/AR00027A006

Ding, K., Ding, K., Corma, A., Maciá-Agulló, J. A., Hu, J. G., Krämer, S., Stair, P. C., & Stucky, G. D. (2015). Constructing Hierarchical Porous Zeolites via Kinetic Regulation. Journal of the American Chemical Society, 137(35), 11238–11241. https://doi.org/10.1021/JACS.5B06791

Dyer, A. (2005). Ion-exchange properties of zeolites (Vol. 157). Elsevier. https://doi.org/10.1016/S0167-2991(05)80011-4

El-Nabarawy, T., & Samra, S. E. (1994). Effect of cation exchange on the sorption properties of zeolites. Adsorption Science & Technology, 11(1), 51–57. https://doi.org/10.1177/026361749401100105

Farrusseng, D., & Tuel, A. (2016). Perspectives on zeolite-encapsulated metal nanoparticles and their applications in catalysis. New Journal of Chemistry, 40(5), 3933–3949. https://doi.org/10.1039/C5NJ02608C

Godifredo, J., Ferrer, J., Seco, A., & Barat, R. (2023). Zeolites for Nitrogen Recovery from the Anaerobic Membrane Bioreactor Permeate: Zeolite Characterization. Water, 15(6), 1007. https://doi.org/10.3390/w15061007

Grifasi, N., Ziantoni, B., Fino, D., & Piumetti, M. (2024). Fundamental properties and sustainable applications of the natural zeolite clinoptilolite. Environmental Science and Pollution Research. https://doi.org/10.1007/s11356-024-33656-5

Huang, T.-Y., Sun, J., Wang, D.-X., & Wang, Q.-Q. (2024). Recent progress in chiral zeolites: Structure, synthesis, characterization and applications. Chinese Chemical Letters. https://doi.org/10.1016/j.cclet.2024.109758

Jiang, J., Jiang, J., Jordá, J. L., Díaz-Cabañas, M. J., Yu, J., & Corma, A. (2010). The Synthesis of an Extra‐Large‐Pore Zeolite with Double Three‐Ring Building Units and a Low Framework Density. Angewandte Chemie, 49(29), 4986–4988. https://doi.org/10.1002/ANIE.201001506

Kanan, S. M., & Moyet, M. A. (2021). Fabricated metal zeolites as photocatalysts for the degradation of organic pollutants. Research on Chemical Intermediates, 47(2), 433–458. https://doi.org/10.1007/S11164-021-04416-8

Karge, H. G., & Beyer, H. K. (2002). Solid-State Ion Exchange in Microporous and Mesoporous Materials (Vol. 33). Springer Berlin Heidelberg. https://doi.org/10.1007/3-540-69750-0_2

Khan, W. A., Jia, X., Wu, Z., Choi, J., & Yip, A. C. K. (2019). Incorporating Hierarchy into Conventional Zeolites for Catalytic Biomass Conversions. A Review. Catalysts, 9(2), 127. https://doi.org/10.3390/CATAL9020127

Kordala, N., & Wyszkowski, M. (2024). Zeolite Properties, Methods of Synthesis, and Selected Applications. Molecules, 29. https://doi.org/10.3390/molecules29051069

Kumari, S., Chowdhry, J., Kumar, M., & Kumari, S. (2024). Zeolites in wastewater treatment: A comprehensive review on scientometric analysis, adsorption mechanisms, and future prospects. Environmental Research, 260, 119782. https://doi.org/10.1016/j.envres.2024.119782

Kwon, D., Numan, M., Kim, J., Yilmaz, M., Park, S.-E., Ihee, H., & Jo, C. S. (2022). Tailoring the CO2 selective adsorption properties of MOR zeolites by post functionalization. Journal of CO2 Utilization, 62, 102064. https://doi.org/10.1016/j.jcou.2022.102064

Lang, Q., Lu, P., Yang, X., & Valtchev, V. (2024). Zeolites for the environment. https://doi.org/10.1016/j.greenca.2024.02.007

Lee, S., Park, Y., & Choi, M. (2024). In Cooperative Interplay of Micropores/Mesopores of Hierarchical Zeolite in Chemical Production. ACS Catalysis. https://doi.org/10.1021/acscatal.3c05170

Lee, S. Y., Kim, J. H., & Park, J. (2021). Advancements in colorimetric biosensors for environmental and food safety applications. Biosensors and Bioelectronics, 172, 112734. https://doi.org/10.1016/j.bios.2021.112734

Li, J., Gao, M., Yan, W., & Yu, J. (2022). Regulation of the Si/Al ratios and Al distributions of zeolites and their impact on properties. Chemical Science, 14(8), 1935–1959. https://doi.org/10.1039/d2sc06010h

Li, Y., & Yu, J. (2021a). Emerging applications of zeolites in catalysis, separation and host–guest assembly. Nature Reviews Materials, 6(12), 1156–1174. https://doi.org/10.1038/S41578-021-00347-3

Li, Y., & Yu, J. (2021b). Emerging applications of zeolites in catalysis, separation and host–guest assembly. Nature Reviews Materials, 6(12), 1156–1174. https://doi.org/10.1038/S41578-021-00347-3

Liu, X., Zhao, S., Yang, W., & Huang, J. (2024). Hierarchical zeolite-encapsulated metal nanoparticles for heterogeneous catalysis. Nanoscale. https://doi.org/10.1039/d4nr02307b

Liu, Z., Zhou, J., Tang, X., Liu, F., Yuan, J., Li, G., Huang, L., Krishna, R., Huang, K., & Zheng, A. (2020). Dependence of zeolite topology on alkane diffusion inside diverse channels. Aiche Journal, 66(8). https://doi.org/10.1002/AIC.16269

Lü, P., Xu, J., Sun, Y., Guillet‐Nicolas, R., Willhammar, T., Fahda, M., Dib, E., Wang, B., Qin, Z., Xu, H., Cho, J., Liu, Z., Yu, H., Yang, X., Lang, Q., Mintova, S., Zou, X., & Valtchev, V. (2024). A stable zeolite with atomically ordered and interconnected mesopore channel. Visual Education, 636(8042), 368–373. https://doi.org/10.1038/s41586-024-08206-1

Mancinelli, M., & Martucci, A. (2025). Exploring the Potential of Zeolites for Sustainable Environmental Applications. https://doi.org/10.20944/preprints202501.0157.v1

Mardiana, S., & Rusli, H. (2023). Removal of Heavy Metal Ions Using Pristine and Functionalized Natural Zeolites. Indonesian Journal of Chemistry, 23(3), 863. https://doi.org/10.22146/ijc.81098

Masoumifard, N., Guillet-Nicolas, R., Kleitz, F., & Kleitz, F. (2018). Synthesis of Engineered Zeolitic Materials: From Classical Zeolites to Hierarchical Core–Shell Materials. Advanced Materials, 30(16), 1704439. https://doi.org/10.1002/ADMA.201704439

Matveeva, V. G., & Bronstein, L. M. (2023). Design of Bifunctional Nanocatalysts Based on Zeolites for Biomass Processing. Nanomaterials, 13. https://doi.org/10.3390/nano13162274

Moliner, M., & Corma, A. (2018). General Aspects on Structure and Reactivity of Framework and Extra-framework Metals in Zeolite Materials. Springer. https://doi.org/10.1007/430_2017_21

Moller, K., & Bein, T. (2013). Mesoporosity – a new dimension for zeolites. Chemical Society Reviews, 42(9), 3689–3707. https://doi.org/10.1039/C3CS35488A

Mudaber, S., & Batur, J. (2023). Differences in Heavy Metals Adsorption on Natural, Modified, and Synthetic Zeolites-A Review. https://doi.org/10.18596/jotcsa.1263041

Nguyen, T. H., Kim, S., Yoon, M., & Bae, T.-H. (2016). Hierarchical Zeolites with Amine-Functionalized Mesoporous Domains for Carbon Dioxide Capture. Chemsuschem, 9(5), 455–461. https://doi.org/10.1002/CSSC.201600004

Pabalan, R. T., & Bertetti, F. P. (2001). Cation-Exchange Properties of Natural Zeolites. Reviews in Mineralogy & Geochemistry, 45(1), 453–518. https://doi.org/10.2138/RMG.2001.45.14

Paillaud, J.-L., Harbuzaru, B., Patarin, J., & Bats, N. (2004). Extra-large-pore zeolites with two-dimensional channels formed by 14 and 12 rings. Science, 304(5673), 990–992. https://doi.org/10.1126/SCIENCE.1098242

Pérez-Ramírez, J., Christensen, C. H., Egeblad, K., Christensen, C. H., & Groen, J. C. (2008). Hierarchical zeolites: Enhanced utilisation of microporous crystals in catalysis by advances in materials design. Chemical Society Reviews, 37(11), 2530–2542. https://doi.org/10.1039/B809030K

Qin, Z., Gilson, J.-P., & Valtchev, V. (2015). Mesoporous zeolites by fluoride etching. Current Opinion in Chemical Engineering, 8, 1–6. https://doi.org/10.1016/J.COCHE.2015.01.002

Qiu, S., Lü, W., Zeng, Z., Su, X., Lai, Y., Liu, X., Gao, X., & Kawi, S. (2024). Zeolite‐based Materials for Catalytic Oxidation of Volatile Organic Compounds. Chemcatchem. https://doi.org/10.1002/cctc.202401443

Qu, H., Ma, Y., Li, B., & Wang, L. (2020). Hierarchical zeolites: Synthesis, structural control, and catalytic applications (Vol. 3, Issue 3, pp. 225–245). https://doi.org/10.1007/S42247-020-00088-Z

Rahmani, A. R., Mahvi, A. H., Mesdaghinia, A., & Nasseri, S. (2004). Investigation of ammonia removal from polluted waters by Clinoptilolite zeolite. International Journal of Environmental Science and Technology, 1(2), 125–133. https://doi.org/10.1007/BF03325825

Rajaei, H., Esmaeilzadeh, F., & Mowla, D. (2021). Elucidation of Si/Al ratio on physicochemical properties of HZSM-5 zeolites. Journal of Thermal Analysis and Calorimetry, 146(2), 581–586. https://doi.org/10.1007/S10973-020-09993-1

Rao, X., Rao, X., Tatoulian, M., Guyon, C., Ognier, S., Chu, C., & Abou Hassan, A. (2019). A Comparison Study of Functional Groups (Amine vs. Thiol) for Immobilizing AuNPs on Zeolite Surface. Nanomaterials, 9(7), 1034. https://doi.org/10.3390/NANO9071034

Rhoda, H. M., Heyer, A. J., Snyder, B. E. R., Plessers, D., Bols, M. L., Schoonheydt, R. A., Sels, B. F., & Solomon, E. I. (2022). Second-Sphere Lattice Effects in Copper and Iron Zeolite Catalysis. Chemical Reviews, 122(14), 12207–12243. https://doi.org/10.1021/acs.chemrev.1c00915

Rhodes, C. J. (2010). Properties and applications of zeolites. Science Progress, 93(3), 223–284. https://doi.org/10.3184/003685010X12800828155007

Rhodes, C. J. (2011). Properties and Applications of Zeolites. ChemInform, 42(36). https://doi.org/10.1002/CHIN.201136208

Ristanović, Z., Hofmann, J. P., Deka, U., Schülli, T. U., Rohnke, M., Beale, A. M., & Weckhuysen, B. M. (2013). Intergrowth structure and aluminium zoning of a zeolite ZSM-5 crystal as resolved by synchrotron-based micro-X-ray diffraction imaging. Angewandte Chemie, 52(50), 13382–13386. https://doi.org/10.1002/ANIE.201306370

Rodríguez-Iznaga, I., Shelyapina, M. G., & Petranovskii, V. (2022). Ion Exchange in Natural Clinoptilolite: Aspects Related to Its Structure and Applications. Minerals, 12(12), 1628. https://doi.org/10.3390/min12121628

Samart, K. (2022). Synthesis and Catalytic Application of Macroscopic Zeolite Beads with Hierarchical Porosity. https://doi.org/10.33612/diss.286267800

Sánchez-López, P., Kotolevich, Y., Yocupicio-Gaxiola, R. I., Antúnez-García, J., Kumar Chowdari, R., Petranovskii, V., & Fuentes-Moyado, S. (2021). Recent Advances in Catalysis Based on Transition Metals Supported on Zeolites. Frontiers in Chemistry, 9, 716745. https://doi.org/10.3389/FCHEM.2021.716745

Sazama, P., Pilar, R., Mokrzycki, L., Vondrová, A., Kaucky, D., Plšek, J., Sklenak, S., Stastny, P., & Klein, P. (2016). Remarkably enhanced density and specific activity of active sites in Al-rich Cu-, Fe- and Co-beta zeolites for selective catalytic reduction of NOx. Applied Catalysis B-Environmental, 189, 65–74. https://doi.org/10.1016/J.APCATB.2016.02.020

Schrettl, S., Schulte, B., & Frauenrath, H. (2016). Templating for hierarchical structure control in carbon materials. Nanoscale, 8(45), 18828–18848. https://doi.org/10.1039/C6NR06695J

Senila, M., & Cadar, O. (2024). Modification of natural zeolites and their applications for heavy metal removal from polluted environments: Challenges, recent advances, and perspectives. Heliyon, 10. https://doi.org/10.1016/j.heliyon.2024.e25303

Serrano, D. P., Serrano, D. P., Escola, J. M., Pizarro, P., & Pizarro, P. (2013). Synthesis strategies in the search for hierarchical zeolites. Chemical Society Reviews, 42(9), 4004–4035. https://doi.org/10.1039/C2CS35330J

Sonoda, J., Kamegawa, T., Kuwahara, Y., Mori, K., & Yamashita, H. (2010). Hydrophobic Modification of Ti-Containing Zeolite (TS-1) and Their Applications in Liquid-Phase Selective Catalytic Reactions. Bulletin of the Chemical Society of Japan, 83(5), 592–594. https://doi.org/10.1246/BCSJ.20090265

Sun, M.-H., Gao, S., Hu, Z., Barakat, T., Liu, Z., Yu, S., Lyu, J., Li, Y., Xu, S., Chen, L.-H., & Su, B.-L. (2022). Boosting molecular diffusion following the generalized Murray’s Law by constructing hierarchical zeolites for maximized catalytic activity. National Science Review, 9(12). https://doi.org/10.1093/nsr/nwac236

Tang, L., Shi, L., Bonneau, C., Sun, J., Yue, H., Ojuva, A., Lee, B. L., Kritikos, M., Bell, R. G., Bacsik, Z., Mink, J., Mink, J., & Zou, X. (2008). A zeolite family with chiral and achiral structures built from the same building layer. Nature Materials, 7(5), 381–385. https://doi.org/10.1038/NMAT2169

Uchida, S., Eguchi, R., & Mizuno, N. (2010). Zeotype Organic–Inorganic Ionic Crystals: Facile Cation Exchange and Controllable Sorption Properties. Angewandte Chemie, 49(51), 9930–9934. https://doi.org/10.1002/ANIE.201005176

Valencia, S. (2021). Zeolitic Microporous Materials and Their Applications. Molecules, 26(3), 730. https://doi.org/10.3390/MOLECULES26030730

Valtchev, V., Majano, G., Mintova, S., & Pérez-Ramírez, J. (2013). Tailored crystalline microporous materials by post-synthesis modification. Chemical Society Reviews, 42(1), 263–290. https://doi.org/10.1039/C2CS35196J

Vishnu, D., Dhandapani, B., Kumar, K. S., Balaji, G., & Mahadevan, S. (2021). Removal of heavy metals from mine waters by natural zeolites. Elsevier. https://doi.org/10.1016/B978-0-12-822965-1.00008-8

Wang, C. (2011). Study on method and application of ion-exchange in zeolite molecular sieve. Mining and Metallurgy.

Wasielewski, S., Rott, E., Minke, R., & Steinmetz, H. (2018). Evaluation of Different Clinoptilolite Zeolites as Adsorbent for Ammonium Removal from Highly Concentrated Synthetic Wastewater. Water, 10(5), 584. https://doi.org/10.3390/W10050584

Weckhuysen, B. M., & Yu, J. (2015). Recent advances in zeolite chemistry and catalysis. Chemical Society Reviews, 44(20), 7022–7024. https://doi.org/10.1039/C5CS90100F

Wichtelová, B., Sobalik, Z., & Dědeček, J. (2003). Redox catalysis over metallo-zeolites Contribution to environmental catalysis. Applied Catalysis B-Environmental, 41(1), 97–114. https://doi.org/10.1016/S0926-3373(02)00196-0

Wu, Q., Ma, Y., Wang, S., Meng, X., & Xiao, F.-S. (2019). 110th Anniversary: Sustainable Synthesis of Zeolites: From Fundamental Research to Industrial Production. Industrial & Engineering Chemistry Research, 58(27), 11653–11658. https://doi.org/10.1021/ACS.IECR.9B02054

Xia, Y., Mokaya, R., Walker, G. S., & Zhu, Y. (2011). Superior CO2 Adsorption Capacity on N‐doped, High‐Surface‐Area, Microporous Carbons Templated from Zeolite. Advanced Energy Materials, 1(4), 678–683. https://doi.org/10.1002/AENM.201100061

Xu, H., & Wu, P. (2022). New progress in zeolite synthesis and catalysis. National Science Review, 9(9). https://doi.org/10.1093/nsr/nwac045

Xue, T., & Yang, L. (2021). Zeolite-Based Materials for the Catalytic Oxidation of VOCs: A Mini Review. Frontiers in Chemistry, 9, 751581. https://doi.org/10.3389/FCHEM.2021.751581

Yang, F., Zhao, H., & Zhang, X. (2023). Recent progress in crosslinking strategies for improving stability and performance of biosensors. Analytical Chemistry, 95, 2284–2293. https://doi.org/10.1021/acs.analchem.2c04321

Yang, L., Lin, Y., Zhao, Y., Li, J., Tian, Z., Wu, Y., Hu, H., Wang, H., & Chen, L. (2024). Facilely Grafting Small Amine Molecules into Co-Exchanged Zeolite for Enhancing CO2 Adsorption. https://doi.org/10.1021/acs.iecr.3c04422

Yu, J., & Zhao, D. (2022a). Preface to special topic on new era of zeolite science. National Science Review, 9(9). https://doi.org/10.1093/nsr/nwac157

Yu, J., & Zhao, D. (2022b). Preface to special topic on new era of zeolite science. National Science Review, 9(9). https://doi.org/10.1093/nsr/nwac157

Yue, Y., Haibo, Z., Wang, T., & Bao, X. (2020). Green fabrication of hierarchical zeolites from natural minerals. National Science Review, 7(11), 1632–1634. https://doi.org/10.1093/NSR/NWAA197

Zaitan, H., Manero, M.-H., & Valdés, H. (2016). Application of high silica zeolite ZSM-5 in a hybrid treatment process based on sequential adsorption and ozonation for VOCs elimination. Journal of Environmental Sciences-China, 41(3), 59–68. https://doi.org/10.1016/J.JES.2015.05.021

Zhang, W., Zhang, T., Lv, Y., Wang, J., Gao, X., Gu, Z., Li, S., Ao, H., & Fang, D. (2024). Recent Progress on the Synthesis and Applications of Zeolites from Industrial Solid Wastes. Catalysts, 14(10), 734. https://doi.org/10.3390/catal14100734

Zhao, Y. (2016). Review of the Natural, Modified, and Synthetic Zeolites for Heavy Metals Removal from Wastewater. Environmental Engineering Science, 33(7), 443–454. https://doi.org/10.1089/EES.2015.0166