COMPARATIVE ANALYSIS OF THE BULK PROPERTIES OF CRUDE OIL SAMPLES FROM FOUR PRODUCING FIELDS IN THE NIGER DELTA, NIGERIA

ABSTRACT

Twelve different crude oil samples were collected from four oil fields in the Niger Delta Nigeria. The bulk properties of these crude oils which include API gravity, specific gravity, reid vapour pressure, kinematic viscosity, dynamic viscosity, moisture, cloud point, pour point, gum content and Sulphur content were analyzed, using standard procedures of American Society for Testing and Materials (ASTM). The results show API gravity values ranged from 30.540 ± 0.100 - 42.460 ± 0.100, Specific gravity 0.813 ± 0.001 – 0.873 ± 0.001, Kinematic viscosities 2.001 ±  0.001 - 5.547±0.010cSt, Dynamic viscosities 1.631±0.000 - 5.057±0.010 cP at 0°C, Gum content 4.676±0.010 - 87.350±0.100 ml, flash point 15.000±0.200 °C - 27.000±0.200 °C, Pour point –16.000±0.200°C - +14.000±0.200°C. The correlation analysis of kinematic viscosity (Kv) and gum content r =0.965 was strongest, indicating increased viscosity with respect to high gum content. These physicochemical properties play a crucial role in determining the crude oil's suitability for refining, transportation, and its environmental impact. The data highlights the need for tailored handling and processing strategies based on the specific characteristics of each crude oil sample.

Key word: API and Specific gravity; pour point; moisture Content;  viscosity; Niger Delta.

1. INTRODUCTION

The Niger Delta is important in crude oil correlation studies because it is one of the major hydrocarbon provinces of the world, with an estimated reserve of about 23 billion barrels of oil and 183 trillion cubic feet of natural gas. Defining and evaluating exploration are helpful to characterize the hydrocarbon source rocks, their range of thermal maturities, and types of products generated. Hydrocarbons within the basin have been found to occur at different productive horizons at very great depths apart. The migration processes that determined the pooling of the hydrocarbons at different depths are yet to be clearly understood, but it is known that the properties and composition of any petroleum systems are controlled by complex geological, physicochemical, and biological processes during generation as well as accumulation in reservoirs. Crude oil, or petroleum, is a naturally occurring yellowish-black liquid mixture of mainly hydrocarbons and is found in geological formations (EIA, 2017). The word petroleum comes from Medieval Latin petroleum (literally 'rock oil'), which comes from Latin petra 'rock' and oleum 'oil.' The origin of the term started from monasteries in southern Italy, where it was in use by the end of the first millennium as an alternative for the older term "naphtha." Over the years the chemical utilization of crude oil and its refined products has been increasing globally (Udeme et al., 2012).

It has been mentioned that the ever-increasing chemical utilization of crude oils and petroleum products calls for a better knowledge of the composition, structure, and properties of the fractions (Okeola et al., 2016; Odebunmi et al., 2002). As a result, concerted efforts are being made to understand its composition, structures, and properties. This understanding guides the processing method and condition to improve the yield and the quality of products. Composition of crude oil determines their characteristics (Carey, 2003). These characteristics, in turn, for any crude oil, depend on the particular source of the oil field. There are different multiple sand reservoirs of tertiary sedimentary deposits in each oil field, resulting in a unique character of crude oil content. The oil fields are characterized by these differences. As a result, there are different proportions of the various hydrocarbons of different molecular types, sizes, and other elemental constituents in the samples of the crude oil. Therefore, there is a need to characterize the oil to ascertain its properties, to design the precaution modality and refining procedure, and to assess its potential as a source of environmental contaminants (Udeme et al., 2012). It has also been established that the quality of the petroleum products plays the major role in consumer demand and the performance of the refineries (Oyekunle et al., 2004).

2. MATERIALS AND METHODS

2.1 Sample location and collection

Crude oil samples were collected from four producing fields in the Niger Delta region of Nigeria: Warri (Delta State), Imo River (Imo State), Nembe/Brass (Bayelsa State), and Bonny/Bonga Offshore Fields (Rivers State). The Warri area is located in the western Niger Delta and is associated with the Agbada Formation. The Imo River Field is an onshore location bordering the Anambra Basin. Samples from Nembe and Brass were obtained near Wilberforce Island, a swampy region rich in oil and gas deposits. Bonny and Bonga are deep offshore fields that produce crude oil from marine reservoirs.

Crude oil samples were obtained from flow stations and storage terminals using sterilized, airtight glass bottles. Sample containers were labeled with field code, date, and well information. GPS coordinates were recorded at each site. To preserve sample integrity, they were stored in cool, dark conditions and transported promptly for analysis. Collection procedures followed Tissot and Welte (1984) to avoid contamination or alteration of crude properties. The sample locations and collection points are presented in Figure 1, which illustrates the spatial distribution of the fields across the Niger Delta basin.

Figure 1: Map of the study locations and crude oil producing fields in the Niger Delta.

Table 1. Sample points and their coordinates in various location fields

| Sample location | WARRI (Delta State) | IMO STATE | NEMBE/BRASS (Bayelsa State) | BONNY/BONGA (Rivers State) |
| --- | --- | --- | --- | --- |
|  | Sample A (5o32’47.7’’N and 5o46’05.9’’E | Sample D (5o30’33.9’’N and 7o02’22.1’’E | Sample G (4o18’36.1’’N and 6o14’35.7’’E | Sample K (4o25’42.4’’N and 7o11’39.6’’E |
| Sample points and their coordinates | Sample B (5o32’53.2’’N and 5o45’55.8’’E) | Sample E (5o30’30.4’’N and 7o02’21.6’’E | Sample H (4o18’33.0’’N and 6o14’36.4’’E | Sample L (4o25’34.3’N and 7o11’39.4’’E |
|  | Sample C (5o32’49.2’’N and 5o46’05.8’’E | Sample F (5o30’26.2’’N and 7o02’20.2’’E | Sample I (4o18’34.3’’N and 6o14’39.8’’E |  |
|  |  |  | Sample J (4o18’25.3’’N and 6o14’43.8’’E |  |

2.2 Sample preparation and analysis

A 50 g portion of each crude oil sample was dissolved in 50 mL dichloromethane and left undisturbed for 30 minutes. The mixture was filtered through Whatman No. 1 paper into a 100 mL volumetric flask and brought to volume with petroleum ether. The resulting solution was stored in 120 mL glass sample bottles for laboratory analysis.

Analyses were carried out at Indorama-Eleme Petrochemical Company Ltd., Port Harcourt, using standard procedures recommended by the American Society for Testing and Materials (ASTM). Parameters analyzed included API gravity, specific gravity, kinematic viscosity, moisture content, gum content, flash point, pour point, cloud point, and sulphur content.

2.2.1 API gravity and specific gravity

Specific gravity and API gravity were determined using a digital density meter in accordance with ASTM D4052. The crude oil was injected into the cell at 15.6°C, ensuring no air bubbles were present. API gravity was calculated using the equation:

API Gravity=141.3Specific gravity of the oil at 60°F-131.4

2.2.2 Kinematic and dynamic viscosity

Viscosity measurements were performed following ASTM D445. A clean viscometer was filled with crude oil, placed in a 40°C bath, and the flow time between calibrated marks was recorded. Kinematic viscosity was calculated as

Kinematic Viscosity (V) = c x t    (c=0.009933)

Dynamic viscosity was obtained using the formula:

µ = p x v

2.2.3 Moisture content

Moisture content was determined by Karl Fischer titration following ASTM D1744. A known volume of crude oil (2–5 mL) was injected into the titration vessel, and the moisture content was displayed on the coulometer.

2.2.4 Gum content

Existent gum content was evaluated according to ASTM D381. Pre-weighed beakers were filled with 10 mL of crude oil and exposed to heated air jets at 160–165°C for 30 minutes. After cooling, beakers were reweighed, and gum content was calculated:

Gum (mg/100 mL) = 10,000 × (A − C)

2.2.5 Flashpoint

The flash point was measured using the Cleveland open cup method, following ASTM D92. Samples were heated, and the temperature at which vapour ignited with a test flame was recorded.

2.2.6 Pour point

The pour point was determined according to ASTM D97. Crude oil samples were preheated, then allowed to cool under controlled conditions. The pour point was recorded as the temperature at which flow ceased in the tilted jar.

3. RESULTS AND DISCUSSION

The physicochemical properties of twelve crude oil samples collected from the Niger Delta were analyzed to determine their suitability for refining and transport. Parameters evaluated included API gravity, specific gravity, kinematic and dynamic viscosities, moisture content, gum content, flash point, and pour point. The results of the analysis are summarized in Table 1. Crude oil samples exhibited varying physical characteristics across locations, reflecting differences in reservoir origin and maturity.  Statistical Analysis was employed (Pearson correlation) for understanding the relationships between each sample using IBM SPSS Statistics 25.

| PARAMETERS | Sample | Sample | Sample | Sample | Sample | Sample | Sample | Sample | Sample | Sample | Sample | Sample |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | A | B | C | D | E | F | G | H | I | J | K | L |
| API@15°C | 42.050±0.050 | 39.230±0.100 | 30.540±0.100 | 35.950±0.100 | 42.460±0.100 | 34.400±0.100 | 40.150±0.100 | 37.200±0.100 | 32.900±0.100 | 32.200±0.100 | 41.400±0.100 | 31.500±0.100 |
| SG@15°C | 0.815±0.000 | 0.829±0.0001 | 0.873±0.001 | 0.845±0.001 | 0.813±0.001 | 0.853±0.001 | 0.815±0.001 | 0.829±0.001 | 0.845±0.001 | 0.853±0.001 | 0.813±0.001 | 0.8733±0.001 |
| KV@40°C(cSt) | 2.001±0.001 | 2.775±0.005 | 5.547±0.010 | 2.559±0.01 | 3.000±0.010 | 2.6531±0.010 | 2.011±0.010 | 2.875±0.010 | 2.581±0.010 | 2.753±0.010 | 3.000±0.010 | 5.447±0.010 |
| Dynamic Viscosity @0°C(cP) | 1.631±0.000 | 2.301±0.0015 | 4.757±0.010 | 2.163±0.01 | 2.156±0.010 | 2.2628±0.010 | 2.630±0.010 | 2.401±0.010 | 2.263±0.010 | 2.363±0.010 | 2.355±0.001 | 5.057±0.010 |
| Moisture Content(V/V) | <0.050±0.000 | 0.500±0.010 | 0.060±0.001 | <0.050±0.000 | 0.020±0.001 | <0.050±0.000 | <0.050±0.000 | 0.550±0.001 | <0.050±0.000 | <0.050±0.000 | 0.022±0.001 | 0.070±0.001 |
| Gum Content (Mg/100ml) | 4.776±0.006 | 21.260±0.050 | 87.350±0.100 | 7.520±0.100 | 7.420±0.100 | 6.920±0.100 | 4.676±0.010 | 20.260±0.100 | 8.520±0.100 | 7.000±0.100 | 6.420±0.100 | 82.350±0.100 |
| Flash Point(°C) | 17.000±0.100 | 16.000±0.100 | 27.000±0.200 | 21.000±0.200 | 19.000±0.200 | 15.000±0.200 | 16.000±0.200 | 16.000±0.200 | 20.000±0.200 | 17.000±0.200 | 19.000±0.200 | 25.000±0.200 |
| Pour Point(°C) | -8.000±0.2000 | 14.000±0.200 | -9.000±0.200 | -16.000±0.200 | 14.000±0.200 | -5.000±0.200 | -6.000±0.200 | 13.000±0.200 | -15.000±0.200 | -5.000±0.200 | 10.000±0.200 | -8.000±0.200 |

Tables 2: Results of the bulk properties of crude oil samples from the producing fields

*cSt = centistroke, cP = centipoise

Table 3. Correlation matrix of bulk properties of the crude oil samples

|  | API@15°C | SG@15°C | RVP@37.7°C(psi) | KV@40°C(cSt) | Dynamic Viscosity @0°C(cP) | Moisture Content(V/V | Gum Content | Flash Point(°C) | Pour Point(°C) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| API@15°C |  |  |  |  |  |  |  |  |  |  |  |
| SG@15°C | -.959** |  |  |  |  |  |  |  |  |  |  |
| RVP@37.7°C(psi) | .b | .b | .b |  |  |  |  |  |  |  |  |
| KV@40°C(cSt) | -.609* | .731** | .b |  |  |  |  |  |  |  |  |
| Dynamic Viscosity @0°C(cP) | -.635* | .734** | .b | .951** |  |  |  |  |  |  |  |
| Moisture Content(V/V) | .106 | -.132 | .b | -.076 | -.106 |  |  |  |  |  |  |
| Gum Content (Mg/100ml) | -.605* | .728** | .b | .965** | .963** | .024 |  |  |  |  |  |
| Flash Point(°C) | -.594* | .602* | .b | .708** | .697* | -.100 | .605* |  |  |  |  |
| Pour Point(°C) | .195 | -.207 | .b | -.094 | -.226 | .353 | -.116 | .205 |  |  |  |
|  | **. Correlation is significant at the 0.01 level (2-tailed). |  |  |  |  |  |  |  |  |  |  |
|  | *. Correlation is significant at the 0.05 level (2-tailed). |  |  |  |  |  |  |  |  |  |  |
|  | b. Cannot be computed because at least one of the variables is constant. |  |  |  |  |  |  |  |  |  |  |

The bulk properties of crude oil and compositions for the studied oils are presented in Table 2, classification on the basis of physical characteristics (Sun et al., 2009; Odebunmi et al., 2002), which are commonly called commercial parameters has remained with the oil industry for the quality evaluation and pricing purposes. The results indicated that the crude oil from which the test samples were obtained are all comparable with crude oil of good or acceptable qualities from other locations in the world (Odebunmi et al., 2002).

API gravity measures how heavy or light crude oil is compared to water. Higher API values shows lighter oil, which is easier and cheaper to refine into high-demand products like gasoline and diesel and ranges from 30.540±0.100 - 42.460±0.100 across all locations. The American Petroleum Institute (API) classifies crude oil as light if API > 31°C, medium between 22.3°C–31.1°C, and heavy if < 22.3°C (Speight, 2014; EIA, 2020). All but one of the samples exceed 31.1° API, classifying them as light crudes. Even the lowest 30.540±0.100 (Sample C) sit just at the medium boundary. Light crudes command higher prices and require less severe cracking than medium or heavy oils (Speight, 2014).

Specific gravity ranges from 0.813±0.001 – 0.873±0.001. Commercial crude typically falls between 0.82-0.93 (Speight, 2006). The result all lie within this range. Lower specific gravity (0.813±0.001 -0.829±0.0001 correlate with the highest API gravity (40.150±0.100 - 42.460±0.100 API), confirming that the oils are very light. Higher specific (0.873±0.001) matches the 31.1°C API range, indicating slightly dense crude, since the API is less than 31.1°C. All samples lies within the normal commercial range and lower density crude oils flow easily in pipelines and require less heating (Speight, 2006).

Kinematic Viscosity (at 40°C) describes how easily oil flows at room temperature. Kinematic Viscosity ranges from 2.001±0.001 - 5.547±0.010cSt. Sample A (2.001±0.001) is thin and easy-flowing, while Sample C (5.547±0.010) is thick and sluggish. Lower viscosity means the crude can flow through pipelines more easily and needs less heating during refining. Viscosity directly affects pumping costs and equipment wear (Speight, 2014). Light crude oils generally range from 1-10 cSt at 400C (ASTM D445, 2015). All samples except C and L with values ranging from 2.001±0.001-3.000±0.010 cSt) sit in the easy flow zone typically of light crudes. Two samples (L and C) ranging from 5.447±0.010 - 5.547±0.010 cSt were below heavy oil levels (hundreds of cSt for tar-like bitumen), but would require modest heating or dilution to pump in colder pipeline (Riazi, 2005). These crude oils are relatively easy to pump and refine with minimal heating or blending.

Dynamic Viscosity (at 0°C) measures internal resistance to flow at higher temperature. Dynamic Viscosity ranges from 1.631±0.000 - 5.057±0.010 cP. Most samples fall between 1.631±0.000 - 2.630±0.010 cP, with the thickest around 5.057±0.010 cP. At refining temperatures, higher viscosity increases operational stress and energy use. Viscosity directly affects pumping costs and equipment wear (Speight, 2014). No absolute limit exists for crude, but value over 3.000 cP at 00C can hinder pipeline flow without heating. Only the single outlier (4.757±0.010 cP) would challenge cold-weather transport, the rest remain pumpable with minimal heating (ASTM D5293, 2016).

Moisture Content (% v/v) water present in crude oil, which can cause rust and interfere with refining. Moisture content ranges from <0.050±0.000 % - 0.500±0.010 %. Six samples < 0.05% and five samples below 0.5% and one at 0.55%. Industry typically requires ≤ 0.5-1.0% BS&W (ASTM D4928, 2017). All the samples were within the range.

Gum Content (mg/100ml) is the nonvolatile residue from oxidation or heavy hydrocarbons, a poxy for stability and fouling potential. Indicates quality degradation potential. Gum content ranges from 4.676±0.010 - 87.350±0.100. High gum is more deposited in engines and refineries. Sample C (87.350±0.100) and sample L (82.350±0.100) may require pretreatment. Finished fuels target ≤ 5-7mg/100 mL (ASTM D381, 2014); crude feed ideally as low as possible (Gary, Handwerk, and Kaiser, 2007). Three samples, A, G, K (4.7-6.9 mg/100 mL) are comparable to refined fuels. Others B, C, H, L (21-82 mg 100 mL) exceed that guideline, indicating potential heater /catalyst fouling and need for pre-treatment (Gary et al., 2007).

The  flash point measures  the temperature at which there is sufficient vapor  above a liquid sample to ignite a significant feature in product applications where it  is  used as a common safety specification (Onojake et al., 2014). Flash points are reflections of the boiling point of crude oils samples. Flash Point (°C) lowest temperature at which oil vapours ignite. Flash point ranges from 15.000±0.200 °C - 27.000±0.200 °C. NFPA classifies flash < 230C as extremely flammable; < 380C as flammable (NFPA, 2018).  Every sample falls in the flammable or extremely flammable class, requiring closed-vessel handling, vapour recovery, and explosion-prof equipment.

Pour Point is the lowest temperature oil still flows (ASTM international, 2016). Pour point ranges from –16.000±0.200°C (Sample D) to +14.000±0.200°C (Sample B). Oils with pour ≥ 00C risk gelling in cool climates. From the result, five samples pour below -5°C which is excellent for cold weather flow, while four exceed +5 °C and two exceed +10 °C, meaning they would need heating or pour point depressant additives in temperature zones (ASTM D97, 2016). Other parameters such as Reid Vapour Pressure due to low volatility, Cloud point, due to low content and Sulfur contents due to extremely low levels were not detected with respect to the geogenic nature of the crude oil in their locations (Coutinho & Daridon, 2005).

The correlation analysis Table 3 shows that the negative strong correlation (r= -0.959) of API and SG indicates, higher API, lower SG. Lower SG corresponds with lighter, high – API crude. SG and KV shows a strong positive correlation (r =0.731), as SG increase, KV tends to increase too, indicating that denser crude oil exhibits greater resistance to flow (higher KV). SG and Dynamic viscosity with r= 0.734, shows that heavier crude oils are more viscous, resisting flow at lower temperatures. KV and Dynamic viscosity with r = 0.951 show a strong correlation and hence related. KV and gum content with a strong correlation (r=0.965), indicates that as viscosity increases, the gum content increases too, this is because heavier fluids easily form residue.  Dynamic viscosity and gum content with a strong correlation r=0.963 indicates that the thicker the fluid, the stickier it gets. The flash point and KV shows a strong correlation of 0.708  which indicates that as thicker or more viscous oils require higher temperature to ignite.

4. CONCLUSION

This study provides a comparative analysis of the bulk properties of crude oil samples from four producing fields in the Niger Delta. Crude oil bulk properties such as API gravity, specific gravity, viscosity, and gum content are closely interrelated and serve as reliable indicators of crude quality. The variations in gum content and pour point suggest the need for selective pre-treatment and handling. These findings contribute to a better understanding of the commercial quality and processing requirements of Niger Delta crudes, aiding in field-specific refining, transport, and pricing strategies. There is  need to use specific gravity and viscosity to estimate other crude oil properties and guide refining decisions for better efficiency and quality control.

DISCLAIMER (ARTIFICIAL INTELLIGENCE)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc) and text-to-image generators have been used during writing or editing of this manuscript. COMPETING

INTERESTS Authors have declared that no competing interests exist.

REFERENCES

ASTM International. (2014). Standard test method for gum content of inhibited mineral oils (ASTM D381). West Conshohocken, PA: ASTM. https://www.savantlab.com/astm-methods/astm-d381-standard-test-method-for-gum-content-in-fuels-by-jet-evaporation/

ASTM International. (2015). Standard test method for kinematic viscosity of transparent and opaque liquids (and calculation of dynamic viscosity) (ASTM D445-15). West Conshohocken, PA: ASTM International. https://doi.org/10.1520/D0445-15

ASTM International. (2016). Standard test method for apparent viscosity of engine oils between –35 °C and –5 °C using the cold-cranking simulator (ASTM D5293-16). West Conshohocken, PA: ASTM International.
 https://kelid1.ir/FilesUp/ASTM_STANDARS_971222/D5293.PDF

ASTM International. (2016). Standard test method for pour point of petroleum products (ASTM D97-16). West Conshohocken, PA: ASTM International. https://doi.org/10.1520/D0097-16

ASTM International. (2016a). Standard test method for pour point of crude oils (ASTM D97). West Conshohocken, PA: ASTM. https://store.astm.org/d0097-15.html

ASTM International. (2016b). Standard test method for measurement of low temperature viscosity of petroleum distillates between −20°C and −55°C using a Stabinger viscometer (ASTM D5293). West Conshohocken, PA: ASTM. https://doi.org/10.1520/D5293-15

ASTM International. (2017). Standard test method for water in crude oil by Karl Fischer reagent (ASTM D4928). West Conshohocken, PA: ASTM. https://store.astm.org/d4928-00.html

Carey, F. A. (2003). Organic chemistry (5th ed., pp. 89–99). McGraw-Hill Press. https://imamhamzatcoed.edu.ng/library/ebooks/resources/organic_chemistry_by_Francis_A_Carey.pdf

Coutinho, J. & Daridon J. (2005). The limitations of cloud point measurement techniques and the influence of the oil composition on its detection. Petroleum Science and Technology, 23 (9-10), 1113-1128. https://path.web.ua.pt/filePST_2005_23_1113.pdf

EIA. (2017). Energy kids: Oil (petroleum). U.S. Energy Information Administration. https://web.archive.org/web/20170707183134/https://www.eia.gov/KIDS/energy.cfm?page=oil_home-basics-k.cfm

Gary, J. H., Handwerk, G. E., & Kaiser, M. J. (2007). Petroleum refining: Technology and economics (5th ed.). CRC Press. https://doi.org/10.4324/9780203907924

National Fire Protection Association. (2018). NFPA 30: Flammable and combustible liquids code. NFPA. https://www.nfpa.org/codes-and-standards/nfpa-30-standard-development/30

Odebunmi, E. O., Ogunsakin, E. A., & Ilkhor, P. E. P. (2002). Characterization of crude oils and petroleum products: (I) Elution liquid chromatographic separation and gas chromatographic analysis. Journal of the Chemical Society of Ethiopia, 16(2), 115–132. http://dx.doi.org/10.4314/bcse.v16i2.20934

Okeola, F. O., Amoloye, M. A., Adebayo, G. B., Abu, T. O., Ameen, O. M., & Obiechina, B. (2016). Comparative study of physicochemical parameters of some crude oil and petroleum products. Nigerian Journal of Pure and Applied Sciences, 29(2), 2987–2993. http://dx.doi.org/10.19240/njpas.2016.A32

Onojake, M. C., Osuji, L. C., & Oforka, N. C. (2014). Bulk Geochemical Characteristics of Crude Oils From the Umutu/Bomu Fields, Niger Delta, Nigeria. Petroleum Science and Technology, 32(5), 618-624.

Oyekunle, L. O., & Famakin, O. A. (2004). Studies of Nigerian crude oils: Characterization of crude oil mixtures. Petroleum Science and Technology, 22(5–6), 665–675. http://dx.doi.org/10.1081/LFT-120034207

Riazi, M. R. (2005). Characterization and properties of petroleum fractions. ASTM International. https://doi.org/10.1520/MNL50-EB

Speight, J. G. (2006). The chemistry and technology of petroleum (4th ed.). CRC Press. https://doi.org/10.1201/9781420008388

Speight, J. G. (2014). The chemistry and technology of petroleum (5th ed.). CRC Press. https://doi.org/10.1201/b16559

Sun, X., Hwang, J. Y., Huang, X., & Li, B. (2009). Petroleum coke particle size effect on the 	treatment of EAF dust through microwave heating. Journal of Materials  Characterization Engineering, 8(4), 249–259. http://dx.doi.org/10.4236/jmmce.2009.84022

Tissot, B. P., & Welte, D. H. (1984). Petroleum formation and occurrence (2nd ed.). Springer-Verlag. https://link.springer.com/book/10.1007/978-3-642-87813-8

Udeme, M., John, D., & Etim, I. U. (2012). Physicochemical studies of Nigeria’s crude oil blends. Petroleum and Coal, 54(3), 243–251. https://www.vurup.sk/wp-content/uploads/dlm_uploads/2017/07/pc_3_2012_dickson_173.pdf