OPTIMIZATION OF TURNING PROCESS PARAMETERS OF ALUMINUM ALLOY COW HORN COMPOSITE USING RSM.

Abstract

This paper examines the optimization of cow horn composite aluminum alloy turning process parameters. Manufacturers must develop an accurate model of the process to maximize the benefits of implementing hard turning. The machining input variables were connected to the machining output parameters. A356/cow horn particles (CHp) composite from Ochieze, 2017, was used to accomplish this and the composite composition by mass is 90% Aluminum alloy and 10% cow-horn reinforcement. To further improve the metal's wettability, magnesium powder (2% weight) was added to the molten metal, and the addition of magnesium powder increased the metal's surface energy, decreasing its surface tension and reducing the interface energy of the matrix reinforcement. The Response Surface Methodology was utilized to create the experiment's design. After optimization, several significant models are shown with a probability value of less than 0.05. The findings of the analyzed result show that the suggested mathematical models obtained from the data can accurately portray the performance within the limitations of the components under discussion. The investigation demonstrates that, as opposed to depth of cut, cutting speed considerably impacts surface roughness and tool wear rate. Adjusting the feed rate, depth of cut, and cutting speed to 900 rpm, 0.25 rev/mm, and 1.5 mm achieve the optimal composite turning process at a surface roughness of 160.256 mm, material removal rate of 15.4011 mm3/min, and tool wear of 0.000362687 mg/mm respectively.

Keywords: Tool Wear Ratio, Aluminum Alloy Cow Horn Composites, Material Removal Rate, Response Surface Methodology, Surface Roughness.

1.0 	INTRODUCTION

Materials having different chemical and physical characteristics that are insoluble in one another are combined to form composite materials [1-5]. Composite materials are well known for their extraordinary qualities, which include the presence of the matrix phase, a vital component that facilitates load transfer, structural integrity, and improved mechanical properties [6-11]. The composite materials' matrix and reinforcement can be constructed using metal, inorganic, and biological elements. Long and short fibers and particles are the two most common and utilized reinforcing materials [10, 12-16].

Composite materials are preferable to metals in various applications due to their high strength-to-weight ratio, which increases the performance level of diverse engineering applications, high stiffness, and good damage resistance under different operating conditions, thereby significantly advancing engineering to a higher level [17-20]. These unique features make them a desirable substitute for conventional materials in many technological applications to improve optimal performance [8, 17, 21, 22]. A few advantages of composite materials are their increased strength and stiffness, improved fatigue resistance, ability to endure heat, wear, corrosion, and decreased weight [23, 24]. Appropriate application-specific properties can be obtained by carefully organizing the metal matrix and adding reinforcement.

Metal Matrix Composites (MMC) are composite materials made from metals such as titanium, magnesium, and aluminum alloys. These materials, including particles, short (whiskers), or long fibers, reinforce MMC [25, 26].

One of the most crucial procedures of machining operations in material removal is metal cutting [27-29]. It has determined that developing optimization strategies for choosing cutting conditions in cutting operations quantitative forecasts of various technological performance metrics, ideally equations [30-34]. The critical technical technology for producing multiple mechanical components and products is machining requires optimum selections of best cutting conditions, thereby reducing material waste, time, and tool [35, 36]. A standard method of material removal in machining operations is turning. Many academics have investigated the geometrical and material properties of machining. A lack of experience and understanding of material machinability has hampered the use of machining in the industry, thereby increasing the rate at which accidents occur, damaging human beings and machines in use [37-40]. Fabricating numerous mechanical components requires dependable patterns and processes, repeatable processes, and precise instruments [41]. One of the common ways of making desired geometry components is through machining [42]. However, aluminum metal matrix composites (AMMCs) are among the most widely utilized composites because of their ease of fabrication, high strength, and lightweight [43, 44]. Disc brake development heavily uses composites in automotive and aerospace engines [45, 46]. In the turning operations machining process, the tool's life, the force required for cutting, the roughness of the machined surfaces, and energy consumption are the most crucial cutting performance indicators [42].

2.0 	MATERIALS AND METHODS

2.1	Materials

Materials incorporated into this project include; Aluminum alloy A356, Cow-horn particles and HSS cutting tool, Venier caliper, Measuring tape, Universal Turning Machining Centre (Micro tools DT  110), Surface tester (Surfcorder SE3500) and Dynamometer (XXR-UN01).

2.2	Methods

The cow-horn were collected and cleaned with a blower to remove impurities. Moisture content was removed by heating in an oven at 1150°C [26]. After being heated and cooled to room temperature, the dried cow horn was processed into a fine powder using a grinding machine. [47]. The powder was sieved to obtain particles of a uniform size of 150µm [47]. The mold samples were preheated for moisture removal and cooled at room temperature. The composite composition by mass is 90% Aluminum alloy and 10% cow-horn reinforcement [48]. The weights of the reinforcements (cow-horn) were determined using a compact electronic scale. The sourced Aluminum alloy weight for the composite was determined using a weighing balance, and pulverized cow horn was kept in a furnace preheated to improve wettability.

The aluminum alloy was heated to a temperature of 550°C in a crucible furnace powered by diesel, coupled to a temperature probe, and tested to ensure complete melting [48]. To further improve the metal's wettability, magnesium powder (2% weight) was added to the molten metal, and the addition of magnesium powder increased the metal's surface energy, decreasing its surface tension and reducing the interface energy of the matrix reinforcement. The preheated pulverized cow-horn particles were mixed with the liquid aluminum using an automated mechanical stirrer [49]. The composite mixture was super-heated at 550°C [48]. The composite was then created by pouring the combined aluminum alloy cow horn into a mold and letting it cure.

3.0	RESULTS

Machining Operation Using Design of Experiment (DOE)

A preliminary study on A356/cow horn particle composite formulation was done by examining how the machining parameters affect the created material. Three (3) excipients were chosen for A356/cow horn particle formulation based on their function. Two of them and the feed rate were used as variables in the I-optimal custom design as they may affect the responses. The variables' ranges were also studied using the I-optimal custom technique in design expert software. Table 1 shows the summary data table of the actual design after the experiment. Table 2 shows Model terms of build information.

Table 1: Summary data table of the actual design after experiment.

|  |  |  | Factor 1 | Factor 2 | Factor 3 | Response 1 | Response 2 | Response 3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Group | Run |  | a: Feed Rate | B: Cutting Speed | C: Depth of Cut | Surface Roughness | Material Removal Rate | Tool wear |
|  |  |  | rev/mm | rpm | mm | mm | mm3/min | mg/mm |
| 1 | AACHC1 | A | 0.15 | 500 | 1 | 121.994 | 24.32 | 0.00074 |
| 1 | AACHC2 | B | 0.15 | 900 | 1.5 | 157.78 | 16.67 | 0.00039 |
| 1 | AACHC3 | C | 0.15 | 900 | 1 | 155.86 | 19.54 | 0.00041 |
| 1 | AACHC4 | D | 0.15 | 500 | 1.5 | 122.211 | 23.34 | 0.00071 |
| 1 | AACHC5 | E | 0.15 | 700 | 0.5 | 124.202 | 22.24 | 0.00065 |
| 2 | AACHC6 | F | 0.15 | 700 | 1 | 127.289 | 20.52 | 0.00063 |
| 2 | AACHC7 | G | 0.15 | 900 | 1.5 | 157.78 | 16.67 | 0.00039 |
| 2 | AACHC8 | H | 0.15 | 700 | 1.5 | 133.484 | 20.29 | 0.00058 |
| 2 | AACHC9 | I | 0.15 | 500 | 0.5 | 119.094 | 30.91 | 0.00092 |
| 2 | AACHC10 | J | 0.15 | 900 | 0.5 | 136.311 | 19.61 | 0.00042 |
| 3 | AACHC11 | K | 0.25 | 900 | 1 | 162.794 | 4.61 | 0.00014 |
| 3 | AACHC12 | L | 0.25 | 900 | 1.5 | 168.47 | 3.75 | 0.00011 |
| 3 | AACHC13 | M | 0.25 | 500 | 0.5 | 131.121 | 15.8 | 0.00037 |
| 3 | AACHC14 | N | 0.25 | 700 | 0.5 | 149.205 | 9.5 | 0.00031 |
| 4 | AACHC15 | O | 0.25 | 900 | 0.5 | 162.194 | 9.31 | 0.00026 |
| 4 | AACHC16 | P | 0.25 | 500 | 1.5 | 158.032 | 12.11 | 0.00034 |
| 4 | AACHC17 | Q | 0.25 | 500 | 1 | 157.88 | 12.5 | 0.00036 |
| 4 | AACHC18 | R | 0.25 | 700 | 1 | 159.992 | 9.48 | 0.0003 |
| 4 | AACHC19 | S | 0.25 | 700 | 1.5 | 161.213 | 7.44 | 0.00028 |

Table 2: Model terms of build information

| Term | Standard Error* | Error df† | VIF | Restricted‡ VIF | Power |
| --- | --- | --- | --- | --- | --- |
| A | 0.5515 | 2 | 1.01974 | 1.00356 | 19.1 % |
| B | 0.2890 | 3 |  |  | 42.2 % |
| B | 0.1704 | 3 |  |  |  |
| C | 0.2930 | 3 |  |  | 41.1 % |
| C | 0.1688 | 3 |  |  |  |
| Ab | 0.2966 | 3 |  |  | 42.0 % |
| aB | 0.1694 | 3 |  |  |  |
| Ac | 0.2918 | 3 |  |  | 39.8 % |
| Ac | 0.1715 | 3 |  |  |  |
| BC | 0.3937 | 3 |  |  | 16.3 % |
| BC | 0.2457 | 3 |  |  |  |
| BC | 0.2173 | 3 |  |  |  |
| BC | 0.1309 | 3 |  |  |  |

The model terms help to determine the significance of the model and its impact in obtaining optimal result. The power ranges in Table 2 shows the true effect of the model and the power ensures reliability of the result generated.

Surface Roughness

Table 3: Model terms of surface roughness

| Source | Term df | Error df | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- |
| Whole-plot | 1 | 1.67 | 7.25 | 0.1380 | not significant |
| a-Feed Rate | 1 | 1.67 | 7.25 | 0.1380 |  |
| Subplot | 12 | 2.95 | 17.25 | 0.0203 | Significant |
| B-Cutting Speed | 2 | 2.93 | 63.28 | 0.0039 |  |
| C-Depth of Cut | 2 | 2.92 | 12.17 | 0.0384 |  |
| Ab | 2 | 2.95 | 2.28 | 0.2524 |  |
| Ac | 2 | 2.95 | 0.1118 | 0.8978 |  |
| BC | 4 | 3.02 | 2.12 | 0.2809 |  |

Table 3 shows the interactions and correlations of surface roughness over various input parameters. The surface roughness of the material is influenced positively by the cutting speed and depth of cut, which have a considerable effect; the surface roughness is not affected by feed rate. The material's surface roughness will rise with increased cutting depth and speed. Table 3 shows that model terms affect the cutting conditions when the P-value is less than 0.0500. B and C are essential model terms in this instance. Model terms are unimportant (have no influence) if their values are more extensive than 0.1000.

Table 4: Fit statistics of surface roughness

| Std. Dev. | 9.11 |  | R² | 0.9818 |
| --- | --- | --- | --- | --- |
| Mean | 145.63 |  | Adjusted R² | 0.8907 |
| C.V. % | 6.26 |  |  |  |

Table 5: Coefficients in terms of coded factors of surface roughness

| Source | Coefficient Estimate | Standard Error | VIF |
| --- | --- | --- | --- |
| Intercept | 144.50 | 4.24 |  |
| Whole-plot Terms: |  |  |  |
| a-Feed Rate | 11.42 | 4.24 | 1.00 |
| Subplot Terms: |  |  |  |
| B[1]-Cutting Speed | 12.16 | 1.11 |  |
| B[2] | 1.77 | 0.6620 |  |
| C[1]-Depth of Cut | 5.43 | 1.14 |  |
| C[2] | -1.09 | 0.6433 |  |
| aB[1] | -1.87 | 1.18 |  |
| aB[2] | -0.9317 | 0.6472 |  |
| aC[1] | -0.4497 | 1.14 |  |
| aC[2] | 0.2149 | 0.6709 |  |
| B[1]C[1] | 3.24 | 1.65 |  |
| B[2]C[1] | 2.45 | 1.07 |  |
| B[1]C[2] | -0.6823 | 0.8819 |  |
| B[2]C[2] | -1.08 | 0.5414 |  |

Table 4 shows the fit statistics for Ra. The table shows that the model added an excellent significant explanation of the data with R2 of 0.9818 and adjusted R2 of 0.8907. The high R2 and adjusted R2 value show that the model explains the data variation instead of being noisy. Obtaining an R-squared of 0.9818, which is in close proximity to 1, indicates that a noteworthy proportion of the data variation is captured by the model. Achieving an adjusted R-squared of 0.8907 suggests that model fit and complexity are well-balanced and also the surface roughness is well explained by input variables. Table 5 evaluates the coefficient in terms of coded factors of Ra.

Final Equation in Terms of Coded Factors

Surface Roughness=+144.50+11.42a+12.16B1+1.77B2+5.43C1-1.09C2-1.87aB1-0.9317aB2-0.4497aC1+0.2149aC2+3.24B1C1+2.45B2C1-0.6823B1C2-1.08B2C[2].

The Ra response can be predicted using the coded factors equation for specific levels of each factor. The coded equation assists in ascertaining the relative significance of the factors using a comparison of their factor coefficients. The link between the coded factors and the response variable is expressed in the final equation. Engineers can grasp how changes in one or more components affect the result by using this summary of the effects of several factors on surface roughness. The equation can be used to predict the reaction for specific factor sets without the need for additional trials. This predictive power helps with parameter optimization by identifying the optimal combination of variables to get the desired outcome.

Final Equation in Terms of Actual Factors

Surface Roughness=500CS×0.5DC+74.29615+254.05677FR×500CS×1DC+80.71898+296.09010FR×500CS×1.5DC+82.68288+287.19312FR×700CS×0.5DC+84.75815+259.7267FR×500CS×1DC+83.28848+301.76010FR+700CS×1.5DC+88.77588+292.86312FR+900CS×0.5DC+126.18321+115.34646FR+900CS×1DC+127.85104+157.37979FR+900CS×1.5DC+134.12148+148.48281FR

For certain levels of each element, the equation expressed in terms of the actual factors predicts the Ra response. Here, each factor's levels should be determined per their original units. Figure 1 shows the graph of predicted values and actual values of surface roughness.

Figure 1: Graph of predicted values and actual values of surface roughness.

The fact that the data points are nearly evenly distributed and have few outliers suggests that the data is normally distributed. The predictive model that was employed to estimate surface roughness is validated by the Figure 1. There is a good model fit as the points are near to the line of perfect agreement.

Material Removal Rate

Table 6: Model terms of MRR

| Source | Term df | Error df | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- |
| Whole-plot | 1 | 1.25 | 87.20 | 0.0412 | Significant |
| a-Feed Rate | 1 | 1.25 | 87.20 | 0.0412 |  |
| Subplot | 12 | 3.00 | 19.15 | 0.0166 | Significant |
| B-Cutting Speed | 2 | 2.83 | 77.05 | 0.0034 |  |
| C-Depth of Cut | 2 | 2.81 | 24.80 | 0.0164 |  |
| Ab | 2 | 2.88 | 0.2280 | 0.8092 |  |
| Ac | 2 | 2.88 | 0.1383 | 0.8763 |  |
| BC | 4 | 3.09 | 2.32 | 0.2535 |  |

Table 6 shows that P-values of the essential factors are significant, satisfying the peak performance of the model terms. Model terms A, B, and C are essential in this context. Table 6 displayed the relationships between material removal rate and input parameters. The relevant input parameters that are used have a beneficial impact on the material's MRR. With more input variables, the MRR will increase.

Table 7. Fit statistics of MRR

| Std. Dev. | 1.62 |  | R² | 0.9932 |
| --- | --- | --- | --- | --- |
| Mean | 15.72 |  | Adjusted R² | 0.9590 |
| C.V. % | 10.30 |  |  |  |

Table 8: Coefficients in terms of coded factors of MRR

| Source | Coefficient Estimate | Standard Error | VIF |
| --- | --- | --- | --- |
| Intercept | 15.59 | 0.6787 |  |
| Whole-plot Terms: |  |  |  |
| a-Feed Rate | -6.33 | 0.6775 | 1.00 |
| Subplot Terms: |  |  |  |
| B[1]-Cutting Speed | -3.63 | 0.2999 |  |
| B[2] | 0.4449 | 0.1796 |  |
| C[1]-Depth of Cut | -2.17 | 0.3103 |  |
| C[2] | 0.2956 | 0.1732 |  |
| aB[1] | 0.2101 | 0.3240 |  |
| aB[2] | -0.0311 | 0.1746 |  |
| aC[1] | -0.0870 | 0.3109 |  |
| aC[2] | 0.0898 | 0.1827 |  |
| B[1]C[1] | 0.8588 | 0.4708 |  |
| B[2]C[1] | -0.2694 | 0.3105 |  |
| B[1]C[2] | -0.5082 | 0.2449 |  |
| B[2]C[2] | 0.0658 | 0.1524 |  |

Table 7 shows the fit statistics for MRR. The table shows that the model added an excellent significant explanation of the data with R2 of 0.9932 and adjusted R2 of 0.9590. The high R2 and adjusted R2 value show that the model explains the data variation instead of being noisy. Table 8 evaluates the coefficient in terms of coded factors of MRR.

Final Equation in Terms of Coded Factors

Material Removal Rate=+15.59-6.33a-3.63B1+0.4449B2-2.17C1+0.2956C2+0.2101aB1-0.0311aB2-0.0870aC1+0.0898aC2+0.8588B1C1-0.2694B2C1-0.5082B1C2+0.0658B2C[2]

The MRR reaction can be predicted using the coded factors equation for specific levels of each factor. The link between the coded factors and the response variable is expressed in the final equation. Engineers can grasp how changes in one or more components affect the result by using this summary of the effects of several factors on material removal rate. The result for specific factor sets can be anticipated using the equation without conducting additional experiments. This predictive power helps with parameter optimization by figuring out the best combination of variables to get the desired outcome.

Final Equation in Terms of Actual Factors

Material Removal Rate=500CS×0.5DC+49.10438-128.74688FR×500CS×1DC+43.91938-127.54688FR×500CS×1.5DC+42.78625-125.30625FR×700CS×0.5DC+40.59938-123.64687FR×700CS×1DC+39.48938-122.44687FR×700CS+1.5DC+37.90625-120.20625FR×900CS×0.5DC+40.28125-129.10625FR×900CS×1DC+37.65625-127.90625FR×900CS×1.5DC+35.40203-125.66563FR

The equation stating the actual factors predicts the MRR response for specific levels of each factor. In this case, the levels of each factor should be stated in their respective units. Figure 2 shows the graph of predicted values and actual values of material removal rate.

Figure 2: Graph of predicted values and actual values of material removal rate.

A normal distribution of the data is suggested by the roughly equal distribution of the data points and the scarcity of outliers. Figure 2 provides confirmation for the prediction model used to measure material removal rate. Considering that the points are close to the line of perfect agreement, there is a good model fit.

Tool Wear

Table 9: Model terms of tool wear

| Source | Term df | Error df | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- |
| Whole-plot | 1 | 1.75 | 28.78 | 0.0436 | significant |
| a-Feed Rate | 1 | 1.75 | 28.78 | 0.0436 |  |
| Subplot | 12 | 2.95 | 50.42 | 0.0043 | significant |
| B-Cutting Speed | 2 | 2.94 | 185.48 | 0.0008 |  |
| C-Depth of Cut | 2 | 2.93 | 25.83 | 0.0137 |  |
| Ab | 2 | 2.95 | 32.88 | 0.0096 |  |
| Ac | 2 | 2.96 | 0.3995 | 0.7021 |  |
| BC | 4 | 3.01 | 3.15 | 0.1858 |  |

Table 9 shows that the P-values of the essential factors (A, B, C, and aB) are significant, satisfying the peak performance of the model terms. Table 9 presents the correlation between input parameters and tool wear. A positive effect on tool wear is produced by the pertinent input parameters that are applied. The wear of the tool will rise with more input variables and vice versa.

Table 10: Fit statistics of tool wear

| Std. Dev. | 0.0001 |  | R² | 0.9952 |
| --- | --- | --- | --- | --- |
| Mean | 0.0004 |  | Adjusted R² | 0.9714 |
| C.V. % | 15.17 |  |  |  |

Table 11: Coefficients in terms of coded factors of tool wear

| Source | Coefficient Estimate | Standard Error | VIF |
| --- | --- | --- | --- |
| Intercept | 0.0004 | 0.0000 |  |
| Whole-plot Terms: |  |  |  |
| a-Feed Rate | -0.0002 | 0.0000 | 1.00 |
| Subplot Terms: |  |  |  |
| B[1]-Cutting Speed | -0.0001 | 6.991E-06 |  |
| B[2] | -4.355E-06 | 4.164E-06 |  |
| C[1]-Depth of Cut | -0.0001 | 7.165E-06 |  |
| C[2] | 6.591E-06 | 4.055E-06 |  |
| aB[1] | 0.0001 | 7.404E-06 |  |
| aB[2] | -4.705E-07 | 4.078E-06 |  |
| aC[1] | -2.881E-06 | 7.182E-06 |  |
| aC[2] | 3.584E-06 | 4.217E-06 |  |
| B[1]C[1] | 0.0000 | 0.0000 |  |
| B[2]C[1] | 5.986E-06 | 6.682E-06 |  |
| B[1]C[2] | -0.0000 | 5.523E-06 |  |
| B[2]C[2] | -1.363E-06 | 3.384E-06 |  |

Table 10 shows the fit statistics for TWR. The table indicates that the model added an excellent significant explanation of the data with R2 of 0.9952 and adjusted R2 of 0.9714. The high R2 and adjusted R2 value show that the model explains the data variation instead of being noisy. Table 11 evaluates the coefficient in terms of coded factors of tool wear.

Final Equation in Terms of Coded Factors

Tool Wear=0.0004-0.0002a-0.0001B1-4.355E-06B2-0.0001C1+6.591E-0.6C2+0.0001aB1-4.705E-07aB2-2.881E-06aC1+3.584-06aC2+0.0000B1C1+5.986E-06B2C1-0.0000B1C2-(1.363E-06B2C[2])

The reaction can be predicted using the coded factors equation for specific levels of each factor. The relative significance of the factors can be ascertained using the coded TWR equation and factor coefficient comparison. The link between the coded factors and the response variable is expressed in the final equation. Engineers can grasp how changes in one or more components affect the result by using this summary of the effects of several factors on tool wear rate. The equation can be used to anticipate the response for specific factor sets without conducting additional trials. This predictive skill supports parameter optimization by identifying the optimal combination of factors to yield the desired outcome.

Final Equation in Terms of Actual Factors

Tool Wear=500CS×0.5DC+0.001546-0.004504FR×500CS×1DC+0.001404-0.00427FR×500CS+1.5DC+0.001370-0.004225FR×700CS×0.5DC+0.001161-0.003404FR×700CS×1DC+0.001099-0.003171FR×700CS×1.5DC+0.001055-0.003125FR×900CS×0.5DC+0.000858-0.002592FR+900CS×1DC+0.000747-0.002358FR+900CS×1.5DC+0.000721-0.002313FR

The TWR for specific levels of each ingredient can be examined using the real factors equation. In this instance, the levels of each element should be stated in their original units. Figure 3 shows the graph of predicted values and actual values of tool wear.

Figure 3: Graph of predicted values and actual values of tool wear

The small number of outliers and the relatively equal distribution of the data points lead to a normal distribution of the data. The prediction model used to calculate the material removal rate is validated in Figure 3. A good model fit is evident given that the points are near the line of complete agreement.

Optimization using RSM

The Design-expert software's module for optimization looks for a mix of factor levels that concurrently satisfies all responses and process factors. By choosing the desired outcomes for each element and response, numerical optimization techniques were applied in this work. The AACHCs' numerical optimization procedure was successful at a desirability function of 1. The optimization depicted in Figure 4 enhances the machining procedure by modifying parameters to accomplish the intended results, which include reduced tool wear, effective material removal, and a better surface polish. The optimization treatments' outcomes are emphasized by the red dots, which draw attention to particular data points.

Figure 4: Graph of numerical optimization of AACHC

Figure 4 shows the graph of numerical optimization of AACHC. The optimal value was achieved when the feed rate, cutting speed, and depth of cut were at 0.16161 rev/mm, 900 rpm, and 1.5 mm, and it gives the best response at a surface roughness of 160.256 mm, material removal rate of 15.4011 mm3/min, and tool wear of 0.000362687 mg/mm respectively.

4.0	CONCLUSION

This paper examines the optimization of cow horn composite aluminum alloy 356 turning process parameters. The samples were investigated for Ra, MRR after machining with the TWR. From the results of the analyses, the following conclusions are drawn:

- AACHC, adopted from Ochieze, 2017 was successfully utilized for this investigation.

- The ANOVA tables of the TWR, Ra, and MRR demonstrate that some models have significant probability values (P-values) less than 0.05.

- Numerical optimization was used to identify combinations of process parameters and to attain the lowest TWR, MRR, and Ra possible.

- The impact of process factors on responses was examined individually and in interaction. Cutting speed has an enormous effect on TWR and Ra, as evidence.

- The TWR and Ra are only a little influenced by the depth of the cut.

- The regression equation model generated can predict the coded, actual factors' Ra, TWR, and MRR.

- Adjusting the feed rate, depth of cut, and cutting speed to 900 rpm, 0.25 rev/mm, and 1.5 mm achieve the optimal composite turning process.

- This research is valuable because it provides information on the optimal input parameters to be used in order to achieve the ideal output parameters. These parameters will minimize material waste, boost energy consumption, and yield the best surface finishing.

5.0	REFERENCES

- Yi, X. S. An Introduction to Composite Materials. In: Yi, XS., Du, S., Zhang, L. (eds) Composite Materials Engineering. Springer, Singapore. 2018;1. https://doi.org/10.1007/978-981-10-5696-3_1.

- Chauhan, A. K., Singh, A., Kumar, D., & Mishra, K. (2021). Properties of Composite Materials. In Composite Materials (pp. 61–78). CRC Press. https://doi.org/10.1201/9781003080633-3.

- Ngo, T.-D. (2020). Introduction to Composite Materials. In Composite and Nanocomposite Materials - From Knowledge to Industrial Applications. IntechOpen. https://doi.org/10.5772/intechopen.91285.

- Reduwan Billah, S. M. (2019). Composites and Nanocomposites (pp. 1–67). https://doi.org/10.1007/978-3-319-92067-2_15-1.

- Yi, X.-S. (2018). An Introduction to Composite Materials. In Composite Materials Engineering, Volume 1 (pp. 1–61). Springer Singapore. https://doi.org/10.1007/978-981-10-5696-3_1.

- Kumar, A.; Grover, N.; Manna, A. et al. Multi-Objective Optimization of WEDM of Aluminum Hybrid Composites Using AHP and Genetic Algorithm.  Arab J Sci Eng. 2022;47:8031–8043. https://doi.org/10.1007/s13369-021-05865-4.

- Hasan, K. M. F., Horváth, P. G., & Alpár, T. (2021). Potential fabric-reinforced composites: a comprehensive review. Journal of Materials Science, 56(26), 14381–14415. https://doi.org/10.1007/s10853-021-06177-6.

- Kangishwar, S., Radhika, N., Sheik, A. A., Chavali, A., & Hariharan, S. (2023). A comprehensive review on polymer matrix composites: material selection, fabrication, and application. Polymer Bulletin, 80(1), 47–87. https://doi.org/10.1007/s00289-022-04087-4.

- M. Dawoud, M., & M. Saleh, H. (2019). Introductory Chapter: Background on Composite Materials. In Characterizations of Some Composite Materials. IntechOpen. https://doi.org/10.5772/intechopen.80960.

- Selvam, J. D. R., Dinaharan, I., & Rai, R. S. (2021). Matrix and Reinforcement Materials for Metal Matrix Composites. In Encyclopedia of Materials: Composites (pp. 615–639). Elsevier. https://doi.org/10.1016/B978-0-12-803581-8.11890-9.

- Singh, H., Singh Brar, G., Kumar, H., & Aggarwal, V. (2021). A review on metal matrix composite for automobile applications. Materials Today: Proceedings, 43, 320–325. https://doi.org/10.1016/j.matpr.2020.11.670.

- Chairi, M., El Bahaoui, J., Hanafi, I., Mata Cabrera, F., & Di Bella, G. (2023). Composite Materials: A Review of Polymer and Metal Matrix Composites, Their Mechanical Characterization, and Mechanical Properties. In Next Generation Fiber-Reinforced Composites - New Insights. IntechOpen. https://doi.org/10.5772/intechopen.106624.

- Egbo, M. K. (2021). A fundamental review on composite materials and some of their applications in biomedical engineering. Journal of King Saud University - Engineering Sciences, 33(8), 557–568. https://doi.org/10.1016/j.jksues.2020.07.007.

- M. Dawoud, M., & M. Saleh, H. (2019). Introductory Chapter: Background on Composite Materials. In Characterizations of Some Composite Materials. IntechOpen. https://doi.org/10.5772/intechopen.80960.

- Pramanik, S., Cherusseri, J., Baban, N. S., Sowntharya, L., & Kar, K. K. (2017). Metal Matrix Composites: Theory, Techniques, and Applications. In Composite Materials (pp. 369–411). Springer Berlin Heidelberg. https://doi.org/10.1007/978-3-662-49514-8_11.

- Rajak, D., Pagar, D., Menezes, P., & Linul, E. (2019). Fiber-Reinforced Polymer Composites: Manufacturing, Properties, and Applications. Polymers, 11(10), 1667. https://doi.org/10.3390/polym11101667.

- Alam, M. A., Ya, H. H., Sapuan, S. M., Mamat, O., Parveez, B., Yusuf, M., Masood, F., & Ilyas, R. A. (2022). Recent Advancements in Advanced Composites for Aerospace Applications: A Review. In Advanced Composites in Aerospace Engineering Applications (pp. 319–339). Springer International Publishing. https://doi.org/10.1007/978-3-030-88192-4_16.

- Asyraf, M. R. M., Ilyas, R. A., Sapuan, S. M., Harussani, M. M., Hariz, H. M., Aiman, J. M., Baitaba, D. M., Sanjay, M. R., Ishak, M. R., Norkhairunnisa, M., Sharma, S., Alam, M. A., & Asrofi, M. (2022). Advanced Composite in Aerospace Applications: Opportunities, Challenges, and Future Perspective. In Advanced Composites in Aerospace Engineering Applications (pp. 471–498). Springer International Publishing. https://doi.org/10.1007/978-3-030-88192-4_24.

- Parveez, B., Kittur, M. I., Badruddin, I. A., Kamangar, S., Hussien, M., & Umarfarooq, M. A. (2022). Scientific Advancements in Composite Materials for Aircraft Applications: A Review. Polymers, 14(22), 5007. https://doi.org/10.3390/polym14225007.

- Rajak, D., Pagar, D., Menezes, P., & Linul, E. (2019). Fiber-Reinforced Polymer Composites: Manufacturing, Properties, and Applications. Polymers, 11(10), 1667. https://doi.org/10.3390/polym11101667.

- Padhan, S.; Dash, L.; Behera, SK.; Das, SR. Modeling and Optimization of Power Consumption for Economic Analysis, Energy-Saving Carbon Footprint Analysis, and Sustainability Assessment in Finish Hard Turning Under Graphene Nanoparticle–Assisted Minimum Quantity Lubrication. Process Integration and Optimization for Sustainability. 2020;4:445-463. https://doi.org/10.1007/s41660-020-00132-9.

- Yi, X.-S. (2018). An Introduction to Composite Materials. In Composite Materials Engineering, Volume 1 (pp. 1–61). Springer Singapore. https://doi.org/10.1007/978-981-10-5696-3_1.

- Ic, YT.; Saraloğlu Güler, E.; Sezer, B. et al. Multi-objective Optimization of Turning Parameters for SiC- or Al2O3-Reinforced Aluminum Matrix Composites. Process Integr Optim Sustain. 2021;5:609–623. https://doi.org/10.1007/s41660-021-00169-4

- Butola, R.; Sharma, V.; Kanwar, S. et al. Optimizing the machining variables in CNC turning of aluminum-based hybrid metal matrix composites. SN Appl. Sci. 2020;2:1356. https://doi.org/10.1007/s42452-020-3155-8.

- Geng, L.; Wu, K. Metal Matrix Composites. In: Yi, XS., Du, S., Zhang, L. (eds) Composite Materials Engineering. Springer, Singapore. 2018;2. https://doi.org/10.1007/978-981-10-5690-1_3.

- Ahamed, S.; Roshan, JD.; Shilpa, PC. A literature review on aluminium-7075 metal matrix composites. International Research Journal of Engineering and Technology. 2019;6(6): 1384-1390.

- Omietimi, H., Afolalu, S. A., Kayode, J. F., Monye, S. I., Lawal, S. L., & Emetere, M. E. (2023). An overview of material removal processes and its importance. E3S Web of Conferences, 391, 01077. https://doi.org/10.1051/e3sconf/202339101077.

- Stephenson, D. A., & Agapiou, J. S. (2018). Metal Cutting Theory and Practice. CRC Press. https://doi.org/10.1201/9781315373119.

- Valaki, J. (2021). Experimental study on feasibility of a novel vegetable oil-based pressurized spray cooling system for sustainable surface grinding process. In Sustainable Manufacturing (pp. 61–86). Elsevier. https://doi.org/10.1016/B978-0-12-818115-7.00005-5.

- Chen, X., Li, C., Tang, Y., Li, L., & Li, H. (2021). Energy efficient cutting parameter optimization. Frontiers of Mechanical Engineering, 16(2), 221–248. https://doi.org/10.1007/s11465-020-0627-x.

- Li, B., Tian, X., & Zhang, M. (2020). Modeling and multi-objective optimization of cutting parameters in the high-speed milling using RSM and improved TLBO algorithm. The International Journal of Advanced Manufacturing Technology, 111(7–8), 2323–2335. https://doi.org/10.1007/s00170-020-06284-9.

- Tefera, A. G., Sinha, D. K., & Gupta, G. (2023). Experimental investigation and optimization of cutting parameters during dry turning process of copper alloy. Journal of Engineering and Applied Science, 70(1), 145. https://doi.org/10.1186/s44147-023-00314-5.

- Trifunović, M., Madić, M., Marinković, D., & Marinković, V. (2023). Cutting Parameters Optimization for Minimal Total Operation Time in Turning POM-C Cylindrical Stocks into Parts with Continuous Profile Using a PCD Cutting Tool. Metals, 13(2), 359. https://doi.org/10.3390/met13020359.

- Wang, J. (2024). Intelligent Optimization of Cutting Parameters (pp. 25–65). https://doi.org/10.1007/978-981-99-2011-2_2.

- Wen, X., Liu, J., Du, C., Qu, P., Sheng, S., Liu, X., Zhou, H., Kang, C., Chen, Y., & Dong, L. (2022). The key technologies of machining process design: a review. The International Journal of Advanced Manufacturing Technology, 120(5–6), 2903–2921. https://doi.org/10.1007/s00170-022-08982-y.

- Zhu, K. (2022). Introduction to the Smart Machining System (pp. 1–18). https://doi.org/10.1007/978-3-030-87878-8_1.

- Finn, M. E., & Tartaglia, J. M. (2022). Prevention of Machining-Related Failures. Journal of Failure Analysis and Prevention, 22(1), 191–202. https://doi.org/10.1007/s11668-021-01329-x.

- Jamil, M., He, N., Wei, Z., Mushtaq, R. T., Khan, A. M., Hegab, H., Gupta, M. K., & Khanna, N. (2024). A state-of-the-art review on sustainability evaluation of machining processes involving the effects of advanced cooling technologies. The International Journal of Advanced Manufacturing Technology, 131(9–10), 4377–4402. https://doi.org/10.1007/s00170-024-13303-6.

- Pimenov, D. Y., Kiran, M., Khanna, N., Pintaude, G., Vasco, M. C., da Silva, L. R. R., & Giasin, K. (2023). Review of improvement of machinability and surface integrity in machining on aluminum alloys. The International Journal of Advanced Manufacturing Technology, 129(11–12), 4743–4779. https://doi.org/10.1007/s00170-023-12630-4.

- Rance, J., Hall, S., de Bartolomeis, A., & Shokrani, A. (2019). Future Direction of the Sustainable Turning of Difficult-to-Machine Materials (pp. 111–120). https://doi.org/10.1007/978-981-13-9271-9_11.

- Finn, M. E., & Tartaglia, J. M. (2022). Prevention of Machining-Related Failures. Journal of Failure Analysis and Prevention, 22(1), 191–202. https://doi.org/10.1007/s11668-021-01329-x.

- Selvakumara, S.; Ravikumar, R. Experimental analysis and mathematical modeling of optimized cutting parameters in micro turning. Indian Journal of Engineering & Materials Sciences. 2014;21:397-408.

- Ayar, M. S., George, P. M., & Patel, R. R. (2021). Advanced research progresses in aluminium metal matrix composites: An overview. 020026. https://doi.org/10.1063/5.0036141.

- Vasava, A. S., & Singh, D. (2021). A Review on the Manufacturing of Aluminum Metal Matrix Composite by Various Stir Casting Method (pp. 341–349). https://doi.org/10.1007/978-981-16-3033-0_32.

- Biswas, P., & Mondal, M. K. (2023). Evaluation of a Cast Al-Mg2Si Composite for Automobile Disk-Brake Rotor Application. Journal of Materials Engineering and Performance. https://doi.org/10.1007/s11665-023-08760-1.

- Singh, M., Garg, H. K., Maharana, S., Muniappan, A., Loganathan, M. K., Nguyen, T. V. T., & Vijayan, V. (2023). Design and Analysis of an Automobile Disc Brake Rotor by Using Hybrid Aluminium Metal Matrix Composite for High Reliability. Journal of Composites Science, 7(6), 244. https://doi.org/10.3390/jcs7060244.

- Prasad, SK.; Krishna, RA. Production and mechanical properties of A356.2/RHA composites. International Journal of Advanced Science and Technology. 2011;33:51–58.

- Ochieze, BQ.; Nwobi-Okoye, CC.; Atamuo, PN. Experimental Study of the Effect of Wear Parameters on the Wear Behavior of A356 alloy/cow Horn Particulate Composites, Journal of Elsevier. 2017;14(1):77-81. https://doi.org/10.1016/j.dt.2017.11.001.

- Nwobi-Okoye, CC.; Uzochukwu, CU. RSM and ANN modeling for production of Al 6351/ Egg Shell Reinforced Composite: Multi objective optimization using genetic algorithm. 2019;PII:S2352-4928(19)30689-0 DOI: https://doi.org/10.1016/j.mtcomm.2019.100674.