Review Article

A Comprehensive Review of Water-Absorbing Superabsorbent Polymers for Enhancing Concrete Performance”

Abstract:

Superabsorbent polymers (SAPs) have become one of the most promising materials for improving the mechanical, durability, and functional performance of modern cementitious systems. This comprehensive review synthesizes findings from existing high-impact literature and studies to provide a unified understanding of SAP behavior in concrete. SAPs exhibit exceptional water absorption and controlled release capabilities. These features directly influence hydration kinetics, internal curing efficiency, shrinkage mitigation, microstructural refinement, and long-term durability. The review examines SAP impacts on compressive and tensile strength, shrinkage (plastic, autogenous, drying), water–cement ratio sensitivity, and ultrasonic pulse velocity (UPV) as an indicator of internal homogeneity. Extensive findings from microstructure analysis reveal that SAPs refine hydration products, modify gel porosity, and influence the interfacial transition zone (ITZ). Moreover, SAP beads (>1 mm) called as water absorbing beads act as spherical internal reservoirs that provide prolonged water release, improving self-desiccation resistance while functioning as intentional lightweight inclusions that adjust density, thermal conductivity, and insulation capacity. SAP-modified concretes show improved resistance to chloride penetration, carbonation, salt-scaling, and mechanical degradation, particularly under low-humidity or sealed-curing environments. Thermal analyses demonstrate dual roles: (1) SAP voids enhance insulation by reducing conductivity; (2) SAP-driven microstructural refinement improves thermal mass stability for building energy applications. This review presents insights into SAP behavior and optimal dosages. The optimal dose of fine granular SAP (<1mm) is recommended as 0.15–0.35% by cement weight in dry form and is 8–12% by volume of coarse aggregates in expanded form for SAP beads (>1mm). Critical research gaps are identified regarding field-scale validation, SAP beads, thermophysical behavior, and multi-physics modeling. Recommendations for mix design, curing protocols, and performance prediction models are presented to support the integration of SAPs into advanced, durable, and sustainable concrete.

Keywords: Superabsorbent Polymer (SAP); Shrinkage; Durability; Microstructure; Concrete; Insulation; Heat Transfer.

1. INTRODUCTION

Concrete remains the most widely used man-made material, yet its performance is increasingly challenged by autogenous shrinkage, early-age cracking, durability degradation, and severe environmental exposure. High-performance concretes (HPCs) with low water-cement ratios (w/c < 0.35) are particularly vulnerable to self-desiccation, leading to internal relative humidity (IRH) drops and microcracking. Traditional external curing techniques often fail to maintain sufficient internal moisture. Control joints or pre-planned cuts in the concrete floor are generally provided to relief random cracks. Superabsorbent polymers (SAPs) are capable of reducing these shrinkage cracks when used in concrete. SAPs absorb water upto 1000 times of their weight (Boshoff et al., 2020; Yang et al., 2019; Hasholt et al., 2015 and 2012).

2. SUPERABSORBENT POLYMERS: CHEMISTRYAND BEHAVIOR

2.1 Chemical Structure and Absorption Mechanisms

Superabsorbent polymers (SAPs) used in cementitious materials encompass a broad range of chemistries, including polyacrylate and polyacrylamide polymer networks, which remain the most widely adopted due to their high water absorption capacity and predictable swelling behavior. Other modern SAP systems include natural polymer–grafted hydrogels, inorganic–organic hybrids such as silica–polymer composites, and functionalized hydrogels engineered to respond to thermal or pH variations within the cement matrix. Their water absorption behavior is strongly dictated by the polymer’s cross-linking density, ionic charge distribution, particle size, and the chemistry of the cement pore solution, particularly its alkalinity and ion concentration. The mixing energy and shear rate during batching further influence SAP swelling kinetics. SAP beads larger than 1 mm typically absorb water more slowly than fine granular SAPs but can retain significantly larger water volumes, thereby functioning as macroscopic spherical internal curing reservoirs.

2.2 Swelling, Desorption, and Timing

The swelling and subsequent water release of SAPs during hydration are controlled by several interrelated mechanisms, including chemical shrinkage–induced suction, internal relative humidity gradients, capillary pressure development, and the rate of cement hydration. These factors determine the timing of desorption, which is critical for effective internal curing. Recent innovations include delayed-absorption SAPs, which are engineered to swell only after the formation of initial hydration shells around cement grains. This controlled swelling minimizes early-age void formation and enhances the mechanical performance of the hardened matrix (Morinaga et al., 2022).

2.3 Influence of SAP Size

SAPs exist in two primary forms:

- Fine granular SAPs (50µm-1mm): There sizes are less than 1mm in dry state. When used in concrete, it improves internal curing, increase matrix density, and enhance hydration, leading to higher compressive strength.

- Spheres or SAP Beads (1-4mm): These are used as water-absorbing lightweight inclusions. They are more effective at reducing shrinkage in concrete but can result in slightly lower strength and stiffness.

Figure 1(a) and 1(b) shows dried form of fine granular SAP and SAP beads respectively.

| Figure 1(a) Fine granular SAP | Figure 1(b) SAP beads >1mm |
| --- | --- |

Extensive research (RILEM TC-260, fib Commission 5, ACI-308) confirms that SAPs enhance hydration, reduce autogenous shrinkage, mitigate restrained stresses, and refine microstructure. At the same time, SAPs influence density, thermal conductivity, and energy absorption behavior. This article provides a multi-scale review of SAP-enhanced concrete, covering mechanical, microstructural, durability, thermal, and rheological perspectives. This review combines advanced multi-physics studies, sustainability and thermally oriented studies on SAPs used in concrete. The objective is to deliver an integrated understanding of SAP effects across all major performance domains. Table 1 describe characteristics of SAP and SAP Beads (>1 mm).

Table 1. Characteristics of Fine granular SAP and SAP Beads (>1 mm)

| Characteristic | SAP or Fine granular SAP | SAP Beads |
| --- | --- | --- |
| Particle size | 100–1000 µm | 1–4 mm |
| Absorption speed | Fast | Slow |
| Water storage | Low–medium | Very high |
| Void size created | Microvoids (50–1000 µm) | Macrovoids (1–12 mm) |
| Strength impact | Minor | Moderate–high reduction |
| Thermal insulation | Moderate | High |
| Best application | HPC, UHPC, shrinkage control | Insulated panels, lightweight concrete |

SAP particle size also plays a decisive role in concrete performance. Small particles in the range of 50–200 μm tend to distribute uniformly throughout the cement paste, dissolving within the hydration products and refining the microstructure (Snoeck, et al., 2015). Medium-sized SAP particles (200 μm to 1 mm) provide an optimal balance between distribution and water-storage capacity, ensuring effective internal curing across a larger microstructural volume. In contrast, SAP beads greater than 1 mm in diameter behave similarly to lightweight inclusions, significantly influencing thermal insulation and acoustic performance while creating larger, stable voids that can function as long-term moisture reservoirs. Together, these size-dependent behaviors highlight the multifunctional role of SAPs in enhancing both structural and thermal performance of concrete.

3. INFLUENCE OF SAPS ON FRESH AND HARDENED CONCRETE PROPERTIES

3.1 Workability and Rheology

SAPs significantly alter the fresh-state rheology of cementitious mixtures. When dry SAPs are added, they immediately absorb a portion of the mix water, reducing the effective water–binder ratio (w/b). This results in increased viscosity, decreased slump, and higher yield stress. Agostinho et al. (2021) demonstrated that nano silica exerts stronger influence on rheology than SAPs, but SAPs still increase paste viscosity by 5–20% depending on dosage and particle size.

Pre-saturated SAPs maintain workability because they do not draw water during mixing. Studies by Huang et al. (2022) and RILEM TC-260 indicate that pre-absorbing SAPs in mixing water (teabag method) produces consistent workability while ensuring immediate internal curing.

SAP beads (>1 mm) behave differently. Their large size and low-density act similarly to lightweight aggregates, improving flowability due to ball-bearing effects, especially in self-compacting concretes (SCC). However, excessive bead content may introduce segregation risks.

3.2 Compressive Strength

SAPs influence compressive strength in two competing ways:

  - Negative effect: Void formation

When SAPs release their absorbed water, empty voids (50µm – 1mm) remain, which can reduce strength:

- Strength drops typically 5–15% for 0.2–0.6% SAP dosage (Zheng et al. 2021).

- Larger SAP beads (>1 mm) cause more pronounced strength reduction at early ages due to high-volume voids.

  - Positive effect: Improved hydration and microstructure

SAPs provide internal water for continued hydration, resulting in:

- Higher degree of hydration

- Lower autogenous shrinkage

- Reduced microcracking

- Denser C–S–H and ITZ

SAP beads typically reduce compressive strength, but when used intentionally as lightweight inclusions, they support insulation and thermal mass objectives. Delayed-absorption SAPs (Morinaga et al., 2022) demonstrated up to 30% higher compressive strength under sealed and low-humidity curing compared to reference concrete. Most studies show slight strength loss is common at 7 days curing age. At 28–90 days, SAP concrete often matches or exceeds reference concrete strength. Under sealed or low-RH conditions, SAP mixes outperform conventional cures.

3.3 Tensile and Flexural Strength

Tensile performance is more sensitive to microcracking than to porosity. SAPs reduce micro strain during hydration, leading to improved tensile strength in many cases.

- SAP + fiber concretes show 15–40% improvements in tensile and flexural strength due to crack control and moisture availability.

- For typical SAP powder additions (0.2–0.4%), tensile strength reductions are limited to <10%.

- When SAP beads are used (>1 mm), tensile strength reduction increases due to larger void formation but can be balanced with fiber reinforcement (polypropylene, basalt, or steel fibers).

4. SHRINKAGE CONTROL WITH SAPS

SAPs represent one of the most effective technologies for reducing plastic, autogenous, and drying shrinkage.

  - Plastic Shrinkage

SAPs mitigate plastic shrinkage by retaining water near the surface, slowing the evaporation process and reducing capillary pressure buildup. Different researchers noted 50–80% reduction in plastic shrinkage cracking area. Complete crack elimination was achieved when SAPs are combined with fibers. This makes SAPs particularly valuable in 3D-printed concrete, pavement slabs, and hot-weather concreting (Van der Putten et al., 2021; Olawuyi, & Boshoff, 2017)

4.2 Autogenous Shrinkage

Autogenous shrinkage is reduced due to internal curing. Numerous studies (Jensen & Hansen, 2001; RILEM 260-RSC; Morinaga et al., 2022) consistently show 60–90% reduction in autogenous shrinkage. Near-zero early-age tensile stress in SAP mixes and excellent performance in high-strength concrete (HSC) and UHPC was noted in past studies due to reduction in autogenous shrinkage. In 3D-printed concrete, SAPs reduced autogenous shrinkage by up to 200% (Van Der Putten et al. 2021).

4.3 Drying Shrinkage

Drying shrinkage is more complex. SAPs reduce early-age drying shrinkage by maintaining internal RH. Prolonged drying may enlarge SAP voids, increasing long-term shrinkage unless mix design is optimized. Studies show 20–40% reduction in drying shrinkage under moderate SAP dosages. Slight long-term increases under high SAP content (>0.6%). SAP–expansive agent (KEA) synergy reduces total shrinkage by up to 20% at 91 days (Zhang et al., 2021).

5. INTERNAL CURING EFFECTIVENESS

Internal curing (IC) is the core function of SAPs. Hydration-induced chemical shrinkage creates a negative capillary pressure inside the cement matrix. SAPs counteract this by releasing stored water, maintaining internal RH >80%.

  - Internal RH Maintenance

Studies using Nuclear Magnetic Resonance (NMR) and humidity sensors shows that SAPs maintain internal humidity 20–40% higher than control mixes. SAP cavities remain water-filled for 9–12 hours after mixing (Ji, Y., et al., 2019). Non-retentive SAPs release water quickly but retain cavities until suction pulls water into the matrix (Zhong et al., 2021)

  - Effect in Low w/c Systems

In systems with w/c < 0.30, SAPs ensure complete hydration of C3S and partial hydration of C2S that results in fewer autogenous cracks. Increased long-term strength and reduced interfacial transition zone (ITZ) porosity is attained for concrete prepared with low water cement ratio. SAP beads (>1 mm) are especially effective internal curing reservoirs due to their large water-holding capacity.

6. EFFECT OF SAP ON WATER–CEMENT RATIO (W/C)

SAP addition changes the effective water–cement ratio (w/c effective):

w/c effective=​W​​​total-WSAP-absorbed​C

Incorporation of dry SAPs reduce w/c effective, increasing strength early but increasing shrinkage risk if not offset by released water. Pre-saturated SAPs maintain consistent w/c during mixing. High-performance concretes with low w/c benefit significantly from SAP-controlled hydration, achieving hydration degrees similar to concretes with much higher w/c.

7. SAP EFFECTS ON ULTRA-PULSE VELOCITY (UPV)

UPV is an excellent indicator of microstructural uniformity, stiffness, crack density and durability. Study shows that UPV decreases initially due to SAP-induced macropores (100µm – 1mm) that reduce elastic modulus. Early-age UPV may drop by 5–20%. UPV correlates with compressive strength in SAP concretes using modified empirical equations:

V=kfcn
where:

V	= UPV (km/s)
fc	= compressive strength
k,n	= SAP-dependent coefficients

SAP beads require modified coefficients due to larger void influence.

UPV increases long-term as internal curing improves hydration and reduces microcracking. Internal curing densifies matrix of concrete. UPV increases by 5–12% over 28–90 days. Even some SAP mixes surpass control mixes after 2 months of curing. This confirms that SAPs enhance long-term structural integrity. SAP in addition with fiber combinations show the highest UPV improvements.

Large spherical SAP beads (> 1mm) cause more significant early-age UPV reduction because wave velocity decreases significantly in the presence of large air cavities. However, their advantages in internal curing and thermal insulation outweigh UPV limitations depending on application.

8. THERMAL MASS, INSULATION, AND HEAT-TRANSFER EFFECTS OF SAPS

Thermal properties of SAP concretes are crucial for building and pavement applications.

8.1 Influence on Thermal Mass:

SAP presence influences thermal properties of concrete through voids (low conductivity), water release (thermal buffering) and lightweight aggregate behavior (for SAP beads). SAP-modified concretes show slight reduction in thermal mass due to void formation. Thermal mass determines a concrete’s ability to absorb and release heat. SAP concrete has more stable thermal gradients and enhanced thermal inertia because of reduced cracking. Geopolymer and SAP concretes used in thermal energy storage (TES) systems (Rahjoo, 2023) show 3.5 times higher heat storage capacity compared to ordinary cement concrete. SAP concretes exhibit lower density that reduces its thermal capacity. Geopolymer–SAP systems improve thermal mass efficiency by 25–40%.

SAP beads (>1 mm) act similarly to lightweight aggregates, slightly lowering thermal mass but improving thermal damping.

8.2 Insulation and Thermal Conductivity:

Insulation Properties of concrete can be improved using SAPs in it. SAPs increase insulation by introducing sealed voids, reducing density of concrete and lowering thermal conductivity. Studies show 10–30% reduction in thermal conductivity for SAP concretes. Reduction in thermal conductivity goes up to 50% in case of SAP beads i.e for SAP size larger than 1mm. SAP beads (>1 mm) significantly reduce, thermal conductivity, density and heat flux transmission. Lower thermal conductivity improves interior insulation, pavement surface cooling and thermal resistance in wall panels. This supports energy-efficient building envelope design. Comparable studies with expanded polystyrene (EPS) beads show reductions up to 93% (Shabbar et al., 2024; Mathew et al., 2023; Canbaz & Türeyen, 2022; Wibowo et al., 2021). SAP beads behave similarly but retain the advantage of internal curing. SAP beads behave as “hydrogel lightweight inclusions”.

8.3 Heat Transfer Performance

Pervious and porous concretes exhibit heat sensitivity based on albedo and thermal inertia. SAP concretes show slower heat rise due to moisture retention. More stable temperature under thermal cycles and reduced thermal cracking due to moisture availability is observed while using SAP in concrete. SAP - PCM (phase change material) hybrid systems reduce supercooling and improve temperature stability (Lee & Park, 2024). Studies show SAP beads when used in concrete retain more water, enhancing evaporative cooling resulting 4–6°C lower surface temperatures (Sarvesh and Abhilash, 2025). It improves urban heat Island (UHI) mitigation under dry climates and Enhancing stormwater cooling potential.

9. DURABILITY ENHANCEMENT IN SAP-MODIFIED CONCRETE

Durability represents one of the most significant advantages of SAP incorporation. Across dozens of experimental studies, SAP-modified concretes demonstrate improved performance against freeze–thaw cycling, chloride ingress, carbonation, permeability, and chemical attack. The mechanisms relate primarily to internal curing, microstructural refinement, and reduced cracking.

9.1 Freeze–Thaw Resistance

SAPs exhibit a dual role during freeze–thaw cycling. When SAPs release absorbed water, they leave stable macro voids (100–300 µm), functioning as pressure relief chambers during ice formation. SAPs reduce autogenous and drying microcracks, lowering pathways for frost damage. Studies from Tenório Filho (2021), Kim (2021), and RILEM TC-260 confirm that freeze–thaw mass loss decreases by 30–60% and scaling depth decreases by 40–55%. SAPX (dual-crosslinked SAP) shows up to 72% reduction in frost damage. SAP beads (>1 mm) behave similarly to lightweight air voids, significantly improving freeze–thaw resistance even at low dosages.

9.2 Chloride Penetration and Permeability

SAP concretes with optimal dosages (0.2–0.4%) demonstrate lower chloride penetration due to formation of densified C–S–H gels. It exhibits better ITZ structure due to deduced cracking. Zheng et al. (2021) and Sokołowska (2024) found 20–40% lower chloride diffusion coefficients, reduced sorptivity by 15–33% and lower water absorption after 28–90 days while using SAP. Excessive SAP (>0.6%) increases permeability due to excessive voids, but SAP–fiber or SAP–silica fume blends reduce this effect. SAP beads show much higher permeability initially but stabilize after microstructure densifies through internal curing.

  - Carbonation Resistance

Carbonation behavior of SAP concrete is influenced by two opposing factors: First, SAP voids provide pathways for CO₂ diffusion. Second, Improved hydration reduces portlandite consumption. Studies by Sokołowska (2024) and Li et al., (2024) show that carbonation depth of SAP concrete remains similar or slightly higher (0–10% variance) compared to control mix and after 3 years, SAP concrete showed 8.6% higher UPV, indicating densification and reduced long-term carbonation susceptibility. Carbonation performance improves when SAPs are pre-saturated, minimizing void connectivity.

9.4 Chemical Resistance

SAP-induced internal curing reduces microcracking, improving chemical durability. Resistance to sulphate and MgSO₄ increased by 15-30%. Acid resistance improved due to reduced porosity and enhanced C–S–H stability. Geopolymer–SAP systems showed exceptional acid resistance, making them attractive for industrial environments.

  - Fire and High-Temperature Behavior

SAPs significantly influence thermal spalling performance. SAP voids act as vapor pressure relief chambers, reducing explosive spalling at 400-600°C. 70-100% reduction in spalling risk in HPC and UHPC was observed. SAP–fiber hybrids provide best combined resistance. SAP beads (>1 mm) provide pronounced spalling mitigation due to large pressure dissipation pores.

10. MICROSTRUCTURE EVOLUTION

Microstructural analysis across uploaded and referenced studies reveals the fundamental mechanisms by which SAPs modify cement paste.

  - Scanning Electron Microscopy (SEM) and Transmission Electron Microscopy (TEM) Analysis

SEM consistently shows spherical voids (50–1000 µm) that SAPs leave in concrete after drying. Voids are well-distributed and non-interconnected (critical for durability). SAP beads (>1 mm) produce large reservoir voids up to 1.5–10 mm.

TEM) reveals enhanced nanostructure of C–S–H aggregates in SAP modified concrete. SAP creates more interconnected nano-gel networks and reduced average pore diameter (<10 nm) in concrete.

SAP-modified pastes display dense C–S–H around SAP voids (internal curing zones). It reduced CH crystal size and increased C–S–H gel density. TEM and SEM show that hydration shells extend 100–120 µm beyond SAP surfaces, confirming active internal curing. This supports findings that SAPs reduce self-desiccation, enabling complete hydration of C3S and secondary hydration of C2S and slag.

  - X-ray Computed Tomography (XCT)

XCT presents 3D visualization of SAP spatial distribution. Microcracks are absent or significantly reduced in SAP mixes. Non-interconnected macro-voids dominate the SAP zone. SAP beads leave large, evenly spaced spheres that behave like engineered voids (Snoeck, et al., 2016).

10.3 Nuclear Magnetic Resonance (NMR)

NMR studies conducted by Zhong et al., (2021) and Nestle, et al., (2009) show SAPs retain water for 9–12 hours post-mixing. Release of water correlates directly with hydration-induced suction. Both retentive and non-retentive SAPs maintain fully water-saturated cavities for extended periods. This proves that SAP desorption kinetics synchronize with hydration needs. SAP beads can retain this water for longer period.

11. DISCUSSION

The collective body of research demonstrates that superabsorbent polymers profoundly influence the hydration kinetics, microstructure, mechanical behavior, thermal properties, and long-term durability of cementitious materials. When SAPs are used in powdered form, they primarily act as nano–micro internal curing reservoirs. When used as beads (>1 mm), SAPs behave as dual-function admixtures: (i) slow-release internal water sources and (ii) engineered lightweight spherical inclusions that reduce density and thermal conductivity.

A consistent finding across studies is the competition between void formation and hydration enhancement. While empty SAP voids reduce compressive strength at early ages, long-term hydration typically compensates for the strength loss. SAP beads, with their large reservoir volumes, create voids that behave more like lightweight aggregates than traditional SAP pores. These beads noticeably reduce density and strength but substantially improve insulation.

Durability performance consistently improves when SAP dosage (dry form) is kept within 0.2–0.4% by cement mass or when SAP beads (saturated form) represent about 12% volumetric replacement of coarse aggregates (Sarvesh and Abhilash, 2025). Optimal performance is observed when SAPs are pre-saturated, reducing early-age void formation and ensuring immediate internal curing. For ultra-low w/c concretes and UHPC, SAPs are indispensable, as they mitigate severe autogenous shrinkage and ensure microstructural stability.

Thermal behavior analysis indicates that SAP concretes exhibit reduced thermal conductivity due to added void content. Nevertheless, SAP concretes retain superior thermal mass stability due to reduced microcracking. SAP beads contribute positively to insulation but reduce heat storage capacity, making them suitable for envelope materials rather than structural members.

Performance in UPV tests initially decreases due to pore introduction but increases at maturity due to microstructural densification. This aligns with SEM/TEM observations showing hydration improvement around SAP voids. XCT and NMR studies confirm the stable behavior of SAP cavities and validate internal curing models used in predictive frameworks.

12. RESEARCH GAPS AND FUTURE PERSPECTIVES

Although lot of research has been made on use of SAP in concrete, multiple research gaps remain, especially concerning large-scale implementation, long-term behavior, and multi-functional performance of different size of SAPs. Most studies are limited to lab-scale specimens. There is insufficient data from full-scale pavements, High-rise structural elements and mass concrete foundations requires further field monitoring.

SAP-related voids may behave differently after years of loading, carbonation, and freeze–thaw cycling. Key unknowns include long-term chemical stability of hydrogel residues, microbial interactions with SAP cavities, SAP-induced changes in creep behavior and microstructural aging of SAP beads (>1 mm). Long-duration XCT and nanoindentation studies are needed.

Mix Design Optimization is required for SAP Beads (>1 mm). There is limited guidance on maximum allowable bead volume fractions, energy absorption and ductility impacts, interaction with fibers, air entrainers, or lightweight aggregates. Computational modeling using Computational Fluid Dynamics (CFD), Discrete Element Method (DEM) and pore-network simulations can provide new insights.

Advanced modeling is required to predict the combined effects of water transport, heat transfer, hydration progression, shrinkage stress development and frost-induced pressure cycles. Multiscale models combining NMR, XCT, and nanoindentation results would greatly enhance SAP design reliability.

13. PRACTICAL GUIDELINES AND DESIGN RECOMMENDATIONS

Based on the review, the following guidelines are recommended:

13.1 SAP Dosage

- Powder SAP (100–1000 μm): 0.15–0.35% by cement weight in dry form.

- SAP beads (>1 mm in saturated form): 8–12% by volume of coarse aggregates depending on desired thermal/structural performance.

13.2 Water–Cement Ratio Considerations

- For w/c < 0.30, SAPs are essential for preventing autogenous shrinkage.

- For w/c 0.30–0.45, SAPs improve durability and resist environmental cracking.

- For w/c > 0.45, SAPs are less critical but still beneficial in hot and dry climates.

13.3 SAP Beads in Thermal Applications

SAP beads (>1 mm) should be utilized for:

- Thermal insulation panels

- Lightweight facade elements

- Pervious pavement heat mitigation

- Passive cooling components

They should be avoided in:

- High-strength structural elements

- Prestressed members

- Heavy load-bearing beams

14. CONCLUSION

Superabsorbent polymers significantly enhance concrete performance by providing controlled internal curing, reducing shrinkage, improving durability, and refining microstructure. Their ability to absorb and gradually release large quantities of water allows concrete to hydrate completely, especially under low water–cement ratios or environmentally challenging curing conditions. SAPs improve autogenous shrinkage resistance by up to 90%, reduce drying shrinkage by 40%, and eliminate early-age tensile stresses under restraint. Although compressive strength may initially decrease due to void formation, long-term strength often matches or exceeds reference values because of superior hydration and reduced micro-cracking. Durability enhancements include improved freeze–thaw resistance (up to 70% mass loss reduction), reduced chloride ingress (up to 40%), and enhanced resistance to thermal cracking and spalling. Microstructural analysis via SEM/TEM/XCT/NMR confirms the development of dense C–S–H gel, refined pore networks, and stable spherical voids that do not compromise long-term durability. SAP beads (>1 mm) emerge as a distinct category, acting not only as internal curing reservoirs but also as engineered lightweight inclusions with significant effects on thermal mass, insulation, heat transfer, and density. These materials offer impactful applications in energy-efficient buildings, pervious pavements, and thermally adaptive infrastructures. Sarvesh and Abhilash (2025) replace aggregates with water absorbing beads in concrete and observed that the lightweight concrete was obtained with the use of water absorbing beads. The use of water absorbing beads beyond 12% in expanded form reduces compressive and tensile strength of concrete. An improvement in thermal properties of concrete was seen with use of water absorbing beads which improves sustainability and thermal comfort of the buildings. The integration of SAPs into cementitious materials represents a major advancement in modern concrete technology. With optimized dosage, proper pre-saturation, and hybridization with other additives, SAP-modified concretes offer exceptional shrinkage control, mechanical stability, durability, and thermal performance. Future research should prioritize long-term field applications, advanced modeling, and integration with sustainable binders. SAPs will continue to play a crucial role in the transition toward resilient, energy-efficient, and sustainable construction materials.

Disclaimer (Artificial intelligence)

Option 1:

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

Option 2:

Author(s) hereby declare that generative AI technologies such as Large Language Models, etc. have been used during the witing or editing of manuscripts. This explanation will include the name, version, model, and source of the generative AI technology and as well as all input prompts provided to the generative AI technology

Details of the AI usage are given below:

1. It is hereby declared that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

REFERENCES:

- Denagbe, W., Mazet, E., Desbrières, J., & Michaud, P. (2025). Superabsorbent polymers: Eco-friendliness and the gap between basic research and industrial applications. In Reactive and Functional Polymers (Vol. 214). Elsevier B.V. https://doi.org/10.1016/j.reactfunctpolym.2025.106278

- Jindal, A., & Mehra, D. (2025). Effects of Inclusion of SAP as an Internal Curing Agent in Concrete, A Review. In Civil Engineering Infrastructures Journal (Vol. 58, Issue 1, pp. 1–13). University of Tehran. https://doi.org/10.22059/ceij.2024.361854.1947

- Ma, Y., Wang, B., Zhang, C., Lin, X., Yang, Y., Chen, Z., & Ji, T. (2025). Relationship of drying shrinkage and the bond strength between alkali-activated steel slag/fly ash lightweight mortar and concrete substrate: Phase assemblage and micro-mechanical property. Journal of Building Engineering, 99. https://doi.org/10.1016/j.jobe.2024.111587

- Mao, Y., Zhang, P., Gao, Z., Zheng, Y., & Zheng, M. (2025). Durability and microstructure of waste slurry based geopolymer concrete. Journal of Materials Research and Technology, 34, 1468–1481. https://doi.org/10.1016/j.jmrt.2024.12.145

- Sarvesh Kumar and Abhilash Thakur (2025), “Thermal Properties of Concrete Prepared with Water Absorbing Beads. Communications on Applied Nonlinear Analysis, 32, 379-395. https://doi.org/10.52783/cana.v32.5069

- Das, S., & Juneja, D. K. (2024). Improving the Performance of Porous Concrete by Utilizing the Pumice Aggregate. IOP Conference Series: Earth and Environmental Science, 1327(1). https://doi.org/10.1088/1755-1315/1327/1/012006

- Marinelli, A., & Rasheed, L. P. H. (2024). Considering Environmental Effects on Porous Concrete Applications: An Experimental Investigation. Procedia Structural Integrity, 54, 332–339. https://doi.org/10.1016/j.prostr.2024.01.091

- Tu, Q. chuan, Xia, Q. hui, Lu, Y., & Bai, Y. hua. (2024). Preparation of a novel foamed concrete modified with carbon fiber and graphite: Mechanical, electro-magnetic and microstructural characteristics based on X-CT. Heliyon, 10(11). https://doi.org/10.1016/j.heliyon.2024.e31665

- Tang, C., Dong, R., Tang, Z., Long, G., Ma, G., Wang, H., & Huang, Y. (2024). Effect of SAP on the properties and microstructure of cement-based materials in the low humidity environment. Case Studies in Construction Materials, 20. https://doi.org/10.1016/j.cscm.2024.e03001

- Shabbar, R., Almusawi, A. M., & Taher, J. K. (2024). Investigation into the mechanical and thermal properties of lightweight mortar using commercial beads or recycled expanded polystyrene. Open Engineering, 14(1). https://doi.org/10.1515/eng-2022-0592

- Wattanavichien, P., & Iwanami, M. (2024). Investigation of the mechanical, microstructure, and durability properties of concrete with fine uniform and non-uniform polyethylene terephthalate (PET) aggregates. Cleaner Materials, 13. https://doi.org/10.1016/j.clema.2024.100267

- Zhou, B., Wang, K., Taylor, P. C., & Gu, Y. (2024). Superabsorbent Polymers for Internal Curing Concrete: An Additional Review on Characteristics, Effects, and Applications. In Materials (Vol. 17, Issue 22). Multidisciplinary Digital Publishing Institute (MDPI). https://doi.org/10.3390/ma17225462

- Sokołowska, J. J. (2024). Durability of Concrete with Superabsorbent Polymer (SAP) Assessed Using Depth of Carbonation and NDT Ultrasonic Methods. Materials, 17(4). https://doi.org/10.3390/ma17040906

- Niu, X., Zhang, Y., Elakneswaran, Y., Sasaki, M., Takayama, T., & Kawai, H. (2024). Effect of Superabsorbent Polymer (SAP) Size on Microstructure and Compressive Strength of Concrete. Polymers, 16(2). https://doi.org/10.3390/polym16020197

- Deng, F., Cao, C., Chi, Y., & Xu, L. (2024). Effect of cellulose nanofiber addition on the microstructure characterization and nano-mechanical behavior of interfacial transition zones in recycled concrete. Journal of Materials Research and Technology, 33, 7572–7585. https://doi.org/10.1016/j.jmrt.2024.11.040

- Lee, S. J., & Park, S. H. (2024). Effects of Superabsorbent Polymer Addition on the Thermal Properties of Eutectic Phase Change Material. Processes, 12(1). https://doi.org/10.3390/pr12010162

- Li, J. R., Kazmi, S. M. S., Wang, X., & Wu, Y. F. (2024). Improving carbonation resistance, strength, and microstructure of concrete through compression casting. Case Studies in Construction Materials, 21. https://doi.org/10.1016/j.cscm.2024.e03804

- Mathew, M., Thahira, A. B., & Jose, A. (2023). Enhancement of Thermal Insulation and Mechanical Properties of Concrete by Expanded Polystyrene Beads. Indian Journal of Engineering and Materials Sciences, 30(1), 172–179. https://doi.org/10.56042/ijems.v1i1.45582

- Mostofinejad, D., Aghamohammadi, O., Bahmani, H., & Ebrahimi, S. (2023). Improving thermal characteristics and energy absorption of concrete by recycled rubber and silica fume. Developments in the Built Environment, 16. https://doi.org/10.1016/j.dibe.2023.100221

- Ziaeemehr, B., Jandaghian, Z., Ge, H., Lacasse, M., & Moore, T. (2023). Increasing Solar Reflectivity of Building Envelope Materials to Mitigate Urban Heat Islands: State-of-the-Art Review. In Buildings (Vol. 13, Issue 11). Multidisciplinary Digital Publishing Institute (MDPI). https://doi.org/10.3390/buildings13112868

- Reshma, T. v., Kumar Patnaikuni, C., Tanu, H. M., & Bharath, A. (2023). Evaluation of strength, durability, and microstructure characteristics of slag-sand-induced concrete. Cleaner Materials, 10. https://doi.org/10.1016/j.clema.2023.100212

- Rahjoo, M., Rojas, E., Goracci, G., Gaitero, J. J., Martauz, P., & Dolado, J. S. (2023). A numerical study of geopolymer concrete thermal energy storage: Benchmarking TES module design and optimizing thermal performance. Journal of Energy Storage, 74. https://doi.org/10.1016/j.est.2023.109389

- Karikatti, V., Chitawadagi, M. v., Devarangadi, M., Sanjith, J., & Gangadhara Reddy, N. (2023). Influence of bagasse ash powder and marble powder on strength and microstructure characteristics of alkali activated slag concrete cured at room temperature for rigid pavement application. Cleaner Materials, 9. https://doi.org/10.1016/j.clema.2023.100200

- Zhang, G. Z., Ma, X., & Liu, Y. (2023). Study on the Synergistic Effect of Superabsorbent Polymer and Crystalline Admixture on Self-Healing Performance of Mortar Based on Image Binarization Method. Buildings, 13(12). https://doi.org/10.3390/buildings13122953

- Momeen Ul Islam, M., Li, J., Roychand, R., & Saberian, M. (2023). Microstructure, thermal conductivity and carbonation resistance properties of sustainable structural lightweight concrete incorporating 100% coarser rubber particles. Construction and Building Materials, 408. https://doi.org/10.1016/j.conbuildmat.2023.133658

- Canbaz, M., & Türeyen, A. C. (2022). Effect of expanded polystyrene beads on the properties of foam concrete containing polypropylene fiber. Challenge Journal of Concrete Research Letters, 13(1), 28–35. https://doi.org/10.20528/cjcrl.2022.01.003

- Eisa, M. S., Basiouny, M. E., & Fahmy, E. A. (2022). Drying shrinkage and thermal expansion of metakaolin-based geopolymer concrete pavement reinforced with biaxial geogrid. Case Studies in Construction Materials, 17. https://doi.org/10.1016/j.cscm.2022.e01415

- Huang, X., Liu, X., Rong, H., Yang, X., Duan, Y., & Ren, T. (2022). Effect of Super-Absorbent Polymer (SAP) Incorporation Method on Mechanical and Shrinkage Properties of Internally Cured Concrete. Materials, 15(21). https://doi.org/10.3390/ma15217854

- Kumar, D., Alam, M., Memon, R. A., & Bhayo, B. A. (2022). A critical review for formulation and conceptualization of an ideal building envelope and novel sustainability framework for building applications. In Cleaner Engineering and Technology (Vol. 11). Elsevier Ltd. https://doi.org/10.1016/j.clet.2022.100555

- Morinaga, Y., Akao, Y., Fukuda, D., & Elakneswaran, Y. (2022). Delayed Absorption Superabsorbent Polymer for Strength Development in Concrete. Materials, 15(8). https://doi.org/10.3390/ma15082727

- Seifeddine, K., Amziane, S., & Toussaint, E. (2022). Thermal behavior of pervious concrete in dry conditions. Construction and Building Materials, 345. https://doi.org/10.1016/j.conbuildmat.2022.128300

- Zhang, G., Chen, P., Si, X., Wang, J., & Han, Y. (2022). Research on Shrinkage and Shrinkage Models of Reinforced Concrete Specimens. The Open Civil Engineering Journal, 16(1). https://doi.org/10.2174/18741495-v16-e221103-2022-37

- Agostinho, L. B., Alexandre,  de C. P., da Silva, E. F., & Toledo Filho, R. D. (2021). Rheological study of Portland cement pastes modified with superabsorbent polymer and nanosilica. Journal of Building Engineering, 34. https://doi.org/10.1016/j.jobe.2020.102024

- Bouzouidja, R., Leconte, F., Kiss, M., Pierret, M., Pruvot, C., Détriché, S., Louvel, B., Bertout, J., Aketouane, Z., Wu, T. V., Goiffon, R., Colin, B., Pétrissans, A., Lagière, P., & Pétrissans, M. (2021). Experimental comparative study between conventional and green parking lots: Analysis of subsurface thermal behavior under warm and dry summer conditions. Atmosphere, 12(8). https://doi.org/10.3390/atmos12080994

- Danish, A., Mosaberpanah, M. A., & Salim, M. U. (2021). Robust evaluation of superabsorbent polymers as an internal curing agent in cementitious composites. In Journal of Materials Science (Vol. 56, Issue 1, pp. 136–172). Springer. https://doi.org/10.1007/s10853-020-05131-2

- Joshima, V. M., Naseer, M. A., & Lakshmi Prabha, E. (2021). Assessing the real-time thermal performance of reinforced cement concrete roof during summer- a study in the warm humid climate of Kerala. Journal of Building Engineering, 41. https://doi.org/10.1016/j.jobe.2021.102735

- Kim, I. S., Choi, S. Y., Choi, Y. S., & Yang, E. I. (2021). Effect of internal pores formed by a superabsorbent polymer on durability and drying shrinkage of concrete specimens. Materials, 14(18). https://doi.org/10.3390/ma14185199

- Mechtcherine, V., Wyrzykowski, M., Schröfl, C., Snoeck, D., Lura, P., de Belie, N., Mignon, A., van Vlierberghe, S., Klemm, A. J., Almeida, F. C. R., Tenório Filho, J. R., Boshoff, W. P., Reinhardt, H. W., & Igarashi, S. I. (2021). Application of super absorbent polymers (SAP) in concrete construction—update of RILEM state-of-the-art report. Materials and Structures/Materiaux et Constructions, 54(2). https://doi.org/10.1617/s11527-021-01668-z

- Tenório Filho, J. R., Vermoesen, E., Mannekens, E., van Tittelboom, K., van Vlierberghe, S., de Belie, N., & Snoeck, D. (2021). Enhanced durability performance of cracked and uncracked concrete by means of smart in-house developed superabsorbent polymers with alkali-stable and -unstable crosslinkers. Construction and Building Materials, 297. https://doi.org/10.1016/j.conbuildmat.2021.123812

- Tenório Filho, J. R., Mannekens, E., van Tittelboom, K., van Vlierberghe, S., de Belie, N., & Snoeck, D. (2021). Innovative SuperAbsorbent Polymers (iSAPs) to construct crack-free reinforced concrete walls: An in-field large-scale testing campaign. Journal of Building Engineering, 43. https://doi.org/10.1016/j.jobe.2021.102639

- Van der Putten, J., Snoeck, D., de Coensel, R., de Schutter, G., & van Tittelboom, K. (2021). Early age shrinkage phenomena of 3D printed cementitious materials with superabsorbent polymers. Journal of Building Engineering, 35. https://doi.org/10.1016/j.jobe.2020.102059

- Wang, C., Wang, Z. H., Kaloush, K. E., & Shacat, J. (2021). Cool pavements for urban heat island mitigation: A synthetic review. In Renewable and Sustainable Energy Reviews (Vol. 146). Elsevier Ltd. https://doi.org/10.1016/j.rser.2021.111171

- Wibowo, A. P., Lianasari, A. E., Wiransyah M., Z. A., & Kurniawan, T. A. (2021). The strength and water absorption of heated expanded polystyrene beads lightweight-concrete. International Journal of GEOMATE, 21(83), 150–156. https://doi.org/10.21660/2021.83.j2146

- Yeon, J. H. (2021). Restrained stress development in hardening mortar internally cured with superabsorbent polymers under autogenous and drying conditions. Polymers, 13(6). https://doi.org/10.3390/polym13060979

- Zhang, M., Aba, M., Sakoi, Y., Tsukinaga, Y., Shimomukai, K., & Kuang, Y. (2021). Synergetic Effect of Expansive Agent (KEA) and Superabsorbent Polymers (SAP) on the Shrinkage, Strength and Pore Structures of Mortars. Journal of Advanced Concrete Technology, 19(1), 26–39. https://doi.org/10.3151/JACT.19.26

- Zheng, X., Han, M., & Liu, L. (2021). Effect of superabsorbent polymer on the mechanical performance and microstructure of concrete. Materials, 14(12). https://doi.org/10.3390/ma14123232

- Zhong, P., Hu, Z., Griffa, M., Wyrzykowski, M., Liu, J., & Lura, P. (2021). Mechanisms of internal curing water release from retentive and non-retentive superabsorbent polymers in cement paste. Cement and Concrete Research, 147. https://doi.org/10.1016/j.cemconres.2021.106494

- Boehm-Courjault, E., Barbotin, S., Leemann, A., & Scrivener, K. (2020). Microstructure, crystallinity and composition of alkali-silica reaction products in concrete determined by transmission electron microscopy. Cement and Concrete Research, 130. https://doi.org/10.1016/j.cemconres.2020.105988

- Boshoff, W., Mechtcherine, V., Snoeck, D., Schröfl, C., de Belie, N., Ribeiro, A. B., Cusson, D., Wyrzykowski, M., Toropovs, N., & Lura, P. (2020). The effect of superabsorbent polymers on the mitigation of plastic shrinkage cracking of conventional concrete, results of an inter-laboratory test by RILEM TC 260-RSC. Materials and Structures/Materiaux et Constructions, 53(4). https://doi.org/10.1617/s11527-020-01516-6

- Carpio, M., González, Á., González, M., & Verichev, K. (2020). Influence of pavements on the urban heat island phenomenon: A scientific evolution analysis. Energy and Buildings, 226. https://doi.org/10.1016/j.enbuild.2020.110379

- De Meyst, L., Kheir, J., Tenório Filho, J. R., van Tittelboom, K., & de Belie, N. (2020). The use of superabsorbent polymers in high performance concrete to mitigate autogenous shrinkage in a large-scale demonstrator. Sustainability (Switzerland), 12(11). https://doi.org/10.3390/su12114741

- Dos Santos, K. F., Ribeiro, A. C. B. S., da Silva, E. F., Manzano, M. A. R., Motta, L. A. de C., & Filho, R. D. T. (2020). Effect of the combination of superabsorbent polymers for autogenous shrinkage control with steel fibers of high-performance concrete under uniaxial tension using DIC. Materials, 13(20), 1–18. https://doi.org/10.3390/ma13204638

- He, R., Tan, Y., Chen, H., Wang, Z., Zhang, J., & Fang, J. (2020). Preparation and properties of novel superabsorbent polymer (SAP) composites for cementitious materials based on modified metakaolin. Construction and Building Materials, 258. https://doi.org/10.1016/j.conbuildmat.2020.119575

- Hong, G., Song, C., & Choi, S. (2020). Autogenous healing of early-age cracks in cementitious materials by superabsorbent polymers. Materials, 13(3). https://doi.org/10.3390/ma13030690

- Kalinowski, M., Woyciechowski, P., & Sokołowska, J. (2020). Effect of mechanically-induced fragmentation of polyacrylic superabsorbent polymer (SAP) hydrogel on the properties of cement composites. Construction and Building Materials, 263. https://doi.org/10.1016/j.conbuildmat.2020.120135

- Lefever, G., Tsangouri, E., Snoeck, D., Aggelis, D. G., de Belie, N., van Vlierberghe, S., & van Hemelrijck, D. (2020). Combined use of superabsorbent polymers and nanosilica for reduction of restrained shrinkage and strength compensation in cementitious mortars. Construction and Building Materials, 251. https://doi.org/10.1016/j.conbuildmat.2020.118966

- Lefever, G., Aggelis, D. G., de Belie, N., Raes, M., Hauffman, T., van Hemelrijck, D., & Snoeck, D. (2020). The influence of superabsorbent polymers and nanosilica on the hydration process and microstructure of cementitious mixtures. Materials, 13(22), 1–16. https://doi.org/10.3390/ma13225194

- Lesovik, V., Popov, D., Fediuk, R., Glagolev, E., & Yoo, D.-Y. (2020). Improvement of Mechanical and Durability Behaviors of Textile Concrete: Effect of Polymineral Composite Binders and Superabsorbent Polymers. Journal of Materials in Civil Engineering, 32(11). https://doi.org/10.1061/(asce)mt.1943-5533.0003417

- Li, L., Dabarera, A. G. P., & Dao, V. (2020). Time-zero and deformational characteristics of high performance concrete with and without superabsorbent polymers at early ages. Construction and Building Materials, 264. https://doi.org/10.1016/j.conbuildmat.2020.120262

- Liu, J., Farzadnia, N., & Shi, C. (2020). Effects of superabsorbent polymer on interfacial transition zone and mechanical properties of ultra-high performance concrete. Construction and Building Materials, 231. https://doi.org/10.1016/j.conbuildmat.2019.117142

- Liu, J., Khayat, K. H., & Shi, C. (2020). Effect of superabsorbent polymer characteristics on rheology of ultra-high performance concrete. Cement and Concrete Composites, 112. https://doi.org/10.1016/j.cemconcomp.2020.103636

- Shen, D., Liu, C., Jiang, J., Kang, J., & Li, M. (2020). Influence of super absorbent polymers on early-age behavior and tensile creep of internal curing high strength concrete. Construction and Building Materials, 258. https://doi.org/10.1016/j.conbuildmat.2020.120068

- Sidiq, A., Gravina, R., Setunge, S., & Giustozzi, F. (2020). The effectiveness of Super Absorbent polymers and superplasticizer in self-healing of cementitious materials. Construction and Building Materials, 253. https://doi.org/10.1016/j.conbuildmat.2020.120068

- Snoeck, D., Moerkerke, B., Mignon, A., & de Belie, N. (2020). In-situ crosslinking of superabsorbent polymers as external curing layer compared to internal curing to mitigate plastic shrinkage. Construction and Building Materials, 262. https://doi.org/10.1016/j.conbuildmat.2020.120819

- Snoeck, D., Pel, L., & de Belie, N. (2020). Autogenous Healing in Cementitious Materials with Superabsorbent Polymers Quantified by Means of NMR. Scientific Reports, 10(1). https://doi.org/10.1038/s41598-020-57555-0

- Snoeck, D., Debo, J., & de Belie, N. (2020). Translucent self-healing cementitious materials using glass fibers and superabsorbent polymers. Developments in the Built Environment, 3. https://doi.org/10.1016/j.dibe.2020.100012

- Sun, B., Wu, H., Song, W., Li, Z., & Yu, J. (2020). Hydration, microstructure and autogenous shrinkage behaviors of cement mortars by addition of superabsorbent polymers. Frontiers of Structural and Civil Engineering, 14(5), 1274–1284. https://doi.org/10.1007/s11709-020-0656-x

- Tenório Filho, J. R., Snoeck, D., & de Belie, N. (2020). Mixing protocols for plant-scale production of concrete with superabsorbent polymers. Structural Concrete, 21(3), 983–991. https://doi.org/10.1002/suco.201900443

- Wyrzykowski, M., Assmann, A., Hesse, C., & Lura, P. (2020). Microstructure development and autogenous shrinkage of mortars with C-S-H seeding and internal curing. Cement and Concrete Research, 129. https://doi.org/10.1016/j.cemconres.2019.105967

- Zhao, S., Jensen, O. M., & Hasholt, M. T. (2020). Measuring absorption of superabsorbent polymers in cementitious environments. Materials and Structures/Materiaux et Constructions, 53(1). https://doi.org/10.1617/s11527-020-1442-x

- Zhong, P., Wang, J., Wang, X., Liu, J., Li, Z., & Zhou, Y. (2020). Comparison of different approaches for testing sorption by a superabsorbent polymer to be used in cement-based materials. Materials, 13(21), 1–17. https://doi.org/10.3390/ma13215015

- Zhou, C., Guo, Y., Wang, Y., He, X., & Xiong, Z. (2020). Flexural behaviour of narrow RC beams strengthened with hybrid anchored CFRP sheets. Journal of Advanced Concrete Technology, 18(3), 54–66. https://doi.org/10.3151/jact.18.139

- de Meyst, L., Mannekens, E., Araújo, M., Snoeck, D., van Tittelboom, K., van Vlierberghe, S., & de Belie, N. (2019). Parameter study of superabsorbent polymers (SAPs) for use in durable concrete structures. Materials, 12(9). https://doi.org/10.3390/ma12091541

- Filho, J. R. T., de Araújo, M. A. P. G., Snoeck, D., & de Belie, N. (2019). Discussing different approaches for the time-zero as start for autogenous shrinkage in cement pastes containing superabsorbent polymers. Materials, 12(18). https://doi.org/10.3390/ma12182962

- Ghourchian, S., Wyrzykowski, M., Plamondon, M., & Lura, P. (2019). On the mechanism of plastic shrinkage cracking in fresh cementitious materials. Cement and Concrete Research, 115, 251–263. https://doi.org/10.1016/j.cemconres.2018.10.015

- He, Z., Shen, A., Guo, Y., Lyu, Z., Li, D., Qin, X., Zhao, M., & Wang, Z. (2019). Cement-based materials modified with superabsorbent polymers: A review. In Construction and Building Materials (Vol. 225, pp. 569–590). Elsevier Ltd. https://doi.org/10.1016/j.conbuildmat.2019.07.139

- Hu, M., Guo, J., Du, J., Liu, Z., Li, P., Ren, X., & Feng, Y. (2019). Development of Ca2+-based, ion-responsive superabsorbent hydrogel for cement applications: Self-healing and compressive strength. Journal of Colloid and Interface Science, 538, 397–403. https://doi.org/10.1016/j.jcis.2018.12.004

- Ji, Y., Sun, Z., Chen, C., Pel, L., & Barakat, A. (2019). Setting characteristics, mechanical properties and microstructure of cement pastes containing accelerators mixed with superabsorbent polymers (SAPs): An NMR study combined with additional methods. Materials, 12(2). https://doi.org/10.3390/ma12020315

- Kim, M., Kang, S. H., Hong, S. G., & Moon, J. (2019). Influence of Effective Water-to-Cement Ratios on Internal Damage and Salt Scaling of Concrete with Superabsorbent Polymer. Materials, 12(23). https://doi.org/10.3390/ma12233863

- Liu, J., Farzadnia, N., Shi, C., & Ma, X. (2019). Effects of superabsorbent polymer on shrinkage properties of ultra-high strength concrete under drying condition. Construction and Building Materials, 215, 799–811. https://doi.org/10.1016/j.conbuildmat.2019.04.237

- Liu, J., Farzadnia, N., Shi, C., & Ma, X. (2019). Shrinkage and strength development of UHSC incorporating a hybrid system of SAP and SRA. Cement and Concrete Composites, 97, 175–189. https://doi.org/10.1016/j.cemconcomp.2018.12.029

- Liu, Y., Li, T., & Yu, L. (2020). Urban heat island mitigation and hydrology performance of innovative permeable pavement: A pilot-scale study. Journal of Cleaner Production, 244. https://doi.org/10.1016/j.jclepro.2019.118938

- Ma, X., Yuan, Q., Liu, J., & Shi, C. (2019). Effect of water absorption of SAP on the rheological properties of cement-based materials with ultra-low w/b ratio. Construction and Building Materials, 195, 66–74. https://doi.org/10.1016/j.conbuildmat.2018.11.050

- Rodríguez, C. R., Figueiredo, S. C., Deprez, M., Snoeck, D., Schlangen, E., & Šavija, B. (2019). Numerical investigation of crack self-sealing in cement-based composites with superabsorbent polymers. Cement and Concrete Composites, 104. https://doi.org/10.1016/j.cemconcomp.2019.103395

- Snoeck, D., & de Belie, N. (2019). Autogenous healing in strain-hardening cementitious materials with and without superabsorbent polymers: An 8-year study. Frontiers in Materials, 6. https://doi.org/10.3389/fmats.2019.00048

- Snoeck, D., Pel, L., & de Belie, N. (2019). Comparison of different techniques to study the nanostructure and the microstructure of cementitious materials with and without superabsorbent polymers. Construction and Building Materials, 223, 244–253. https://doi.org/10.1016/j.conbuildmat.2019.06.225

- Tan, Y., Chen, H., Wang, Z., Xue, C., & He, R. (2019). Performances of cement mortar incorporating superabsorbent polymer (SAP) using different dosing methods. Materials, 12(10). https://doi.org/10.3390/ma12101619

- Yang, J., Wang, F., Liu, Z., Liu, Y., & Hu, S. (2019). Early-state water migration characteristics of superabsorbent polymers in cement pastes. Cement and Concrete Research, 118, 25–37. https://doi.org/10.1016/j.cemconres.2019.02.010

- Yang, H., Liu, J., Zhou, Q., & Ji, H. (2019). The re-swelling behavior of superabsorbent polymers (SAPs) in hardened cement paste with an artificial crack. Materials and Structures/Materiaux et Constructions, 52(5). https://doi.org/10.1617/s11527-019-1394-1

- Zhong, P., Wyrzykowski, M., Toropovs, N., Li, L., Liu, J., & Lura, P. (2019). Internal curing with superabsorbent polymers of different chemical structures. Cement and Concrete Research, 123. https://doi.org/10.1016/j.cemconres.2019.105789

- Aday, A. N., Osio-Norgaard, J., Foster, K. E. O., & Srubar, W. v. (2018). Carrageenan-based superabsorbent biopolymers mitigate autogenous shrinkage in ordinary portland cement. Materials and Structures/Materiaux et Constructions, 51(2). https://doi.org/10.1617/s11527-018-1164-5

- Almeida, F. C. R., & Klemm, A. J. (2018). Efficiency of internal curing by superabsorbent polymers (SAP) in PC-GGBS mortars. Cement and Concrete Composites, 88, 41–51. https://doi.org/10.1016/j.cemconcomp.2018.01.002

- Deng, H., & Liao, G. (2018). Assessment of influence of self-healing behavior on water permeability and mechanical performance of ECC incorporating superabsorbent polymer (SAP) particles. Construction and Building Materials, 170, 455–465. https://doi.org/10.1016/j.conbuildmat.2018.03.094

- Farzanian, K., & Ghahremaninezhad, A. (2018). Desorption of superabsorbent hydrogels with varied chemical compositions in cementitious materials. Materials and Structures/Materiaux et Constructions, 51(1). https://doi.org/10.1617/s11527-017-1128-1

- Farzanian, K., & Ghahremaninezhad, A. (2018). On the effect of chemical composition on the desorption of superabsorbent hydrogels in contact with a porous cementitious material. Gels, 4(3). https://doi.org/10.3390/gels4030070

- Ghourchian, S., Wyrzykowski, M., & Lura, P. (2018). A poromechanics model for plastic shrinkage of fresh cementitious materials. Cement and Concrete Research, 109, 120–132. https://doi.org/10.1016/j.cemconres.2018.04.013

- Gupta, S., Kua, H. W., & Pang, S. D. (2018). Combination of polypropylene fibre and superabsorbent polymer to improve physical properties of cement mortar. Magazine of Concrete Research, 70(7), 350–364. https://doi.org/10.1680/jmacr.17.00193

- Kang, S. H., Hong, S. G., & Moon, J. (2018). Importance of monovalent ions on water retention capacity of superabsorbent polymer in cement based solutions. Cement and Concrete Composites, 88, 64–72. https://doi.org/10.1016/j.cemconcomp.2018.01.015

- Kang, S. H., Hong, S. G., & Moon, J. (2018). Shrinkage characteristics of heat-treated ultra-high performance concrete and its mitigation using superabsorbent polymer based internal curing method. Cement and Concrete Composites, 89, 130–138. https://doi.org/10.1016/j.cemconcomp.2018.03.003

- Kang, S. H., Hong, S. G., & Moon, J. (2018). The effect of superabsorbent polymer on various scale of pore structure in ultra-high performance concrete. Construction and Building Materials, 172, 29–40. https://doi.org/10.1016/j.conbuildmat.2018.03.193

- Lee, H. X. D., Wong, H. S., & Buenfeld, N. R. (2018). Effect of alkalinity and calcium concentration of pore solution on the swelling and ionic exchange of superabsorbent polymers in cement paste. Cement and Concrete Composites, 88, 150–164. https://doi.org/10.1016/j.cemconcomp.2018.02.005

- Mechtcherine, V., Snoeck, D., Schröfl, C., de Belie, N., Klemm, A. J., Ichimiya, K., Moon, J., Wyrzykowski, M., Lura, P., Toropovs, N., Assmann, A., Igarashi, S. ichi, de La Varga, I., Almeida, F. C. R., Erk, K., Ribeiro, A. B., Custódio, J., Reinhardt, H. W., & Falikman, V. (2018). Testing superabsorbent polymer (SAP) sorption properties prior to implementation in concrete: results of a RILEM Round-Robin Test. Materials and Structures/Materiaux et Constructions, 51(1). https://doi.org/10.1617/s11527-018-1149-4

- Meschke, G., Pichler, Bernhard., & Rots, J. G. . (2018). Computational modelling of concrete structures : proceedings of the Conference on Computational Modelling of Concrete and Concrete Structures (EURO-C 2018), 26 February 26 - 1 March, 2018, Bad Hofgastein, Austria. CRC Press. https://doi.org/10.1201/9781315182964

- Oh, S., & Choi, Y. C. (2018). Superabsorbent polymers as internal curing agents in alkali activated slag mortars. Construction and Building Materials, 159, 1–8. https://doi.org/10.1016/j.conbuildmat.2017.10.121

- Park, B., & Choi, Y. C. (2018). Self-healing capability of cementitious materials with crystalline admixtures and super absorbent polymers (SAPs). Construction and Building Materials, 189, 1054–1066. https://doi.org/10.1016/j.conbuildmat.2018.09.061

- Schabbach, L. M., Marinoski, D. L., Güths, S., Bernardin, A. M., & Fredel, M. C. (2018). Pigmented glazed ceramic roof tiles in Brazil: Thermal and optical properties related to solar reflectance index. Solar Energy, 159, 113–124. https://doi.org/10.1016/j.solener.2017.10.076

- Shafigh, P., Asadi, I., & Mahyuddin, N. B. (2018). Concrete as a thermal mass material for building applications - A review. In Journal of Building Engineering (Vol. 19, pp. 14–25). Elsevier Ltd. https://doi.org/10.1016/j.jobe.2018.04.021

- Shah, L. A., Khan, M., Javed, R., Sayed, M., Khan, M. S., Khan, A., & Ullah, M. (2018). Superabsorbent polymer hydrogels with good thermal and mechanical properties for removal of selected heavy metal ions. Journal of Cleaner Production, 201, 78–87. https://doi.org/10.1016/j.jclepro.2018.08.035

- Snoeck, D., de Schryver, T., & de Belie, N. (2018). Enhanced impact energy absorption in self-healing strain-hardening cementitious materials with superabsorbent polymers. Construction and Building Materials, 191, 13–22. https://doi.org/10.1016/j.conbuildmat.2018.10.015

- Snoeck, D., Schröfl, C., & Mechtcherine, V. (2018). Recommendation of RILEM TC 260-RSC: testing sorption by superabsorbent polymers (SAP) prior to implementation in cement-based materials. Materials and Structures/Materiaux et Constructions, 51(5). https://doi.org/10.1617/s11527-018-1242-8

- Snoeck, D., Pel, L., & de Belie, N. (2018). Superabsorbent polymers to mitigate plastic drying shrinkage in a cement paste as studied by NMR. Cement and Concrete Composites, 93, 54–62. https://doi.org/10.1016/j.cemconcomp.2018.06.019

- Wang, J., Meng, Q., Tan, K., Zhang, L., & Zhang, Y. (2018). Experimental investigation on the influence of evaporative cooling of permeable pavements on outdoor thermal environment. Building and Environment, 140, 184–193. https://doi.org/10.1016/j.buildenv.2018.05.033

- Wyrzykowski, M., Igarashi, S. I., Lura, P., & Mechtcherine, V. (2018). Recommendation of RILEM TC 260-RSC: using superabsorbent polymers (SAP) to mitigate autogenous shrinkage. Materials and Structures/Materiaux et Constructions, 51(5). https://doi.org/10.1617/s11527-018-1241-9

- Al-Nasra, M., & Daoud, M. (2017). STUDY OF THE ABILITY OF CRACKED CONCRETE TO BLOCK WATER FLOW, CONCRETE MIXED WITH SUPER ABSORBENT POLYMER. 12(1). https://aurak.ac.ae/publications/Study-of-the-Ability-of-Cracked-Concrete-to-Block-Water-Flow,-Concrete-Mixed-with-Super-Absorbent-Polymer.pdf

- Dang, J., Zhao, J., & Du, Z. (2017). Effect of superabsorbent polymer on the properties of concrete. Polymers, 9(12). https://doi.org/10.3390/polym9120672

- Davis, C. R., Kelly, S. L., & Erk, K. A. (2017). Comparing laser diffraction and optical microscopy for characterizing superabsorbent polymer particle morphology, size, and swelling capacity. Journal of Applied Polymer Science, 135(14). https://doi.org/10.1002/app.46055

- Hong, G., & Choi, S. (2017). Rapid self-sealing of cracks in cementitious materials incorporating superabsorbent polymers. Construction and Building Materials, 143, 366–375. https://doi.org/10.1016/j.conbuildmat.2017.03.133

- Kang, S. H., Hong, S. G., & Moon, J. (2017). Absorption kinetics of superabsorbent polymers (SAP) in various cement-based solutions. Cement and Concrete Research, 97, 73–83. https://doi.org/10.1016/j.cemconres.2017.03.009

- Krafcik, M. J., Macke, N. D., & Erk, K. A. (2017). Improved concrete materials with hydrogel-based internal curing agents. Gels, 3(4). https://doi.org/10.3390/gels3040046

- Ma, X., Liu, J., Wu, Z., & Shi, C. (2017). Effects of SAP on the properties and pore structure of high performance cement-based materials. Construction and Building Materials, 131, 476–484. https://doi.org/10.1016/j.conbuildmat.2016.11.090

- Mechtcherine, V., Schröfl, C., Wyrzykowski, M., Gorges, M., Lura, P., Cusson, D., Margeson, J., de Belie, N., Snoeck, D., Ichimiya, K., Igarashi, S. I., Falikman, V., Friedrich, S., Bokern, J., Kara, P., Marciniak, A., Reinhardt, H. W., Sippel, S., Bettencourt Ribeiro, A., … Weiss, J. (2017). Effect of superabsorbent polymers (SAP) on the freeze–thaw resistance of concrete: results of a RILEM interlaboratory study. Materials and Structures/Materiaux et Constructions, 50(1). https://doi.org/10.1617/s11527-016-0868-7

- Mignon, A., Snoeck, D., Dubruel, P., Vlierberghe, S. van, & de Belie, N. (2017). Crack mitigation in concrete: Superabsorbent polymers as key to success? In Materials (Vol. 10, Issue 3). MDPI AG. https://doi.org/10.3390/ma10030237

- Mignon, A., Vagenende, M., Martins, J., Dubruel, P., van Vlierberghe, S., & de Belie, N. (2017). Development of amine-based pH-responsive superabsorbent polymers for mortar applications. Construction and Building Materials, 132, 556–564. https://doi.org/10.1016/j.conbuildmat.2016.12.031

- Mignon, A., Vermeulen, J., Snoeck, D., Dubruel, P., van Vlierberghe, S., & de Belie, N. (2017). Mechanical and self-healing properties of cementitious materials with pH-responsive semi-synthetic superabsorbent polymers. Materials and Structures/Materiaux et Constructions, 50(6). https://doi.org/10.1617/s11527-017-1109-4

- Mohajerani, A., Bakaric, J., & Jeffrey-Bailey, T. (2017). The urban heat island effect, its causes, and mitigation, with reference to the thermal properties of asphalt concrete. In Journal of Environmental Management (Vol. 197, pp. 522–538). Academic Press. https://doi.org/10.1016/j.jenvman.2017.03.095

- Olawuyi, B. J., & Boshoff, W. P. (2017). Influence of SAP content and curing age on air void distribution of high performance concrete using 3D volume analysis. Construction and Building Materials, 135, 580–589. https://doi.org/10.1016/j.conbuildmat.2016.12.128

- Pelto, J., Leivo, M., Gruyaert, E., Debbaut, B., Snoeck, D., & de Belie, N. (2017). Application of encapsulated superabsorbent polymers in cementitious materials for stimulated autogenous healing. Smart Materials and Structures, 26(10). https://doi.org/10.1088/1361-665X/aa8497

- Riyazi, S., Kevern, J. T., & Mulheron, M. (2017). Super absorbent polymers (SAPs) as physical air entrainment in cement mortars. Construction and Building Materials, 147, 669–676. https://doi.org/10.1016/j.conbuildmat.2017.05.001

- Schröfl, C., Snoeck, D., & Mechtcherine, V. (2017). A review of characterisation methods for superabsorbent polymer (SAP) samples to be used in cement-based construction materials: report of the RILEM TC 260-RSC. Materials and Structures/Materiaux et Constructions, 50(4). https://doi.org/10.1617/s11527-017-1060-4

- Snoeck, D., Pel, L., & de Belie, N. (2017). The water kinetics of superabsorbent polymers during cement hydration and internal curing visualized and studied by NMR. Scientific Reports, 7(1). https://doi.org/10.1038/s41598-017-10306-0

- Taleghani, M. (2017). Outdoor thermal comfort by different heat mitigation strategies- A review. In Renewable and Sustainable Energy Reviews (Vol. 81, pp. 2011–2018). Elsevier Ltd. https://doi.org/10.1016/j.rser.2017.06.010

- Wehbe, Y., & Ghahremaninezhad, A. (2017). Combined effect of shrinkage reducing admixtures (SRA) and superabsorbent polymers (SAP) on the autogenous shrinkage, hydration and properties of cementitious materials. Construction and Building Materials, 138, 151–162. https://doi.org/10.1016/j.conbuildmat.2016.12.206

- Azarijafari, H., Kazemian, A., Rahimi, M., & Yahia, A. (2016). Effects of pre-soaked super absorbent polymers on fresh and hardened properties of self-consolidating lightweight concrete. Construction and Building Materials, 113, 215–220. https://doi.org/10.1016/j.conbuildmat.2016.03.010

- Farzanian, K., Pimenta Teixeira, K., Perdigão Rocha, I., de Sa Carneiro, L., & Ghahremaninezhad, A. (2016). The mechanical strength, degree of hydration, and electrical resistivity of cement pastes modified with superabsorbent polymers. Construction and Building Materials, 109, 156–165. https://doi.org/10.1016/j.conbuildmat.2015.12.082

- Gruyaert, E., Debbaut, B., Snoeck, D., Díaz, P., Arizo, A., Tziviloglou, E., Schlangen, E., & de Belie, N. (2016). Self-healing mortar with pH-sensitive superabsorbent polymers: Testing of the sealing efficiency by water flow tests. Smart Materials and Structures, 25(8). https://doi.org/10.1088/0964-1726/25/8/084007

- Krafcik, M. J., & Erk, K. A. (2016). Characterization of superabsorbent poly(sodium-acrylate acrylamide) hydrogels and influence of chemical structure on internally cured mortar. Materials and Structures/Materiaux et Constructions, 49(11), 4765–4778. https://doi.org/10.1617/s11527-016-0823-7

- Liu, H., Bu, Y., Sanjayan, J. G., Nazari, A., & Shen, Z. (2016). The application of coated superabsorbent polymer in well cement for plugging the microcrack. Construction and Building Materials, 104, 72–84. https://doi.org/10.1016/j.conbuildmat.2015.12.058

- Marangoni, M., Nait-Ali, B., Smith, D. S., Binhussain, M., Colombo, P., & Bernardo, E. (2016). White sintered glass-ceramic tiles with improved thermal insulation properties for building applications. Journal of the European Ceramic Society, 37(3), 1117–1125. https://doi.org/10.1016/j.jeurceramsoc.2016.10.019

- Mechtcherine, V. (2016). Use of superabsorbent polymers (Sap) as concrete additive. RILEM Technical Letters, 1, 81–87. https://doi.org/10.21809/rilemtechlett.2016.18

- Mignon, A., Snoeck, D., D’Halluin, K., Balcaen, L., Vanhaecke, F., Dubruel, P., van Vlierberghe, S., & de Belie, N. (2016). Alginate biopolymers: Counteracting the impact of superabsorbent polymers on mortar strength. Construction and Building Materials, 110, 169–174. https://doi.org/10.1016/j.conbuildmat.2016.02.033

- Secrieru, E., Mechtcherine, V., Schröfl, C., & Borin, D. (2016). Rheological characterisation and prediction of pumpability of strain-hardening cement-based-composites (SHCC) with and without addition of superabsorbent polymers (SAP) at various temperatures. Construction and Building Materials, 112, 581–594. https://doi.org/10.1016/j.conbuildmat.2016.02.161

- Shen, D., Wang, X., Cheng, D., Zhang, J., & Jiang, G. (2016). Effect of internal curing with super absorbent polymers on autogenous shrinkage of concrete at early age. Construction and Building Materials, 106, 512–522. https://doi.org/10.1016/j.conbuildmat.2015.12.115

- Snoeck, D., Dewanckele, J., Cnudde, V., & de Belie, N. (2016). X-ray computed microtomography to study autogenous healing of cementitious materials promoted by superabsorbent polymers. Cement and Concrete Composites, 65, 83–93. https://doi.org/10.1016/j.cemconcomp.2015.10.016

- Wang, F., Yang, J., Hu, S., Li, X., & Cheng, H. (2016). Influence of superabsorbent polymers on the surrounding cement paste. Cement and Concrete Research, 81, 112–121. https://doi.org/10.1016/j.cemconres.2015.12.004

- Esteves, L. P. (2015). Recommended method for measurement of absorbency of superabsorbent polymers in cement-based materials. Materials and Structures/Materiaux et Constructions, 48(8), 2397–2401. https://doi.org/10.1617/s11527-014-0324-5

- Hasholt, M. T., & Jensen, O. M. (2015). Chloride migration in concrete with superabsorbent polymers. Cement and Concrete Composites, 55, 290–297. https://doi.org/10.1016/j.cemconcomp.2014.09.023

- Justs, J., Wyrzykowski, M., Bajare, D., & Lura, P. (2015). Internal curing by superabsorbent polymers in ultra-high performance concrete. Cement and Concrete Research, 76, 82–90. https://doi.org/10.1016/j.cemconres.2015.05.005

- Kong, X. ming, Zhang, Z. lin, & Lu, Z. chen. (2015). Effect of pre-soaked superabsorbent polymer on shrinkage of high-strength concrete. Materials and Structures/Materiaux et Constructions, 48(9), 2741–2758. https://doi.org/10.1617/s11527-014-0351-2

- Lee, H. X. D., Wong, H. S., & Buenfeld, N. R. (2016). Self-sealing of cracks in concrete using superabsorbent polymers. Cement and Concrete Research, 79, 194–208. https://doi.org/10.1016/j.cemconres.2015.09.008

- Mechtcherine, V., Secrieru, E., & Schröfl, C. (2015). Effect of superabsorbent polymers (SAPs) on rheological properties of fresh cement-based mortars - Development of yield stress and plastic viscosity over time. Cement and Concrete Research, 67, 52–65. https://doi.org/10.1016/j.cemconres.2014.07.003

- Mignon, A., Snoeck, D., Schaubroeck, D., Luickx, N., Dubruel, P., van Vlierberghe, S., & de Belie, N. (2015). PH-responsive superabsorbent polymers: A pathway to self-healing of mortar. Reactive and Functional Polymers, 93, 68–76. https://doi.org/10.1016/j.reactfunctpolym.2015.06.003

- Mignon, A., Graulus, G. J., Snoeck, D., Martins, J., de Belie, N., Dubruel, P., & van Vlierberghe, S. (2015). pH-sensitive superabsorbent polymers: a potential candidate material for self-healing concrete. Journal of Materials Science, 50(2), 970–979. https://doi.org/10.1007/s10853-014-8657-6

- Oktay, H., Yumrutaş, R., & Akpolat, A. (2015). Mechanical and thermophysical properties of lightweight aggregate concretes. Construction and Building Materials, 96, 217–225. https://doi.org/10.1016/j.conbuildmat.2015.08.015

- Qin, Y. (2015). A review on the development of cool pavements to mitigate urban heat island effect. In Renewable and Sustainable Energy Reviews (Vol. 52, pp. 445–459). Elsevier Ltd. https://doi.org/10.1016/j.rser.2015.07.177

- Schroefl, C., Mechtcherine, V., Vontobel, P., Hovind, J., & Lehmann, E. (2015). Sorption kinetics of superabsorbent polymers (SAPs) in fresh Portland cement-based pastes visualized and quantified by neutron radiography and correlated to the progress of cement hydration. Cement and Concrete Research, 75, 1–13. https://doi.org/10.1016/j.cemconres.2015.05.001

- Senff, L., Modolo, R. C. E., Ascensão, G., Hotza, D., Ferreira, V. M., & Labrincha, J. A. (2015). Development of mortars containing superabsorbent polymer. Construction and Building Materials, 95, 575–584. https://doi.org/10.1016/j.conbuildmat.2015.07.173

- Snoeck, D., Jensen, O. M., & de Belie, N. (2015). The influence of superabsorbent polymers on the autogenous shrinkage properties of cement pastes with supplementary cementitious materials. Cement and Concrete Research, 74, 59–67. https://doi.org/10.1016/j.cemconres.2015.03.020

- Snoeck, D., Velasco, L. F., Mignon, A., van Vlierberghe, S., Dubruel, P., Lodewyckx, P., & de Belie, N. (2015). The effects of superabsorbent polymers on the microstructure of cementitious materials studied by means of sorption experiments. Cement and Concrete Research, 77, 26–35. https://doi.org/10.1016/j.cemconres.2015.06.013

- Assmann, A., & Reinhardt, H. W. (2014). Tensile creep and shrinkage of SAP modified concrete. Cement and Concrete Research, 58, 179–185. https://doi.org/10.1016/j.cemconres.2014.01.014

- Beushausen, H., & Gillmer, M. (2014). The use of superabsorbent polymers to reduce cracking of bonded mortar overlays. Cement and Concrete Composites, 52, 1–8. https://doi.org/10.1016/j.cemconcomp.2014.03.009

- Justs, J., Wyrzykowski, M., Winnefeld, F., Bajare, D., & Lura, P. (2014). Influence of superabsorbent polymers on hydration of cement pastes with low water-to-binder ratio: A calorimetry study. Journal of Thermal Analysis and Calorimetry, 115(1), 425–432. https://doi.org/10.1007/s10973-013-3359-x

- Lura, P., & Terrasi, G. pietro. (2014). Reduction of fire spalling in high-performance concrete by means of superabsorbent polymers and polypropylene fibers: Small scale fire tests of carbon fiber reinforced plastic-prestressed self-compacting concrete. Cement and Concrete Composites, 49, 36–42. https://doi.org/10.1016/j.cemconcomp.2014.02.001

- Lura, P., Wyrzykowski, M., Tang, C., & Lehmann, E. (2014). Internal curing with lightweight aggregate produced from biomass-derived waste. Cement and Concrete Research, 59, 24–33. https://doi.org/10.1016/j.cemconres.2014.01.025

- Qin, Y., & Hiller, J. E. (2014). Understanding pavement-surface energy balance and its implications on cool pavement development. Energy and Buildings, 85, 389–399. https://doi.org/10.1016/j.enbuild.2014.09.076

- Snoeck, D., Schaubroeck, D., Dubruel, P., & de Belie, N. (2014). Effect of high amounts of superabsorbent polymers and additional water on the workability, microstructure and strength of mortars with a water-to-cement ratio of 0.50. Construction and Building Materials, 72, 148–157. https://doi.org/10.1016/j.conbuildmat.2014.09.012

- Wang, J. Y., Snoeck, D., van Vlierberghe, S., Verstraete, W., & de Belie, N. (2014). Application of hydrogel encapsulated carbonate precipitating bacteria for approaching a realistic self-healing in concrete. Construction and Building Materials, 68, 110–119. https://doi.org/10.1016/j.conbuildmat.2014.06.018

- Zhu, Q., Barney, C. W., & Erk, K. A. (2014). Effect of ionic crosslinking on the swelling and mechanical response of model superabsorbent polymer hydrogels for internally cured concrete. Materials and Structures/Materiaux et Constructions, 48(7), 2261–2276. https://doi.org/10.1617/s11527-014-0308-5

- Laustsen, S., Hasholt, M. T., & Jensen, O. M. (2013). Void structure of concrete with superabsorbent polymers and its relation to frost resistance of concrete. Materials and Structures/Materiaux et Constructions, 48(1–2), 357–368. https://doi.org/10.1617/s11527-013-0188-0

- Pourjavadi, A., Fakoorpoor, S. M., Hosseini, P., & Khaloo, A. (2013). Interactions between superabsorbent polymers and cement-based composites incorporating colloidal silica nanoparticles. Cement and Concrete Composites, 37(1), 196–204. https://doi.org/10.1016/j.cemconcomp.2012.10.005

- Wyrzykowski, M., & Lura, P. (2013). Controlling the coefficient of thermal expansion of cementitious materials - A new application for superabsorbent polymers. Cement and Concrete Composites, 35(1), 49–58. https://doi.org/10.1016/j.cemconcomp.2012.08.010

- Hasholt, M. T., Jensen, O. M., Kovler, K., & Zhutovsky, S. (2012). Can superabsorbent polymers mitigate autogenous shrinkage of internally cured concrete without compromising the strength? Construction and Building Materials, 31, 226–230. https://doi.org/10.1016/j.conbuildmat.2011.12.062

- Schröfl, C., Mechtcherine, V., & Gorges, M. (2012). Relation between the molecular structure and the efficiency of superabsorbent polymers (SAP) as concrete admixture to mitigate autogenous shrinkage. Cement and Concrete Research, 42(6), 865–873. https://doi.org/10.1016/j.cemconres.2012.03.011

- Siriwatwechakul, W., Siramanont, ; J, & Vichit-Vadakan, W. (2012). Behavior of Superabsorbent Polymers in Calcium-and Sodium-Rich Solutions. https://doi.org/10.1061/(ASCE)MT.1943-5533.0000449

- Snoeck, D., van Tittelboom, K., Steuperaert, S., Dubruel, P., & de Belie, N. (2014). Self-healing cementitious materials by the combination of microfibres and superabsorbent polymers. Journal of Intelligent Material Systems and Structures, 25(1), 13–24. https://doi.org/10.1177/1045389X12438623

- Snoeck, D., Steuperaert, S., van Tittelboom, K., Dubruel, P., & de Belie, N. (2012). Visualization of water penetration in cementitious materials with superabsorbent polymers by means of neutron radiography. Cement and Concrete Research, 42(8), 1113–1121. https://doi.org/10.1016/j.cemconres.2012.05.005

- Wyrzykowski, M., Lura, P., Pesavento, F., & Gawin, D. (2012). Modeling of Water Migration during Internal Curing with Superabsorbent Polymers. Journal of Materials in Civil Engineering, 24(8), 1006–1016. https://doi.org/10.1061/(asce)mt.1943-5533.0000448

- Nestle, N., Kühn, A., Friedemann, K., Horch, C., Stallmach, F., & Herth, G. (2009). Water balance and pore structure development in cementitious materials in internal curing with modified superabsorbent polymer studied by NMR. Microporous and Mesoporous Materials, 125(1–2), 51–57. https://doi.org/10.1016/j.micromeso.2009.02.024