Sustainable Processing and Technical Textile Potential of Ramie and its blends:

A Comprehensive Review

Abstract

Ramie (Boehmeria nivea L. Gaud) is one of the important plant fibres known for its remarkable tensile strength, high cellulose purity, natural sheen and resistance to microbial attack. It has gained increased attention as an environmentally benign substitute for synthetic fibres and resource-intensive crops like cotton due to increasing emphasis on green textiles, sustainability and circular economy. However, the usage of ramie is limited by intrinsic disadvantages such as stiffness, brittleness, low elongation, high crease propensity and the presence of natural sticky gum that complicate further physical and chemical processing. Recent developments in enzymatic degumming methods that dramatically lower chemical use, energy use and effluent load while maintaining fibre strength and quality are reviewed after the difficulties with conventional chemical degumming. In order to improve the hand feel, dimensional stability, durability and functional performance of ramie fabrics, sustainable post-treatments like enzymatic bio-polishing, eco-friendly dyeing and sustainable surface modification are analyzed. The study also emphasizes on blending with various fibres as a crucial tactic to get over pure ramie's drawbacks leading to improvement in end-use performances. The study explores the growing use of blended ramie fabrics as a sustainable alternative in technical textiles, such as composites, geotextiles, protective apparel, agrotextiles, nonwovens and medical textiles. Lastly, the study concludes that ramie can be converted into a flexible, high-performance fibre appropriate for sophisticated technical textile applications through sustainable processing and appropriate blending with other natural fibres.

Keywords: blend, degumming, ramie, sustainable, technical textile

- Introduction

Ramie is one of the earliest known natural fibre in the textile industry. Interest in ramie has increased recently as it is produced from safe, recyclable and biodegradable plants and has led to environmental consciousness. Ramie is widely prized for its strength, brilliance, superior resistance to microbes and hygienic qualities. Ramie is recognized as the strongest of all natural bast fibres in the world which is known as Riha in Assam. It is a perennial shrub of the urticacease family yielding fibre from the bark of the canes. One of the disadvantages of ramie fibre is the stiffness and gummy substances. The demand for ramie fibre is mainly felt in the fields of blending with other fibre. Ramie can be blended with cotton, flax, wool, polyester, acrylic and silk. In the current global shift toward "Green Textiles" and circular economies, ramie has gained renewed attention as a high-performance alternative to synthetic fibres and water-intensive crops like cotton (Cook JG 1984; Pandey, 2001; Lewin 2007).

- Fibre structure and morphology

Boehmeria nivea (L.) Gaud, commonly known as Ramie, is one of the oldest and strongest natural plant fibres used in textile production. Ramie is classified as a bast fibre, meaning the fibres are located in the phloem (inner bark) of the plant's stalk. Ramie is a shallow-rooted perennial that attains heights of about 1–2.5 m under favourable conditions. The crop is adapted to warm, humid climates and can be harvested multiple times per year (typically 2–6 harvests under good management), which contributes to its high annual fibre yields compared with many other bast crops. Varietal selection, plant age at harvest and local agro-climatic conditions strongly influence both yield and fibre quality.  In the stem the fibres occur as bundles of “ultimate fibres” cemented together by gummy materials. It is renowned for having the longest individual plant cells of any vegetable fibre, with lengths ranging from 120 mm to 250 mm (and sometimes up to 600 mm). Under a microscope, ramie fibres appear as elongated, thick-walled cylinders with a well-defined central lumen. The surface is characterized by small ridges and striations, which contribute to its unique mechanical "grip" in textile blends. It possesses a high degree of molecular crystallinity, making the fibre exceptionally stiff and rigid compared to cotton. Ramie fibre is distinguished by its very high cellulose content and the chemical makeup of ramie is what defines its superior strength and the difficulty of its processing, cellulose 68% - 91% (high purity), hemicellulose 13% - 16%, pectin 2% - 5%, lignin  0.5% - 1.5%, gums/waxes 10% - 30% (Jiang et al., 2025).

- Distinctive Physical Properties of Ramie

Ramie is one of the strongest natural fibres. Remarkably, its strength increases by approximately 25% when wet, making it ideal for marine and high-humidity applications. It has a natural, silk-like gloss and a pure white color. Due to its chemical structure, it is naturally resistant to bacteria, mildew and rot, a property that historically made it the preferred material for Egyptian mummy wrappings. It is highly porous and breathable, with a moisture regain superior to cotton, which makes it excellent for summer apparel.

- Sustainable Degumming of Ramie fibre

The dominant processing challenge for ramie fibre is degumming. Degumming is the process that includes removal of the pectic and hemicellulosic matrix that binds fibre bundles. Traditional strong-alkali chemical degumming is effective but is posing to be environmentally problematic leading to large effluent loads and fibre damage. Consequently, focus has been shifted towards combined or alternative approaches such as milder alkali followed by enzymatic treatment, purely enzymatic or microbial bio-degumming or physical-chemical hybrids, to reduce chemical demand, preserve fibre strength and lower effluent toxicity. Growing evidence shows that enzyme-based treatments (pectinases, hemicellulases, xylanases, etc.), either alone or coupled with mild chemical pretreatment, can achieve satisfactory gum removal with better fibre integrity and substantially lower environmental impact. Abidin et al 2023 experimented the enzymatic degumming process in the shaker incubator at a temperature of 50 °C with pH 9 and 150 rpm. The degumming treatment involved 3% v/v xylanase, 1% v/v pectinase, 1% v/v surfactant and 0.05% v/v NaClO2 and the results show that the bleaching treatment resulted in higher fibre weight loss (9.52%), whiteness index (87.87%), tenacity (20.08 g/Tex) and fineness (1.05 denier) compared to the non-bleaching treatment. Biological degumming method reduces the harsh scouring or bleaching process and saves a large number of chemical reagents with fibre quality improvement. Thus, biological degumming is an efficient, energy-saving and eco-friendly method, is the first choice in ramie processing (Cheng et al 2020)

- Sustainable Post Treatments

Sustainable post-treatments of Ramie are essential for mitigating the fibre’s inherent drawbacks, such as its stiff prickle sensation and high shrinkage rate. The research focus has shifted toward biological and waterless finishing techniques that will align with global green textile standards.

5.1 Enzymatic Bio-Polishing & Softening: The most critical post-treatment for ramie is the removal of surface fuzz and residual gums that cause skin irritation. Jiang et al 2025 explored that a combination of cellulase, pectinase and laccase is significantly more effective than single-enzyme treatments. Cellulase selectively hydrolyzes protruding microfibrils (pilling), while pectinase softens the fabric by breaking down inter-fibre pectin. This process can reduce the prickle sensation score by over 43%, transforming the fabric’s hand feel from rough to silk-like without the use of toxic chemical softeners (Jin C and Maekawa M 2001).

5.2 Sustainable Dyeing: Ramie's high crystallinity traditionally requires high temperatures and heavy salt concentrations for dyeing. Recently, successful utilisation of agricultural waste (e.g., Oolong tea stems) as a natural dye source is being observed. With the assistance of chitosan (a bio-mordant), these dyes achieve excellent wash fastness (Grade 4+) and provide inherent antibacterial properties. The use of supercritical carbon dioxide as a solvent for dyeing ramie-polyester blends has emerged as a major sustainability milestone. This method eliminates water consumption and effluent discharge entirely while ensuring deeper dye penetration (Elsisi H et al 2025).

5.3 Dimensional Stability (Shrinkage Control): Ramie is prone to high shrinkage (>8%). Sustainable post-processing uses mechanical and enzymatic stabilization instead of formaldehyde-releasing resins. A green alternative to traditional mercerisation is treating ramie fabric with liquid ammonia at low temperatures reorganizes the cellulose crystals, reducing shrinkage to <1.5% and improving the fabric's luster and wrinkle resistance.

5.4 Functional Finishing (Antimicrobial & UV Protection): Instead of synthetic biocides, researchers now utilize sustainable chemicals like phytochemicals. Application of Ocimum sanctum (Tulsi) or Aloe vera by pad-dry-cure method can provide an Ultraviolet Protection Factor (UPF) of 50+ and an inhibition rate of >99% against S. aureus and E. coli (Riaz and Ashraf 2020).

5.5 Plasma and other dry surface treatments: Cold plasma (e.g., air, oxygen, helium) modifies the ramie surface at nanoscale and cleans as well as increases surface energy (better wetting, adhesion), roughens surface for coatings and can also reduce surface waxes/gums. Plasma is water-free and generates minimal effluent (Hamad SF et al 2019).

5.6 Bio-based flame retardants: Phytic acid (a phosphorus-rich plant molecule), chitosan and biochar combinations act as halogen-free, bio-based flame retardant systems and layer-by-layer (LbL) deposition or pad-dry-cure of these components can produce significant flame retardancy with improved char formation (Cheng X et al 2022).

5.7 Fluorine-free durable water repellent (DWR) finishes: Fluorinated chemistries are being phased out due to its toxicity. Sustainable DWRs use siloxane/polysiloxane hybrids, long-chain alkyl-modified polysaccharides and sol–gel silica–organic hybrids to impart hydrophobicity. These can be chemically bonded for improved durability. Chemically bonded organic–inorganic nanohybrid (rSiO₂–CAHPS) emulsions have been demonstrated on cotton and are applicable to ramie through pad-dry-cure sequences to produce wash-durable hydrophobicity (Yu C et al 2021).

5.8 Natural dyes and sustainable coloration: Using plant-derived dyes (indigo, madder, tannin-based) with bio-mordants (e.g., metal-free mordants, tannin-based adhesives) reduces metal load and effluent toxicity. Enzymes can assist dye fixation and reduce chemical auxiliaries and pose to have lower ecotoxicity but have limitations such as color fastness issue, shade reproducibility and scale-up challenges (Ghosh J et al 2025).

- Blending of Ramie

Blending ramie is the most effective way to neutralize its inherent brittleness. According to Pandey (2001), blending ramie with softer or more extensible fibres significantly improves its wear comfort while maintaining high strength and durability. Table 1 explores the most commonly used blends of Ramie with other fibres along with key performance benefits. The main objectives of blending ramie include:

- Reduction of stiffness and harsh handle

- Improvement in flexibility, drape and crease recovery

- Enhancement of spinnability and yarn evenness

- Modification of moisture management and thermal comfort

- Cost reduction and improved consumer acceptance

Table 1: Blending of ramie with other fibres

| Blend Type | Typical Ratio | Key Performance Benefit | Primary Application |
| --- | --- | --- | --- |
| Ramie + Cotton | 55:45 or 35:65 | Increases softness and reduces prickle," Improves durability by 25–30%. | Casual shirts, summer trousers, denim. |
| Ramie + Silk | 30:70 | Adds structural integrity to silk while maintaining a luxurious drape and gloss. | Formal blouses, high-end scarves, evening wear. |
| Ramie + Wool | 50:50 | Significantly reduces wool shrinkage and adds microbial resistance. | Mid-weight knitwear, winter coats. |
| Ramie + Tencel | 40:60 | Combines high tensile strength with extreme moisture-wicking and softness. | Activewear, premium basics. |
| Ramie + Polyester | 70:30 | Exceptional wrinkle resistance and mechanical robustness. | Industrial workwear, uniforms, upholstery. |

(Szoneier, 2025; OAJI, 2024; Textile Exchange, 2025; Filiciott L & Rothenberg G 2021; Lewin, 2007; Mukhopadhyay & Midha, 2008;  Pandey, 2001).

7. Applications of Blended Ramie Fabrics in Technical Textiles

Technical textiles are textile materials engineered primarily for functional and performance requirements rather than aesthetics. Natural fibres are increasingly being explored for technical textile applications due to growing concerns regarding sustainability, biodegradability and environmental impact.  In the 2024–2025 technical textile landscape, Ramie is no longer seen just as a luxury linen alternative. Its extreme tenacity and wet strength retention have positioned it as a critical raw material for high-performance industrial applications. Blended ramie fabrics are used in a wide range of applications including shirts, trousers, dresses, jackets, curtains, table linen, upholstery, canvas, ropes, furnishing fabrics, technical textiles and bio-composites. Blending significantly enhances the versatility and commercial viability of ramie fibre (Ramesh M et al 2017).

7.1 Agrotextiles
In the realm of agrotextiles, ramie-blended fabrics are increasingly favored for mulch mats, crop covers, and plant support nets. Beyond basic protection, the exceptional moisture management of ramie allows for controlled evaporation, ensuring that soil humidity remains constant even during temperature fluctuations.

Unlike petroleum-based plastic films, ramie-based textiles are fully biodegradable, breaking down into organic matter that enriches the soil rather than contributing to microplastic pollution. Studies by Mukhopadhyay and Midha (2008) highlight that ramie’s high cellulose content makes it resistant to premature rotting while in use, yet it decomposes efficiently once tilled back into the earth. This dual nature—durability during the growing season and biodegradability afterward—makes it a premium choice for sustainable precision farming.

7.2 Automotive & Aerospace Composites
Ramie is emerging as a powerhouse in green composites, serving as a high-performance bio-reinforcement to replace traditional glass fibers. Glass fiber is strong but is notoriously heavy, energy-intensive to produce and nearly impossible to recycle. Ramie, by contrast, offers a significantly lower carbon footprint. It is currently utilized in non-structural interior components such as door panels, seat backs, and dashboard scaffolds. Research by Zhang et al 2015 demonstrated that ramie/polypropylene hybrid composites achieved a 49% increase in tensile strength over pure polymer matrices, proving that natural doesn't mean weak. For the Electric Vehicle (EV) sector, weight is the enemy of range. Ramie’s low density allows for lighter interior assemblies, which directly enhances battery efficiency. Furthermore, its natural vibration-damping properties provide a quieter cabin experience compared to the brittle resonance of glass-reinforced plastics. In aerospace, these composites are being trialed for cabin linings where weight reduction and fire-retardant coatings can be easily integrated.

7.3 Canvas, Conveyor Belts, and Industrial Fabrics
In heavy-duty industrial sectors, ramie and ramie–cotton blends are the preferred materials for canvas, conveyor belts and tarpaulins. Dimensional stability—the ability of a fabric to resist stretching or sagging under tension—is where ramie truly outshines other natural fibers. While cotton provides the necessary flexibility and ease of handling for folding or rolling, ramie acts as the "backbone," imparting high load-bearing capacity and rigidity. This synergy is vital for industrial conveyor belts that must transport heavy loads without elongating. Additionally, ramie’s natural resistance to bacteria and mildew makes these industrial fabrics ideal for maritime use and outdoor storage, where high humidity would typically degrade standard cotton canvas within months (Pandey, 2001).

### 7.4 Fire-Retardant and Thermal Insulation Textiles

Ramie’s high cellulose content and crystalline structure make it a prime candidate for advanced fire-safety textiles. Recent research has shifted toward bio-based flame retardants, such as phytic acid–chitosan systems, which move away from toxic halogenated chemicals. When exposed to heat, these treatments catalyze the formation of a stable char layer on the ramie surface. This char acts as a physical barrier, insulating the underlying fibers and preventing the release of flammable gases.In thermal insulation, ramie-blended fabrics are used as interlayers in protective workwear. Because ramie is naturally breathable, it allows metabolic heat to escape while providing a buffer against external thermal radiation. This balance is critical for industrial hot zone workers who require protection without the risk of heat stroke caused by non-breathable synthetic insulators.

### 7.5 Geotextiles & Environmental Engineering

In environmental engineering, ramie is valued for its unique ability to thrive in "wet" stress environments. Its natural resistance to mildew is a biological advantage, allowing it to remain structurally sound in damp soil longer than jute or flax. Furthermore, ramie exhibits a capacity for phosphorus absorption, making it a tool for phytoremediation in runoff zones where excess nutrients might otherwise cause algal blooms. In coastal regions like Indonesia, ramie "geobags" are used to stabilize shorelines and protect fragile mangrove seedlings. Unlike plastic sandbags that eventually degrade into microplastics, ramie bags provide a temporary, sturdy structure that eventually merges with the local ecosystem. For agriculture, biodegradable ramie/starch nonwoven films are revolutionizing soil management; they provide a 20% better oxygen supply to the root zone compared to traditional polyethylene films, promoting healthier crop yields.

### 7.6 Marine & Industrial Applications

Ramie is one of the few natural fibers that actually gains tensile strength when wet (a property shared with linen but significantly higher in ramie). This makes it indispensable for maritime gear. While cotton may rot and nylon may stretch excessively under heavy moisture, ramie maintains its dimensional stability. Industrial brands have leveraged this by creating ramie–polyester hybrids for high-stress applications like tent anchors and sail reinforcements. For instance, a German outdoor equipment manufacturer reported a 35% reduction in fabric failure under extreme wind and rain conditions after integrating ramie. In industrial filtration, ramie’s resistance to bacteria and fungi ensures that liquid filters (used in food processing or wastewater) do not become breeding grounds for contaminants during downtime.

### 7.7 Medical and Hygienic Textiles

The medical field is rediscovering ramie due to its intrinsic antimicrobial properties and high absorbency. Unlike synthetic fibers that can harbor bacteria in their grooves, ramie’s smooth, crystalline surface is less hospitable to microbial growth. When used in wound dressings and bandages, ramie provides excellent "wicking" capabilities, pulling exudate away from the wound while allowing the skin to breathe. Ramie–cotton blends are particularly effective here, combining the "soft hand" of cotton with the structural integrity of ramie. This ensures that bandages do not lose their shape or become "slushy" when saturated. Furthermore, because ramie is lint-free, it reduces the risk of fiber contamination in surgical settings, making it a safer alternative for sterile environments.

7.8 Polymer Matrix Composites

In the world of materials science, ramie is the "gold standard" for bio-reinforcement in polymer matrices (epoxy, polyester, and polypropylene). The primary challenge with natural fibers is the interfacial bonding between the hydrophilic fiber and the hydrophobic plastic. However, through surface treatments like silane coupling or alkali washing, ramie’s bonding strength can be significantly enhanced. These "green composites" boast high specific tensile strength, meaning they offer incredible toughness relative to their weight. This makes them ideal for:

- Automotive interiors: Replacing heavy glass-fiber door panels.

- Lightweight construction: Use in eco-friendly acoustic panels.

- Furniture: Providing a "natural" aesthetic with the durability of a modern composite.

### 7.9 Protective & Fire-Resistant Textiles

Because ramie is composed of high-purity cellulose, it accepts functional chemical finishes more readily than many other natural fibers. In firefighter turnout gear and industrial uniforms, ramie serves as a robust substrate for phosphorus-based coatings. By using the "pad–dry–cure" application method, researchers have achieved a Limited Oxygen Index (LOI) of 29. To put that in perspective, any material with an LOI above 21 is considered flame-retardant, and 29 allows it to meet rigorous international safety standards. These fabrics do not melt or drip when exposed to flame—a common and dangerous failure point for synthetic protective gear—instead forming a protective carbonaceous shield.

### 7.10 Ropes, Cords, and Twines

Historically known as "China Grass," ramie has been used for centuries in maritime ropes and fishing nets. Its high abrasion resistance means it can withstand the constant friction of pulleys and docks without fraying. Modern applications often blend ramie with polyester to create a "best of both worlds" cordage. The ramie provides the raw tensile strength and resistance to "creep" (permanent stretching over time), while the polyester adds a degree of elastic recovery. This makes these ropes ideal for applications where the line must remain taut under heavy, constant loads, such as in shipping or heavy-duty agriculture.

### 7.11 Technical Nonwovens

Technical nonwovens are the "hidden" workers of the textile world. Ramie fibers are increasingly used in needle-punched or spunlace nonwovens for air and liquid filtration. Their natural irregularity and high surface area make them excellent at trapping particulates while maintaining high air permeability. In the automotive and construction sectors, these nonwovens serve as acoustic insulation and cushioning layers. The dense, fibrous network of a ramie-blend nonwoven is exceptionally good at dampening low-frequency sounds. Furthermore, using ramie in these layers helps manufacturers meet "end-of-life" vehicle directives, as the bio-content makes the vehicle easier to shred and recycle compared to those filled with 100% synthetic foams.

8.Conclusion

Ramie (Boehmeria nivea) is one of the natural fibre that has resurfaced as a very promising fibre in the face of global shift into a sustainable and high-performance textile. It is an outstanding tensile strength, high wet strength retention, high cellulose purity, natural antimicrobial resistance and biodegradability among most other bast fibre. These qualities render Ramie especially desirable to be used in the areas where durability, hygiene and environmental friendliness is of paramount importance. Nevertheless, it has never been widely adopted due to the presence of gummy substances, high crystallinity, stiffness and processing problems, particularly when it comes to the process of degumming. Recent developments in the greener processing technologies have made a great difference towards the sustainability and quality of ramie fibres. Enzyme, microbial and hybrid degumming methods have shown good ability to remove non-cellulosic contents without degrading fibre strength and minimising the use of chemicals, water and toxic effluents. The comfortable working, dimensional and functional performances of ramie are further improved by sustainable post-treatments like enzymatic bio-polishing, plasma surface modification, natural dyeing, fluorine-free water repellents and bio-based flame-retardant finishes, without affecting the ecological security. These green interventions are rather compatible with the principles of the circular economy and international sustainability. Blending has been one of the major strategies of addressing the stiffness and brittle nature of ramie. The blends of Ramie give better consumer acceptance and a larger commercial feasibility. In the field of technical textile, ramie and its mixes have significant potential in many applications such as agrotextiles, geotextiles, automotive and aerospace composites, protective and fire-retardant textiles, filtration media, medical textiles and marine. The fact that it can be used in place of synthetic fibres by being a high specific strength, biodegradable and compatible with polymer matrices makes ramie a sustainable substitute. In conclusion, to transform the entire potential of ramie into a high-performance fibre of sustainable and technical textile fibre system, the advantages of entire eco-friendly processing, strategic blending and application-oriented materials design are required.

Disclaimer (Artificial intelligence)

Option 1:

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

References

Abidin, K. Y., Nurhayati, N., Nandyawati, D., & Sabbathini, G. C. (2023). Enzymatic degumming using xylanase and pectinase to improve brightness and fineness quality of ramie fibre (Boehmeria nivea L.) as textile raw material. Jurnal Bioteknologi dan Biosains Indonesia, 10(1), 76–85.

Alongi, J., Carosio, F., & Malucelli, G. (2015). Current emerging techniques to impart flame retardancy to fabrics: An overview. Polymer Degradation and Stability, 113, 119–129.

Cheng, L., Duan, S., Feng, X., Zheng, K., Yang, Q., Xu, H and Peng, Y. (2020). Ramie-degumming methodologies: A short review. Journal of Engineered fibres and Fabrics, 15, 1558925020940105.

Cheng, X., Shi, L., Fan, Z., Yu, Y., & Liu, R. (2022). Bio-based coating of phytic acid, chitosan, and biochar for flame-retardant cotton fabrics. Polymer Degradation and Stability, 199, 109898.

Cook, J. G. (1984). Handbook of textile fibres: Natural fibres (Vol. 1). Merrow Publishing.

Elsisi, H., Elmaaty, T. A., Negm, E., & Abouelenin, S. (2025). Dyeing wool fabrics with specialized dyes and their mixtures using supercritical CO₂. Scientific Reports, 15(1), 40377.

Faruk, O., Bledzki, A. K., Fink, H. P., & Sain, M. (2012). Biocomposites reinforced with natural fibres: 2000–2010. Progress in Polymer Science, 37(11), 1552–1596.

Filiciotto, L., & Rothenberg, G. (2021). Biodegradable plastics: standards, policies, and impacts. ChemSusChem, 14(1), 56-72.

Ghosh, J., Rupanty, N. S., Noor, T., Asif, T. R., Islam, T., & Reukov, V. (2025). Functional coatings for textiles: Advancements in flame resistance, antimicrobial defense, and self-cleaning performance. RSC Advances, 15(14), 10984–11022.

Hamad, S. F., Stehling, N., Hayes, S. A., Foreman, J. P., & Rodenburg, C. (2019). Exploiting plasma-exposed natural surface nanostructures in ramie fibres for polymer composite applications. Materials, 12(10), 1631.

Jiang, Y., et al. (2025). Synergistic action of enhanced xylanase activity in microbial degumming of Boehmeria nivea. Bioresource Technology, 392, 130112.

Jin, C., & Maekawa, M. (2001). Evaluating an enzyme treatment of ramie fabrics. Textile Research Journal, 71(9), 779–782.

Lewin, M. (2007). Handbook of fibre chemistry (3rd ed.). CRC Press.

Mukhopadhyay, S. K., & Midha, V. K. (2008). A review on designing the fabric structure for improved comfort. Journal of the Textile Institute, 99(3), 225–246.

OAJI. (2024). Properties of ramie and its blends: A comparative study with silk waste.

Pandey, S. N. (2001). Ramie fibre: Part I—Chemical composition and properties. International Journal of Clothing Science and Technology, 13(3/4), 156–161.

Ramesh, M., Palanikumar, K., & Reddy, K. H. (2017). Plant fibre based bio-composites: Sustainable and renewable green materials. Renewable and Sustainable Energy Reviews, 79, 558–584.

Riaz, S., & Ashraf, M. (2020). Recent advances in development of antimicrobial textiles. In Advances in Functional Finishing of Textiles (pp. 129–168).

Szoneier Fabrics. (2025). Ramie blended fabrics guide: Cotton, polyester & silk insights. Technical Report.

Szoneier Fabrics. (2025). Ramie in textiles: Properties, sustainability & global impact.

Taylor & Francis. (2024). Application of ramie-based eco-friendly material in coastal protection structures: Feasibility study focusing on strength and biodegradability. Journal of Sustainable Development.

Textile Exchange. (2025). The 2025 recycled polyester challenge dashboard: Natural fibre integration.

Textile Institute. (2012). Textile terms and definitions (11th ed.). The Textile Institute.

Yang, J. X., Sun, Y., Song, W. M., & Liu, Y. (2024). A novel phosphorus/boron-containing flame retardant for improving the flame retardancy of ramie fiber reinforced epoxy composites. Construction and Building Materials, 451, 138814.

Yu, C., Shi, K., Ning, J., Zheng, Z., Yu, H., Yang, Z., & Liu, J. (2021). Preparation and application of fluorine-free finishing agent with excellent water repellency for cotton fabric. Polymers, 13(17), 2980.

Zhang, Y., Wen, B., Cao, L., Li, X., & Zhang, J. (2015). Preparation and properties of unmodified ramie fiber reinforced polypropylene composites. Journal of Wuhan University of Technology-Mater. Sci. Ed., 30(1), 198-202.