Valorization of cow bone waste into HCl-activated biochar for the removal of Congo red dye and heavy metals from wastewater

ABSTRACT

The work investigated the potential of biochar derived from cow bones as a low-cost and effective adsorbent for the removal of Congo red dye and heavy metals (Pb²⁺ and Cd²⁺) from simulated wastewater. Cow bone biochar was prepared via pyrolysis at 400 to 700 °C under oxygen-free conditions and activated with hydrochloric acid to enhance its adsorption properties. Unactivated biochar exhibited very low adsorption efficiency (less than 4%) and removed negligible amounts of Congo red. In contrast, HCl-activated biochar achieved a removal efficiency of 88% at 20 mg/L and maintained approximately 50% removal at 100 mg/L, indicating effective adsorption even at high initial concentrations. Biochar adsorbed 59.6% of Pb²⁺ at 20mg/L and 32.2% at 80mg/L of simulated wastewater. It also absorbed 94.45% of Cd²⁺ at 20mg/L and 55.26% at 80mg/L of wastewater. The reduced metal removal at higher concentrations was attributed to saturation of the adsorption location. These results indicated that biochar had a high affinity for Cd ions and had a strong potential to remove dyes and heavy metals from aqueous solutions. This work highlights the utilization of cow bone waste as a precursor for high-performance biochar. Acid-activated cow bone biochar was found to be an effective and low-cost adsorbent for wastewater remediation, indicating its suitability for industrial wastewater remediation.

KEYWORDS: Cow bone biochar; hydrochloric acid activation; Congo red dye removal; heavy metal adsorption; wastewater treatment; sustainable adsorbents

INTRODUCTION

Industrial processes and anthropogenic activities generate industrial effluents, wastewater, and other contaminants into surface and groundwater bodies, and this adversely impacts ecosystems, human health, and water security worldwide (Ibrahim et al. 2021; Saravanakumar et al. 2022; Oladimeji et al. 2024; Rajan et al. 2024; Singh et al. 2024). Among the various pollutants present in wastewater, synthetic dyes and heavy metals have particularly detrimental impacts on water resources (Forgacs et al. 2004; Fu and Wang 2011; Yaseen and Scholz 2019; Kato and Kansha 2024; Mnyango et al. 2025). This is due to their toxicity, persistence, and resistance to conventional treatment methodologies (Li et al. 2023; Patel et al. 2024; Abhisek et al. 2025). Synthetic dyes, e.g., Congo red, are generated during diverse industrial processes such as leather manufacturing, textile manufacturing, and dye manufacture (Al-Tohamy et al. 2022; Siddiqui et al. 2023; Islam et al. 2025). Congo red is a benzidine-based diazo dye characterized by complex aromatic compounds that make it highly stable and resistant to biodegradation (Hernández-Zamora and Martínez-Jerónimo 2019; Khan et al. 2022). Congo red has strong coloration properties that persist even at very low concentrations. When present within the ecosystem, it reduces light penetration, alters photosynthetic activity, and impacts aquatic life (Hernández-Zamora et al. 2014; El-Ahmady et al. 2020; Oladoye et al. 2022; Kağızman et al. 2025).

Heavy metals (e.g., Pb²⁺ and Cd²⁺) are also found in industrial wastewater. Lead is highly toxic, impacting neurological development in children and causing kidney and cardiovascular problems in adults (Sanders 2009; Hou et al. 2013; Collins et al. 2022; Larsen and Sánchez-Triana 2023; Gonzalez-Villalva et al. 2025). Cadmium is carcinogenic, and its bioaccumulation in biological systems poses long-term health risks (Genchi et al. 2020; Khan et al. 2022; Qu and Zheng 2024; Rani et al. 2025; Rasin et al. 2025). The simultaneous presence of dyes and heavy metals in wastewater is therefore a toxic combination for the ecosystem. Conventional methods used to remove both pollutants fail to eliminate them both efficiently and cost-effectively.

In recent times, adsorption has emerged as a viable strategy for eliminating toxicants from wastewater (Rathi and Kumar 2021; Iqbal et al. 2022; Kato and Kansha 2024; Sharma et al. 2024; Meftah et al. 2025). Adsorption is dependent on the interaction mechanisms between the pollutant to be eliminated and the adsorbent surface of the removing agent (Alkhaldi et al. 2024; Wang et al. 2024; Atangana et al. 2025). The efficiency of pollutant removal in adsorption is highly dependent on the porosity of the adsorbent, the surface area of the adsorbent, and the existence of functional chemical groups with the capacity to bind the contaminants to the absorbent (Ambaye et al. 2021; Yu et al. 2023; Wang et al. 2024; Phiri et al. 2024; Kumari et al. 2025). Commercially activated carbon has high adsorption capacities; however, its high cost precludes frequent use in the removal of dyes and heavy metals from wastewater. There has therefore been increasing interest in the development of cost-effective adsorbents from organic and agricultural waste matter (Haris et al. 2024; Erdem et al. 2025; Shabbirahmed et al 2025; Lukić et al. 2025; Tang et al. 2025). The utilization of such absorbents for wastewater remediation will reduce the load of waste disposal and equally serve as an alternative to expensive commercial adsorbents (Nguyen et al. 2013; Puglla et al. 2020; Le et al. 2021; Ungureanu et al. 2023; Sen 2023;

The pyrolysis of biomass under oxygen-deficient conditions generates biochar, which has found wide applications in environmental remediation (Rangabhashiyam et al. 2022; Kumar et al. 2023; Rajput et al. 2024; Dong et al. 2026). Most biochars are highly porous with a wide surface area, making them particularly optimal for pollutant adsorption. Their chemical activation via activators like hydrochloric acid (HCl) further increases the adsorption properties of the biochar (Ambaye et al. 2021; Pathy et al. 2023; Ren et al. 2023; Zhang et al. 2025; Sun et al. 2025). They also increase the porosity of the biochar surface and the number of acidic functional groups that enhance ionic interactions (Amalina et al. 2022; Lima et al 2025). Biochar from plant residues like rice husk, coconut shells, and sawdust has been investigated in the literature (Chikri et al. 2020; Konneh et al, 2021; Rashad et al. 2023; Rezvani et al. 2025; Lugo-Arias et al. 2026); however, the research on biochar derived from animal bones is limited. Cow bones are particularly rich in carbon and minerals, making them an excellent precursor for biochar production. The subjection of cow bones to pyrolysis and HCl activation increases their surface area, porosity, and adsorbent capacity.

The work, therefore, aimed to evaluate the adsorption performance of both unactivated and HCl-activated cow bone biochar for the removal of Congo red dye and Pb²⁺/Cd²⁺ ions from simulated wastewater. The adsorption efficiency at diverse contaminant concentrations will be evaluated to provide vital information on the capacity and efficiency of contaminant removal. Via demonstrating the feasibility of valorizing cow bone waste into a contaminant adsorbent, this research contributes to the investigation of effective, low-cost solutions to wastewater remediation.

MATERIALS AND METHODS

Cow bones were collected from slaughterhouses and washed with distilled water to eliminate impurities. The bones were then dissected into tiny, uniform pieces, which were oven-dried for 24 hours at 105 °C to remove residual moisture. The oven-dried samples were stored in airtight containers to prevent contamination. The dried cow bone samples were heated in a muffle furnace between 400 and 700 °C under oxygen-free conditions. This converted the organic matter within the cow bones into carbon-rich biochar. The material was allowed to cool gradually to room temperature, and the cooled biochar was then ground and sieved to obtain a uniform particle size suitable for adsorption experiments.

The biochar was then chemically activated using 3M hydrochloric acid, the overall goal being to improve adsorption performance. The chemical activation using HCl involved mixing biochar with the acid solution and allowing it to soak for several hours, the goal being to increase interaction between the acid and biochar. After activation with HCl, the biochar material was thoroughly washed with distilled water until the filtrate reached a neutral pH. This was done to remove residual acid and soluble impurities within the activated biochar. The biochar was then oven-dried at 105 °C and stored in airtight containers.

Simulated wastewater solutions were prepared by dissolving known concentrations of Congo red dye or heavy metal salts (Pb²⁺ and Cd²⁺) in distilled water. The pH and temperature of the solutions were maintained at conditions similar to those commonly observed in real wastewater. Adsorption experiments were then performed to assess the removal efficiency of the activated biochar. Different time intervals of 15, 20, 40, 60, 80, and 100 minutes were used as the agitation contact time for the experiments. After each experiment, the suspension was filtered through a 0.45 µm membrane filter to remove biochar particles. Congo red dye concentration in solution was measured with a UV–Visible spectrophotometer, while heavy metal concentrations in solution after adsorption were measured using Atomic Absorption Spectroscopy (AAS).

RESULTS AND DISCUSSION

Table 1 presents the results of the adsorption performance of unactivated biochar obtained from cow bone waste for the removal of Congo red dye from wastewater.

Table 1: Adsorption performance of unactivated biochar obtained from cow bone waste for the removal of Congo red dye from wastewater

| Initial conc. of Congo red dye wastewater (mg/L) | Equilibrium conc (mg/L) | Amount adsorbed (mg/L) | Percentage adsorbed (%) |
| --- | --- | --- | --- |
| 20.00 | 19.28 | 0.72 | 3.59 |
| 40.00 | 38.83 | 1.17 | 2.92 |
| 60.00 | 58.03 | 1.97 | 3.28 |
| 80.00 | 76.86 | 3.14 | 3.92 |
| 100.00 | 96.06 | 3.96 | 3.94 |

The results indicated that adsorption occurred at all the tested concentrations of Congo red dye in wastewater (20 to 100mg/L). However, the percentage adsorption remained low (2.92 to 3.94%), indicating an overall very low efficiency of adsorption. At an initial dye concentration of 20mg/L, the equilibrium concentration reduced to 19.28mg/L, implying that 0.72mg/L of dye was adsorbed. The removal efficiency here was 3.59%. When the initial concentration increased to 40mg/L, the amount of dye adsorbed increased to 1.17mg/L, and the percentage adsorption decreased to 2.92%. This reduction in percentage adsorption in spite of the increment in adsorption amount was attributed to the unavailability of active adsorption locations on the unactivated biochar surface. A similar trend was observed when the initial concentration was increased to 60 mg/L.  Here, 1.97mg/L of dye was removed, and the percentage adsorption was 3.28%. An increment in the initial concentration to 80mg/L lead to adsorption values of 3.14 mg/L (with an adsorption percentage of 3.92), whereas an increment of the initial concentration to 100mg/L led to adsorption values of 3.96 mg/L (with an adsorption percentage of 3.94%).

The results indicate that the total amount of dye adsorbed increased with an increase in initial dye concentration, a result of the increasing concentration gradient between the dye solution and the adsorbent surface. However, the adsorption percentage was very low (2.92 to 3.94%), indicating that the adsorption capacity of unactivated cow bone biochar was very low. Hence, although biochar derived from cow bones had the potential to adsorb Congo dye, the chemical/thermal activation process might be vital in increasing adsorption efficiency.

Table 2 presents the results of the adsorption performance of Congo red dye from wastewater using 3m HCl-activated biochar produced from cow bone waste at 45 °C.

Table 2: Adsorption performance of Congo red dye from wastewater using 3m HCl-activated biochar at 45 °C.

| Initial conc. of Congo red dye wastewater (mg/L) | Equilibrium conc (mg/L) | Amount adsorbed (mg/L) | Percentage adsorbed (%) |
| --- | --- | --- | --- |
| 20.00 | 2.40 | 17.60 | 88.00 |
| 40.00 | 6.47 | 33.53 | 83.80 |
| 60.00 | 14.51 | 45.49 | 75.82 |
| 80.00 | 38.46 | 41.54 | 51.00 |
| 100.00 | 50.55 | 49.45 | 49.50 |

The results indicated that the HCl-activated biochar exhibited higher adsorption efficiencies compared with unactivated biochar (Figure 1). This demonstrates the role of chemical activation in improving adsorption capacity. The amount of dye adsorbed increased with an increment in initial dye concentration. The percentage adsorption, on the other hand, decreased with increasing dye concentration.

Figure 1: Comparison of the percentage removal of dye at different initial concentrations (20–100 mg/L) using unactivated cow bone biochar and HCl-activated cow bone biochar. The results show significantly improved adsorption efficiency after acid activation.

The high adsorption efficiencies observed at reduced initial concentration indicated that 3M HCL activation enhanced the adsorption properties of the cow bone biochar.  Acid activation increased the surface area, improved pore structure, and generally enhanced the interaction between the adsorbent surface and the Congo red dye molecules.  On the other hand, the reduced absorption efficiencies at high concentrations indicated a saturation of the available adsorption locations and a competition among the dye molecules for the limited active sites on the biochar surface.

Table 3 presents the adsorption performance using 3m HCl-activated biochar for the removal of lead (Pb²⁺) ions from aqueous solution.

Table 3: Adsorption of Pb ion using 3M HCl-activated biochar produced from cow bone

| Initial conc. of Congo red dye wastewater (mg/L) | Equilibrium conc (mg/100ml) | Amount adsorbed (mg/100ml) | Percentage adsorbed (%) |
| --- | --- | --- | --- |
| 20.00 | 8.08 | 11.92 | 59.60 |
| 40.00 | 22.61 | 17.39 | 43.48 |
| 60.00 | 37.53 | 22.47 | 37.45 |
| 80.00 | 54.24 | 25.76 | 32.20 |

The results indicated that biochar was able to remove Pb ions from solution, although adsorption efficiency decreased with an increase in initial concentration. This was attributed to the increasing number of Pb ions competing for a limited number of active adsorption locations. High concentrations increased the mass transfer driving force, leading to an increment in the quantity of ions adsorbed. However, this led to competition for the limited active sites, reducing the removal efficiency.

Table 4 presents the adsorption performance using 3m HCl-activated biochar for the removal of cadmium (Cd²⁺) ions from aqueous solution.

Table 4: Adsorption of Cd ion using 3M HCl-activated biochar produced from cow bone

| Initial conc. of Congo red dye wastewater (mg/L) | Equilibrium conc (mg/100ml) | Amount adsorbed (mg/100ml) | Percentage adsorbed (%) |
| --- | --- | --- | --- |
| 20.00 | 0.31 | 19.69 | 98.45 |
| 40.00 | 13.42 | 26.58 | 66.45 |
| 60.00 | 26.07 | 33.93 | 56.55 |
| 80.00 | 35.79 | 44.21 | 55.26 |
| 100.00 | 49.68 | 50.32 | 50.32 |

The results indicated that biochar was able to remove Cd ions from solution, although adsorption efficiency decreased with an increase in initial concentration. Similar to Pb, this was attributed to an increasing number of Cd ions competing for a limited number of active adsorption locations (Figure 2).

Figure 2: Comparison of the percentage removal of Pb and Cd ions at different initial concentrations (20–80 mg/L) using HCl-activated cow bone biochar. The results show significantly improved adsorption efficiency for Cd, indicating a high affinity of Cd ions for the biochar surface.

These results, therefore, indicated that HCL-activated cow bone biochar had the potential to serve as a low-cost adsorbent for the removal of dyes, Pb, and Cd ions from contaminated wastewater.

Conclusion

This work evaluated the potential of biochar generated from cow bone waste to remove Congo red dye. Pb²⁺, and Cd²⁺ from solution. Unactivated biochar had very low efficiencies for Congo red dye (< 4%), while HCl-activated biochar showed significant increments in adsorption efficiencies. The adsorption efficiency for HCl-activated biochar used to remove Pb²⁺ from simulated wastewater solution varied from 59.6% at 20mg/L to 32.2% at 80mg/L of simulated wastewater. The absorption efficiency for the removal of Cd2+ varied from 98.25% at 20mg/L to 50.32% at 80mg/L. The stronger adsorption of Cd2+ implied a higher affinity of the activated biochar for cadmium ions. This was possibly a result of favorable electrostatic interactions and ion exchange processes.

This work has therefore contributed to the field of sustainable waste management by converting an agricultural waste product into material for remediating wastewater. This work has also indicated that acid activation of biochar improves overall adsorption efficiencies. Dyes and heavy metal contaminants resulting from industrial processes and anthropogenic activities pollute water bodies. The development of a low-cost and effective adsorbent in the form of cow bone biochar, therefore, offers a practical strategy for the remediation of contaminated waterbodies, while at the same time, solving the problem of animal waste disposal.

DATA AVAILABILITY

All relevant data are included in the paper or its Supplementary Information.

COMPETING INTERESTS STATEMENTS

The authors have no competing interests to declare that are relevant to the content of this article.

REFERENCES

Ahisek, K., Vhatkar, S.S., Mathew, H.T., Singh, P. and Oraon, R., 2025. A critical review on the challenges and techno-economic assessment of dyes removal technologies from waste water. Discover Chemistry, 2(1), p.41. https://doi.org/10.1007/s44371-025-00111-4

Alkhaldi, H., Alharthi, S., Alharthi, S., AlGhamdi, H.A., AlZahrani, Y.M., Mahmoud, S.A., Amin, L.G., Al-Shaalan, N.H., Boraie, W.E., Attia, M.S. and Al-Gahtany, S.A., 2024. Sustainable polymeric adsorbents for adsorption-based water remediation and pathogen deactivation: a review. RSC advances, 14(45), pp.33143-33190. https://doi.org/10.1039/d4ra05269b

Al-Tohamy, R., Ali, S.S., Li, F., Okasha, K.M., Mahmoud, Y.A.G., Elsamahy, T., Jiao, H., Fu, Y. and Sun, J., 2022. A critical review on the treatment of dye-containing wastewater: Ecotoxicological and health concerns of textile dyes and possible remediation approaches for environmental safety. Ecotoxicology and environmental safety, 231, p.113160. https://doi.org/10.1016/j.ecoenv.2021.113160

Amalina, F., Abd Razak, A.S., Krishnan, S., Sulaiman, H., Zularisam, A.W. and Nasrullah, M., 2022. Biochar production techniques utilizing biomass waste-derived materials and environmental applications–A review. Journal of Hazardous Materials Advances, 7, p.100134. https://doi.org/10.1016/j.hazadv.2022.100134

Ambaye, T.G., Vaccari, M., van Hullebusch, E.D., Amrane, A. and Rtimi, S.J.I.J.O.E.S., 2021. Mechanisms and adsorption capacities of biochar for the removal of organic and inorganic pollutants from industrial wastewater. International Journal of Environmental Science and Technology, 18(10), pp.3273-3294. https://doi.org/10.1007/s13762-020-03060-w

Atangana, E., Ajiboye, T.O., Mafolasire, A.A., Ghosh, S. and Hakeem, B., 2025. Adsorption of organic pollutants from wastewater using chitosan-based adsorbents. Polymers, 17(4), p.502. https://doi.org/10.3390/polym17040502

Chikri, R., Elhadiri, N., Benchanaa, M. and El Maguana, Y., 2020. Efficiency of sawdust as low‐cost adsorbent for dyes removal. Journal of Chemistry, 2020(1), p.8813420. https://doi.org/10.1155/2020/8813420

Collin, M.S., Venkatraman, S.K., Vijayakumar, N., Kanimozhi, V., Arbaaz, S.M., Stacey, R.S., Anusha, J., Choudhary, R., Lvov, V., Tovar, G.I. and Senatov, F., 2022. Bioaccumulation of lead (Pb) and its effects on human: A review. Journal of Hazardous Materials Advances, 7, p.100094. https://doi.org/10.1016/j.hazadv.2022.100094

Dong, Y., Guan, X. and Lin, H., 2026. Biochar for simultaneous soil remediation and carbon sequestration: application, mechanism, and development prospect–a comprehensive review. Environmental Earth Sciences, 85(4), p.98. https://doi.org/10.1007/s12665-026-12834-3

El-Ahmady El-Naggar, N., Rabei, N.H. and El-Malkey, S.E., 2020. Eco-friendly approach for biosorption of Pb2+ and carcinogenic Congo red dye from binary solution onto sustainable Ulva lactuca biomass. Scientific Reports, 10(1), p.16021. https://doi.org/10.1038/s41598-020-73031-1

Erdem, M. and Öner, A., 2025. Preparation and characterization of low-cost bio-sorbent and a novel activated carbon from agro-wastes for efficient Cr (VI) removal. Water, Air, & Soil Pollution, 236(5), p.291. https://doi.org/10.1007/s11270-025-07910-6

Forgacs, E., Cserháti, T. and Oros, G., 2004. Removal of synthetic dyes from wastewaters: a review. Environment international, 30(7), pp.953-971. https://doi.org/10.1016/j.envint.2004.02.001

Fu, F. and Wang, Q., 2011. Removal of heavy metal ions from wastewaters: a review. Journal of environmental management, 92(3), pp.407-418. https://doi.org/10.1016/j.jenvman.2010.11.011

Genchi, G., Sinicropi, M.S., Lauria, G., Carocci, A. and Catalano, A., 2020. The effects of cadmium toxicity. International journal of environmental research and public health, 17(11), p.3782. https://doi.org/10.3390/ijerph17113782

Gonzalez-Villalva, A., Marcela, R.L., Nelly, L.V., Patricia, B.N., Guadalupe, M.R., Brenda, C.T., Eugenia, C.V.M., Martha, U.C., Isabel, G.P. and Fortoul, T.I., 2025. Lead systemic toxicity: A persistent problem for health. Toxicology, 515, p.154163. https://doi.org/10.1016/j.tox.2025.154163

Haris, M., Amjad, Z., Usman, M., Saleem, A., Dyussenova, A., Mahmood, Z., Dina, K., Guo, J. and Wang, W., 2024. A review of crop residue-based biochar as an efficient adsorbent to remove trace elements from aquatic systems. Biochar, 6(1), p.47. https://doi.org/10.1007/s42773-024-00341-2

Hernández-Zamora, M. and Martínez-Jerónimo, F., 2019. Congo red dye diversely affects organisms of different trophic levels: a comparative study with microalgae, cladocerans, and zebrafish embryos. Environmental Science and Pollution Research, 26(12), pp.11743-11755. https://doi.org/10.1007/s11356-019-04589-1

Hernández-Zamora, M., Martínez-Jerónimo, F., Cristiani-Urbina, E. and Cañizares-Villanueva, R.O., 2016. Congo red dye affects survival and reproduction in the cladoceran Ceriodaphnia dubia. Effects of direct and dietary exposure. Ecotoxicology, 25(10), pp.1832-1840. https://doi.org/10.1007/s10646-016-1731-x

Hernández-Zamora, M., Perales-Vela, H.V., Flores-Ortíz, C.M. and Cañizares-Villanueva, R.O., 2014. Physiological and biochemical responses of Chlorella vulgaris to Congo red. Ecotoxicology and Environmental Safety, 108, pp.72-77. https://doi.org/10.1016/j.ecoenv.2014.05.030

Hou, S., Yuan, L., Jin, P., Ding, B., Qin, N., Li, L., Liu, X., Wu, Z., Zhao, G. and Deng, Y., 2013. A clinical study of the effects of lead poisoning on the intelligence and neurobehavioral abilities of children. Theoretical Biology and Medical Modelling, 10(1), p.13. https://doi.org/10.1186/1742-4682-10-13

Ibrahim, A.A., Ibrahim, M.A. and Yusuf, A.G., 2021. Implications of industrial effluents on surface water and ground water. World Journal of Advanced Research and Reviews, 9(3), pp.330-336. https://doi.org/10.30574/wjarr.2021.9.3.0110

Iqbal, Z., Tanweer, M.S. and Alam, M., 2022. Recent advances in adsorptive removal of wastewater pollutants by chemically modified metal oxides: A review. Journal of Water Process Engineering, 46, p.102641. https://doi.org/10.1016/j.jwpe.2022.102641

Islam, M.M., Aidid, A.R., Mohshin, J.N., Mondal, H., Ganguli, S. and Chakraborty, A.K., 2025. A critical review on textile dye-containing wastewater: Ecotoxicity, health risks, and remediation strategies for environmental safety. Cleaner Chemical Engineering, 11, p.100165. https://doi.org/10.1016/j.clce.2025.100165

Kağızman, E., Ergen, Ş.F. and Taştan, B.E., 2025. Evaluation of bioaccumulation and toxicity of Congo Red on Pseudochloris wilhelmii and Daphnia magna. Communications Faculty of Sciences University of Ankara Series C Biology, 34(1), pp.36-47. https://doi.org/10.53447/communc.1656451

Kato, S. and Kansha, Y., 2024. Comprehensive review of industrial wastewater treatment techniques. Environmental Science and Pollution Research, 31(39), pp.51064-51097. https://doi.org/10.1007/s11356-024-34584-0

Khan, R.R.M., Qamar, H., Hameed, A., Rehman, A.U., Pervaiz, M., Saeed, Z., Adnan, A. and Ch, A.R., 2022. Biological and photocatalytic degradation of Congo red, a diazo sulfonated substituted dye: a review. Water, Air, & Soil Pollution, 233(11), p.468. https://doi.org/10.1007/s11270-022-05935-9

Khan, Z., Elahi, A., Bukhari, D.A. and Rehman, A., 2022. Cadmium sources, toxicity, resistance and removal by microorganisms-A potential strategy for cadmium eradication. Journal of Saudi Chemical Society, 26(6), p.101569. https://doi.org/10.1016/j.jscs.2022.101569

Konneh, M., Wandera, S.M., Murunga, S.I. and Raude, J.M., 2021. Adsorption and desorption of nutrients from abattoir wastewater: Modelling and comparison of rice, coconut and coffee husk biochar. Heliyon, 7(11). https://doi.org/10.1016/j.heliyon.2021.e08458

Kumar, A., Bhattacharya, T., Shaikh, W.A., Roy, A., Chakraborty, S., Vithanage, M. and Biswas, J.K., 2023. Multifaceted applications of biochar in environmental management: a bibliometric profile. Biochar, 5(1), p.11. https://doi.org/10.1007/s42773-023-00207-z

Kumari, A., Yadav, M., Bhatia, A., Sharma, M. and Bhateria, R., 2025. A review and bibliometric analysis on recent modification of biochar for effective and sustainable remediation of heavy metals in aqueous medium. Discover Chemical Engineering, 5(1), p.21. https://doi.org/10.1007/s43938-025-00088-7

Larsen, B. and Sánchez-Triana, E., 2023. Global health burden and cost of lead exposure in children and adults: a health impact and economic modelling analysis. The Lancet Planetary Health, 7(10), pp.e831-e840. https://doi.org/10.1016/s2542-5196(23)00166-3

Le, P.T., Bui, H.T., Le, D.N., Nguyen, T.H., Pham, L.A., Nguyen, H.N., Nguyen, Q.S., Nguyen, T.P., Bich, N.T., Duong, T.T. and Herrmann, M., 2021. Preparation and characterization of biochar derived from agricultural by-products for dye removal. Adsorption Science & Technology, 2021, p.9161904. https://doi.org/10.1155/2021/9161904

Lima, M.A., Islam, M.H., Neogi, S., Nasrin, K., Sen, A., Masood, A., David, G.S., Pathan, M.M., Olalekan, B.A., Bordin, C. and Al Mamun Hridoy, M.A., 2025. Recent advances in biochar technology for aquatic pollution control: a critical review of applications, barriers, and future opportunities. Discover Sustainability, 6(1), p.980. https://doi.org/10.1155/2021/9161904

Lin, J., Ye, W., Xie, M., Seo, D.H., Luo, J., Wan, Y. and Van der Bruggen, B., 2023. Environmental impacts and remediation of dye-containing wastewater. Nature Reviews Earth & Environment, 4(11), pp.785-803. https://doi.org/10.1038/s43017-023-00489-8

Lugo-Arias, J., González-Álvarez, J. and Maturana, A., 2026. Mg-impregnated rice husk biochar in fixed-bed columns: high-capacity continuous-flow removal of nitrate and phosphate from wastewater. Biomass Conversion and Biorefinery, 16(4), p.149. https://doi.org/10.1007/s13399-026-07093-y

Lukić, D., Vasić, V., Živančev, J., Antić, I., Panić, S., Petronijević, M. and Đurišić-Mladenović, N., 2025. Adsorption performance assessment of agro-waste-based biochar for the removal of emerging pollutants from municipal WWTP effluent. Molecules, 30(24), p.4803. https://doi.org/10.3390/molecules30244803

Meftah, S., Meftah, K., Babassa, N., Malous, K., Drissi, M., Amahrous, A., Jabri, N., Fathi, J., Aguerchi, K., Laababid, Y. and Adnouss, O., 2025. The versatility and effectiveness of bio-adsorbents in the removal of chemical pollutants from water: adsorption mechanisms, optimization by ANN and RSM, SWOT analysis, and contribution to the 3rd and 6 th Sustainable Development Goals. Discover Sustainability, 6(1), p.971. https://doi.org/10.1007/s43621-025-01359-7

Mnyango, J.I., Nyoni, B., Phiri, C., Fouda-Mbanga, B.G., Amusat, S.O., Maringa, A., Yalala-Ndlovu, B., Hlabano-Moyo, B., Tywabi-Ngeva, Z. and Hlangothi, S.P., 2025. Sustainable wastewater treatment: Mechanistic, environmental, and economic insights into biochar for synthetic dye removal. Next Materials, 9, p.100974. https://doi.org/10.1016/j.nxmate.2025.100974

Nguyen, T.A.H., Ngo, H.H., Guo, W.S., Zhang, J., Liang, S., Yue, Q.Y., Li, Q. and Nguyen, T.V., 2013. Applicability of agricultural waste and by-products for adsorptive removal of heavy metals from wastewater. Bioresource technology, 148, pp.574-585. https://doi.org/10.1016/j.biortech.2013.08.124

Oladimeji, T.E., Oyedemi, M., Emetere, M.E., Agboola, O., Adeoye, J.B. and Odunlami, O.A., 2024. Review on the impact of heavy metals from industrial wastewater effluent and removal technologies. Heliyon, 10(23). https://doi.org/10.1016/j.heliyon.2024.e40370

Oladoye, P.O., Bamigboye, M.O., Ogunbiyi, O.D. and Akano, M.T., 2022. Toxicity and decontamination strategies of Congo red dye. Groundwater for Sustainable Development, 19, p.100844. https://doi.org/10.1016/j.gsd.2022.100844

Patel, D., Singh, A., Ambati, S.R., Singh, R.S. and Sonwani, R.K., 2024. An overview of recent advances in treatment of complex dye-containing wastewater and its techno-economic assessment. Journal of Environmental Management, 370, p.122804. https://doi.org/10.1016/j.jenvman.2024.122804

Pathy, A., Pokharel, P., Chen, X., Balasubramanian, P. and Chang, S.X., 2023. Activation methods increase biochar's potential for heavy-metal adsorption and environmental remediation: A global meta-analysis. Science of The Total Environment, 865, p.161252. https://doi.org/10.1016/j.scitotenv.2022.161252

Phiri, Z., Moja, N.T., Nkambule, T.T. and de Kock, L.A., 2024. Utilization of biochar for remediation of heavy metals in aqueous environments: A review and bibliometric analysis. Heliyon, 10(4). https://doi.org/10.1016/j.heliyon.2024.e25785

Puglla, E.P., Guaya, D., Tituana, C., Osorio, F. and García-Ruiz, M.J., 2020. Biochar from agricultural by-products for the removal of lead and cadmium from drinking water. Water, 12(10), p.2933. https://doi.org/10.3390/w12102933

Qu, F. and Zheng, W., 2024. Cadmium exposure: mechanisms and pathways of toxicity and implications for human health. Toxics, 12(6), p.388. https://doi.org/10.3390/toxics12060388

Rajan, M., Karunanidhi, D., Jaya, J., Preethi, B., Subramani, T. and Aravinthasamy, P., 2024. A comprehensive review on human health hazards due to groundwater contamination: A global perspective. Physics and Chemistry of the Earth, Parts A/B/C, 135, p.103637. https://doi.org/10.1016/j.pce.2024.103637

Rajput, V., Saini, I., Parmar, S., Pundir, V., Kumar, V., Kumar, V., Naik, B. and Rustagi, S., 2024. Biochar production methods and their transformative potential for environmental remediation. Discover Applied Sciences, 6(8), p.408. https://doi.org/10.1007/s42452-024-06125-4

Rangabhashiyam, S., dos Santos Lins, P.V., de Magalhães Oliveira, L.M., Sepulveda, P., Ighalo, J.O., Rajapaksha, A.U. and Meili, L., 2022. Sewage sludge-derived biochar for the adsorptive removal of wastewater pollutants: A critical review. Environmental Pollution, 293, p.118581. https://doi.org/10.1016/j.envpol.2021.118581

Rani, L., Kaushal, J., Srivastav, A.L., Abdulla, S., Prabha, C. and Joshi, H., 2025. Cadmium toxicity, health risk and its remediation using low-cost biochar adsorbents. Open Life Sciences, 20(1), p.20251131. https://doi.org/10.1515/biol-2025-1131

Rashad, E., Saleh, H.N., Eltaweil, A.S., Saleh, M.E., Sillanpaa, M. and Mostafa, A.R., 2023. Pinewood sawdust biochar as an effective biosorbent for PAHs removal from wastewater. Biomass Conversion and Biorefinery, 13(15), pp.13443-13459. https://doi.org/10.1007/s13399-021-02181-7

Rasin, P., Ashwathi, A.V., Basheer, S.M., Haribabu, J., Santibanez, J.F., Garrote, C.A., Arulraj, A. and Mangalaraja, R.V., 2025. Exposure to cadmium and its impacts on human health: A short review. Journal of Hazardous Materials Advances, 17, p.100608. https://doi.org/10.1016/j.hazadv.2025.100608

Rathi, B.S. and Kumar, P.S., 2021. Application of adsorption process for effective removal of emerging contaminants from water and wastewater. Environmental Pollution, 280, p.116995. https://doi.org/10.1016/j.envpol.2021.116995

Ren, Y., Yang, Y., Qu, G., Ning, P., Ren, N., Chen, X., Wang, Z. and Hu, Y., 2023. HCl-assisted KOH activated Chinese medicine residue biochar as a new method to improve the purification capacity of lead-containing wastewater: Experimental and mechanism studies. Sustainable Chemistry and Pharmacy, 33, p.101063. https://doi.org/10.1016/j.scp.2023.101063

Rezvani, B., Hallajisani, A. and Tavakoli, O., 2025. Super-effective biochar adsorbents from Co-pyrolysis of rice husk and sewage sludge: Adsorption performance, advanced regeneration, and economic analysis. Bioresource Technology Reports, 29, p.102046. https://doi.org/10.1016/j.biteb.2025.102046

Sanders, T., Liu, Y., Buchner, V. and Tchounwou, P.B., 2009. Neurotoxic effects and biomarkers of lead exposure: a review. Reviews on environmental health, 24(1), p.15. https://doi.org/10.1515/reveh.2009.24.1.15

Saravanakumar, K., De Silva, S., Santosh, S.S., Sathiyaseelan, A., Ganeshalingam, A., Jamla, M., Sankaranarayanan, A., Veeraraghavan, V.P., MubarakAli, D., Lee, J. and Thiripuranathar, G., 2022. Impact of industrial effluents on the environment and human health and their remediation using MOFs-based hybrid membrane filtration techniques. Chemosphere, 307, p.135593. https://doi.org/10.1016/j.chemosphere.2022.135593

Sen, T.K., 2023. Agricultural solid wastes based adsorbent materials in the remediation of heavy metal ions from water and wastewater by adsorption: a review. Molecules, 28(14), p.5575. https://doi.org/10.3390/molecules28145575

Shabbirahmed, A.M., Jacob, A., Dey, P., Somu, P. and Haldar, D., 2025. Biomass as eco-friendly adsorbents for the removal of emerging pollutants from wastewater: A review. Discover Applied Sciences, 7(7), p.771. https://doi.org/10.1007/s42452-025-07463-7

Sharma, N., Yadav, A., Yadav, S., Panghal, P., Singh, S., Deep, A. and Kumar, S., 2024. Biomass-based adsorbents for wastewater remediation: A systematic review on removal of emerging contaminants. Microchemical Journal, 207, p.111880. https://doi.org/10.1016/j.microc.2024.111880

Siddiqui, S.I., Allehyani, E.S., Al-Harbi, S.A., Hasan, Z., Abomuti, M.A., Rajor, H.K. and Oh, S., 2023. Investigation of Congo red toxicity towards different living organisms: a review. Processes, 11(3), p.807. https://doi.org/10.3390/pr11030807

Singh, P.K., Kumar, U., Kumar, I., Dwivedi, A., Singh, P., Mishra, S., Seth, C.S. and Sharma, R.K., 2024. Critical review on toxic contaminants in surface water ecosystem: sources, monitoring, and its impact on human health. Environmental Science and Pollution Research, 31(45), pp.56428-56462. https://doi.org/10.1007/s11356-024-34932-0

Sun, L.M., McIntyre, S.R., Iacomi, P., Everden, K., Williams, P.T., Zong, S., Liu, X., Zhu, X., Yang, Y., Li, S. and Wu, G., 2025. Biochar production, activation, and applications: A comprehensive technical review. Carbon Capture Science & Technology, 16, p.100421. https://doi.org/10.1016/j.ccst.2025.100421

Tang, R., Qiu, S., Wu, C. and Tan, J., 2025. Biochar: from agricultural waste byproducts to novel adsorbents for ammonia and micro/nanoplastics (MNPs). Biochar, 7(1), p.122. https://doi.org/10.1007/s42773-025-00554-z

Ungureanu, E.L., Mocanu, A.L., Stroe, C.A., Panciu, C.M., Berca, L., Sionel, R.M. and Mustatea, G., 2023. Agricultural byproducts used as low-cost adsorbents for removal of potentially toxic elements from wastewater: a comprehensive review. Sustainability, 15(7), p.5999. https://doi.org/10.3390/su15075999

Wang, Y., Chen, L., Zhu, Y., Fang, W., Tan, Y., He, Z. and Liao, H., 2024. Research status, trends, and mechanisms of biochar adsorption for wastewater treatment: a scientometric review. Environmental Sciences Europe, 36(1), p.25. https://doi.org/10.1186/s12302-024-00859-z

Yaseen, D.A. and Scholz, M., 2019. Textile dye wastewater characteristics and constituents of synthetic effluents: a critical review. International journal of environmental science and technology, 16(2), pp.1193-1226. https://doi.org/10.1007/s13762-018-2130-z

Yu, H., Li, C., Yan, J., Ma, Y., Zhou, X., Yu, W., Kan, H., Meng, Q., Xie, R. and Dong, P., 2023. A review on adsorption characteristics and influencing mechanism of heavy metals in farmland soil. RSC advances, 13(6), pp.3505-3519. https://doi.org/10.1039/d2ra07095b

Zhang, X., Lv, D., Liu, Z., Xu, D., Yang, F., Tang, Q., Zhong, L., Liang, Z. and Jia, Q., 2025. From waste to Resource: Engineering biochar through optimized HCl activation for microplastic mitigation. Chemical Engineering Science, 304, p.121091. https://doi.org/10.1016/j.ces.2024.121091