In Situ Ophthalmic Gels Meet Nanotechnology: Nanoparticle-Laden Smart Hydrogels for Precision Ocular Drug Delivery

Background:
Topical ocular therapy is dominated by eye drops, yet drug delivery to ocular tissues is frequently inefficient because of rapid tear dilution, blinking, nasolacrimal drainage, and layered anatomical barriers. These limitations can lead to low bioavailability, frequent dosing, variable clinical response, and avoidable systemic exposure. Stimuli-responsive in situ gels and drug nanocarriers have each been developed to address parts of this problem, motivating integrated “nano-in-gel” systems.

Objective:
To summarize and critically analyze nanoparticle-laden in situ ophthalmic gels as precision drug-delivery platforms for anterior and posterior segment diseases, focusing on design rationale, materials, performance outcomes, and translational barriers.

Method:
This narrative review synthesizes peer-reviewed research on ophthalmic in situ gelling systems (thermo-, pH-, and ion-activated) and nanocarriers (polymeric nanoparticles, lipid nanoparticles, liposomes, micelles, dendrimers, and nanogels), with emphasis on hybrid formulations in which nanoparticles are dispersed within an in situ gelling matrix. Key formulation variables, characterization methods, and in vitro/ex vivo/in vivo evaluation approaches are summarized.

Results:
Across reported studies, nanoparticle-laden in situ gels consistently improve precorneal residence time and enable sustained drug release, often translating into higher corneal permeation and enhanced pharmacodynamic effects in models of glaucoma, keratitis, dry eye disease, and ocular inflammation. Performance is driven by dual mechanisms: gel-mediated retention and nanoparticle-mediated protection, solubilization, and controlled release. However, clinical translation is constrained by sterilization compatibility, long-term stability, scalable manufacturing, and regulatory complexity for combination products.

Conclusion:
Nanoparticle-laden in situ gels are promising, adaptable platforms that can reduce dosing burden and improve ocular exposure, but progress to routine clinical use will depend on robust quality-by-design development, standardized characterization, and clinically relevant safety and efficacy validation.

Keywords

In situ gel; ophthalmic drug delivery; nanoparticle-laden in situ gel; stimuli-responsive hydrogel; thermos-responsive gel; pH-sensitive gel; ion-activated gel; ocular bioavailability.

01. INTRODUCTION

1.1 Global ocular disease burden and projected growth

Ocular diseases continue to impose a major global health burden because they reduce independence, restrict educational and employment opportunities, and increase care needs across the lifespan. The WHO World report on vision (2019) estimates that at least 2.2 billion people live with vision impairment or blindness, and at least 1 billion of these cases are preventable or remain unaddressed due to gaps in access and service coverage [01]. Large-scale burden-of-disease analyses reinforce that this is not a marginal problem: the GBD 2019 Blindness and Vision Impairment Collaborators reported substantial global prevalence of blindness and moderate-to-severe vision impairment around 2020, with cataract, glaucoma, undercorrected refractive error, age-related macular degeneration, and diabetic retinopathy among key contributors [02]. Beyond health consequences, the economic rationale for better eye care is strong WHO has summarized estimates suggesting that global productivity losses associated with unaddressed vision impairment are on the order of ~US$ 410.7 billion, far exceeding the estimated investment required to close major service gaps [03].

1.2 Why ocular drug delivery is intrinsically difficult

Despite the availability of potent drug molecules, ocular pharmacotherapy is constrained by the eye’s anatomy and physiology, which are optimized to exclude foreign material. From a formulation standpoint, the ocular surface is protected by fast dynamic clearance (tear turnover, reflex lacrimation, and blinking) and directional drainage through the nasolacrimal system, all of which rapidly reduce drug contact time. In addition, static barriers especially the corneal epithelium with tight junctions limit passive diffusion, while deeper targets are further protected by blood–ocular barriers. Reviews of ocular dosage forms consistently highlight that successful delivery is not simply about drug potency; it depends on overcoming multiple coordinated barriers that act within minutes of topical administration [04,05].

1.3 Limitations of conventional ophthalmic dosage forms

Topical eye drops dominate routine care because they are inexpensive, familiar, and suitable for self-administration. However, their performance is fundamentally limited by low viscosity, short ocular residence time, and large “functional losses” immediately after instillation (overflow and drainage). Standard pharmaceutics references note that topical delivery is inefficient, with only ~1–5% of an instilled dose typically reaching the aqueous humor; the same sources also emphasize that eye drops make up over 90% of ophthalmic preparations used in clinical practice, despite their well-known bioavailability limitations [06]. This mismatch high clinical reliance but low delivery efficiency drives frequent dosing, increases exposure to preservatives/excipients, and can worsen adherence in chronic conditions such as glaucoma and dry eye. Alternative approaches (ointments, inserts, injections) may improve residence time or posterior targeting but often trade convenience for blurred vision, discomfort, invasiveness, and procedure-related risks [04,06].

1.4 Rise of nanotechnology for precision ocular delivery

Nanotechnology has become a central strategy in modern ocular drug delivery because nanoscale carriers can be engineered to address several formulation problems at once: improving the apparent solubility of poorly water-soluble drugs, protecting labile molecules, modulating release kinetics, and tailoring surface properties to increase interaction with ocular mucus or epithelial surfaces. Broad reviews describe how platforms such as polymeric nanoparticles, lipid nanoparticles, liposomes, nanoemulsions, and micelles can enhance local exposure and reduce dosing frequency by enabling sustained release and better tissue interaction [07,08]. However, nanoparticles delivered as simple aqueous dispersions can still be cleared rapidly from the ocular surface, limiting the time available for permeation so improved retention strategies are often required to translate nanocarrier advantages into clinically meaningful exposure gains [07,08].

1.5 Emergence of in situ gelling ophthalmic systems

In situ gelling systems were developed to extend residence time without sacrificing dosing convenience. These formulations are instilled as low-viscosity drops and then undergo sol-to-gel transformation on the ocular surface, typically triggered by physiological cues such as temperature, pH, or tear electrolytes. Recent high-level reviews describe in situ gels as a practical route to longer precorneal retention, sustained release, and improved patient compliance while maintaining accurate dosing as a liquid prior to gelation [09,10]. Gel-based ophthalmic materials literature further shows that commonly used polymers (e.g., gellan gum, carbomers, poloxamers, alginates, and cellulose derivatives) can be selected and blended to tune gelation speed, strength, mucoadhesion, and comfort during blinking [11].

1.6 The combined approach: nanoparticle-laden smart hydrogels

Because nanoparticles excel at drug protection and controlled release, while in situ gels excel at ocular retention, integrating both into one platform is a logical next step. Nanoparticle-laden in situ gels are designed to (i) hold the formulation on the eye by gelling in the cul-de-sac and (ii) deliver drug in a controlled fashion from embedded nanoparticles, potentially improving penetration and sustaining exposure. This hybrid “gel + nanocarrier” concept has since become a foundation for precision topical platforms aimed at reducing dosing frequency while improving local efficacy and tolerability [09–12].

02. ANATOMY OF THE EYE & OCULAR BARRIERS

2.1 Ocular anatomy

For drug-delivery purposes, the eye is often discussed as two functional compartments: the anterior segment and the posterior segment. The anterior segment includes the cornea (epithelium, stroma, endothelium), anterior chamber filled with aqueous humor, iris, ciliary body, and the lens. This region is the main target of topical therapy for conditions such as conjunctivitis, keratitis, dry eye disease, and many glaucoma treatments. In contrast, the posterior segment comprises the vitreous humor, retina, choroid, and optic nerve, and is implicated in sight-threatening diseases such as diabetic retinopathy and age-related macular degeneration conditions that are difficult to treat with conventional eye drops because the target tissues lie deeper and are protected by stronger physiological barriers. Conceptually, the lens and vitreous act as internal “checkpoints” that limit the passive diffusion of drug from the front of the eye to the retina, even if some drug enters the aqueous humor. [13]

Fig No 01 - Nano-in-Gel Convergence: Mechanism of Ocular Drug Delivery After Instillation

Figure 1. Schematic illustration of nano-in-gel convergence showing instillation, stimulus-triggered gelation (temperature, pH, ions), gel depot formation, dual-controlled drug release, and improved therapeutic outcomes in ocular delivery

2.2 Ocular barriers to drug delivery

Ocular barriers can be grouped into static barriers (tissue-structure barriers that restrict diffusion) and dynamic barriers (physiological clearance processes that rapidly remove drug from the ocular surface). Together, these barriers explain why topical administration is convenient yet typically inefficient, and why posterior-segment exposure from standard drops is usually minimal. [13]

2.2.1 Static barriers

Corneal barrier (epithelium–stroma–endothelium): The cornea is the principal gateway for topical delivery into the eye, but it is also a highly selective filter. The corneal epithelium, with tight junctions, strongly limits paracellular transport and preferentially restricts large and hydrophilic molecules. Reviews describe this epithelial “seal” as allowing only very small pathways (often discussed on the nanometer scale), making transcorneal transport highly dependent on molecular size, lipophilicity, and ionization. Beneath it, the stroma is collagen-rich and hydrophilic, tending to impede lipophilic molecules that cross the epithelium. The endothelium is a thin inner layer separating the stroma from the aqueous humor and offers comparatively less resistance than the epithelium, but it still contributes to overall selectivity. [17]

Scleral barrier: The sclera (the “white” of the eye) is sometimes described as a potential alternative route for delivery toward posterior tissues, especially for periocular approaches. Compared with the cornea, scleral transport is often less governed by lipophilicity and more by molecular size (radius), but access is still limited by drug loss into local blood/lymphatic pathways and by downstream barriers (notably choroid and retinal barriers). [13]

Blood–aqueous barrier (BAB): Even if a drug reaches systemic circulation, entry into the anterior chamber is limited by the BAB, which is formed by tight junctions and specialized cellular layers in the iris–ciliary body region. Importantly, the BAB is not merely a passive wall; it expresses multiple influx/efflux transporters that can reduce drug entry from blood to aqueous humor and can actively contribute to drug elimination from aqueous humor further lowering intraocular exposure after systemic dosing. [18]

Blood–retinal barrier (BRB): The posterior segment is protected by the BRB, one of the tightest biological barriers in the body. It has two key components: the inner BRB (tight junctions between retinal capillary endothelial cells) and the outer BRB (tight junctions at the retinal pigment epithelium). This barrier tightly regulates movement of ions, proteins, and water, and its integrity is central to retinal homeostasis. From a delivery standpoint, this is a major reason why systemic drugs and topical drops rarely achieve therapeutic retinal levels without specialized strategies. [19]

2.2.2 Dynamic barriers

Precorneal dilution and tear turnover (washout): Immediately after instillation, the drop mixes with the tear film and is rapidly diluted. Normal tear-film volume is commonly reported in the single-digit microliter range (e.g., ~6–10 μL), and tear film turnover has been reported on the order of ~16% per minute under typical conditions meaning the ocular surface environment is continuously refreshed, which shortens drug contact time. [15]

Reflex lacrimation and blinking: Instillation itself can trigger reflex tearing and blinking, accelerating clearance. Under typical room conditions, the blink rate in normal adults is often reported around 15–20 blinks per minute, and blinking actively redistributes tears while also contributing to mechanical clearance of instilled material from the ocular surface. [16]

Nasolacrimal drainage and systemic absorption: A substantial fraction of an instilled dose is lost via nasolacrimal drainage into the nasal cavity, where it can undergo systemic absorption an issue particularly relevant for potent drugs (e.g., some glaucoma agents). Quantitatively, reviews report an initial first-order drainage rate around ~1.2 μL/min in humans, and emphasize that drug residence on the ocular surface can be very brief (often on the order of minutes), depending on drop volume and reflex responses. [14]

Aqueous humor turnover (intraocular clearance): Once drug enters the anterior chamber, it does not remain indefinitely. It is cleared with aqueous humor outflow via trabecular and uveoscleral pathways an important reason why sustained delivery systems are valuable even after successful corneal penetration. [17]

2.3 Implications for drug-delivery design (why nanoparticle-laden in situ gels help)

Because ocular loss is driven by both rapid external clearance (tears, blinking, drainage) and strong tissue barriers (cornea, BAB/BRB), successful topical systems increasingly rely on multifunctional designs. In situ gels primarily address the dynamic problem by increasing precorneal residence time after sol-to-gel transition, thereby reducing immediate washout. Nanoparticles, meanwhile, can protect drug, improve apparent solubility, tune release kinetics, and enhance interaction with ocular tissues helping overcome static constraints such as epithelial tight junction resistance and the “lipophilic–hydrophilic sandwich” nature of the cornea. The combined platform (nanoparticles dispersed in a gelling matrix) therefore targets the two biggest failure modes of conventional drops: insufficient contact time and insufficient penetration/retention at the site of action. In posterior delivery contexts, material properties such as nanoparticle surface charge also matter because charged carriers can interact differently with gel-like biological matrices such as the vitreous. [14,20]

Table 1. Summary of ocular barriers and their impact on drug delivery

| Barrier type | Specific barrier | Main effect on drug delivery | Practical outcome |
| --- | --- | --- | --- |
| Dynamic | Tear dilution/turnover | Rapid dilution + washout | Short exposure window; frequent dosing needed |
| Dynamic | Reflex lacrimation | Increased tear flow after instillation | Faster loss of drug from precorneal area |
| Dynamic | Blinking | Mechanical clearance + redistribution | Reduced residence time; variable absorption |
| Dynamic | Nasolacrimal drainage | Physical drainage + systemic uptake | Lower ocular bioavailability; possible systemic side effects |
| Static | Corneal epithelium | Tight junctions restrict hydrophilic/large drugs | Low permeability; formulation must aid transport |
| Static | Corneal stroma | Hydrophilic collagen matrix resists lipophilic diffusion | “Second barrier” for lipophilic molecules |
| Static | Sclera/choroid route | Size-dependent permeability + vascular clearance | Limits sustained posterior exposure |
| Static | BAB | Tight junctions + transporters limit blood→aqueous entry | Systemic dosing inefficient for anterior chamber |
| Static | BRB | Very tight inner/outer barriers | Systemic/topical dosing inefficient for retina |
| Static/Dynamic | Vitreous | Gel structure + electrostatic interactions | Particle diffusion depends on size/charge |

03. CONVENTIONAL OCULAR DRUG DELIVERY SYSTEMS & THEIR LIMITATIONS

3.1 Eye drops (solutions, suspensions, emulsions)

Conventional eye drops remain the dominant dosage form in ophthalmology because they are inexpensive, portable, non-invasive, and straightforward for self-administration. In practice, drops are formulated mainly as aqueous solutions, suspensions, or emulsions, depending on drug solubility and stability requirements. However, even when patient technique is optimal, topical drops typically suffer from very low ocular bioavailability because most of the instilled dose is rapidly removed by tear turnover, blinking, and nasolacrimal drainage before meaningful corneal uptake occurs. As a result, topical exposure is often short-lived and variable, which explains the frequent-dosing schedules used for many chronic therapies. [21,22]

Solutions are generally preferred when feasible because they offer dose uniformity, ease of manufacturing, and good tolerability but many modern drug candidates are poorly water soluble, limiting the practicality of simple solution drops. [23] Suspensions are widely used for hydrophobic drugs; they can, in theory, prolong contact time as particles reside transiently in the conjunctival cul-de-sac and dissolve gradually. In reality, suspensions are formulation-challenging: particle size must be controlled (commonly kept below ~10 μm for comfort), and inadequate shaking or sedimentation can lead to dose inconsistency and irritation. [23] Emulsions (especially oil-in-water) help keep lipophilic drugs in solution and can reduce some suspension-related variability, but they introduce their own constraints (surfactant selection, droplet-size control, physical stability, and occasional discomfort). [23]

Fig No 02 – Therapeutic Applications and Translational Roadmap for Nano-in-Gel Technologies

Figure 02. Schematic overview of disease application mapping and translational pathway of nano-in-gel systems. The figure highlights key therapeutic areas (e.g., ocular, cancer, infectious, and inflammatory diseases) alongside stages of development, including formulation design, preclinical evaluation, clinical trials, regulatory approval, and clinical implementation.

3.2 Ointments

Ophthalmic ointments are semisolid systems (often based on mineral oil/petrolatum-type bases) that can meaningfully increase ocular contact time compared with drops. Reviews note that ointments may extend residence and create a depot effect, which can enhance local exposure for certain drugs. [23] Their major limitation is poor patient acceptability, largely due to blurred vision, greasy sensation, and difficulty applying a consistent dose (a reproducible “ribbon” length). For this reason, ointments are frequently reserved for bedtime use or for specific indications where prolonged surface contact is prioritized over daytime visual clarity. [23]

3.3 Intravitreal injections (IVT)

For posterior-segment diseases, intravitreal injection has become a cornerstone of modern therapy because it can achieve high local drug concentrations in the vitreous and retina levels that topical administration rarely reaches. Intravitreal injections are among the most commonly performed ophthalmic procedures, but their effectiveness comes with clear trade-offs. Even when performed under appropriate aseptic technique, sight-threatening complications can occur, including endophthalmitis and retinal detachment; medication- or procedure-related inflammatory events have also been described. [24]

A practical clinical drawback is that many regimens require repeated injections, which increases treatment burden, reduces long-term adherence, and cumulatively raises procedural risk exposure. In addition to infection and detachment, reported adverse outcomes across intravitreal delivery strategies include hemorrhage, intraocular inflammation, and intraocular pressure (IOP) elevation (risk profiles vary by drug class and patient factors). [24,26]

3.4 Implants (biodegradable and non-biodegradable)

Ocular implants were developed to reduce dosing frequency by providing long-acting release (weeks to years) inside or adjacent to ocular compartments. Broadly, implants may be biodegradable (designed to break down in vivo) or non-biodegradable (designed as long-term reservoirs). Material-focused reviews emphasize that non-biodegradable implants can be effective drug depots but may be less attractive clinically because they can require surgical removal at end-of-life and carry procedure-related risks. [25] System-level reviews of intravitreal delivery further discuss that implant-based strategies while extending treatment duration can be associated with complications such as cataract formation, IOP elevation, hemorrhage, retinal detachment, endophthalmitis, or device-related issues (e.g., dislocation), depending on device type and indication. [26]

3.5 Contact lenses (therapeutic/drug-eluting lenses)

Drug-eluting contact lenses represent a compelling conventional-to-transitional platform because they sit directly on the ocular surface and can, in principle, sustain drug release into the tear film for longer durations than a drop. Systematic reviews highlight their potential for improved bioavailability and extended delivery without repeated instillation. [27] However, translation remains limited by challenges in comfort, oxygen permeability, infection risk, patient-to-patient variability, and the technical difficulty of achieving predictable loading and reproducible release kinetics under real-world wear conditions. [27]

Table 2. Conventional ocular dosage forms advantages, limitations & bioavailability

| Dosage form | Typical ocular bioavailability (general) | Key limitation |
| --- | --- | --- |
| Eye drops (solutions) | Often <5% of instilled dose | Rapid precorneal drainage and short residence time |
| Suspensions | Variable (often low; depends on particle size/dissolution) | Dose non-uniformity, need for shaking, irritation risk |
| Emulsions | Variable | Physical stability/surfactant tolerability; formulation complexity |
| Ointments | Slightly higher surface residence than drops | Blurred vision, discomfort, dosing variability |
| Intravitreal injections | High (local) | Invasive; risk of endophthalmitis/retinal detachment; repeat-visit burden |
| Implants | Sustained (weeks–years) | Surgical/injectable procedure; device-related and steroid-related risks |
| Drug-eluting contact lenses | Potentially improved vs drops (depends on design) | Comfort, safety (infection), and reproducible release control |

04. IN SITU GEL SYSTEMS   CONCEPT, MECHANISMS & POLYMERS

4.1 Concept and rationale

Ophthalmic in situ gels are formulations instilled as low-viscosity liquids (sols) that transform into a gel depot on the ocular surface after administration. The core idea is simple: dosing remains as convenient as an eye drop, but once the formulation encounters ocular conditions (temperature, tear pH, and/or tear ions), it thickens into a structured gel that resists immediate removal. This approach has been widely reviewed as a practical strategy to address one of the biggest limitations of topical therapy short precorneal residence time thereby supporting more sustained drug exposure and potentially reducing dosing frequency. [28–31]

Mechanistically, many in situ gels are built from polymers that undergo reversible phase transitions. In ophthalmic use, the gel must satisfy competing requirements: it should be fluid enough in the bottle and during instillation, then quickly form a gel in the cul-de-sac, while still remaining comfortable during blinking. A key concept here is pseudoplastic (shear-thinning) behavior: the gel can be relatively viscous at rest (helping retention), yet thin under shear (helping spreadability and minimizing blink interference). This “high viscosity when still, lower viscosity when moving” profile is repeatedly highlighted in gel-based ocular delivery literature as desirable for patient comfort and performance. [29–31]

From a formulation-design viewpoint, in situ gelling systems are typically justified by four main advantages:

- Longer residence time on the ocular surface (less washout),

- Sustained/controlled release (drug remains available longer),

- Improved ocular bioavailability compared with simple drops (more time to permeate), and

- Better adherence and convenience (reduced dosing frequency supports compliance). [28,30] 1

Finally, these systems also create a platform for combination strategies e.g., loading drug in nanoparticles and then dispersing those nanoparticles into an in situ gel vehicle. Several reviews explicitly note that in situ gels can act as carriers for drug-loaded nano/microparticles, which is directly relevant to “nanoparticle-laden smart hydrogels” discussed later in your review. [31,32]

Fig No 03 -Ocular Anatomy and Barrier Overlay Highlighting Challenges in Topical Drug Delivery

Figure 03. Schematic representation of ocular anatomy overlaid with key barriers to topical drug delivery. The figure illustrates precorneal factors (tear film turnover, blinking, and nasolacrimal drainage), corneal barriers (epithelium with tight junctions, hydrophilic stroma, and endothelium), and conjunctival/scleral pathways. These combined static and dynamic barriers significantly limit drug residence time and ocular bioavailability.

4.2 Stimuli-responsive mechanisms of in situ gelation

In ocular formulations, gelation is most commonly triggered by temperature, pH, and ionic strength, because these stimuli are predictable at the ocular surface and can be exploited without external devices. The triggers can be used individually or combined to fine-tune gelation speed, gel strength, and stability. [28,30,33]

4.2.1 Temperature-triggered (thermoresponsive) systems

Thermoresponsive in situ gels are designed so that the formulation is a free-flowing solution at room temperature but forms a gel near ocular surface temperature. In many systems, the transition is discussed in terms of an LCST-type behavior: below a threshold temperature the polymer chains remain hydrated and more soluble; above it, hydrophobic interactions strengthen, polymer chains collapse or reorganize, and gel structure develops. [33,43]

Poloxamers (especially Poloxamer 407/F127, often blended with Poloxamer 188) are among the best-known thermogelling excipients in ophthalmics. A practical way to understand poloxamer gelation is micelle formation and packing: as temperature rises (and concentration is sufficient), polymer self-assembly increases and a continuous network form, producing a gel-like structure. The concentration dependence is crucial classic rheology work showed that increasing poloxamer concentration lowers the sol–gel transition temperature and increases elasticity, but dilution by tears can shift behavior and limit performance if formulation design is not optimized. [33,34]

Recent mechanistic/formulation studies continue to emphasize that drug and polymer blends (e.g., adding HPMC) can influence gel strength and gelation temperature sometimes improving adhesion and slowing gel erosion, which can help sustain release. [29,35]

Beyond poloxamers, PNIPAAm (poly(N-isopropylacrylamide))-based hydrogels are a classic thermoresponsive class with LCST around the low-30°C range. Posterior-segment oriented work (developed as injectable thermoresponsive hydrogels) highlights PNIPAAm’s fast, reversible phase change but also notes design challenges such as incomplete release (residual entrapped protein), motivating material modifications (e.g., macroporous structures or copolymers). [43]

A clinically relevant thermogelling family for longer-acting ocular depots is PLGA-PEG-PLGA. Studies have shown PLGA-PEG-PLGA solutions can gel near ocular temperatures and substantially increase intraocular exposure compared with conventional drops. For example, a PLGA-PEG-PLGA formulation for dexamethasone acetate reported a critical solution temperature close to the ocular surface temperature and markedly higher anterior-chamber exposure than eye drops. [40] Thermosensitive PLGA-PEG-PLGA hydrogels have also been investigated as intravitreal depots for sustained release of biologics such as bevacizumab with reports of in situ gel formation after injection and extended retention/release in vivo. [41]

4.2.2 pH-triggered systems

pH-triggered ocular in situ gels are engineered so the product remains a pourable solution at a lower formulation pH but becomes a gel when exposed to tear fluid pH (commonly discussed around pH ~7.4). The molecular driver is typically ionization of acidic/basic pendant groups: as pH changes, polymer charge increases, electrostatic repulsion expands the network, and viscosity rises sharply. [29,36,38]

Carbopol/Carbomer (poly(acrylic acid) derivatives) are the most frequently cited pH-sensitive gelling polymers in ophthalmics. Because very acidic formulations can irritate before neutralization, carbomers are often blended with viscosity modifiers (e.g., HPMC) to balance comfort, gelation efficiency, and rheology. A representative example is the pH-triggered Carbopol/HPMC dorzolamide system, designed to flow under non-physiological conditions yet gel under physiological conditions (tear pH and ocular temperature), with evaluations including rheology, permeability, and pharmacodynamic IOP lowering. [29,36]

Other pH-triggered systems include cellulose acetophthalate (CAP) latex, frequently described as coagulating when pH increases from acidic conditions (around pH ~4–5) to tear pH. Reviews of nanoparticle-laden and stimulus-responsive ocular gels cite CAP latex alongside carbomers and polycarbophil as classic pH-triggerable choices. [38]

4.2.3 Ion-activated (ionotropic) systems

Ion-activated in situ gels are particularly attractive for ocular delivery because tear fluid naturally contains mono- and divalent cations that can trigger gelation without changing pH or temperature. In these systems, the formulation is instilled as a solution; after contact with tears, polymer chains crosslink or reorganize in response to ionic strength, increasing viscosity and forming a gel. [29,39]

A flagship polymer here is gellan gum (often referenced by the trade name Gelrite®). Gelrite® is described as a low-acyl gellan gum that forms transparent gels in the presence of tear ions; gel formation has been linked to prolonged residence and improved ocular exposure for drugs such as timolol, and gellan systems are repeatedly cited as clinically meaningful examples of ion-triggered gel technology. [29,39]

Other important ion-sensitive polysaccharides include sodium alginate and low-methoxy pectin, both of which can gel in the presence of divalent ions (especially Ca²⁺) through “egg-box” type junctions. Reviews of stimuli-sensitive ophthalmic hydrogels summarize alginate and pectin gelation behavior and discuss how ion-driven gelation can support sustained release while preserving drop-like dosing. [39]

Modern work continues to optimize ion-activated gels for ocular surface disorders. For instance, a 2025 MDPI study developed ion-sensitive in situ gels using low-acyl gellan gum, reporting improved tear-film exposure (AUC) and enhanced residence time versus a non-gelling comparator in rabbit studies, consistent with the retention logic of ion-triggered gelation. [44]

4.2.4 Multi-stimuli responsive systems

In practice, single-trigger systems can be sensitive to dilution, patient-to-patient variability in tears, and the need to keep polymer concentration within comfort limits. Multi-stimuli designs (e.g., thermo + pH, ion + thermo) help tune gelation to occur reliably after instillation while minimizing premature thickening in the bottle. Reviews on in situ gels across administration routes explicitly describe these systems as responsive to multiple endogenous stimuli and highlight the usefulness of polymer combinations and mucoadhesive additives to prolong residence time. [32,33]

A concrete ophthalmic example is dual thermo-/pH-responsive nanocarrier-in-gel systems, reported in the literature as sustained ocular delivery platforms with in vivo evaluation. [45] Similarly, broad ophthalmic in situ gel reviews summarize hybrid systems where polymer blending is used to optimize gelation temperature, gel strength, and release. [31,33]

4.3 Key polymers used in ophthalmic in situ gels

Selection is typically driven by: trigger reliability, comfort (osmolality/pH), clarity, mucoadhesion, sterilization compatibility, and rheology (especially shear-thinning). The table below summarizes polymers most commonly discussed in ophthalmic in situ gel literature. [28–33,39]

Table 3. Polymers used in ophthalmic in situ gel systems

| Polymer | Type | Primary trigger | Typical role in ocular gels | Notes relevant to performance |
| --- | --- | --- | --- | --- |
| Poloxamer 407 (F127) | Synthetic | Temperature | Main thermogelling matrix | Strong concentration dependence; often blended to tune gel point. [33–35] |
| Poloxamer 188 | Synthetic | Temperature | Co-polymer/modifier | Used to adjust gelation temperature and rheology. [33,35] |
| PNIPAAm / PNIPAM | Synthetic | Temperature (LCST) | Thermoresponsive depot (often injectables) | Fast reversible transition; drug-release completeness can be a limitation. [43] |
| PLGA-PEG-PLGA | Synthetic/biodegradable | Temperature | Thermogelling biodegradable depot | Reported to improve exposure vs drops; used for anterior and posterior strategies. [40–42] |
| Carbopol/Carbomer (e.g., 934/940/974) | Synthetic | pH | pH-triggered gel former; mucoadhesive | Often combined with HPMC to balance comfort and gelation. [29,36,37] |
| Polycarbophil | Synthetic | pH | Bioadhesion + pH response | Discussed as pH-triggerable alongside carbomers. [38] |
| CAP latex (cellulose acetophthalate) | Semi-synthetic | pH | pH-triggered coagulating latex | Classic example of acidic sol → tear-pH gel/coagulation behavior. [38] |
| Gellan gum (Gelrite®) | Natural | Ions | Ion-activated gel former | Tear ions promote gelation; widely cited for prolonged retention. [29,39,44] |
| Sodium alginate | Natural | Ions | Ionotropic gel former | Ca²⁺-mediated gelation; often blended with viscosity enhancers. [39] |
| Pectin (low-methoxy) | Natural | Ions | Ionotropic gel former | Ca²⁺-responsive gelation; supports sustained release concepts. [39] |
| Chitosan | Natural | pH / mucoadhesion | Mucoadhesive co-polymer; permeation support | Commonly used with carbomers; improves retention/adhesion. [37] |
| HPMC / cellulose derivatives | Semi-synthetic | (Often modifier; sometimes thermo) | Viscosity/rheology modifier; stabilizer | Can lower gelation temperature and strengthen networks in blends. [29,35] |

05. NANOTECHNOLOGY IN OCULAR DRUG DELIVERY

5.1 Overview of nanocarriers for ocular delivery

Nanotechnology has reshaped ophthalmic formulation research by offering carrier systems that can be engineered rather than merely mixed to address the key reasons conventional eye drops fail: rapid precorneal clearance, poor corneal permeation, and inadequate exposure at the intended tissue. Comprehensive reviews consistently report that nanocarriers can (i) protect drugs from chemical/enzymatic degradation, (ii) improve apparent solubility of poorly soluble drugs, (iii) prolong residence time through mucoadhesion or viscosity enhancement, and (iv) enable sustained or stimuli-responsive release profiles that better match disease needs. Collectively, these features can improve local exposure while reducing dosing frequency and systemic spillover via nasolacrimal drainage. [46–49]

Importantly, nanocarriers are not a single technology but a toolbox. Lipid- and polymer-based nanoparticles, nanoemulsions, micelles, dendrimers, and nanogels each offer different strengths, and the “best” platform depends on the target site (ocular surface vs. anterior chamber vs. retina), the drug’s physicochemical properties, and practical constraints such as sterilization and scale-up. Many modern review papers therefore frame ocular nanomedicine as a design space in which particle size, surface charge, composition, and release mechanisms are tuned to overcome both static barriers (e.g., corneal epithelium) and dynamic barriers (tears and blinking). [46–49]

5.2 Types of nanoparticles used in ophthalmic formulations

5.2.1 Polymeric nanoparticles (PLGA, PLA, chitosan, PCL)

Polymeric nanoparticles are among the most widely studied ocular nanocarriers because their drug loading and release can be adjusted by polymer selection, polymer ratio, molecular weight, and fabrication method. They can encapsulate drug within a polymer matrix (nanospheres) or within a core surrounded by a polymer shell (nanocapsules), supporting sustained release and drug protection. Reviews also emphasize that particle size and surface characteristics strongly influence ocular performance; for topical administration, particles in the few-hundred-nanometer range are often discussed as a practical balance between stability, comfort, and corneal/conjunctival interaction. [49]

Among these polymers, PLA/PLGA occupy a special position because they have a long clinical history. PLA/PLGA materials were approved by the US FDA in the 1970s for bioresorbable sutures and later became reference polymers for sustained-release products. [50] 3 A large body of drug-delivery literature also explicitly describes PLGA as an FDA-approved polymer used in versatile drug-delivery carriers (including nanoparticles). [51]

For intraocular sustained delivery, PLGA-based particles have been intensively explored, including for posterior-segment indications. A dedicated review in Experimental Eye Research highlights PLGA as a versatile copolymer used to construct nano/microparticles and scaffolds for intraocular delivery, with relevance to chronic retinal diseases. [52]

Fig No 04 - Stimuli-Responsive In Situ Gelation Mechanisms for Ocular Drug Delivery

Figure 04. Schematic illustration of three major stimuli-responsive in situ gelation mechanisms used in ocular drug delivery. (A) Thermoresponsive systems undergo sol-to-gel transition at ocular surface temperature (~35 °C), forming a micellar gel network. (B) pH-triggered systems transition from acidic formulation pH (~4–6) to tear fluid pH (~7.4), leading to polymer ionization and chain expansion. (C) Ion-activated systems gel upon interaction with tear fluid ions (e.g., Na⁺, Ca²⁺, Mg²⁺), resulting in ionic crosslinking (egg-box model). These mechanisms enhance viscosity, prolong precorneal residence time, and enable sustained drug release.

5.2.2 Solid lipid nanoparticles (SLNs) and nanostructured lipid carriers (NLCs)

SLNs and NLCs are lipid-based nanoparticle platforms frequently positioned as biocompatible alternatives to some polymeric systems, particularly for lipophilic drugs. Recent ophthalmic-focused reviews emphasize that SLNs/NLCs can enhance ocular bioavailability, enable controlled release, and that their performance can be improved through surface modification (e.g., cationic coatings to increase ocular surface interaction). [53]

A practical distinction often emphasized is that NLCs (which incorporate a mixture of solid and liquid lipids) are designed to address limitations of earlier solid-lipid systems especially drug loading and drug expulsion during storage while still retaining the comfort and biodegradability advantages of lipid excipients. [53]

Notably for your review’s theme (nanoparticles embedded in smart gels), the same SLN/NLC literature explicitly discusses incorporating lipid nanoparticles into semisolid or in situ gelling formulations as a strategy to further enhance ocular residence and therapeutic performance. [53]

5.2.3 Liposomes

Liposomes are vesicular carriers with an aqueous core and lipid bilayers, allowing encapsulation of hydrophilic drugs (core) and lipophilic drugs (bilayer). They are also amenable to surface functionalization, which can support targeting or enhanced retention. In an anterior-segment nanomedicine review in Journal of Controlled Release, liposome–polymer hybrid systems are described for ocular indications (e.g., liposome/HPMC systems investigated for glaucoma-related therapy design), illustrating how liposomes are increasingly used as components in multi-material ophthalmic platforms rather than as stand-alone vesicles. [47]

5.2.4 Nanoemulsions and nanomicelles

Nanoemulsions are colloidal dispersions (typically oil-in-water for ophthalmics) that can solubilize lipophilic drugs and improve ocular comfort and transparency when properly formulated. A dedicated review in Journal of Molecular Liquids reports nanoemulsion droplet sizes commonly discussed within roughly 20–600 nm, and frames nanoemulsions as a route to enhance ocular bioavailability and contact time compared with conventional dispersions. [54]

Nanomicelles, formed by self-assembly of amphiphilic molecules or block copolymers, are especially valuable for poorly water-soluble drugs because the hydrophobic core can solubilize drug while the hydrophilic shell maintains clarity and tolerability. An ophthalmic micelle review in Nanoscale Advances highlights micelle systems not only as simple carriers but also as composites, including micelle-loaded hydrogels, reinforcing their relevance to nanoparticle-in-gel strategies. [56]

A key translational indicator is that ocular nanocarriers are no longer purely academic. The Journal of Controlled Release review provides an FDA-approved nanocarrier table for anterior-segment disease showing approved products based on nanoemulsions (e.g., Restasis®) and nanomicelles (e.g., Cequa®) among others evidence that nanoformulation strategies can reach the market when the manufacturing and quality package is robust. [47]

5.2.5 Dendrimers

Dendrimers are highly branched macromolecules with controlled architecture, multivalent surface functionality, and tunable size/charge properties that can be exploited for solubilization, mucoadhesion, and conjugation-based sustained delivery. In the Journal of Controlled Release anterior-segment review, dendrimers are discussed as promising but nuanced platforms; examples include dendrimer-based systems developed for glaucoma therapy and even hybrid “dendrimer–hydrogel–particle” designs reporting markedly improved corneal permeation compared with drug solution in experimental settings. [47]

5.2.6 Nanogels

Nanogels are nanoscale hydrogel particles that conceptually merge the benefits of nanoparticles (small size, tunable surfaces) with hydrogels (high water content, biocompatibility, bioadhesion). A recent nanogel-focused review explicitly frames nanogels as “integrating the advantages of nanoparticles and hydrogels,” emphasizing enhanced corneal retention/mucoadhesion and controlled release while also highlighting translational needs such as scalable manufacturing and sterilization. [58]

5.3 Advantages and limitations of nanocarriers

Across platforms, key advantages include drug protection, improved solubilization, sustained release, and the ability to tune surface properties to enhance ocular interaction. However, major limitations repeatedly noted in the literature include: (i) manufacturing scale-up without changing critical quality attributes, (ii) sterilization compatibility (especially for complex colloids), (iii) long-term physical stability (aggregation, leakage, Ostwald ripening for emulsions), and (iv) regulatory expectations for reproducible characterization and batch-to-batch control. These issues are discussed as central barriers to clinical translation in broad ocular nanomedicine reviews and in nanoemulsion quality-control focused papers. [46,55,58]

Table 4. Comparison of nanocarrier types for ocular drug delivery

| Nanocarrier | Typical size range (reported/commonly used) | Key advantage | Key limitation |
| --- | --- | --- | --- |
| Polymeric NPs (e.g., PLGA/PLA/PCL) | ~200–400 nm often discussed for topical uptake; generally <1000 nm | Tunable release; drug protection; versatile payloads | Burst release possible; scale-up/sterilization complexity [49,52] |
| SLN | ~50–500 nm | Biocompatible lipids; good for lipophilic drugs | Drug loading limitations; polymorphic transitions/stability issues [53] |
| NLC | ~100–500 nm | Higher loading vs SLN; controlled release; modifiable surface | Formulation complexity; characterization/QC burden [53] |
| Liposomes | ~50–1000 nm | Encapsulate hydrophilic + lipophilic drugs; modifiable surface | Leakage/physical instability; process sensitivity [47] |
| Nanoemulsions | ~20–600 nm (droplets) | Solubilize lipophilic drugs; clear systems possible | Thermodynamic instability; surfactant tolerability constraints [54,55] |
| Nanomicelles | ~10–100 nm | Excellent for hydrophobic drug solubilization; transparent | Dilution-related instability; rapid clearance unless retained/combined [49,56] |
| Dendrimers | few–tens of nm (generation dependent) | Precise architecture; multivalent functionalization | Toxicity/irritation depends on surface groups; synthesis cost/complexity [47] |
| Nanogels | ~50–500 nm (design dependent) | High mucoadhesion + controlled release; “NP + gel” synergy | Sterilization, scalable manufacturing, and long-term stability challenges [58] |

06. NANOPARTICLE-LADEN IN SITU GEL SYSTEMS   THE CONVERGENCE

6.1 Rationale for combining nanoparticles with in situ gels

Nanoparticles and in situ gels solve different failure points of topical ocular delivery, so combining them is not merely additive it is often synergistic. Nanoparticles can protect the drug, enhance apparent solubility for poorly soluble molecules, and enable controlled release via diffusion through (or degradation of) the carrier matrix. In situ gels, in contrast, primarily address the “time problem”: they increase formulation residence in the cul-de-sac by transforming from a low-viscosity instillable liquid to a viscous gel under ocular conditions, thereby reducing rapid precorneal washout. When nanoparticles are dispersed within a gelling vehicle, the gel helps retain the particulate carriers at the ocular surface long enough for meaningful permeation, while the nanoparticles regulate release and tissue interaction. This concept is explicitly discussed in early “nanoparticle-laden in situ gel” work with sparfloxacin PLGA nanoparticles dispersed in a chitosan in situ gel, where the authors highlight that the combined system was developed specifically to improve precorneal residence time and ocular bioavailability. [59].

The retention advantage of the hybrid approach is supported by in vivo imaging-based assessments. In the sparfloxacin study, gamma scintigraphy was used to compare a marketed formulation, in situ gel, nanosuspension, and nanoparticle-laden in situ gel. The marketed product cleared rapidly from the corneal region with activity detected in kidney/bladder (consistent with nasolacrimal drainage and systemic exposure), whereas the gel- and nanoparticle-based systems showed longer ocular retention. The authors further note “good spreading and retention” and a slower fall in time–activity curves for the nanoparticle-laden gel, indicating prolonged ocular surface residence. [59].

A second, less obvious advantage is that the gel can act as a stabilizing microenvironment for nanoparticles. For instance, studies using PLGA nanoparticles suspended in thermosensitive gels report that embedding nanoparticles within a gel matrix can markedly reduce or eliminate burst release and shift profiles toward more sustained, often near zero-order, release because the gel adds an additional diffusion barrier and reduces rapid drug escape from the particle surface. [60].

6.2 Formulation strategies

Hybrid systems vary widely, but most designs fall into a few recurring architectures: polymeric nanoparticles in thermogels, chitosan-based nanoparticles in pH gels, lipid nanoparticles (NLC/SLN) in gels, nanosuspension-based “nano-in-gel” systems, and smart polymer-coated nanoparticle composites (often dual-trigger).

6.2.1 PLGA nanoparticles in thermoresponsive in situ gels

PLGA nanoparticle–in–thermogel systems are commonly pursued for corticosteroids and anti-inflammatory drugs because sustained ocular exposure is often needed while limiting local irritation. A representative example is a hydrocortisone butyrate study where HB-loaded PLGA nanoparticles were suspended in a thermosensitive PLGA-PEG-PLGA gel. The authors report that nanoparticle-in-gel formulations produced minimal burst release and could sustain delivery over extended periods; they also discuss mechanistic reasons (diffusional resistance and/or polymeric adhesion within a semisolid network) and report linear zero-order release for nanoparticle-in-gel systems over multiple weeks in vitro. [60].

6.2.2 Chitosan-based nanoparticles in pH-responsive in situ gels

A strong contemporary example is the timolol system developed by Rahbar et al., where timolol-loaded chitosan–carbomer nanoparticles (prepared via polyelectrolyte complexation) were incorporated into a carbomer-based pH-responsive in situ gel. The optimized nanoparticles were ~196 nm with ~69% encapsulation efficiency; importantly, the zeta potential shifted from –16 mV (NPs) to +11 mV (NP-laden gel), consistent with changes in surface environment and potentially stronger interaction with the negatively charged ocular mucin layer. The authors report higher mucoadhesion for the NP-laden gel and a significantly more sustained IOP-lowering effect compared with timolol solution and nanoparticles alone. [61].

6.2.3 NLC-loaded in situ gels (lipid nanoparticles + gel retention)

Lipid nanoparticles, especially nanostructured lipid carriers (NLCs), are frequently combined with gels to exploit (i) improved loading of lipophilic drugs and (ii) extended residence time.

Beyond “simple” NLC-in-gel mixing, smart crosslinking approaches are also used. Yu et al. developed a dual pH- and thermo-sensitive hydrogel (carboxymethyl chitosan + poloxamer 407) crosslinked with genipin, and combined it with quercetin-loaded NLCs. They report improved uptake indicators and a 4.4-fold higher AUC for quercetin in the NLC–gel group versus eye drops, attributing gains to longer precorneal retention and the penetration advantages of NLCs. [64].

A closely related open-access platform (baicalin model drug) reports that an NLC–hydrogel composite increased apparent permeability (reported as 4.46-fold vs eye drops), showed no significant corneal irritation based on hydration assessment, and prolonged precorneal residence time using a flow-through retention method. [65].

6.2.4 Nanosuspension-loaded “in situ nano gel” systems

For flurbiprofen, a thermosensitive in situ “nano gel” was investigated using Pluronic F127 and Carbopol 934. The authors report ~95% in vitro release at 6 h, along with increased precorneal residence time and higher aqueous humor concentrations compared with conventional flurbiprofen drops, linking improvements to (i) improved saturation solubility from nanosizing and (ii) prolonged retention via gel matrix formation. [69].

6.2.5 Smart polymer-coated / multi-trigger composite systems

“Smart” design in NP-laden gels often means either dual/multi-stimuli gelation (e.g., pH + temperature) or chemically crosslinked networks that resist rapid tear dilution while remaining biocompatible.

Genipin-crosslinked systems (CMCS/F127) discussed above are a clear example, combining dual responsiveness and improved tolerability relative to harsher crosslinkers in comparative designs. [64,65].

Hybrid systems are also being evaluated head-to-head across nanoparticle classes. In an Acanthamoeba keratitis-oriented study, chitosan nanoparticles, NLCs, and liposomes were separately incorporated into an F127/chitosan in situ gel. The authors report that raising pH/temperature promoted gelation with gelation temperatures ~33–34.8 °C, gelation times generally within seconds-to-<1 minute depending on formulation, and markedly higher viscosity at 37 °C. They also report sustained release over 24 h for nanoparticle-loaded gels versus marketed eye drops. [70].

6.3 Key outcomes reported across studies

Across the literature, three outcome categories recur:

- Retention and residence time: Imaging/retention tools (gamma scintigraphy, flow-through retention models) consistently show longer ocular surface persistence for NP-laden gels compared with conventional drops. [59,65].

- Higher permeation and exposure: Ex vivo permeation and PK studies frequently report increased corneal permeation and higher ocular AUC/Cmax when nanoparticles are delivered within gels rather than as solution or standalone nanoparticles. A dexamethasone nanoparticle-loaded in situ gel study explicitly reports higher ex vivo permeation and higher ocular bioavailability versus drug solution and a marketed comparator. [62].

- Improved pharmacodynamic effect: For glaucoma models, NP-laden gels can extend and strengthen IOP reduction compared with timolol solution or nanoparticles alone, consistent with prolonged exposure. [61].

A particularly quantitative example of “added value” from the composite approach is the thermosensitive dexamethasone NPs-gel work reporting a phase transition around 33.2 °C, stronger adhesion/gel strength than in situ gel alone, and an AUC that was 3.08× that of nanoparticles and 1.51× that of in situ gel alone (in their comparative design). [63].

Table 5. Summary of key nanoparticle-laden in situ gel studies

| Study / Drug | Nanocarrier | In situ gel matrix (trigger) | Key reported outcome |
| --- | --- | --- | --- |
| Sparfloxacin | PLGA nanoparticles | Chitosan gel (pH-responsive) | Gamma scintigraphy: longer ocular retention vs marketed; reduced systemic drainage signal |
| Hydrocortisone butyrate | PLGA nanoparticles | PLGA-PEG-PLGA thermogel (temperature) | Minimal burst; sustained/near zero-order release from NP-in-gel vs drug-in-gel |
| Timolol (glaucoma) | Chitosan–carbomer nanoparticles | Carbomer in situ gel (pH-responsive) | Higher mucoadhesion; more sustained IOP reduction than solution/NPs |
| Dexamethasone | Nanoparticles in in situ gel | Poloxamer-based in situ gel | Higher ex vivo permeation; slower controlled release; higher ocular bioavailability vs marketed |
| Dexamethasone | Cross-linked thermosensitive NPs-gel | Thermosensitive gel (33.2 °C transition) | Higher adhesion/gel strength; AUC 3.08× NPs and 1.51× in situ gel alone |
| Quercetin | NLC + genipin-crosslinked hydrogel | CMCS/P407 gel (dual pH + temperature) | AUC 4.4× vs eye drops; better cytocompatibility vs GA-crosslinked control |
| Baicalin | NLC + crosslinked “smart” hydrogel | CMCS/P407 + genipin (dual pH + temperature) | Papp 4.46× vs drops; longer precorneal retention; no significant corneal irritation |
| Oxytetracycline (keratitis) | Polymeric NPs in thermogel | Poloxamer thermogel | Gelation ~28–31 °C; pH ~7–7.45; tolerated in rabbits; sustained release |
| Ketoconazole (antifungal) | Ketoconazole nanoparticles | Poloxamer/HPMC/alginate blends (temperature) | Gelation temperature tunable (e.g., ~34.7 °C at 16% P407); near-neutral pH; stability/gelation tracked |
| Loratadine | NLC | Carbopol 934 + HPMC gel | High entrapment; mucoadhesive gel; non-irritating; better corneal retention with sustained release |
| Flurbiprofen | Drug nanoparticles (“nano gel”) | F127 + Carbopol 934 (temperature) | ~95% release at 6 h; increased precorneal residence and aqueous humor concentration vs drops |
| Propamidine isethionate systems (Acanthamoeba keratitis) | CS NPs / NLC / liposomes in gel | F127 + chitosan gel (temperature + pH effects) | Gelation temps ~33–34.8 °C; viscosity rises sharply at 37 °C; sustained release vs marketed drops |

07. FORMULATION & EVALUATION PARAMETERS

7.1 Formulation considerations

Developing a nanoparticle-laden in situ gel (NP–ISG) is essentially a two-level formulation problem: (i) design a stable, reproducible nanoparticle dispersion (or dry nanoparticles suitable for redispersion) and (ii) design an in situ gelling vehicle that can gel rapidly under ocular conditions without causing discomfort or instability. In practice, the final performance is governed by the interaction between these two subsystems e.g., gel viscosity can slow nanoparticle diffusion, while nanoparticle surface charge can change gel microstructure and mucoadhesion. [71]

Drug–polymer compatibility. Preformulation compatibility is typically assessed using FTIR (functional group shifts/interaction evidence) and DSC (changes in melting transitions, crystallinity, and interaction-driven thermal events). These tools are frequently reported in nanoparticle-in-gel development papers to justify that the drug remains chemically compatible with the chosen polymers/surfactants and that no unexpected interaction compromises stability or release. [72]

Sterility strategy (non-negotiable for ophthalmics). Ophthalmic dosage forms must be sterile, but sterilization can be technically difficult for nanosystems because heat, radiation, and filtration may change particle size, drug loading, or gelation behavior. One common approach when the formulation tolerates moist heat is terminal autoclaving of the filled container, and at least one nanoparticles-loaded in situ gel study reports autoclaving at 121 °C for 20 minutes at 15 psi. [72] 2
When heat-sensitive nanocarriers are involved, sterile filtration (0.22 μm) may be used for solutions, but it can be impractical for many nanoparticle dispersions (because particles may be larger than the pore size or may be lost on the filter). Reviews focused on ophthalmic nanopharmaceuticals discuss the need to select sterilization method case-by-case and emphasize confirming post-sterilization changes in particle attributes and formulation performance (size distribution, loading, viscosity, etc.). [73]

pH adjustment and gelation intent. For pH-triggered systems, the formulation is typically prepared at a lower pH (often in the ~4.0–6.0 range) to remain pourable, then thickens after exposure to tear fluid near pH ~7.4. In experimental gelation testing, simulated tear fluid at pH 7.4 and physiological temperature is commonly used to confirm gelation capacity and integrity. [72]

Osmolarity and isotonicity. Isotonicity is adjusted (commonly with NaCl and/or suitable tonicity agents) to avoid reflex tearing, irritation, and rapid clearance that can erase the residence-time benefit of gels. In practice, isotonicity is treated as a comfort- and safety-critical specification alongside pH. [73]

Optimization using DoE/QbD. A Quality-by-Design mindset is increasingly applied to NP–ISG development because multiple variables interact nonlinearly (polymer concentration, surfactant level, mixing energy, crosslinking degree, etc.). A recent NP–ISG study reports a structured multi-step optimization workflow using screening and response-surface designs (Plackett–Burman, steepest ascent, and Box–Behnken design) to optimize nanoparticle attributes and final ocular performance. [71]

7.2 Evaluation parameters

Characterization should confirm three things: (i) nanoparticles are stable and within target size distribution; (ii) the gel behaves as intended (sol in bottle → gel in eye); and (iii) the combined product releases drug in a sustained manner without irritation.

Table 6. Comprehensive evaluation parameters for NP-laden in situ gels

| Parameter | Method | Typical target / acceptable range (practical) |
| --- | --- | --- |
| Nanoparticle characterization |  |  |
| Particle size | DLS / Zetasizer | ~100–300 nm often targeted for topical comfort & stability |
| PDI | DLS | < 0.3 (narrow distribution) |
| Entrapment efficiency | UV–Vis / HPLC | Often > 60% desirable (drug/platform-dependent) |
| Morphology | SEM / TEM | Spherical/regular; minimal aggregation |
| In situ gel characterization |  |  |
| Clarity & appearance | Visual | Clear/transparent; no particulates |
| pH | Calibrated pH meter | Typically ~6.8–7.4 for comfort (trigger systems may start lower) |
| Viscosity (sol and gel) | Brookfield / rheometer | Low viscosity in bottle; high viscosity after gelation |
| Gelation temperature (thermogels) | Tube inversion / rheology | Usually targeted around 32–37 °C |
| Gelation time | Visual / rheological | Often targeted < 60 s |
| Gel strength | Texture analysis | Sufficient to resist drainage but not blur excessively |
| Drug release & permeation |  |  |
| In vitro release | Dialysis / Franz diffusion | Sustained release (commonly ≥ 8 h, indication-dependent) |
| Ex vivo corneal permeation | Excised rabbit/goat cornea | Higher flux/permeation vs control formulation |
| Release kinetics modeling | Zero-order / Higuchi / Korsmeyer–Peppas | Model-dependent; used to infer mechanisms |
| Safety |  |  |
| Ocular irritation | HET-CAM; Draize (rabbit); cell viability | Non-irritant / well tolerated |
| Sterility | Membrane filtration / direct inoculation | Sterile (no microbial growth) |
| Stability |  |  |
| Accelerated stability | ICH-aligned design | Often 3–6 months accelerated + long-term program |

08. DISEASE-SPECIFIC APPLICATIONS

8.1 Glaucoma

Glaucoma management is fundamentally exposure-driven: intraocular pressure (IOP) control depends on maintaining adequate drug levels at tissues that regulate aqueous humor production and outflow, especially the ciliary body (production) and the trabecular meshwork/outflow pathway. Conventional eye drops can lower IOP, but they often require long-term, frequent dosing and are vulnerable to rapid precorneal loss both of which contribute to non-adherence and variable therapeutic control. Nanotechnology-enabled systems are therefore increasingly discussed as a means to improve glaucoma therapy by prolonging drug residence time, improving penetration, and enabling more localized (and potentially tissue-targeted) delivery that reduces systemic exposure through nasolacrimal drainage. A comprehensive review in Discover Nano explicitly highlights that nanotechnology can enable targeted delivery to tissues such as the trabecular meshwork and ciliary body, improving efficacy while minimizing systemic side effects. [75]

In the context of nanoparticle-laden in situ gels, the logic is particularly strong: the in situ gel extends retention on the ocular surface (time to absorb), while the nanoparticles provide controlled release and can be engineered for mucoadhesion or improved epithelial interaction. Drug examples frequently explored within nano-enabled glaucoma delivery include timolol, brinzolamide, and latanoprost (often selected because they represent major therapeutic classes and require sustained exposure for best outcomes). [75]

8.2 Ocular infections (bacterial keratitis, fungal keratitis, HSV keratitis)

Infectious keratitis is a practical stress test for topical delivery systems because antibiotics often must be instilled frequently to maintain concentrations above the pathogen’s inhibitory threshold. A notable “nano-in-gel” example is a moxifloxacin-loaded nanoparticles-laden in situ gel developed to sustain release and improve ocular tolerance. In an ex vivo caprine keratitis model, the formulation produced a ~4-log reduction (CFU/mL) in infected corneas, and histopathology supported recovery of the corneal epithelium. Safety screening using HET-CAM indicated the formulation was non-irritant at the tested dose. These outcomes collectively support the core claim of NP–ISG systems in infections: prolong drug contact time and sustain local concentrations while maintaining tolerability. [76]

8.3 Dry eye disease (DED)

DED is increasingly understood as a disease of tear-film instability coupled with ocular-surface inflammation, where oxidative stress can amplify epithelial injury and inflammatory signaling. An innovative nanotechnology–hydrogel approach reported by Ou et al. used aldehyde-functionalized Pluronic F127 (AF127) hydrogel eye drops to deliver ultrasmall Cu₂₋ₓSe nanoparticles with antioxidant/nanozyme-like activity. The authors report that these nanoparticles display superoxide dismutase (SOD)-like and glutathione peroxidase (GPx)-like behavior, enabling reactive oxygen species (ROS) scavenging and mitigation of oxidative damage; mechanistic experiments linked effects to modulation of NRF2 and p38 MAPK pathways. The AF127 hydrogel also provided ocular-surface adhesion via Schiff-base bonding, which supports longer residence and better therapeutic contact. [77]

8.4 Uveitis and ocular inflammation

Uveitis treatment illustrates a key boundary of conventional eye drops: even potent anti-inflammatory drugs may not reach intraocular inflammatory sites efficiently because of tissue barriers and clearance. A biomaterials-centered strategy described by Zou et al. developed an injectable, thermo-sensitive hydrogel platform (PNMHTI) based on NIPAAm-co-MAA chemistry with an indomethacin-conjugated component. The hydrogel showed a sol–gel conversion temperature around ~33°C, enabling gelation under physiological conditions, and sustained indomethacin release for over two weeks in enzyme-containing media. In a rabbit uveitis model, the formulation was injected into the vitreous and showed biocompatibility and anti-inflammatory effects supported by histopathology. While this approach is more invasive than topical gels, it demonstrates how “smart gel” principles (triggered gelation + sustained release) can be translated to intraocular inflammation when topical exposure is insufficient. [78]

8.5 Posterior segment diseases (AMD, DR)

Posterior diseases such as wet AMD are commonly treated with anti-VEGF agents, but the need for repeated injections creates high burden and cumulative procedural risk. A particularly influential example of an in situ–forming gel depot for posterior targeting is the suprachoroidal anti-VEGF hydrogel reported by Jung et al. They developed an in situ forming bevacizumab–hyaluronic acid (Bev–HA) hydrogel crosslinked with PEG diacrylate, delivered into the suprachoroidal space using a microneedle. The study reports >6 months of bevacizumab release in vivo in rabbit eyes (assay- and formulation-dependent), broad posterior distribution, and good tolerability assessed by clinical examination, fundus imaging, histology, and IOP monitoring. This work is widely cited because it demonstrates a credible pathway to reduce dosing frequency while leveraging the anatomical advantage of suprachoroidal delivery for choroid/retina-adjacent targets. [79]

Fig No 05 - Classification of Ocular Nanocarriers: Types, Characteristics, and Limitations

Figure 05. Schematic overview of major nanocarrier systems used in ocular drug delivery. The figure categorizes polymeric nanoparticles (PLGA, PLA, PCL, chitosan), solid lipid nanoparticles (SLN), nanostructured lipid carriers (NLC), liposomes, nanoemulsions, nanomicelles, dendrimers, and nanogels, along with their typical size ranges, key advantages (e.g., improved solubility, controlled release, enhanced stability), and limitations (e.g., low drug loading, instability, complex manufacturing). These systems are designed to overcome ocular barriers and improve drug bioavailability.

9. CHALLENGES, FUTURE PERSPECTIVES & EMERGING TECHNOLOGIES

9.1 Current challenges

Despite strong preclinical performance, nanoparticle-enabled gels (and smart ocular biomaterials more broadly) still face a persistent “translation gap.” A central reason is that ocular delivery systems must satisfy simultaneously (i) sensitive biological constraints (comfort, vision clarity, irritation potential), (ii) demanding quality requirements (sterility, reproducibility, stability), and (iii) practical clinical workflows (simple use, low visit burden). Recent reviews of smart ocular materials emphasize that conventional therapies remain limited by poor targeting, penetration, and retention, and that even advanced systems do not automatically solve all barriers especially for posterior-segment needs where drug residence time and safety are critical. [78]

(a) Controlling degradation and long-term biocompatibility -In situ gels and hydrogel depots are attractive because they can localize therapy and sustain release, but their clinical adoption depends heavily on predictable degradation kinetics and the safety of both the intact network and its byproducts. Broad hydrogel translation discussions highlight that overly rapid degradation can shorten efficacy and provoke inflammation, while overly slow degradation may lead to persistent foreign-body response, fibrosis, or prolonged exposure to crosslinked material. Achieving “just-right” degradation is difficult because small changes in polymer molecular weight, crosslink density, and environmental conditions (pH/ions/enzymes) can substantially alter erosion and drug release. [79]

(b) Sterilization and shelf-life constraints -Sterility is non-negotiable for ophthalmic products, but it is one of the hardest hurdles for complex soft materials. Hydrogels may be sensitive to autoclaving, gamma irradiation, or ethylene oxide, and each method can change polymer structure, mechanical strength, or residual chemistry. The hydrogel manufacturing and regulatory literature also notes practical limitations of UV sterilization (poor penetration) and sterile filtration (often only feasible for low-viscosity precursor solutions, not for finished gels or many nanoparticle dispersions). These sterilization realities intersect directly with shelf-life: high water content increases microbial risk, and gels may shrink, dry, or degrade during storage unless packaging and cold-chain strategies are carefully engineered. [79]

(c) Chemical crosslinking risks and residue control (important for safety perception)
Many “smart” gels rely on chemical crosslinking to maintain strength under tear dilution and blinking shear. However, translation-focused hydrogel reviews repeatedly caution that residual monomers, crosslinkers, or initiators can contribute to cytotoxicity if purification is incomplete, and that regulators expect robust evidence that residues are controlled and that degradation products are safe. This is particularly relevant when the gel is designed to carry sensitive payloads (proteins, peptides, nucleic acids), because crosslinking conditions can also damage the drug itself. [79]

(d) Scale-up, batch reproducibility, and quality-by-design expectations
Formulations that work at bench scale may not reproduce at manufacturing scale because nanoparticle size distribution, gelation temperature, viscosity, and drug release can be highly sensitive to mixing energy, temperature history, and raw-material variability. Manufacturing discussions emphasize that hydrogels especially those made by polymerization/crosslinking reactions can be difficult to reproduce at industrial scale because small environmental shifts (humidity, pH, temperature) can move critical attributes. Consequently, translation often demands tighter process control, in-line testing, and a QbD-style control strategy. [79]

(e) Regulatory complexity for combination products (nano + gel = “more than the sum”)
From a regulatory standpoint, nano-in-gel systems are frequently “combination-like” products: they blur boundaries between a drug, a device-like matrix, and sometimes even a biologic if the payload is a protein or gene therapy. Regulatory overviews of hydrogel commercialization highlight that products may fall under multiple FDA pathways (device classes, NDA/BLA routes, or formal combination product pathways), requiring coordinated review and extensive evidence of sterility, biocompatibility, stability, and manufacturing controls often increasing development time and cost. [79]

9.2 Future perspectives and emerging technologies

Current innovation is moving toward integrated systems that combine materials, triggers, and delivery routes to improve precision and reduce treatment burden. A recent review of smart ocular materials points out that the next generation of ocular DDS increasingly includes not only nanoparticles and hydrogels, but also microneedles and contact-lens platforms, selected according to disease location and required duration of exposure. [78]

(a) Smarter responsiveness: “on-demand” and multi-stimuli release A clear trajectory is toward hydrogels that respond to ocular-relevant cues (temperature, pH, ions, inflammation-associated signals) to provide more controlled, situational release. Smart-materials reviews emphasize that stimulus-responsive behavior can support longer retention, higher penetration efficiency, and more patient-friendly dosing, provided that responsiveness is reliable and reproducible. [78]

(b) Device–material convergence: microneedles and contact-lens delivery For posterior targets, microneedle-enabled placement (e.g., suprachoroidal or other minimally invasive compartments) can combine anatomical advantage with in situ-forming depots, potentially reducing repeated intravitreal injections. In parallel, drug-eluting contact lenses represent a surface-based sustained-release strategy that can complement gel systems, especially for ocular-surface disease though oxygen permeability and infection risk must be managed. This “material + device” direction is explicitly highlighted as a growing branch of smart ocular delivery. [78]

(c) AI/ML-guided formulation and advanced manufacturing (3D/4D printing)
Hydrogel translation literature increasingly points to computational tools for rational design using data-driven methods to predict gel properties, optimize compositions, and reduce experimental iteration. The same sources also discuss 3D/4D bioprinting and microfabrication as enabling technologies for personalized or anatomically tailored hydrogel systems, while acknowledging that regulatory and reproducibility barriers remain substantial. [79,80]

(d) Nanozyme–hydrogel hybrids (therapeutic + immunomodulatory functions)
A particularly innovative emerging direction is the use of nanozyme-loaded hydrogels that provide both drug delivery and microenvironment modulation (e.g., ROS control or immune-pathway regulation). For example, Zhang et al. reported a carbon-nanotube (CNT) nanozyme–based thixotropic anionic hydrogel coating loaded with itraconazole for fungal keratitis. The study described antifungal activity against Aspergillus fumigatus (including CFU and biofilm reduction), good biocompatibility in cell testing, and downregulation of inflammatory mediators with inhibition of p38 MAPK phosphorylation.

Conclusion –

Nanoparticle-laden in situ gelling ophthalmic formulations represent a rational, next-generation strategy to overcome the fundamental limitations of conventional ocular dosage forms. Traditional eye drops are convenient but typically provide short precorneal contact time and low ocular bioavailability due to tear turnover, blinking, and nasolacrimal drainage. In situ gels address this challenge by undergoing a sol-to-gel transition on the ocular surface, forming a viscoelastic depot that resists rapid clearance and sustains drug availability. Nanocarriers complement this approach by improving drug solubilization, protecting labile molecules, enabling controlled release, and enhancing interactions with ocular tissues. When integrated, the hybrid “nano-in-gel” architecture can simultaneously prolong residence time and optimize release and permeation, resulting in improved exposure profiles and stronger pharmacodynamic outcomes in models of glaucoma, keratitis, dry eye disease, and other ocular conditions.

Despite promising results, clinical translation remains limited by sterilization feasibility, long-term stability, scalable manufacturing, and regulatory complexity for combination nano–hydrogel products. Future progress will likely depend on rigorous quality-by-design development, standardized characterization, and clinically relevant efficacy and safety endpoints. With these advances, nanoparticle-laden in situ gels have strong potential to reduce dosing frequency, improve adherence, and deliver more precise and durable ocular therapy.

List of abbreviations used

- AHA   Amino-functionalized hyaluronic acid

- AMD   Age-related macular degeneration

- AUC   Area under the concentration–time curve

- BAB   Blood–aqueous barrier

- Bev   Bevacizumab

- BRB   Blood–retinal barrier

- CAP   Cellulose acetophthalate

- CFU   Colony-forming units

- CMCS   Carboxymethyl chitosan

- CNT   Carbon nanotube

- CuPC   Copper-proanthocyanidins (nanozyme component)

- Cu₂₋ₓSe   Copper selenide nanoparticles (non-stoichiometric copper-deficient copper selenide)

- DED   Dry eye disease

- DLS   Dynamic light scattering

- DoE   Design of experiments

- DSC   Differential scanning calorimetry

- EE   Entrapment efficiency

- FDA   U.S. Food and Drug Administration

- FTIR   Fourier transform infrared spectroscopy

- GA   Glutaraldehyde

- GBD   Global Burden of Disease

- GPx   Glutathione peroxidase

- HET-CAM   Hen’s egg test chorioallantoic membrane

- HPMC   Hydroxypropyl methylcellulose

- HSV   Herpes simplex virus

- ICH   International Council for Harmonisation of Technical Requirements for Pharmaceuticals for Human Use

- IOP   Intraocular pressure

- ISG   In situ gel

- IVT   Intravitreal (intravitreal injection)

- LCST   Lower critical solution temperature

- MN   Microneedle

- NHC   Nanozyme-thixotropic anionic hydrogel coating

- NLC   Nanostructured lipid carrier

- NP   Nanoparticle

- NP–ISG   Nanoparticle-laden in situ gel

- NRF2   Nuclear factor erythroid 2-related factor 2

- P407 / P188   Poloxamer 407 / Poloxamer 188

- Papp   Apparent permeability coefficient

- PCL   Poly(ε-caprolactone)

- PDI   Polydispersity index

- PEG   Poly(ethylene glycol)

- PEGDA   Poly(ethylene glycol) diacrylate

- PLA   Poly(lactic acid)

- PLGA   Poly(lactic-co-glycolic acid)

- PNIPAAm / PNIPAM   Poly(N-isopropylacrylamide)

- PNMHTI   (As used in cited study) thermo-sensitive hydrogel system name for indomethacin delivery

- QbD   Quality by Design

- QC   Quality control

- ROS   Reactive oxygen species

- SEM   Scanning electron microscopy

- SLN   Solid lipid nanoparticle

- SOD   Superoxide dismutase

- TEM   Transmission electron microscopy

- TFOS DEWS II   Tear Film & Ocular Surface Society Dry Eye Workshop II

- WHO   World Health Organization

Refercnes –

1.	Khan R, Khan M. Use of collagen as a biomaterial: An update. J Indian Soc Periodontol. 2013;17(4):539. doi:10.4103/0972-124X.118333

2.	Nabili M, Patel H, Mahesh SP, Liu J, Geist C, Zderic V. Ultrasound-Enhanced Delivery of Antibiotics and Anti-Inflammatory Drugs Into the Eye. Ultrasound in Medicine & Biology. 2013 Apr;39(4):638–46. doi:10.1016/j.ultrasmedbio.2012.11.010

3.	Bhandari P, Novikova G, Goergen CJ, Irudayaraj J. Ultrasound beam steering of oxygen nanobubbles for enhanced bladder cancer therapy. Sci Rep. 2018 Feb 15;8(1):3112. doi:10.1038/s41598-018-20363-8

4.	Cheng YH, Tsai TH, Jhan YY, Chiu AW hsiang, Tsai KL, Chien CS, et al. Thermosensitive chitosan-based hydrogel as a topical ocular drug delivery system of latanoprost for glaucoma treatment. Carbohydrate Polymers. 2016 Jun;144:390–9. doi:10.1016/j.carbpol.2016.02.080

5.	Hamcerencu M, Desbrieres J, Popa M, Riess G. Thermo-sensitive gellan maleate/N-isopropylacrylamide hydrogels: initial “in vitro” and “in vivo” evaluation as ocular inserts. Polym Bull. 2020 Feb;77(2):741–55. doi:10.1007/s00289-019-02772-5

6.	Nabili M, Geist C, Zderic V. Thermal safety of ultrasound‐enhanced ocular drug delivery: A modeling study. Medical Physics. 2015 Oct;42(10):5604–15. doi:10.1118/1.4929553

7.	Ludwig A. The use of mucoadhesive polymers in ocular drug delivery. Advanced Drug Delivery Reviews. 2005 Nov 3;57(11):1595–639. doi:10.1016/j.addr.2005.07.005

8.	Chen J, Li Q, Xu J, Huang Y, Ding Y, Deng H, et al. Study on Biocompatibility of Complexes of Collagen–Chitosan–Sodium Hyaluronate and Cornea. Artificial Organs. 2005 Feb;29(2):104–13. doi:10.1111/j.1525-1594.2005.29021.x

9.	Liu Z, Li J, Nie S, Liu H, Ding P, Pan W. Study of an alginate/HPMC-based in situ gelling ophthalmic delivery system for gatifloxacin. International Journal of Pharmaceutics. 2006 Jun;315(1–2):12–7. doi:10.1016/j.ijpharm.2006.01.029

10.	Wang Y, Shim MS, Levinson NS, Sung H, Xia Y. Stimuli‐Responsive Materials for Controlled Release of Theranostic Agents. Adv Funct Materials. 2014 Jul;24(27):4206–20. doi:10.1002/adfm.201400279

11.	Mahlumba P, Choonara Y, Kumar P, Du Toit L, Pillay V. Stimuli-Responsive Polymeric Systems for Controlled Protein and Peptide Delivery: Future Implications for Ocular Delivery. Molecules. 2016 Jul 30;21(8):1002. doi:10.3390/molecules21081002

12.	Mura S, Nicolas J, Couvreur P. Stimuli-responsive nanocarriers for drug delivery. Nature Mater. 2013 Nov;12(11):991–1003. doi:10.1038/nmat3776

13.	Kushwaha S, Rai A, Saxena P. Stimuli sensitive hydrogels for ophthalmic drug delivery: A review. Int J Pharma Investig. 2012;2(2):54. doi:10.4103/2230-973X.100036

14.	Myles M, Neumann D, Hill J. Recent progress in ocular drug delivery for posterior segment disease: Emphasis on transscleral iontophoresis. Advanced Drug Delivery Reviews. 2005 Dec 13;57(14):2063–79. doi:10.1016/j.addr.2005.08.006

15.	Gaudana R, Jwala J, Boddu SHS, Mitra AK. Recent Perspectives in Ocular Drug Delivery. Pharm Res. 2009 May;26(5):1197. doi:10.1007/s11095-008-9694-0

16.	Vigani B, Rossi S, Sandri G, Bonferoni MC, Caramella CM, Ferrari F. Recent Advances in the Development of In Situ Gelling Drug Delivery Systems for Non-Parenteral Administration Routes. Pharmaceutics. 2020 Sep 10;12(9):859. doi:10.3390/pharmaceutics12090859

17.	Barbu E, Verestiuc L, Nevell TG, Tsibouklis J. Polymeric materials for ophthalmic drug delivery: trends and perspectives. J Mater Chem. 2006;16(34):3439. doi:10.1039/b605640g

18.	Cao Y, Zhang C, Shen W, Cheng Z, Yu L (Lucy), Ping Q. Poly(N-isopropylacrylamide)–chitosan as thermosensitive in situ gel-forming system for ocular drug delivery. Journal of Controlled Release. 2007 Jul;120(3):186–94. doi:10.1016/j.jconrel.2007.05.009

19.	Mi S, Chen B, Wright B, Connon CJ. Plastic compression of a collagen gel forms a much improved scaffold for ocular surface tissue engineering over conventional collagen gels. J Biomedical Materials Res. 2010 Nov;95A(2):447–53. doi:10.1002/jbm.a.32861

20.	Bao Q, Jog R, Shen J, Newman B, Wang Y, Choi S, et al. Physicochemical attributes and dissolution testing of ophthalmic ointments. International Journal of Pharmaceutics. 2017 May;523(1):310–9. doi:10.1016/j.ijpharm.2017.03.039

21.	S KI, F R, I S. pH Triggered In-situ Gelling Ophthalmic Drug Delivery System. IJDDT. 2018 Apr 20;8(01). doi:10.25258/ijddt.v8i01.11900

22.	Moiseev RV, Morrison PWJ, Steele F, Khutoryanskiy VV. Penetration Enhancers in Ocular Drug Delivery. Pharmaceutics. 2019 Jul 9;11(7):321. doi:10.3390/pharmaceutics11070321

23.	Huang D, Chen YS, Rupenthal ID. Overcoming ocular drug delivery barriers through the use of physical forces. Advanced Drug Delivery Reviews. 2018 Feb;126:96–112. doi:10.1016/j.addr.2017.09.008

24.	Jung JH, Chiang B, Grossniklaus HE, Prausnitz MR. Ocular drug delivery targeted by iontophoresis in the suprachoroidal space using a microneedle. Journal of Controlled Release. 2018 May;277:14–22. doi:10.1016/j.jconrel.2018.03.001

25.	Lai JY, Ma DHK, Cheng HY, Sun CC, Huang SJ, Li YT, et al. Ocular Biocompatibility of Carbodiimide Cross-Linked Hyaluronic Acid Hydrogels for Cell Sheet Delivery Carriers. Journal of Biomaterials Science, Polymer Edition. 2010 Jan;21(3):359–76. doi:10.1163/156856209X416980

26.	Huang L, Huang XH, Yang X, Hu JQ, Zhu YZ, Yan PY, et al. Novel nano-drug delivery system for natural products and their application. Pharmacological Research. 2024 Mar;201:107100. doi:10.1016/j.phrs.2024.107100

27.	Fulgêncio GDO, Viana FAB, Ribeiro RR, Yoshida MI, Faraco AG, Cunha-Júnior ADS. New Mucoadhesive Chitosan Film for Ophthalmic Drug Delivery of Timolol Maleate: In Vivo Evaluation. Journal of Ocular Pharmacology and Therapeutics. 2012 Aug;28(4):350–8. doi:10.1089/jop.2011.0174

28.	Chavhan R. Nanosuspensions: Enhancing drug bioavailability through nanonization. Annales Pharmaceutiques Françaises. 2025 Mar;83(2):251–71. doi:10.1016/j.pharma.2024.06.003

29.	Ma Y, Cong Z, Gao P, Wang Y. Nanosuspensions technology as a master key for nature products drug delivery and In vivo fate. European Journal of Pharmaceutical Sciences. 2023 Jun;185:106425. doi:10.1016/j.ejps.2023.106425

30.	Patel V, Agrawal Y. Nanosuspension: An approach to enhance solubility of drugs. J Adv Pharm Technol Res. 2011;2(2):81. doi:10.4103/2231-4040.82950

31.	Kumar D, Jain N, Gulati N, Nagaich U. Nanoparticles laden in situ gelling system for ocular drug targeting. J Adv Pharm Technol Res. 2013;4(1):9. doi:10.4103/2231-4040.107495

32.	Gupta H, Aqil M, Khar R, Ali A, Bhatnagar A, Mittal G. Nanoparticles laden in situ gel for sustained ocular drug delivery. J Pharm Bioall Sci. 2013;5(2):162. doi:10.4103/0975-7406.111824

33.	Jamard M, Hoare T, Sheardown H. Nanogels of methylcellulose hydrophobized with N-tert-butylacrylamide for ocular drug delivery. Drug Deliv and Transl Res. 2016 Dec;6(6):648–59. doi:10.1007/s13346-016-0337-4

34.	El Bejjaji S, Ramos-Yacasi G, Suñer-Carbó J, Mallandrich M, Goršek L, Quilchez C, et al. Nanocomposite Gels Loaded with Flurbiprofen: Characterization and Skin Permeability Assessment in Different Skin Species. Gels. 2024 May 24;10(6):362. doi:10.3390/gels10060362

35.	Patra JK, Das G, Fraceto LF, Campos EVR, Rodriguez-Torres MDP, Acosta-Torres LS, et al. Nano based drug delivery systems: recent developments and future prospects. J Nanobiotechnol. 2018 Dec;16(1):71. doi:10.1186/s12951-018-0392-8

36.	Kumar S, Himmelstein KJ. Modification of in Situ Gelling Behavior of Carbopol Solutions by Hydroxypropyl Methylcellulose. Journal of Pharmaceutical Sciences. 1995 Mar;84(3):344–8. doi:10.1002/jps.2600840315

37.	Eljarrat-Binstock E, Domb AJ. Iontophoresis: A non-invasive ocular drug delivery. Journal of Controlled Release. 2006 Feb;110(3):479–89. doi:10.1016/j.jconrel.2005.09.049

38.	Bonfioli AA, Damico FM, Curi ALL, Orefice F. Intermediate Uveitis. Seminars in Ophthalmology. 2005 Jan;20(3):147–54. doi:10.1080/08820530500232035

39.	Du Toit LC, Carmichael T, Govender T, Kumar P, Choonara YE, Pillay V. In Vitro, In Vivo, and In Silico Evaluation of the Bioresponsive Behavior of an Intelligent Intraocular Implant. Pharm Res. 2014 Mar;31(3):607–34. doi:10.1007/s11095-013-1184-3

40.	Huhtala A, Pohjonen T, Salminen L, Salminen A, Kaarniranta K, Uusitalo H. In vitro biocompatibility of degradable biopolymers in cell line cultures from various ocular tissues: Direct contact studies. J Biomedical Materials Res. 2007 Nov;83A(2):407–13. doi:10.1002/jbm.a.31319

41.	Oishi N, Montes-Moreno S, Feldman AL. In situ neoplasia in lymph node pathology. Seminars in Diagnostic Pathology. 2018 Jan;35(1):76–83. doi:10.1053/j.semdp.2017.11.001

42.	Ahmed B, Jaiswal S, Naryal S, Shah RM, Alany RG, Kaur IP. In situ gelling systems for ocular drug delivery. Journal of Controlled Release. 2024 Jul;371:67–84. doi:10.1016/j.jconrel.2024.05.031

43.	Al Khateb K, Ozhmukhametova EK, Mussin MN, Seilkhanov SK, Rakhypbekov TK, Lau WM, et al. In situ gelling systems based on Pluronic F127/Pluronic F68 formulations for ocular drug delivery. International Journal of Pharmaceutics. 2016 Apr;502(1–2):70–9. doi:10.1016/j.ijpharm.2016.02.027

44.	Lin HR, Sung KC, Vong WJ. In Situ Gelling of Alginate/Pluronic Solutions for Ophthalmic Delivery of Pilocarpine. Biomacromolecules. 2004 Nov 1;5(6):2358–65. doi:10.1021/bm0496965

45.	Liu Y, Liu J, Zhang X, Zhang R, Huang Y, Wu C. In Situ Gelling Gelrite/Alginate Formulations as Vehicles for Ophthalmic Drug Delivery. AAPS PharmSciTech. 2010 Jun;11(2):610–20. doi:10.1208/s12249-010-9413-0

46.	Kolawole OM, Cook MT. In situ gelling drug delivery systems for topical drug delivery. European Journal of Pharmaceutics and Biopharmaceutics. 2023 Mar;184:36–49. doi:10.1016/j.ejpb.2023.01.007

47.	Agrawal AK, Das M, Jain S. In situ gel systems as ‘smart’ carriers for sustained ocular drug delivery. Expert Opinion on Drug Delivery. 2012 Apr;9(4):383–402. doi:10.1517/17425247.2012.665367

48.	Bain MK, Bhowmik M, Ghosh SN, Chattopadhyay D. In situ fast gelling formulation of methyl cellulose for in vitro ophthalmic controlled delivery of ketorolac tromethamine. J of Applied Polymer Sci. 2009 Jul 15;113(2):1241–6. doi:10.1002/app.30040

49.	Keino H, Horie S, Sugita S. Immune Privilege and Eye-Derived T-Regulatory Cells. Journal of Immunology Research. 2018;2018:1–12. doi:10.1155/2018/1679197

50.	Kirchhof S, Goepferich AM, Brandl FP. Hydrogels in ophthalmic applications. European Journal of Pharmaceutics and Biopharmaceutics. 2015 Sep;95:227–38. doi:10.1016/j.ejpb.2015.05.016

51.	Hoare TR, Kohane DS. Hydrogels in drug delivery: Progress and challenges. Polymer. 2008 Apr;49(8):1993–2007. doi:10.1016/j.polymer.2008.01.027

52.	Chang D, Park K, Famili A. Hydrogels for sustained delivery of biologics to the back of the eye. Drug Discovery Today. 2019 Aug;24(8):1470–82. doi:10.1016/j.drudis.2019.05.037

53.	Fathi M, Barar J, Aghanejad A, Omidi Y. Hydrogels for ocular drug delivery and tissue engineering. Bioimpacts. 2015 Dec 28;5(4):159–64. doi:10.15171/bi.2015.31

54.	Hamidi M, Azadi A, Rafiei P. Hydrogel nanoparticles in drug delivery. Advanced Drug Delivery Reviews. 2008 Dec;60(15):1638–49. doi:10.1016/j.addr.2008.08.002

55.	Dua HS, Faraj LA, Said DG, Gray T, Lowe J. Human Corneal Anatomy Redefined. Ophthalmology. 2013 Sep;120(9):1778–85. doi:10.1016/j.ophtha.2013.01.018

56.	Jung HJ, Abou-Jaoude M, Carbia BE, Plummer C, Chauhan A. Glaucoma therapy by extended release of timolol from nanoparticle loaded silicone-hydrogel contact lenses. Journal of Controlled Release. 2013 Jan;165(1):82–9. doi:10.1016/j.jconrel.2012.10.010

57.	Mandal S, Prabhushankar G, Thimmasetty M, Geetha M. Formulation and evaluation of an in situ gel-forming ophthalmic formulation of moxifloxacin hydrochloride. Int J Pharma Investig. 2012;2(2):78. doi:10.4103/2230-973X.100042

58.	Oh DH, Din FU, Kim DW, Kim JO, Yong CS, Choi HG. Flurbiprofen-loaded nanoparticles prepared with polyvinylpyrrolidone using Shirasu porous glass membranes and a spray-drying technique: nano-sized formation and improved bioavailability. Journal of Microencapsulation. 2013 Nov;30(7):674–80. doi:10.3109/02652048.2013.774447

59.	Pignatello R, Bucolo C, Spedalieri G, Maltese A, Puglisi G. Flurbiprofen-loaded acrylate polymer nanosuspensions for ophthalmic application. Biomaterials. 2002 Aug;23(15):3247–55. doi:10.1016/S0142-9612(02)00080-7

60.	Dewan M, Bhowmick B, Sarkar G, Rana D, Bain MK, Bhowmik M, et al. Effect of methyl cellulose on gelation behavior and drug release from poloxamer based ophthalmic formulations. International Journal of Biological Macromolecules. 2015 Jan;72:706–10. doi:10.1016/j.ijbiomac.2014.09.021

61.	Kaji H, Nagai N, Nishizawa M, Abe T. Drug delivery devices for retinal diseases. Advanced Drug Delivery Reviews. 2018 Mar;128:148–57. doi:10.1016/j.addr.2017.07.002

62.	Attama AA, Reichl S, Müller-Goymann CC. Diclofenac sodium delivery to the eye: In vitro evaluation of novel solid lipid nanoparticle formulation using human cornea construct. International Journal of Pharmaceutics. 2008 May 1;355(1–2):307–13. doi:10.1016/j.ijpharm.2007.12.007

63.	Li X, Zhang Z, Chen H. Development and evaluation of fast forming nano-composite hydrogel for ocular delivery of diclofenac. International Journal of Pharmaceutics. 2013 May;448(1):96–100. doi:10.1016/j.ijpharm.2013.03.024

64.	Makwana SB, Patel VA, Parmar SJ. Development and characterization of in-situ gel for ophthalmic formulation containing ciprofloxacin hydrochloride. Results in Pharma Sciences. 2016;6:1–6. doi:10.1016/j.rinphs.2015.06.001

65.	Bíró T, Aigner Z. Current Approaches to Use Cyclodextrins and Mucoadhesive Polymers in Ocular Drug Delivery—A Mini-Review. Sci Pharm. 2019 Jun 28;87(3):15. doi:10.3390/scipharm87030015

66.	Natu MV, Sardinha JP, Correia IJ, Gil MH. Controlled release gelatin hydrogels and lyophilisates with potential application as ocular inserts. Biomed Mater. 2007 Dec;2(4):241–9. doi:10.1088/1748-6041/2/4/006

67.	Adepu S, Ramakrishna S. Controlled Drug Delivery Systems: Current Status and Future Directions. Molecules. 2021 Sep 29;26(19):5905. doi:10.3390/molecules26195905

68.	Yang H, Zhao M, Xing D, Zhang J, Fang T, Zhang F, et al. Contact lens as an emerging platform for ophthalmic drug delivery: A systematic review. Asian Journal of Pharmaceutical Sciences. 2023 Sep;18(5):100847. doi:10.1016/j.ajps.2023.100847

69.	Ameeduzzafar, Ali J, Fazil M, Qumbar M, Khan N, Ali A. Colloidal drug delivery system: amplify the ocular delivery. Drug Delivery. 2016 Mar 23;23(3):700–16. doi:10.3109/10717544.2014.923065

70.	Martens TF, Remaut K, Deschout H, Engbersen JFJ, Hennink WE, Van Steenbergen MJ, et al. Coating nanocarriers with hyaluronic acid facilitates intravitreal drug delivery for retinal gene therapy. Journal of Controlled Release. 2015 Mar;202:83–92. doi:10.1016/j.jconrel.2015.01.030

71.	Duttagupta D, Jadhav V, Kadam V. Chitosan: A Propitious Biopolymer for Drug Delivery. CDD. 2015 Jul 29;12(4):369–81. doi:10.2174/1567201812666150310151657

72.	Chen X, Li X, Zhou Y, Wang X, Zhang Y, Fan Y, et al. Chitosan-based thermosensitive hydrogel as a promising ocular drug delivery system: Preparation, characterization, and in vivo evaluation. J Biomater Appl. 2012 Nov;27(4):391–402. doi:10.1177/0885328211406563

73.	Bhattarai N, Gunn J, Zhang M. Chitosan-based hydrogels for controlled, localized drug delivery. Advanced Drug Delivery Reviews. 2010 Jan;62(1):83–99. doi:10.1016/j.addr.2009.07.019

74.	Eljarrat-Binstock E, Orucov F, Aldouby Y, Frucht-Pery J, Domb AJ. Charged nanoparticles delivery to the eye using hydrogel iontophoresis. Journal of Controlled Release. 2008 Mar;126(2):156–61. doi:10.1016/j.jconrel.2007.11.016

75.	Bhattacharya S. Central Composite Design for Response Surface Methodology and Its Application in Pharmacy. In: Kayaroganam P, editor. Response Surface Methodology in Engineering Science [Internet]. IntechOpen; 2021 [cited 2026 Mar 23]. Available from: https://www.intechopen.com/books/response-surface-methodology-in-engineering-science/central-composite-design-for-response-surface-methodology-and-its-application-in-pharmacy doi:10.5772/intechopen.95835

76.	Hassan H, Adam SK, Alias E, Meor Mohd Affandi MMR, Shamsuddin AF, Basir R. Central Composite Design for Formulation and Optimization of Solid Lipid Nanoparticles to Enhance Oral Bioavailability of Acyclovir. Molecules. 2021 Sep 7;26(18):5432. doi:10.3390/molecules26185432

77.	Yessentayeva NA, Galiyeva AR, Sadyrbekov DT, Daribay AT, Tazhbayev YM. Central Composite Design for Formulation and Optimization of Rifampicin Loaded Polylactide-Co-Glycolide Nanoparticles [Internet]. Chemistry and Materials Science; 2024 [cited 2026 Mar 23]. Available from: https://www.preprints.org/manuscript/202406.1644/v1 doi:10.20944/preprints202406.1644.v1

78.	Jacob J, Haponiuk JT, Thomas S, Gopi S. Biopolymer based nanomaterials in drug delivery systems: A review. Materials Today Chemistry. 2018 Sep;9:43–55. doi:10.1016/j.mtchem.2018.05.002

79.	Lee SS, Hughes P, Ross AD, Robinson MR. Biodegradable Implants for Sustained Drug Release in the Eye. Pharm Res. 2010 Oct;27(10):2043–53. doi:10.1007/s11095-010-0159-x

80.	Jain D, Carvalho E, Banerjee R. Biodegradable hybrid polymeric membranes for ocular drug delivery. Acta Biomaterialia. 2010 Apr;6(4):1370–9. doi:10.1016/j.actbio.2009.11.001