Review Article

THE BOON OF 3D PRINTING IN COSMETIC PRODUCT DEVELOPMENT

Abstract

The advent of 3D printing technology is shaking up various pharmaceutical and healthcare industries, with cosmetic industries. This technology also called as additive manufacturing that creates 3D objects using material by deposition layer-by-layer and includes several techniques like fused deposition model, and stereolithography. It has the ability to create complex, customizable cosmetic products. These advancements have led to the development of innovative delivery systems, comprising skin patch and microarray patches for efficient skin delivery of active ingredients. 3D printed microneedles and skin patches have shown exceptional promise in enhancing the penetration and bioavailability of active ingredients that conventionally face barriers due to skin protective layers. By using biocompatibile material and CAD designs, these technologies facilitate the effective delivery of compounds such as caffeine, salicylic acid and various vitamins directly to the skin. Studies indicate that 3D printing not only improves the efficacy of these cosmetic formulations but also allows for a high degree of personalization, catering to individual skin type. The study concludes the influence of 3D printing on the cosmetic field, highlighting key technology advancement, material used, and the ability for future developments. The combination of 3D printing in cosmetics appears to be promising for the development of personalized skin care, presenting customization and efficacy in beauty treatments.

Keywords: Personalized skin care, additive manufacturing, stereolithography, fused deposition model, microneedle, and skin patch.

Introduction

The skin is the largest part of the body, covering an extensive expanse of approximately 1.7 square meters. It represents about 16% of an average person's total body mass. Primarily, the skin act as a protective barrier against microbes, UV rays, chemicals, allergen, and water loss. It has three main layers: the epidermis(outer layer with stratum corneum), the dermis (middle supportive layer), and the hypodermis (inner fatty layer for insulation)(Herskovitz et al., 2016; Richardson, 2003)

By collaborating, these three layers maintain the integrity and functionality of the skin, allowing it to fulfill its essential role in protecting the body and dealing with the external environment.Top of Form

The outermost layer of the skin, alias the stratum corneum (SC), functions as a highly effective barrier, preventing the penetration of physical, chemical, and microbial substances into the skin. While this barrier function is crucial for protecting the body, it limits the penetration cosmetic active ingredients, also called actives, into the deeper layer of skin. The penetration of actives from topical formulations is generally inefficient, resulting in low bioavailability, typically less than 2% of the applied dose. The stratum corneum acts as a formidable barrier, compromises the dermal delivery of these actives. This limits the effectiveness of topical formulations in delivering these ingredients to their intended targets. The low bioavailability observed is a result of the skin's protective mechanisms, which aim to minimize the entry of foreign substances.(Mian et al., 2019)

Caffeine is a well-researched active ingredient in both cosmetic and pharmaceutical application and is commonly used as a representative hydrophilic compound in skin toxicology studies. A review of various topical caffeine formulations reported that conventional ointments showed a maximum skin penetration of just 0.0062%.(Luo & Lane, 2015)

Optimizing the dermal delivery of active ingredients is a key area of research. To overcome the skin barrier, researchers have developed multiple strategies, ranging from passive techniques like chemical enhancers and supersaturation to to sophisticated systems like liposomes, niosomes, transferosomes and lipid nanoparticle as well as physical enhancement tools like microneedle arrays. Recently, the use of 3D printed platforms as carriers has emerged as a promising, patient centric approach to optimizing drug delivery for improved delivery.(Lunter et al., 2024)

Digital –to- physical cosmetic mapping

Figure 1: Digital –to- physical cosmetic mapping

The development of Additive Manufacturing (AM), or 3D printing, has streamlined the production of microneedles by allowing the entire fabrication process to be carried out in a single step Figure No. 1. Designing the desired dimensions and shape is done using Computer-Aided Design (CAD) software, followed by fabrication. 3D printing offers not only simplicity but also pliability, allowing for easy modifications to designs using computer software. It has the power to transform personalized treatment by enabling the production of pharmaceutical formulations tailored to individual patient characteristics, including customized drug doses. 3D printed arrays have the capability to deliver multiple active ingredients simultaneously, with dosages specific to each individual. While various 3D printing techniques are used in pharmaceutics, stereolithography (SLA) shows promise for its precision. However, further research is needed to fully explore SLA for fabricating 3D printed microneedles.(Jiao et al., 2022)

Types of 3D printing technology with their application in cosmetics

For printing skin delivery platforms, there are two dominant 3D printing technologies: FDM and SLA. Recent studies has also inspect the application of Digital Light Processing (DLP) and Two Photon Polymerization (TPP) techniques. Additionally, Inkjet Printing is utilized during post-platform fabrication processes to incorporate active ingredients into the platforms.(Lakkala et al., 2023)

Ink jet printing

Inkjet printing technique to personalized medicine comes from the same technique of computer – operated inkjet printing. It is also a form of additive manufacturing where ink is replaced with pharmaceutical solutions containing drugs. Small drops are sprayed in a level- by – level manner on a suitable substrate that finally solidifies into the solid dosage form. Inkjet printing methods primarily categorized into two techniques as shown in Figure No. 2– Continuous inkjet printing (CIJ) and Drop on demand (DOD).(Carou‐Senra et al., 2024)

Figure 2: Classification of inkjet printing

Continuous inkjet printing

As the term suggests, continuous inkjet printers operate by emitting a nonstop stream of ink droplets onto the printing surface at high speed, regardless of whether all the droplets are required. In the flow of ink, the pressure wave is initiated which results in the breakup of the ink into uniformly sized droplets, and then with the help of nozzles, these droplets are ejected out.

Uncharged drops are sent out again and liquid reutilized. Charged drops pass through an electric field between deflector plates on the substrates. It features rapid, uninterrupted formation of ink droplets, which helps prevent the nozzle from getting clogged.

As a continuous flow of ink is used at high speed, this technology causes a high degree of wastage of inks. In Continuous inkjet systems, any excess ink that isn’t used during printing is captured and sent back to the reservoir for reuse, whereas in drop-on- demand printing, the print head releases ink only at the exact moments it is required.

Drop on demand inkjet printing

Drop on demand divides into two technologies, one that utilizing heat (Thermal drop on demand) and those utilizing piezoelectricity (Piezoelectric drop on demand). In drop on demand, the ink comes out of the nozzle if there is a requirement of ink.

Thermal drop on demand printing

Thermal inkjet printing uses a heating element and this heating element produces heat to vaporize the ink and this vaporization creates a bubble. When the bubble expands it forces the ink out of the nozzle.

Piezoelectric drop on demand printing

Piezoelectric inkjet printing utilizes a small crystal situated at the rear of the ink reservoir in nozzle. Electrical current is applied to the crystal that makes the crystal vibrate. When the crystal vibrates it expands and pushes the ink through the nozzle and when the crystal shrinks, it drags more ink from the reservoir.(Varghese et al., 2022)

Application

Polymeric microneedle patches for transdermal insulin delivery were fabricated in this study using stereolithography, a 3D printing technique. The process involved using a biocompatible resin to construct microneedle designs in the shape of pyramids and cones, followed by the application of insulin formulations using inkjet printing. Trehalose, mannitol, and xylitol were employed as carrier agents to help preserve insulin’s structure and stability, while also supporting its quick release. Assessment using circular dichroism and Raman spectroscopy showed that each carrier maintained insulin in its native state, with xylitol exhibiting the best overall performance. In vitro Franz cell release studies conducted on porcine skin demonstrated rapid release of insulin within a span of 30 minutes, regardless of the specific microneedle design. This research underscores the effectiveness of 3D printing as a scalable and biocompatible approach for producing microneedle patches.(Pere et al., 2018)

Fused Deposition Modelling-

Fused deposition modeling, also known as fused filament fabrication (FFF) or filament freeform fabrication works on an “additive” principle by putting down material in layers. It produces a part by using a continuous filament of a thermoplastic material. In this beads of heated plastic are used instead of ink, and these beads are released from the print head and build the object.

It contains a printer platform, a printer head (nozzle), and the raw material in the form of the filament.

Printer platform- The print platform is a bed that is made up of metal, ceramic or hard plastic, and each continuous layer is set down on this platform.

Nozzle / Print Head – An extruder is made up of two main sections: a cold end and a hot end. The cold end draws filament from the spool, with its movement regulated by a stepper motor that controls the feed rate. This material is then guided into the hot end, which contains a heating zone and a nozzle. Inside the heating zone, the material is melted into a flowable state. It is then forced through the nozzle, where it is deposited as a fine, semi-molten strand that sticks to the surface beneath it. The printing resolution in fused filament fabrication (FFF) is largely determined by the nozzle size and the layer height. Various nozzle types are available, and the choice depends on the specific material being used for printing.

The raw material- Any thermoplastic material can be used as raw material for FDM printer. When exposed to heat, the thermoplastic material can melt again and again and be resolidified when the heat is withdrawn. A large variety of filament materials are extruded.(Dhinakaran et al., 2020)

Working process-

Figure 3: Workflow of Fused Deposition Model

Application

- Stevic et al studied about the application of 3D printing (3DP) technology for the development of customized lipstick products. The study explored to assess the viability of using commercially available 3D scanning and printing equipment to devise personalized lipstick applicators. To capture accurate lip data, a lip scan was performed, generating digital profiles of the lips. These profiles were then utilized to create a digital representation of the lips was designed using Autodesk 3ds Max, a software tool for 3D computer graphics. For the production of personalized lipstick applicators, three essential elements were considered: a lipstick mould, base, and cap. To determine the most appropraite 3D printing technique for manufacturing personalized lipsticks, the three applicator components were created using both stereolithography (SLA) and fused deposition modeling (FDM) printers.(Stevic, 2017)

- Goyanes et al studied about acne, a common inflammatory skin condition, is known for its multifactorial nature. This study investigated the use of 3D printing to create personalized, adaptable anti-acne drug devices incorporating salicylic acid. Two different 3D printing technologies, Fused Deposition Modeling (FDM) and Stereolithography (SLA), were used to evaulate their potential in creating such devices. The process involved utilizing 3D scanning technology to capture the individual's nose morphology and generate a personalized 3D model.(Goyanes et al., 2016)

- Wang et al This study presents a pioneering approach in the field of acne treatment through the development of a customized 3D printed niosomal hydrogel (NH) loaded with CPT (a drug for acne). Unlike conventional acne treatment products like facemasks, which lack personalization and tailored medication dosing, 3D-printed drug delivery systems offer individualized solutions. Employing 3D Printed hydrogels for acne therapy provides unique benefits that are rarely highlighted in conventional studies: (i) the ability to tailor drug doses according to individual needs; (ii) customization of hydrogel size, thickness, or area to target specific acne symptoms; and (iii) a simplified drug loading process. This innovative approach highlights unique features that set it apart from existing literature.(Wang et al., 2020)

- In research conducted by Wu et al., a novel method was utilized to create a microneedle patch system designed for minimally invasive, glucose-responsive insulin delivery in the management of diabetes. The technique combined material extrusion 3D printing with post-stretching processes. The produced microneedle patch featured a 6 × 6 array of microneedles, where insulin release occurred exclusively from the microneedles in response to glucose. Importantly, the microneedles showed adequate mechanical strength to pierce the skin of mice and successfully delivered insulin in a glucose-dependent manner, both in glucose solutions and in type 1 diabetic mice. This study introduces a promising fabrication method for microneedle patch systems that hold potential for transdermal systems applications in the future.(Wu et al., 2020)

Stereolithography (SLA)

SLA is the most extensively researched photopolymerisation technology for creating skin delivery platforms. Stereolithography is the technique in which the liquid polymer or resin solidifies by a CNC laser or automated laser systems. There is a surface of the photopolymer vat where the UV laser will draw a pre-programmed design or shape. It is not a quick process because it takes 6 to 12 hours or for a large object, it takes several days. This technique fabricates nearly any design so it can be of big-budget.(Huang et al., 2020)

Working process-

Figure 4: Workflow of Stereolithography

Application

Microneedle arrays for transdermal insulin administration were effectively produced using a biocompatible resin through stereolithography (SLA), with design optimization carried out to improve their ability to penetrate the skin. The microneedles were constructed by polymerizing successive layers of a light sensitive polymer resin. To facilitate insulin delivery, thin layers of insulin and carriers such as sugar alcohols or disaccharides were selectively deposited on the microneedle surface using inkjet printing. By refining the printing parameters, the fabricated microneedles showed improved ability to penetrate the skin compared to conventional metal arrays, requiring only low insertion forces in the range of 2–5 N. Additionally, micro-CT imaging verified that the coated films remained firmly attached to the microneedle surface even after insertion into the skin. In vivo animal trials demonstrated rapid insulin action, effective hypoglycemia control, and lower glucose levels achieved within 60 minutes. Additionally, steady-state plasma glucose levels were maintained over a 4-hour period compared to subcutaneous injections. These findings underscore the significant potential of 3D printed microneedle arrays in enabling efficient and precise transdermal insulin delivery, leading to improved therapeutic outcomes in diabetes management.(Economidou et al., 2019)

Published Research on 3D Printing for Cosmetic API Delivery System

Recent research in 3D printing technology have widened new chances in the cosmetic field, mostly for delivering APIs. Advancements in this area aim to make cosmetic products customizable and effective using 3D printing technology. Table 1 shows about some skin treatment, API used and their 3D printing method.

Table 1: Skin treatment, API used and their 3D printing method

| Skin Treatment Effects | API | 3D Printing Method | Reference |
| --- | --- | --- | --- |
| Skin Rejuvenation | Retinol | Stereolithography | (Islam et al., 2023) |
| Anti-acne | Salicylic acid | Fused Deposition Model (FDM) | (Goyanes et al., 2016) |
| Anti-aging | Acetyl-hexapeptide 3 (AHP-3) | Digital Light Processing (DLP) | (Lim et al., 2021) |
| Skin hydration and firming | Hyaluronic acid | Fused Deposition Model (FDM) | (Antezana et al., 2022) |
| Skin whitening | Hydroquinone | Stereolithography | (Jiao et al., 2022) |

Advanced 3D Printed Delivery Platforms

Skin patches and microneedles- based delivery system, both 3D printed platforms, have gained attention for their potential in delivering cosmetic and pharmaceutical products to the skin. They aim to make skin delivery more effective and convenient. In this section, we'll explore developments in both skin patches and microneedles.(Nazary Abrbekoh et al., 2022)

Skin Patches

Skin patches are a common and well-researched method for delivering active substances to the skin. They have been utilized for many years to address skin issues and enable transdermal delivery. Recent investigations have primarily concentrated on conventional skin patches, examining elements such as their active components, materials, methods to improve delivery, ways to analyze them, and their outcomes.

Figure 5: Skin Patch

Common techniques for making skin patches include using solvents, hydrogels, and hot melt processes. These patches as shown in Figure No. 5 securely to the skin and may be designed either with or without additional adhesive support. The adhesive qualities of these patches have a significant impact on how effectively they deliver active ingredients. They create a continuous seal, which helps active ingredients penetrate the skin more effectively by assisting their diffusion.

Overall, skin patches have attracted widespread attention thanks to their ability to effectively and flexibly deliver active ingredients. By forming a continuous seal on the skin, they enhance the penetration of these ingredients, ultimately improving their effectiveness in addressing various skin conditions and facilitating transdermal delivery.

Cosmetic patches seem promising for dealing with common beauty issues like wrinkles, pigmentation problems, and signs of aging on your skin. However, regular patches have a problem: they can't hold and release enough of the good stuff that helps your skin. When we use patch-like things to put medicine on our skin, the medicine has to get out of the patch, go through the top skin layer, and sometimes it gets stuck there like tiny crystals, which can slow things down. Skin patches face a challenge because the way active ingredients spread can be inconsistent. It varies from person to person based on factors like how hydrated your skin is, your age, and your ethnicity. The skin’s outermost layer, known as stratum corneum, serves as a protective shield that can hinder the rate at which substances spread. Additionally, the effectiveness of delivering active ingredients depends on the unique characteristics of each specific ingredient. Material used in skin patch are shown in table 2.

Traditional adhesive patches usually have multiple layers and are classified based on where the drug or active ingredient is placed within these layers. This requires a multi-step manufacturing process. On the other hand, 3D printed patches are often made from a single layer and a single material, although it's possible to print them with multiple layers. Scientists have been investigating the application of 3D printed mesh or grid patches that contain drugs, either for inserting into tissues or offering support for organs.(Mohammed et al., 2021; Wong et al., 2023)

\Materials used in 3D Printed Skin Patch

Table 2: Material used in skin patch

| Skin Patch |  |  |
| --- | --- | --- |
| Material used | Method | Finding |
| Polycaprolactone (PCL), thermoplastic polyurethane and polylactic acid | FDM and SLA | Development of anti-acne cosmetic patch formulated with salicylic acid. FDM was not suitable as it cause degradation of salicylic acid. SLA method was adaptable |
| Lignin and PLA | Modified Hot melt extrusion FDM | Fabrication of hydrogel-based patches intended for wound care appliaction. This was adaptable and has the potential to carry high drug loading. |
| Chitosan-modifies nano-silica particle. | Direct Ink Writing (DIW) | Production of emulsion-based cosmetic patch. |
| Polylactic acid/phycocyanin-alginate | Casting | Production of spirulina extract was used for cosmetic patch with excellent adaptability. |

Advancements in 3D printed patch platforms are an exciting and evolving area of study, with the potential to enhance current designs and transform the world of skin delivery systems.

Microneedles

Microneedles (MNs) combine aspects of both skin based drug delivery (patches) and hypodermic needles. They bring several advantages, including easy application, very little interfering, and effective delivery of active ingredients. A tiny needle-like structures integrated into a patch, known as a microneedle patch (MNP), which makes them easy to use. Compare to conventional patches and topical formulation, MNs offer greater versatility and deliver active ingredients more effectively deeper into the skin.(Waghule et al., 2019)

Instead of relying on passive diffusion, microneedles work by actively creating tiny opening in the skin’s outer layer (epidermis) and, when designed appropriately, can reach the deeper layer (dermis), forming tiny channels. These micro-punctures successfully bypass the skin's natural barrier, offering a painless and minimally invasive method to enhance the delivery of drugs or cosmetic products. Some advanced microneedles also double as wearable therapeutic devices for monitoring in real-time.(Tuan-Mahmood et al., 2013) Classification of 3D printed microneedles are shown in table 3.

Table3: Classification of 3D Printed Microneedles.

| Types of Microneedle | Definition | Material used in Microneedle |
| --- | --- | --- |
| Solid MNs | These are meant to applied drug topically. These are utilized to make microchannels in the skin. They solidly built, painless and simple in design. | Polylactic acid (PLA), Polycaprolactone (PCL), Polyglycolic acid (PGA) |
| Coated MNs | These have a coating of drug on MNs surface. Coatings are designed to dissolve once inserted into the skin, allowing the drug to be released. | poly(lactic-co-glycolic acid) (PLGA), polyvinyl alcohol (PVA), and polyethylene glycol, stainless steel |
| Dissolving MNs | These MNs are made up of biodegradable polymers that contains drug and dissolve thoroughly in the skin, delivering the drug they carry. | Gelatin, polylactico-glycolic acid (PLGA), Polyvinylpyrrolidone (PVA) |
| Hollow MNs | These MNs feature hollow channels that enable the direct delivery of liquid drugs into the skin. | Silicon, Glass |
| Swellable MNs | When these MNs comes in contact with skin moisture, they swell up and permits controlled and sustained drug release. | Polyethylene glycol, carboxymethyl cellulose (CMC), hyaluronic acid. |

In a recent inclusive review, researchers have investigated the ability of microneedles (MNs) in cosmetic area. They have grouped these studies based on the distinct skin issues they aim to address. Additionally, the review delves into the use of 3D printing technology in the production of MN platforms.

The use of 3D printing in MN production can be categorized into three primary methods:

- Development of Master Molds: 3D printing allow for the precise fabrication of master molds. These molds serve as templates for producing MNs using different manufacturing methods.

- Coating Active Ingredients onto Prepared MNs: 3D printing can be employed to coat active ingredients onto MNs that are pre-fabricated. This enhances the functionality of the MNs.

- Printing Complete MN Structures: It is also possible to 3D print the entire MN structures, integrating active ingredients directly during the printing process.

While the domain of 3D printed cosmetic microneedles is relatively new, published research papers and patents have already shown effective delivery of hydrophilic and lipophilic active ingredients using alternative techniques. These findings provide compelling evidence that the use of 3D printing for microneedles in cosmetic applications holds great promise and feasibility.(Park et al., 2022)

Methods of MNs Production

Conventional methods of fabricating microneedles include moulding method, lithography, and centrifugal lithography. Moulding use PLA or PCL into a mould to create microneedles. Lithography fabricate patterns by using light on a photosensitive substrate. Centrifugal lithography uses spinning to create microneedles without UV light. However these conventional methods have some drawbacks like lack of precision required for high quality microneedles, complex method and costly. To address these drawbacks, novel 3D printed technologies have been developed like FDM, SLA, and DLP as shown in table 4. These novel methods permits for more precise, versatile and efficient microneedle that improves drug delivery systems.(Lyu et al., 2023)

Table 4: Difference between conventional and 3D printed method

| Conventional MNs Fabrication Method | Moulding Method | Lithography | Centrifugal Lithography |
| --- | --- | --- | --- |
|  | This method creates a shape of MNs using a mould. Materials like drug are incorporated or injected into the mould and permits to knuckle down. | This technique fabricate patterns by using light on a photosensitive substrate. | Centrifugal force is used on viscous polymer dispensed between rotating plates to design MNs. |
| 3D Printed MNs Fabrication Method | FDM | SLA | DLP |
|  | FDM fabricates objects layer by layer by extruding melted thermplastic filament. it is the most widely used because of its feasibility. | A UV laser is employed to solidify liquid resin, constructing the final product layer by layer. | Digital light projector is used to cure on entire layer at once, this speeding in the process. |

A study conducted to assess wrinkle reduction compared dissolving MNs (DMNs) to a standard hyaluronic acid formulation. The results showed that over an eight-week treatment period, MNs were significantly more effective. In addition to enhancing skin delivery through microchannels, MNs have the potential to stimulate the production and deposition of elastin and collagen, thereby encouraging natural skin healing and metabolic activity.

Although a few studies have explored the production of DMNs through 3D printing, none of them have specifically investigated the utilization of sugar-based biopolymers. The challenge of ensuring these dissolvable polymers are suitable for printing poses significant hurdles, limiting the application of 3D printing techniques for DMN manufacturing, except for micro-molding approaches.(Qureshi & Saleem, 2024)

Quality assessment of 3D Printed Skin Patch and Microneedle

A structured overview of the various features of 3D printed platforms characterization, method and their description is shown in table 5.(Olowe et al., 2022)

Table 5: Quality assessment of 3D Printed Skin Patch and Microneedle

| Features | Methods | Description |
| --- | --- | --- |
| Morphology and Geometry | Optical Microscopy and SEM | Examine surface morphology and dimensional accuracy, high resolution imaging to inspect surface features. |
| In vivo imaging techniques | In vivo imaging techniques | Examine practical application and uniformity of microneele arrays on biological surfaces. |
| Mechanical properties | Mechanical Tester | Measure parameters like puncture force and deformation. |
| Rheological Properties | Rheometers | Assess flow characteristics and viscoelastic behaviour of printing ink and form stable structure during printing. |
| pH Evaluation | pH Meter | Evaluate compatability with the pH of human skin to avoid irritation and ensure efficacy of cosmetics product |
| Filament Polymer | Differential Scanning Calorimetry (DSC) | Measure heat flow associated with phase transitions in polymer. |
| Degradation and Stability | SEM | Observe changes in microneedle structure over time or analyse porosity and surface defects. |
|  | DSC/ X-ray Diffraction | Track material degradation and dissolution pattern. |
|  | Transepidermal Water Loss (TEWL) | Evaluate effects of MNs penetration on skin barrier. |

Growth in 3D Bioprinting for Skin and Cosmetics

The future of 3D printing in cosmetics is assured to transform the industry with a new research and applications. Personalization of cosmetic products is one big area of advancement. 3D printing permits the fabrication of tailored skin care and other cosmetics according to an individual skin type, tone to increase the product efficacy and satisfaction by delivery drug. Research in new biocompatible and biodegradable materials will also play an important role in the production of cosmetic product such as microneedle and skin patch.

3D bioprinting has received significant attention from the cosmetic industry for new product testing. Olejnik et al 2022 studied about 3D bioprinting applications for skin, showing its ability for more exact and social testing method(Olejnik et al., 2022). Fossil based fibres are often used in conventional cosmetic facial mask which are not environment friendly. Recently, a biodegradable cosmetic patch was fabricated using environment friendly alternative blend poly (hydroxyalkoanates) and starch by 3D printing technology.

Zhang et al 2021 introduced the idea of “all-purpose ice microneedle” ability of delivering active ingredients and macromolecules to the skin which is difficult to make from conventional method. The micro-molding method was used to fabricate these microneedles. This technique involves freezing water in MN gel formulation. This research overcame the drawbacks of standard 3D printable material, ability to lead to next generation of MNs(Zhang et al., 2021).

Moreover, 3D printing can combine smart technology to print devices that can observe skin conditions in real-time and alter the release of active ingredients. Personalized treatment can be provided by these smart devices. Research and development in this field are likely to continue expanding the possibilities of 3D printing in cosmetics. We can expect more sophisticated and multifunctional cosmetic products that not only enhance beauty but also promote skin health.(Jiao et al., 2022)

Conclusion

In conclusion, the application of 3D printing technology in a cosmetic industry represents a significant advancement with the ability to transform traditional method to product development, testing, and delivery. This review provides an overview and critical assessment of th principles and main types of 3D printing technology. Focusing on the production of two skin delivery system- skin patch and microneedle. It also explores topical active ingredients used in these platforms aiming to inspire new application of 3D printing in cosmetics. 3D printing offers the potential for personalized solutions, addressing some drawbacks of traditional skin delivery system. 3D bioprinting offers new possibilities for ethical and accurate safety testing, while the development of eco-friendly cosmetic patches address environmental concerns associated with traditional material. As research and development continue, the incorporation of advanced technologies such as nanotechnology, artificial intelligence, and bioengineering will likely drive further innovation. This present a significant opportunity to create an efficient cosmetic delivery platforms using 3D printing technology.

Disclaimer (Artificial Intelligence)

ChatGPT was used solely for grammar and language correction, and not for data analysis, interpretation, content generation, or development of scientific ideas

Abbreviations:

3D: 3 Dimensional

CAD: Computer- Aided Drug

SC: Stratum Corneum

AM: Additive Manufacturing

SLA: Stereolithography

FFF: fused filament fabrication

FDM: Fused Deposition Model

API: Active Pharmaceutical Ingredients

DLP: Digital Light Processing

AHP-3: Acetyl-hexapeptide 3

PCL: Polycaprolactone

PLA: Polylactic Acid

DIW: Direct Ink Writing

MNP: Microneedle Patch

PCL: Polycaprolactone), Polyglycolic acid (PGA)

PLGA: poly(lactic-co-glycolic acid)

PVA: Polyvinyl alcohol

CMC: Carboxymethyl cellulose

CIJ: Continuous inkjet printing

DOD: Drop on demand

TEWL: Transepidermal Water Loss

SEM: Scanning electron microscope

References

- Antezana, P. E., Municoy, S., Álvarez-Echazú, M. I., Santo-Orihuela, P. L., Catalano, P. N., Al-Tel, T. H., Kadumudi, F. B., Dolatshahi-Pirouz, A., Orive, G., & Desimone, M. F. (2022). The 3D Bioprinted Scaffolds for Wound Healing. Pharmaceutics, 14(2), 464. https://doi.org/10.3390/pharmaceutics14020464

- Carou‐Senra, P., Rodríguez‐Pombo, L., Awad, A., Basit, A. W., Alvarez‐Lorenzo, C., & Goyanes, A. (2024). Inkjet Printing of Pharmaceuticals. Advanced Materials, 36(11), 2309164. https://doi.org/10.1002/adma.202309164

- Dhinakaran, V., Manoj Kumar, K. P., Bupathi Ram, P. M., Ravichandran, M., & Vinayagamoorthy, M. (2020). A review on recent advancements in fused deposition modeling. Materials Today: Proceedings, 27, 752–756. https://doi.org/10.1016/j.matpr.2019.12.036

- Economidou, S. N., Pere, C. P. P., Reid, A., Uddin, Md. J., Windmill, J. F. C., Lamprou, D. A., & Douroumis, D. (2019). 3D printed microneedle patches using stereolithography (SLA) for intradermal insulin delivery. Materials Science and Engineering: C, 102, 743–755. https://doi.org/10.1016/j.msec.2019.04.063

- Goyanes, A., Det-Amornrat, U., Wang, J., Basit, A. W., & Gaisford, S. (2016). 3D scanning and 3D printing as innovative technologies for fabricating personalized topical drug delivery systems. Journal of Controlled Release, 234, 41–48. https://doi.org/10.1016/j.jconrel.2016.05.034

- Herskovitz, I., Macquhae, F., Fox, J. D., & Kirsner, R. S. (2016). Skin movement, wound repair and development of engineered skin. Experimental Dermatology, 25(2), 99–100. https://doi.org/10.1111/exd.12916

- Huang, J., Qin, Q., & Wang, J. (2020). A Review of Stereolithography: Processes and Systems. Processes, 8(9), 1138. https://doi.org/10.3390/pr8091138

- Islam, H., Poly, T. S., Tisha, Z. T., Rahman, S., Naveed, A. I. J., Ahmed, A., Ahmed, S. N., Hassan, J., Uddin, Md. J., & Das, D. B. (2023). 3D Printed Hollow Microneedles for Treating Skin Wrinkles Using Different Anti-Wrinkle Agents: A Possible Futuristic Approach. Cosmetics, 10(2), 41. https://doi.org/10.3390/cosmetics10020041

- Jiao, Y., Stevic, M., Buanz, A., Uddin, M. J., & Tamburic, S. (2022). Current and Prospective Applications of 3D Printing in Cosmetics: A Literature Review. Cosmetics, 9(6), 115. https://doi.org/10.3390/cosmetics9060115

- Lakkala, P., Munnangi, S. R., Bandari, S., & Repka, M. (2023). Additive manufacturing technologies with emphasis on stereolithography 3D printing in pharmaceutical and medical applications: A review. International Journal of Pharmaceutics: X, 5, 100159. https://doi.org/10.1016/j.ijpx.2023.100159

- Lim, S. H., Kathuria, H., Amir, M. H. B., Zhang, X., Duong, H. T. T., Ho, P. C.-L., & Kang, L. (2021). High resolution photopolymer for 3D printing of personalised microneedle for transdermal delivery of anti-wrinkle small peptide. Journal of Controlled Release, 329, 907–918. https://doi.org/10.1016/j.jconrel.2020.10.021

- Lunter, D., Klang, V., Eichner, A., Savic, S. M., Savic, S., Lian, G., & Erdő, F. (2024). Progress in Topical and Transdermal Drug Delivery Research—Focus on Nanoformulations. Pharmaceutics, 16(6), 817. https://doi.org/10.3390/pharmaceutics16060817

- Luo, L., & Lane, M. E. (2015). Topical and transdermal delivery of caffeine. International Journal of Pharmaceutics, 490(1–2), 155–164. https://doi.org/10.1016/j.ijpharm.2015.05.050

- Lyu, S., Dong, Z., Xu, X., Bei, H.-P., Yuen, H.-Y., James Cheung, C.-W., Wong, M.-S., He, Y., & Zhao, X. (2023). Going below and beyond the surface: Microneedle structure, materials, drugs, fabrication, and applications for wound healing and tissue regeneration. Bioactive Materials, 27, 303–326. https://doi.org/10.1016/j.bioactmat.2023.04.003

- Mian, M., Silfvast-Kaiser, A. S., Paek, S. Y., Kivelevitch, D., & Menter, A. (2019). A Review of the Most Common Dermatologic Conditions and their Debilitating Psychosocial Impacts. International Archives of Internal Medicine, 3(2). https://doi.org/10.23937/2643-4466/1710018

- Mohammed, A. A., Algahtani, M. S., Ahmad, M. Z., Ahmad, J., & Kotta, S. (2021). 3D Printing in medicine: Technology overview and drug delivery applications. Annals of 3D Printed Medicine, 4, 100037. https://doi.org/10.1016/j.stlm.2021.100037

- Nazary Abrbekoh, F., Salimi, L., Saghati, S., Amini, H., Fathi Karkan, S., Moharamzadeh, K., Sokullu, E., & Rahbarghazi, R. (2022). Application of microneedle patches for drug delivery; doorstep to novel therapies. Journal of Tissue Engineering, 13, 204173142210853. https://doi.org/10.1177/20417314221085390

- Olejnik, A., Semba, J. A., Kulpa, A., Dańczak-Pazdrowska, A., Rybka, J. D., & Gornowicz-Porowska, J. (2022). 3D Bioprinting in Skin Related Research: Recent Achievements and Application Perspectives. ACS Synthetic Biology, 11(1), 26–38. https://doi.org/10.1021/acssynbio.1c00547

- Olowe, M., Parupelli, S. K., & Desai, S. (2022). A Review of 3D-Printing of Microneedles. Pharmaceutics, 14(12), 2693. https://doi.org/10.3390/pharmaceutics14122693

- Park, S., Lee, K., & Ryu, W. (2022). Research progress on detachable microneedles for advanced applications. Expert Opinion on Drug Delivery, 19(9), 1115–1131. https://doi.org/10.1080/17425247.2022.2121388

- Pere, C. P. P., Economidou, S. N., Lall, G., Ziraud, C., Boateng, J. S., Alexander, B. D., Lamprou, D. A., & Douroumis, D. (2018). 3D printed microneedles for insulin skin delivery. International Journal of Pharmaceutics, 544(2), 425–432. https://doi.org/10.1016/j.ijpharm.2018.03.031

- Qureshi, F., & Saleem, K. (2024). Towards Greener Manufacturing: Exploring Biodegradable Polymers for Sustainable 3D Printing. Unpublished. https://doi.org/10.13140/RG.2.2.10441.56168

- Richardson, M. (2003). Understanding the structure and function of the skin. Nursing Times, 99(31), 46–48.

- Stevic, M. C. (2017). Exploring the use of 3D Printing Technology in the Fabrication of Personalised Lipstick Applicators. Journal of Dermatology & Cosmetology, 1(4). https://doi.org/10.15406/jdc.2017.01.00024

- Tuan-Mahmood, T.-M., McCrudden, M. T. C., Torrisi, B. M., McAlister, E., Garland, M. J., Singh, T. R. R., & Donnelly, R. F. (2013). Microneedles for intradermal and transdermal drug delivery. European Journal of Pharmaceutical Sciences: Official Journal of the European Federation for Pharmaceutical Sciences, 50(5), 623–637. https://doi.org/10.1016/j.ejps.2013.05.005

- Varghese, R., Salvi, S., Sood, P., Karsiya, J., & Kumar, D. (2022). Recent advancements in additive manufacturing techniques employed in the pharmaceutical industry: A bird’s eye view. Annals of 3D Printed Medicine, 8, 100081. https://doi.org/10.1016/j.stlm.2022.100081

- Waghule, T., Singhvi, G., Dubey, S. K., Pandey, M. M., Gupta, G., Singh, M., & Dua, K. (2019). Microneedles: A smart approach and increasing potential for transdermal drug delivery system. Biomedicine & Pharmacotherapy, 109, 1249–1258. https://doi.org/10.1016/j.biopha.2018.10.078

- Wang, Z., Liu, L., Xiang, S., Jiang, C., Wu, W., Ruan, S., Du, Q., Chen, T., Xue, Y., Chen, H., Weng, L., Zhu, H., Shen, Q., & Liu, Q. (2020). Formulation and Characterization of a 3D-Printed Cryptotanshinone-Loaded Niosomal Hydrogel for Topical Therapy of Acne. AAPS PharmSciTech, 21(5), 159. https://doi.org/10.1208/s12249-020-01677-1

- Wong, W. F., Ang, K. P., Sethi, G., & Looi, C. Y. (2023). Recent Advancement of Medical Patch for Transdermal Drug Delivery. Medicina, 59(4), 778. https://doi.org/10.3390/medicina59040778

- Wu, M., Zhang, Y., Huang, H., Li, J., Liu, H., Guo, Z., Xue, L., Liu, S., & Lei, Y. (2020). Assisted 3D printing of microneedle patches for minimally invasive glucose control in diabetes. Materials Science and Engineering: C, 117, 111299. https://doi.org/10.1016/j.msec.2020.111299

- Zhang, X., Fu, X., Chen, G., Wang, Y., & Zhao, Y. (2021). Versatile Ice Microneedles for Transdermal Delivery of Diverse Actives. Advanced Science, 8(17), 2101210. https://doi.org/10.1002/advs.202101210