



A Comprehensive Review of Three-Way Catalytic Converters for Automotive Exhaust Emission Control: Materials, Performance, and Challenges.
Abstract
Catalytic converters are essential emission control devices used in internal combustion engine vehicles to reduce harmful exhaust gases such as carbon monoxide (CO), hydrocarbons (HC), and nitrogen oxides (NOx). This paper presents a comprehensive review of catalytic converter technologies, with particular emphasis on three-way catalytic converters (TWC). The study examines catalyst materials, structural configurations, reaction mechanisms, and performance factors that affect catalytic converters. A systematic review of recent literature (2003–2025) highlights advancements in exhaust emission control technology using three-way catalytic converters and strategies aimed at improving catalytic efficiency and reducing reliance on expensive noble metals. The review further identifies key limitations affecting performance under real driving conditions and proposes future research directions focused on cost-effectiveness, thermally stability, and environmentally sustainable catalytic systems suitable for developing economies.
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1.0 Introduction 
              The rapid increase in global vehicle usage has significantly contributed to environmental pollution through the emission of harmful exhaust gases. Major pollutants from internal combustion engines include carbon monoxide (CO), unburned hydrocarbons (HC), and nitrogen oxides (NOx), all of which pose serious risks to human health and the environment (1). Governments worldwide have introduced regulations aimed at reducing automotive emissions and promoting environmentally friendly vehicles. These standards differ across countries based on policy readiness and infrastructure support (1). Life cycle studies show that emissions and fuel consumption from internal combustion engines significantly affect environmental load, with mileage and maintenance practices being key influencing factors (1). Nowadays, automotive manufacturers use platinum-group metals (PGM) or precious metals such as Platinum (Pt), Ruthenium (Rt), Rhodium (Rh), and Palladium (Pd) as catalysts, where these metals have specific activities and higher ability than other types of metals [2]. However, the weakness in the use of this type of precious metal is the cost required is quite expensive to manufacture [2]. Also, exhausts equipped with catalytic converters with valuable metal materials are generally designed to be built up or cannot be assembled. Catalytic converters are emission control devices installed in the exhaust systems of internal combustion engine vehicles. Their primary function is to convert harmful pollutants present in exhaust gases into less harmful substances through catalytic chemical reactions (3). To mitigate these emissions, catalytic converters have been widely adopted as a standard emission control technology. Among these, the three-way catalytic converter (TWC) is particularly effective due to its ability to simultaneously oxidize CO and HC while reducing NOx under near-stoichiometric air–fuel conditions. Despite substantial progress in catalytic converter technology, several challenges remain. These include high dependence on expensive noble metals such as platinum (Pt), palladium (Pd), and rhodium (Rh), catalyst deactivation over time, and reduced efficiency during cold-start conditions. Additionally, there is limited research on cost-effective catalyst alternatives suitable for developing countries (3). The majority of automobile catalytic converters have a design of a monolithic structure, which is coated with an alumina wash-coat. The monolithic structure is referred to as the core of the catalytic converter, where the core is typically a ceramic monolith with a honeycomb configuration (4). Catalytic converters use metallic catalysts to promote the desired reactions at lower temperatures. Common metal catalysts used could be a base metal (such as chromium) and noble metals, such as platinum, palladium, and rhodium (4). In Indonesia, the level of pollutant air in the atmosphere has reached alarming levels. Many factors influence the enhancement of this air pollution, one of them being the high exhaust emissions produced by motorized vehicles, especially in urban areas (5). The organization (WHO) has stated that polluted air is one of the risk environments to health, and more than 80% of the population is the most vulnerable. Pollution in the air is closely related to diseases that are not infectious, including cardiovascular disease, chronic respiratory disease, and lung cancer. In Jakarta, disease No infectious accounted for 79% (36,000 deaths) of total deaths in 2019(5). A catalytic converter initiates oxidation and reduction processes to the CO, HC and NOX. and reduces the level of emission. Catalytic converter includes substrates, catalyst and heat insulation material (6). An exhaust system is a gadget used to decrease the poisonous quality of discharges from an inner burning motor. Exhaust systems, fit in arrangement with the fumes pipe of gas-powered vehicles, nitrogen and water vapor, since exhaust systems were first fit to autos in 1974. The minimization of fuel utilization and the decrease of emanations have been two main thrusts for motor improvement all through the most recent decades (7). The useful life of the catalytic converters is up to 36 months, so they should be replaced at least every three years (8). Seventy percent of pollutants discharged into the atmosphere come from motor vehicles. Fuel systems' evaporation process poses a risk to human health and the environment, mainly because it releases harmful substances such lead dust particles, hydrocarbons, oxides of nitrogen (NOx), Sulphur dioxide, and carbon monoxide (CO) (9). The search for alternative fuels which are eco-friendly and can be used as a substitute to conventional HC based fuels is in demand due to concerns about depletion of fossil fuel reserves (10). Exhaust emissions are the remaining results of fuel combustion in internal combustion engines, the formation of vehicle exhaust emissions when the engine is running due to imperfect combustion caused by insufficient or excessive air and fuel mixture conditions (11). A catalytic converter is a device installed on the exhaust pipe that functions to reduce gas emissions from incomplete fuel combustion so that when the gas exits the exhaust pipe the level of exhaust gas emissions is reduced, to reduce exhaust gas emissions, a copper catalytic converter is used, apart from being more affordable, it can also be used as an oxidation catalyst and reducing catalyst to reduce the concentration of CO and HC in exhaust gas(12). To meet ever more stringent government legislation imposed on automotive tailpipe emissions, after-treatment technology has become increasingly sophisticated (13). Catalytic converters generally consist of a chemical wrapped in a metal casing specially designed to direct the exhaust gas flow towards a metal catalyst. Developing catalytic converters without using precious metal materials to reduce exhaust emissions of carbon monoxide (CO) in internal combustion engines is a difficult challenge (14). Catalytic converters are mounted in the exhaust method of all ICE (internal combustion engine) of vehicles, especially buses, trains, generators, and trucks. A catalytic converter fitted to the exhaust method is found in nearly all ICE vehicles. Using basic redox processes, a catalytic converter is a minimalist gadget that lowers the amount of pollution that cars release (15). The catalytic converter has been in use for the past 30 years as an efficient and economical solution for the reduction of pollutants emitted by the internal combustion engine, the latter being the powertrain for almost all vehicles in use today. The primary objective of the automotive industry is to build cost-effective exhaust lines that will enable the vehicle to succeed in the legislated driving cycle tests (16). In gasoline engine applications, the toxicity of exhaust emissions is reduced by employing catalytic converters as an afterburning reactor. The catalytic converter is usually a multiple-channel reactor with a honeycomb structure. The catalytic combustion reactions occur in a thin wash-coat of a catalyst on the reactor wall (17). The environmental concern originated by mobile sources is due to the fact that the majority of engines employ combustion of fuels derived from crude oil as a source of energy. Burning of hydrocarbon (HC) ideally leads to the formation of water and carbon dioxide, however, due to non-perfect combustion control and the high temperatures reached in the combustion chamber, the exhaust contains significant amounts of pollutants which need to be transformed into harmless compounds (18). 

2.0 Problem statement
                The use of fossil fuels in the transport sector has increased the greenhouse gas emissions during the last decades. Fossil transport fuels such gasoline or diesel release exhaust gases composed by carbon dioxide, methane, nitrous oxide, carbon monoxide and hydrofluorocarbons. Indeed, the greenhouse gas from the transport sector amounts 28% of the total US emissions. This percentage is lower (19.4%) for European Union, but still important. The reduction of these emissions is a big challenge for breaking the climate change cycle (4). According to the United Nations Economic Commission for Africa, transport contributes about 42% of fuel-combustion greenhouse gas emissions in Africa, with road transport accounting for approximately 50% of transport emissions in the environment.
3.0 Literature review 
                                 Three-way catalytic converters (TWCs) have become one of the most important technologies for automotive exhaust emission control because of their capability to simultaneously reduce carbon monoxide (CO), hydrocarbons (HC), and nitrogen oxides (NOx). Their effectiveness depends on catalyst composition, structural design, operating temperature, and durability throughout the vehicle lifespan. Recent studies have focused on improving catalyst performance, reducing cost, enhancing thermal efficiency, and addressing operational limitations such as catalyst degradation and cold-start emissions. Basri et al. (2025) investigated catalytic converter degradation in relation to emission reduction performance under varying mileage, engine capacity, and transmission conditions. Their study revealed that catalytic efficiency decreases significantly with increasing operational lifespan. Nitrogen oxide reduction exhibited the highest degradation factor, while some converter types showed relatively stable performance for CO and THC reduction. The study emphasized that catalyst material composition strongly influences converter degradation characteristics and highlighted the importance of maintaining catalyst effectiveness throughout the vehicle life cycle(1). Ariyanto et al. (2025) conducted a comparative literature review on transition metallic catalytic converters and platinum group metal (PGM) catalysts. The authors reported that conventional PGM catalysts achieve extremely high conversion efficiencies exceeding 95% for CO and HC reduction. However, due to their high cost, alternative transition metals including copper, chromium, manganese, titanium dioxide, brass, and nickel have been explored. Among the investigated materials, manganese-coated copper catalysts demonstrated the highest reduction capability for CO and HC emissions(2). Although transition metals provide significant emission reduction and lower production costs, they still do not fully match the superior performance of PGM-based systems. Oluremi David (2025) highlighted the importance of catalytic converters in modern automotive emission control systems. The study explained that catalytic converters have substantially contributed to reducing harmful pollutants and improving air quality. The author further emphasized that future developments in automotive technologies, including hybrid and electric vehicles, will require advanced catalytic systems with improved efficiency, sustainability, and reduced cost. Continued collaboration among industries, researchers, and regulatory bodies was recommended for the development of next-generation catalytic technologies(3). Kritsanaviparkporn et al. (2021) provided a fundamental overview of TWC technology and identified the major components of the converter system, including the honeycomb substrate, wash-coat, and catalyst support layer. Cordierite was identified as the most commonly used substrate material, while alumina-based wash-coats and platinum group metals were reported as the predominant catalyst materials. The study demonstrated that TWCs can achieve conversion efficiencies between 90% and 99.9% under optimal operating temperatures. The authors further highlighted future challenges associated with stricter environmental regulations and cold-start emission reduction requirements)(4). Sundar (2025) examined cold-start emission reduction through the application of electric heater-assisted catalytic converters. The findings showed that integrating a heating element significantly reduced emissions during the initial engine operation period by accelerating catalyst light-off temperature attainment. The system reduced CO emissions substantially and improved gas flow characteristics by lowering pressure drop. The study concluded that heater-assisted converters represent an effective strategy for addressing one of the most challenging aspects of catalytic converter operation, namely cold-start emissions(5). 
                           Patel et al. (2022) reviewed the use of non-noble catalysts for automotive emission reduction and reported that these materials offer advantages related to low cost and structural stability. However, challenges associated with long-term durability and operational performance remain. The authors suggested that catalyst performance may be improved through noble metal doping and optimization of converter geometrical parameters such as diffuser angles, taper length, and flow characteristics(6). SengoleRayan et al. (2019) investigated fabricated three-way catalytic converters coated with silicon dioxide and aluminum oxide. Their study demonstrated significant reductions in NOx, CO, and HC emissions under varying engine load conditions. The findings indicate that alternative coating materials can effectively improve emission reduction performance and potentially provide lower-cost alternatives to conventional catalyst systems(7). Majidi-Jirandehi et al. (2021) studied catalytic converter lifespan and emission standards. Their results showed that catalytic converters effectively reduce CO and HC emissions but experience considerable performance decline after approximately three years of use. The study recommended periodic replacement of converters to maintain emission compliance and emphasized the importance of maintaining proper air-fuel ratio values for optimal converter performance(8). Wagino et al. (2024) explored the use of banana peel-based catalytic converter materials with biogasoline fuel. The findings showed measurable reductions in CO emissions and improved oxygen concentration levels. The study highlighted the potential of bio-based catalyst materials as environmentally friendly alternatives while emphasizing the need for further studies on durability and flow resistance characteristics(9). Ariyanto et al. (2025) evaluated alternative copper-based catalytic converter materials and observed superior CO and HC reduction performance compared with conventional exhaust systems. The study demonstrated that copper-based systems can provide stable emission reduction performance and may serve as viable low-cost alternatives for automotive applications(10). Kumar et al. (2013) investigated the combined application of exhaust gas recirculation and three-way catalytic converters in diesel engines. The authors found that integrating both technologies reduced NOx emissions effectively without significant reduction in thermal efficiency. The results suggest that combining emission control technologies can improve the overall performance of automotive exhaust treatment systems(11). 
                           McAtee et al. (2012) compared platinum, palladium-rhodium, and palladium catalysts under ethanol-containing exhaust conditions. The study demonstrated that catalyst composition significantly influences conversion behavior and pollutant selectivity. Although increased metal loading improved performance slightly, the benefits were relatively limited compared with cost implications(12). Kumar et al. (2013) further demonstrated the effectiveness of three-way catalytic converters in reducing NOx emissions in engines fueled with biodiesel blends. Rhodium-based catalysts were identified as contributing significantly to NOx reduction through oxygen storage and reduction mechanisms(13).  Warju et al. (2021) investigated brass-based catalytic converters and observed notable reductions in CO and HC emissions. Their findings indicate that brass-based catalysts may provide economically viable alternatives for emission control applications(14). Jena et al. (2025) reviewed environmental implications of catalytic converter technology and emphasized the importance of catalyst monitoring systems for maintaining converter efficiency and reducing pollutant emissions throughout operational life(15). Hilmi et al. (2025) investigated the effect of copper catalyst thickness on emission reduction and reported that catalyst geometry significantly influences catalytic performance. The study suggested that optimization of catalyst dimensions can enhance conversion efficiency while maintaining cost effectiveness(16).  Pontikakis et al (2004) presented modeling approaches for TWC design and optimization. The study demonstrated that advanced mathematical models can accurately predict converter performance and serve as essential engineering tools for designing high-efficiency, low-emission automotive catalytic systems developed and evaluated a modeling approach for three-way catalytic converters as an engineering design tool. Their findings demonstrated that advanced catalytic converter models can accurately predict CO, HC, and NOx emissions and are valuable for designing ultra-low-emission vehicles. The study concluded that modeling techniques provide indispensable support for the optimization of catalytic exhaust after-treatment systems.(17). Hilmi et al. (2025) investigated the effect of copper plate thickness in catalytic converters on hydrocarbon (HC) and carbon monoxide (CO) emissions using a Honda Vario 125 motorcycle. The study evaluated copper thicknesses of 0.2 mm, 0.5 mm, and 0.7 mm as alternative catalyst materials for exhaust emission reduction. The findings revealed that a copper thickness of 0.7 mm produced the greatest reduction in CO emissions, achieving an average value of 0.36% compared to 0.47% under standard conditions without a catalyst. Conversely, a thickness of 0.5 mm demonstrated superior HC reduction performance, reducing emissions to an average of 105 ppm compared to 131 ppm under standard conditions. The study further established that catalytic efficiency improved with increasing engine speed, particularly between 4000 and 7000 rpm, due to higher exhaust temperatures and increased gas residence time that enhanced oxidation reactions. Copper acted as an oxidation catalyst by facilitating oxygen adsorption and promoting the conversion of CO and HC into less harmful products such as CO₂ and H₂O. Despite these promising results, the researchers noted that inappropriate catalyst design could increase exhaust backpressure and adversely affect combustion efficiency. The study concluded that copper offers a cost-effective alternative to expensive platinum-based catalysts, especially for developing countries, although further studies are required to investigate broader thickness ranges and hybrid catalyst approaches(18).
                       Tempilis et al. (2019) examined mass and heat transfer coefficients within automotive exhaust catalytic converter channels, focusing on the transport phenomena governing catalytic converter performance. The study proposed mass and heat transfer correlations capable of accurately predicting coefficient profiles along monolith channel lengths using a two-dimensional computational fluid dynamics (CFD) model across various operating conditions and flow velocities. The proposed correlations demonstrated satisfactory performance across different reaction rates and channel diameters of 0.9 mm and 1.3 mm. The researchers observed deviations when comparing their findings with previously published correlations, particularly at the initial sections of the channel where mass transfer coefficients varied with channel length. These differences were attributed to assumptions involving constant wall flux and wall concentration conditions in earlier models. Furthermore, the developed one-dimensional plug flow reactor (PFR) model integrated with gas-solid mass and heat transfer effects successfully replicated the results of the more complex two-dimensional CFD model. The study highlighted the significance of heat and mass transfer mechanisms in determining catalytic converter effectiveness and provided predictive models that could assist in optimizing converter design and improving emission reduction efficiency. Kašpar et al. (2003) reviewed the development and future prospects of automotive catalytic converters, noting significant improvements in catalyst performance and durability over the previous decades. The study identified the introduction of CeO₂–ZrO₂ technology as a major advancement that enhanced the durability and oxygen storage capacity of three-way catalytic converters (TWCs). The authors emphasized that stricter emission regulations would require catalysts with greater thermal stability and higher conversion efficiency throughout a vehicle's lifespan. They also highlighted persistent challenges in NOx reduction under lean conditions and identified the NOx storage-reduction (NSR) concept as a promising approach. Furthermore, the study discussed the increasing need for diesel particulate emission control and suggested that future developments may shift toward preventive technologies such as hydrogen fuel-cell systems. Overall, the study concluded that material innovation and improved catalyst design are essential for meeting future emission control requirements(19).
                   Kašpar et al. (2003) examined the current status and future prospects of automotive catalytic converters. Their study highlighted the significant improvement in three-way catalyst (TWC) durability through the use of CeO₂–ZrO₂ technology. They emphasized the need for thermally stable materials capable of operating above 1100°C while maintaining high conversion efficiencies. The authors also identified challenges associated with NOx reduction under oxidizing conditions and suggested that future developments should focus on advanced catalytic materials and hydrogen fuel-cell technologies(20) Wilner et al. (2015) investigated the extraction of metals from spent automotive catalytic converters using a biometallurgical method. Their results showed that biological oxidation played a significant role in the recovery of iron and chromium, while aluminum recovery occurred mainly through chemical oxidation. The study demonstrated the potential of bioleaching as an environmentally friendly method for recycling catalytic converter materials(21). Kanchan (2016) explored the performance enhancement of three-way catalytic converters using an external heating source. Experimental results revealed that preheating the converter significantly improved the conversion efficiencies of CO, HC, and NOx during engine start-up conditions. The study confirmed that reducing catalyst warm-up time can substantially improve emission control performance(22). Kumar et al. (2017) reviewed three-way catalytic converter technologies and reported that TWCs remain the most effective solution for controlling CO, HC, and NOx emissions in stoichiometric engines. They further suggested that ferric oxide (Fe₂O₃) could serve as a potential catalyst for NOx reduction, although its effect on HC and CO reduction was comparatively limited(23). Abdolmaleki et al. (2019) compared fresh and aged automotive three-way catalysts under driving cycle conditions. Their findings showed that catalyst aging increases light-off temperature and reduces the conversion efficiencies of HC, CO, and especially NOx. The study attributed these performance losses to catalyst sintering, metal particle agglomeration, and changes in catalyst selectivity, highlighting the need for further research on catalyst degradation mechanisms(24). Desantes et al. (2020) evaluated the global warming impact and NOx emissions of conventional and hydrogen-powered vehicle technologies. Their life-cycle assessment revealed that hydrogen produced through steam methane reforming (SMR) with CO₂ sequestration offers the lowest greenhouse gas emissions among hydrogen production methods. The study concluded that fuel-cell vehicles could play a crucial role in future low-emission transportation systems, particularly when combined with cleaner hydrogen production technologies(25). Patel et al. (2022) reviewed the design and development of automotive catalytic converters using non-noble catalysts. They reported that non-noble catalysts possess robust crystal structures, lower costs, and good redox properties. The authors also emphasized the need for catalyst modification and geometric optimization of converter components to improve flow uniformity, reaction time, durability, and overall emission reduction performance(26). Misra et al. (2025) investigated air pollution control in diesel engines using a temperature-activated catalytic tube system. Their mathematical analysis indicated that the proposed technology could effectively reduce harmful SOx and NOx emissions. However, they recommended further research on material durability, prototype development, and field validation before large-scale implementation. Adebayo (2025) reviewed the role of catalytic converters in automobile exhaust gas purification. The study reaffirmed the importance of catalytic converters in reducing carbon monoxide, hydrocarbons, and nitrogen oxides, thereby improving air quality and public health. The author concluded that continued innovation in catalyst materials, durability, and integration with emerging vehicle technologies will be essential for meeting future emission regulations and sustainability goals (27).

4.0 Research Gaps and Challenges
Despite significant advancements in catalytic converter technology, several challenges still persist. The high cost of noble metal catalysts remains a major concern, as it increases the overall production cost of catalytic systems. In addition, catalytic converters often exhibit reduced efficiency during cold-start conditions because the catalyst requires sufficient temperature to achieve optimal performance. The limited durability of alternative catalyst materials also presents challenges in maintaining long-term effectiveness and stability. Furthermore, there is a lack of localized and cost-effective solutions specifically designed for developing economies. These challenges emphasize the need for continued research and the development of innovative, affordable, and efficient catalytic technologies. The reviewed studies have extensively investigated catalyst materials, catalyst aging, converter design optimization, performance enhancement, emission reduction, modeling techniques, and recycling approaches. However, there remains limited research on the development and performance evaluation of low-cost, locally sourced catalyst materials that can effectively replace expensive noble metals in three-way catalytic converters while maintaining high conversion efficiencies and long-term durability. This gap provides an opportunity for further investigation into alternative catalyst formulations for sustainable and cost-effective emission control systems(18-27).

5.0 Method 
This review is based on a systematic analysis of peer-reviewed literature obtained from databases including Scopus, ScienceDirect, ResearchGate and Google Scholar. Relevant publications from 2003 to 2025 were selected using keywords such as “three-way catalytic converter,” “automotive emissions,” “NOx reduction,” and “alternative catalyst materials.”
Studies were included based on:
· Relevance to catalytic converter performance 
· Experimental or simulation-based validation 
· Contribution to catalyst material development or emission reduction strategies 
The selected literature was critically analyzed to identify trends, limitations, and research gaps.
6.0 Key findings
6.1 Overview of Catalytic Converter Technology
6.1.1   Function and Working Principle
A catalytic converter is an emission control device that facilitates chemical reactions to convert toxic exhaust gases into less harmful substances. It is typically installed in the exhaust system between the engine and the muffler. The converter contains a honeycomb-structured substrate coated with catalyst materials that promote oxidation and reduction reactions without being consumed (4).
6.2 Types of Catalytic Converters
6.2.1 Two-Way Catalytic Converter
Two-way catalytic converters perform only oxidation reactions and are commonly used in diesel engines. Since diesel engines generate high levels of nitrogen oxides (NOₓ), additional emission control technologies such as Exhaust Gas Recirculation (EGR) and Selective Catalytic Reduction (SCR) are required for effective NOₓ reduction. In SCR systems, urea is injected and thermally decomposed to produce ammonia, which acts as the reducing agent for NOₓ removal. These catalysts convert CO into less harmful carbon dioxide (CO₂) and transform unburned hydrocarbons into CO₂ and water (H₂O). The catalytic process occurs as exhaust gases pass through substrates coated with precious metals such as platinum and palladium, which accelerate chemical reactions. The oxidation reactions generate significant heat, causing exhaust gases leaving the converter to have higher temperatures than incoming gases and necessitating the use of heat shields (4). Although two-way converters operate effectively under lean fuel conditions, they have limited capability for controlling nitrogen oxide emissions. A two-way catalytic converter performs oxidation reactions to convert:
· Carbon monoxide (CO) → Carbon dioxide (CO₂) 
· Hydrocarbons (HC) → Carbon dioxide (CO₂) and water (H₂O) 
However, it does not reduce nitrogen oxides (NOx), limiting its effectiveness.
6.2.2 Three-Way Catalytic Converter (TWC)
HC, NO, and CO make up the waste gases. As outlined earlier, the catalytic converter primarily decreases the release of initial hazardous gases to the minimal standard permitted by using catalyzed chemical processes. Thus, it's essential to carefully consider the layout of ICE before letting the gas out into its surroundings (2). The catalytic converter is a part of an automobile's exhaust system that reduces the quantity of pollutants in the vehicle's exhaust emissions (2). Another important component of a catalytic converter is the metal shell that encloses the catalyst core. This metallic casing directs and regulates the flow of exhaust gases through the catalyst bed while providing structural support and protection to the internal components. Stainless steel is commonly used for the catalytic converter housing because of its excellent resistance to corrosion and high temperatures, although lower-temperature catalyst systems may permit the use of alternative materials.
In summary, the three-way catalytic converter (TWC) controls vehicle emissions through simultaneous reduction and oxidation reactions. Specifically, it reduces nitrogen oxides (NOx) while oxidizing carbon monoxide (CO) and hydrocarbons (HC). In contrast, two-way catalytic converters primarily facilitate oxidation reactions for CO and HC and are therefore unable to effectively reduce NOx emissions. Consequently, TWCs offer improved emission control performance due to their ability to simultaneously address all three major pollutants (12-15).
The oxidation of hydrocarbons (HC) occurs when hydrocarbon compounds react with oxygen present in the exhaust gases, breaking the chemical bonds and producing carbon dioxide (CO₂) and water vapor (H₂O). An example involving the oxidation of benzene is represented as:
2C₆H₆ + 15O₂ → 12CO₂ + 6H₂O
Platinum and palladium are commonly used as catalysts for hydrocarbon oxidation because of their high catalytic activity. Palladium is often preferred in certain applications due to its improved thermal stability and resistance to catalyst deactivation under some operating conditions, thereby maintaining catalytic efficiency over extended use (15).
Similarly, carbon monoxide oxidation occurs through catalytic reactions facilitated by platinum or palladium. During this process, oxygen molecules are adsorbed onto the catalyst surface, where they dissociate into active oxygen species that react with carbon monoxide to form carbon dioxide:
2CO + O₂ → 2CO₂
Both platinum and palladium exhibit similar physical and chemical properties, making them effective catalysts for this oxidation reaction.
The reduction of nitrogen oxides (NOx) is typically facilitated by rhodium catalysts, which promote the conversion of NOx into nitrogen and oxygen gases. Rhodium is generally combined with platinum or palladium because of its high cost and limited availability (5-10). A simplified reduction reaction is represented as:
2NOx → xO₂ + N₂
The oxygen concentration in the exhaust gas is a critical parameter influencing these redox reactions. A lean operating condition occurs when excess oxygen is present in the exhaust stream relative to the stoichiometric requirement. Under such conditions, oxidation reactions involving HC and CO are favored, whereas NOx reduction becomes less effective due to the abundance of oxygen (4,15).
The three-way catalytic converter is widely used in modern gasoline engines due to its ability to simultaneously control three major pollutants:
· Oxidation of CO:
CO + ½O₂ → CO₂ 
· Oxidation of hydrocarbons:
CₓHᵧ + O₂ → CO₂ + H₂O 
· Reduction of NOx:
2NO → N₂ + O₂ 
The diagram below in fig.1 shows a well-labelled diagram of a three-way catalytic converter.
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                                                       Fig. 1 Three-Way Catalytic converter (TWC)
6.3 Air-Fuel Ratio
Air-Fuel Ratio (A/F Ratio) is the ratio of the mass of air to the mass of fuel supplied to an internal combustion engine during the combustion process.The performance of a three-way catalytic converter (TWC) is strongly influenced by the air-fuel (A/F) ratio of the engine(20).
· Under rich mixture conditions: The exhaust gas contains a higher concentration of carbon monoxide (CO) and a lower concentration of oxygen. These conditions favor the activity of the reduction catalyst, particularly rhodium (Rh), which effectively converts nitrogen oxides (NOₓ) into nitrogen gas (N₂). At the same time, the oxidation catalysts continue to function efficiently through the utilization of oxygen previously stored within the catalyst. This contributes to high overall conversion efficiency near the stoichiometric air-fuel ratio.

· Under lean mixture conditions: The exhaust contains excess oxygen and reduced carbon monoxide levels. These conditions enhance the performance of the oxidation catalysts, which convert carbon monoxide (CO) and unburned hydrocarbons (HC) into carbon dioxide (CO₂) and water vapor (H₂O). During this phase, the catalyst stores excess oxygen, which is subsequently released during rich operating conditions to support oxidation reactions. This oxygen storage capability enables the catalyst to maintain high conversion efficiencies despite fluctuations in the air-fuel ratio(18,19). Overall, the highest efficiency of a three-way catalytic converter is achieved within a narrow air-fuel ratio window around the stoichiometric point, where both oxidation and reduction reactions occur effectively. Figure 1.2 below shows the air fuel ratio for a three-way catalytic converter and the conversion percentage in the lean and rich regions.





[image: ]
                                 Fig 1.2 Air fuel ratio for a three-way catalytic converter adapted from(20)

6.4 Design of a catalytic converter Patel et al.,(2022)
                    Another important aspect of catalytic converter performance is its design parameters. Proper design is essential to provide sufficient residence time for exhaust gases to react effectively with the catalyst, thereby maximizing pollutant conversion efficiency. Pressure losses within a catalytic converter primarily occur at the inlet and outlet junctions of the monolith substrate. These losses are reflected in the total pressure difference experienced during the entry and exit of exhaust gases through the converter. Studies have also shown that velocity distribution within the monolith is not uniform, with higher velocities occurring near the center region and lower velocities away from the center. Although minor losses contribute to the overall pressure drop, their effect is relatively small compared to the major flow losses. Ivan Cornejo of the Department of Chemical and Materials Engineering, University of Alberta, investigated the influence of catalytic converter design parameters using a multi-region flow model. The study concluded that the multi-region model provides a more realistic representation of flow behavior than models assuming a single permeability throughout the monolith. The results revealed velocity peaks at the center and near the wall regions, while lower velocities were observed in other areas. However, the effects of angled flow entry were not fully considered, and further studies were recommended for alternative monolith cross-sectional geometries. The engineering design of a three-way catalytic converter (TWC) focuses on maximizing the conversion of harmful exhaust pollutants, including carbon monoxide (CO), hydrocarbons (HC), and nitrogen oxides (NOₓ), into less harmful products such as carbon dioxide (CO₂), water vapor (H₂O), and nitrogen gas (N₂). The effectiveness of the converter depends on several design factors, including catalyst composition, substrate geometry, flow distribution, thermal management, pressure drop, and durability.  A typical TWC consists of a stainless-steel casing that houses a ceramic or metallic honeycomb substrate coated with a wash-coat containing catalyst materials. The washcoat, commonly made of alumina and ceria-zirconia compounds, provides a large surface area for the deposition of active catalytic metals such as platinum (Pt), palladium (Pd), and rhodium (Rh).
The honeycomb substrate is designed to maximize catalyst surface area while minimizing exhaust flow resistance. Parameters such as cell density, wall thickness, substrate length, and diameter are optimized to ensure sufficient contact time between exhaust gases and the catalyst. Uniform flow distribution is achieved through the proper design of inlet diffusers, outlet cones, and transition sections, often with the aid of Computational Fluid Dynamics (CFD) analysis.
Thermal performance is another critical consideration, as catalytic reactions become effective only after the catalyst reaches its light-off temperature. Therefore, the converter must be capable of rapid warm-up while maintaining stability under high operating temperatures. In addition, materials used in the catalyst and substrate must resist thermal degradation, poisoning, and mechanical wear to ensure long-term performance.
Recent developments in catalytic converter design have focused on reducing reliance on expensive noble metals by exploring alternative catalyst materials, improved substrate structures, and optimized flow configurations. These innovations aim to enhance emission control efficiency, reduce production costs, and meet increasingly stringent environmental regulations.

                       
6.5 Structure and components of Three-Way Catalytic Converters

· Substrate (Monolith Structure)
The substrate is the structural core of a catalytic converter that supports the wash-coat and catalyst materials. It is one of the most important components of the converter because it provides the physical surface through which exhaust gases flow and where catalytic reactions take place (4,15). The substrate is usually designed in a honeycomb structure containing numerous small channels. This design provides a very large surface area while allowing exhaust gases to pass through with minimal flow resistance or back-pressure. The substrate is typically made of ceramic materials such as cordierite, designed in a honeycomb structure to provide a large surface area and low flow resistance. Inside a catalytic converter, the substrate is located between the outer metal shell and the wash-coat layer. This is the internal structure that supports the catalyst materials. It is usually made of ceramic or metal and has a honeycomb shape to provide a large surface area for exhaust gases to flow through efficiently (15). 
· Catalyst Materials
Material can be said as a catalyst metal and can be used as a catalytic converter if it can provide a reduction and oxidation reaction to a dangerous gas produced by combustion in the cylinder. Hazardous gases coming out of the exhaust tip must be converted to harmless gases so that they do not cause adverse effects when inhaled by humans (1-4). The oxidation process theoretically occurs when carbon monoxide (CO) gas passes through the oxidation catalyst. During this process, CO reacts with oxygen supplied by metal oxides such as copper oxide, resulting in the formation of carbon dioxide (CO₂). A similar mechanism applies to hydrocarbon (HC) emissions. As HC gases pass through the oxidation catalyst, they react with oxygen from the metal oxide surface, leading to oxidation reactions that produce carbon dioxide (CO₂) and water (H₂O). Various catalyst materials have been identified as effective for promoting the oxidation of CO and HC emissions into CO₂ and H₂O. These include precious metals such as platinum and palladium, as well as non-precious metals and their oxides, including manganese, copper, chromium, nickel, iron, vanadium, and cobalt(13-15).
The active catalytic layer consists of noble metals:
· Platinum (Pt) – oxidation reactions 
· Palladium (Pd) – oxidation reactions 
· Rhodium (Rh) – NOx reduction 
Although highly effective, these materials are expensive and susceptible to deactivation.
· Wash coat
The wash-coat is a very important component of a catalytic converter because it provides the surface on which the catalytic reactions occur. It is a thin layer of porous material coated onto the surface of the catalyst substrate, usually the honeycomb ceramic or metallic monolith inside the converter. The wash-coat is a porous layer coated onto the substrate. It increases the surface area available for catalytic reactions and helps hold the catalyst materials firmly on the substrate. Common wash-coat materials include alumina, ceria, and zirconia.  The primary purpose of the wash-coat is to increase the effective surface area available for catalyst deposition and exhaust gas reactions. Without the wash-coat, the surface area of the substrate would be too small to support efficient catalytic activity. A porous layer, typically made of aluminum oxide (Al₂O₃), increases surface area and enhances catalyst dispersion.
· Casing and Insulation
The converter is enclosed in a stainless-steel casing with thermal insulation to withstand high temperatures and mechanical stresses. A thin-walled metal casing is desired; this can allow better heat transfer to the surrounding to prevent converter from reaching temperature of up to 1000°C. The designer of a three-way catalytic converter should take the thermal expansion differences and yield strength of various materials into consideration (4,15).
· Catalytic Converter Housing
This is the stainless-steel outer shell that encloses and protects the internal components from heat, vibration, and mechanical damage (15). 

· Insulation/Mat Layer
A heat-resistant mat is placed between the substrate and the housing. It holds the substrate firmly in place and provides thermal insulation. 
· Oxygen Sensors (Lambda Sensors)
These sensors are usually installed before and after the catalytic converter. They monitor the oxygen content in the exhaust gases and help maintain the correct air–fuel ratio for efficient catalytic operation. 


· Inlet and Outlet Pipes
These pipes allow exhaust gases to enter and leave the catalytic converter during operation
6.6 Performance Factors Affecting Catalytic Converters
· Temperature (Light-off Characteristics)
The temperature light-off characteristic is one of the most important performance parameters of a catalytic converter. It describes the temperature at which the catalyst becomes sufficiently active to efficiently convert harmful exhaust pollutants into less harmful substances (4). The term “light-off temperature” refers to the minimum temperature at which the catalytic converter achieves approximately 50% conversion efficiency for pollutants such as: Carbon monoxide (CO), Unburned hydrocarbons (HC), Nitrogen oxides (NOₓ) 
Before reaching this temperature, the catalytic reactions occur very slowly, and the converter cannot effectively reduce exhaust emissions. Catalytic converters require a minimum temperature (≈250–300°C) to become effective. Cold-start conditions significantly reduce efficiency. 
· Thermal Sintering in Three-Way Catalytic Converters (TWC)
           Thermal sintering is one of the major causes of performance deterioration in a three-way catalytic converter. It occurs when the converter is exposed to excessively high temperatures, usually above 800–1000°C, during engine operation. These temperatures may result from engine misfire, rich fuel mixtures, incomplete combustion, or prolonged high-load driving conditions (3).  In a TWC, noble metal catalysts such as platinum (Pt), palladium (Pd), and rhodium (Rh) are finely dispersed on a porous wash-coat, commonly made of alumina (Al₂O₃). During thermal sintering, these tiny catalyst particles agglomerate and grow into larger particles due to heat exposure. As the particle size increases, the active surface area available for catalytic reactions decreases significantly. The effects of thermal sintering include:
· Reduction in catalytic activity 
· Lower conversion efficiency of CO, HC, and NOₓ 
· Increased light-off temperature 
· Reduced oxygen storage capacity of ceria-based materials 
· Permanent loss of catalyst effectiveness 
Thermal sintering also affects the wash-coat structure by collapsing its pores, thereby reducing the surface area required for effective gas–solid reactions.
· Poisoning in Three-Way Catalytic Converters
Catalyst poisoning refers to the deactivation of catalytic materials due to contamination by unwanted chemical substances present in fuel, lubricating oil, or exhaust gases. These contaminants chemically bond to the active catalyst sites and block them from participating in oxidation and reduction reactions. Common catalyst poisons include:
· Sulfur compounds 
· Lead 
· Phosphorus 
· Zinc 
· Silicon compounds 
Lead poisoning was historically a major problem before unleaded gasoline became standard. Even very small amounts of lead can permanently deactivate platinum-group metals by covering their active surfaces (3). Sulfur poisoning occurs when sulfur in fuel forms sulfur oxides (SOₓ) during combustion. These compounds adsorb onto catalyst surfaces and reduce their ability to convert pollutants. Phosphorus and zinc, often originating from engine oil additives, can accumulate on the wash-coat and block catalyst pores.
The major effects of poisoning are:
· Reduced catalytic conversion efficiency 
· Slower oxidation and reduction reactions 
· Increased exhaust emissions 
· Shortened catalyst lifespan 
· Reduced oxygen storage performance 
Some poisoning effects, such as sulfur poisoning, may be partially reversible at high operating temperatures, while others, such as lead poisoning, are generally permanent.
· Thermal Degradation in Three-Way Catalytic Converters
Thermal degradation is the gradual deterioration of the physical and chemical properties of catalytic converter materials due to long-term exposure to elevated temperatures. It is broader than thermal sintering because it includes structural damage to the catalyst substrate, wash-coat, and support materials (3). Continuous thermal cycling during engine operation causes repeated expansion and contraction of the converter materials. Over time, this leads to:
· Cracking of the ceramic substrate 
· Wash-coat detachment 
· Loss of mechanical strength 
· Melting or collapse of honeycomb structures 
· Decrease in catalyst dispersion 
At extremely high temperatures, the ceramic monolith may melt or become mechanically damaged, resulting in blockage of exhaust flow and increased engine backpressure. Thermal degradation also accelerates: Noble metal migration, Phase transformation of alumina wash-coat , Reduction in surface area, Decline in oxygen storage capacity. The consequences include poor emission control performance, reduced fuel efficiency, engine performance issues, and eventual catalytic converter failure.
6.7       Relationship Between Thermal Sintering, Poisoning, and Thermal Degradation
These degradation mechanisms are closely related and often occur simultaneously in practical engine conditions 
· Thermal sintering mainly affects catalyst particle size and active surface area. 
· Poisoning chemically blocks active catalytic sites. 
· Thermal degradation affects the overall structural integrity and durability of the converter system. 
Together, they reduce the efficiency of the three-way catalytic converter in converting harmful gases such as carbon monoxide (CO), hydrocarbons (HC), and nitrogen oxides (NOₓ) into less harmful products like carbon dioxide (CO₂), nitrogen (N₂), and water vapor (H₂O).

6.8 Mitigation Strategies to reduce degradation effects
Several approaches are used to reduce these degradation effects:
· Use of thermally stable wash-coat materials such as ceria-zirconia 
· Improved engine control systems to prevent overheating 
· Use of low-sulfur and unleaded fuels 
· Optimization of air–fuel ratio near stoichiometric conditions 
· Development of durable catalyst support materials 
· Proper engine maintenance to avoid oil leakage and misfire 
These strategies help improve the durability, efficiency, and lifespan of three-way catalytic converters in automotive emission control systems.
6.9    Cold Start Inefficiency in Catalytic Converters
Cold start inefficiency is one of the most significant challenges affecting the performance of automotive catalytic converters, especially three-way catalytic converters (TWCs). It occurs during the initial engine startup period when the catalytic converter has not yet reached its effective operating temperature, commonly known as the “light-off temperature.” A catalytic converter functions efficiently only when it becomes sufficiently hot, typically between 250°C and 400°C depending on the catalyst material and converter design. During engine startup, especially after the vehicle has been parked for several hours, both the engine and catalytic converter are cold. At this stage, the catalyst surface lacks enough thermal energy to promote the oxidation and reduction reactions needed for emission control (4,5). As a result, harmful pollutants produced immediately after ignition pass through the exhaust system largely untreated. Studies have shown that a significant percentage of total vehicle emissions are generated during the cold-start phase.

7.0 Catalyst ageing 
Catalyst aging refers to the gradual loss of catalytic activity over time and is a critical factor affecting the performance of three-way catalytic converters (TWCs). Catalyst deactivation occurs when changes in the catalyst's structure and chemical state lead to the loss of active sites on its surface, resulting in reduced catalytic efficiency. The causes of catalyst deactivation are generally classified into three main categories: chemical, thermal, and mechanical degradation. Although significant progress has been achieved in reducing vehicle emissions through the widespread application of three-way catalytic converters, improvements in real-world driving emissions have been considerably less pronounced than those observed under legislative test conditions. The factors influencing real-world emissions can be categorized into three major groups. The first category comprises engine-out (pre-catalyst) emissions under both steady-state and transient engine operating conditions, particularly during cold-start and warm-up periods. The second category relates to the conversion efficiency of fresh and aged three-way catalytic converters during steady-state engine operation. The third category concerns the performance of fresh and aged catalytic converters under transient engine operating conditions, which more closely represent actual driving situations. Catalyst age with prolonged usage(24). It is recommended that catalytic converters should be replaced every three years.

8.0 Importance of exhaust emission control using three-way catalytic converter to scientific community
Three-way catalytic converters (TWCs) have significantly advanced materials science through extensive research on the optimal combination of precious metals such as platinum, palladium, and rhodium. Their development also stimulated innovations in surface area engineering, leading to the creation of highly porous ceramic honeycomb substrates that maximize contact between exhaust gases and catalytic surfaces. Furthermore, the demanding operating conditions of vehicle exhaust systems necessitated the development of thermally stable wash-coats, such as aluminum oxide, capable of withstanding extreme temperatures while maintaining catalytic performance.
TWCs have also contributed greatly to the advancement of chemical kinetics by demonstrating that reduction and oxidation reactions can occur simultaneously within a single catalytic system. While nitrogen oxides are reduced to harmless nitrogen, carbon monoxide and unburned hydrocarbons are oxidized into less harmful products at the same time. In addition, TWCs introduced the application of cerium-based oxides for oxygen storage and release, enabling efficient catalyst operation under varying engine conditions. They have also provided valuable insights into oscillation chemistry by revealing how catalysts respond to rapidly alternating rich and lean air-fuel mixtures.
Beyond catalyst development, TWCs have become an important foundation for atmospheric and climate-related studies. They provide reliable baseline data on pollutant emissions from modern internal combustion engines, helping scientists assess the effectiveness of emission control technologies. This information supports atmospheric chemistry models that evaluate the impact of reduced vehicle emissions on urban smog formation and ozone concentrations. Moreover, the cleaner air resulting from TWC implementation has enabled medical researchers to establish stronger correlations between reduced pollution levels and lower incidences of respiratory diseases.
The scientific knowledge gained from TWCs has also influenced the development of alternative energy and industrial emission control technologies. The understanding of surface chemistry and catalytic reactions acquired through TWC research has contributed directly to the advancement of hydrogen fuel cell systems. Similarly, catalytic converter principles have been adapted for use in industrial scrubbers, which are employed to reduce harmful emissions from factory smokestacks and power generation facilities. These applications highlight the broader impact of TWC technology beyond the automotive sector.
9.0 Importance of exhaust emission control to the environment
Three-way catalytic converters (TWCs) are among the most effective technologies for reducing hazardous tailpipe emissions, preventing billions of tons of toxic pollutants from being released into the environment. They play a vital role in mitigating acid rain by converting nitrogen oxides (NOₓ) into harmless nitrogen gas, thereby reducing the formation of nitric acid in rainfall. This helps protect ecosystems, preserves the health of forests by preventing the loss of essential soil nutrients, and safeguards aquatic life by reducing the acidification of lakes, rivers, and streams.
TWCs also contribute significantly to the reduction of ground-level smog by oxidizing unburned hydrocarbons into carbon dioxide and water vapor. By reducing both hydrocarbons and nitrogen oxides, they limit the chemical reactions responsible for the formation of urban smog and ground-level ozone. As a result, air visibility is improved, and the occurrence of the dense brown haze commonly associated with heavily populated cities is reduced. Lower ozone concentrations also help protect vegetation by minimizing damage to crops, forests, and other plant life.
In addition, TWCs enhance air quality and public health by converting highly toxic carbon monoxide (CO) into the less harmful carbon dioxide (CO₂). The reduction of harmful pollutants in the atmosphere decreases exposure to respiratory irritants, contributing to lower rates of asthma attacks and other respiratory illnesses. Cleaner air also benefits wildlife, particularly animals living in urban environments, by reducing the risk of chronic respiratory damage.
Furthermore, TWCs contribute to climate protection by limiting the release of nitrous oxide (N₂O), a potent greenhouse gas with a global warming potential significantly higher than that of carbon dioxide. By reducing smog-forming pollutants and particulate matter, they also help lessen the urban heat island effect, contributing to a more balanced urban climate and a healthier environment

10.0 Suggestions and Future Scope
         Recent studies have explored various approaches to improve the performance of catalytic converters. Alternative catalyst materials such as copper, nickel, and metal oxides have been investigated as low-cost substitutes for noble metals; however, concerns regarding their long-term durability remain. In efforts to reduce cold-start emissions, electrically heated catalytic converters have demonstrated significant improvements, achieving up to a 40% reduction in carbon monoxide (CO) emissions during the initial stages of engine operation. Furthermore, catalyst monitoring systems that utilize sensor-based technologies have been developed to enhance maintenance practices and improve performance tracking. Structural optimization has also received considerable attention, with advancements in monolith design contributing to improved exhaust gas flow distribution and increased reaction efficiency. Despite these promising developments, balancing cost, catalytic efficiency, and durability continues to present a major challenge in catalytic converter technology (19).
                       Hybrid vehicles require catalytic converters because their internal combustion engines or range extenders still produce harmful emissions that must be controlled. Catalytic converters help reduce pollutants such as carbon monoxide (CO), hydrocarbons (HC), and nitrogen oxides (NOx), ensuring compliance with environmental regulations. Current research focuses on reducing dependence on expensive platinum group metals through the development of non-precious metal catalysts such as iron, cobalt, and nickel, alongside nanotechnology-based materials with enhanced catalytic performance(3,4). Recycling catalytic converters has also become increasingly important due to the high value and limited availability of precious metals such as platinum, palladium, and rhodium. Recent advancements in catalytic converter technology have focused on improving performance, reducing costs, and enhancing durability. Researchers are exploring nanostructured catalysts with higher surface areas and improved metal dispersion, which provide greater catalytic activity and resistance to poisoning. In addition, transition metal oxides and other non-precious metal catalysts are being investigated as cost-effective alternatives to platinum-group metals, helping to address supply limitations while maintaining high conversion efficiencies. Significant progress has also been made in substrate design. Metallic substrates are increasingly being adopted because of their superior thermal conductivity, faster heat-up rates, and greater mechanical strength compared to conventional ceramic substrates. Furthermore, innovative substrate geometries and improved wash-coat formulations have been developed to increase catalyst surface area, reduce pressure losses, and improve catalyst durability under severe operating conditions.
                    Beyond conventional catalytic converters, alternative emission-control technologies are gaining prominence. Selective Catalytic Reduction (SCR) systems and Lean NOₓ Traps (LNTs) are being continuously improved for more effective nitrogen oxide reduction. Other complementary technologies, such as exhaust gas recirculation (EGR), advanced onboard diagnostics, and cleaner fuel formulations, further contribute to emission reduction. Emerging approaches, including plasma-assisted catalysis and photocatalysis, also show considerable potential for improving exhaust treatment efficiency, particularly at lower operating temperatures. These innovations are expected to play a vital role in the future of sustainable and efficient vehicle emission control systems(19).
11.0 Conclusion
Overall, the reviewed studies indicate that while conventional platinum group metal-based Three-Way Catalytic Converters continue to exhibit superior performance, increasing attention has been directed toward alternative catalyst materials, improved thermal management systems, optimized geometries, and advanced modeling approaches. Major challenges remain in reducing catalyst cost, improving cold-start performance, minimizing degradation, and increasing long-term durability while satisfying increasingly stringent environmental regulations. The reviewed studies also demonstrated that catalytic converter performance is influenced by multiple factors, including material composition, operating temperature, exhaust flow dynamics, and aging. While three-way catalytic converters remain the dominant technology, challenges such as cold-start emissions, catalyst degradation, and high material costs persist. Emerging solutions—such as alternative catalyst materials, integrated heating systems, and real-time monitoring technologies—offer promising pathways for improving efficiency and sustainability. However, further research is required to optimize these innovations for practical, cost-effective implementation, particularly in developing economies. Three-way catalytic converters remain the most effective technology for controlling automotive exhaust emissions. Their ability to simultaneously reduce CO, HC, and NOx has made them indispensable in modern vehicles. However, challenges related to catalyst cost, durability, and cold-start inefficiencies limit their overall performance. Advancements in alternative materials and system optimization are essential for improving efficiency and sustainability, particularly in developing regions. Continued research and innovation will play a critical role in achieving cleaner and more efficient automotive emission control systems.
[bookmark: _Hlk218868534][bookmark: _Hlk229240739]
[bookmark: _Hlk221624953]Disclaimer (Artificial intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript. 








References 
1.Basri, H., Nugroho, A. A. N., Pratiwi, A., Rhee, J. S., Adnan, F. A. F., & Ginting, D. (2025). assessing catalytic converter degradation in emission reduction: comparative study of co, thc, and nox across mileage, engine capacity, and transmission type. Borneo Science | The Journal of Science and Technology, 46(1). https://doi.org/10.51200/bsj.v46i1.5948

2.Rizki Ariyanto, S., Warju, W., Isnomo Abdi, F., Tri Umaroh, S., Sa’diyah Yuniar Arifianti, L., Setiya Widoretno, Y., & Syifa’ Nugraha, A. (2025). Catalyst conversion comparison efficiency from the use of transition metallic catalytic converters: A literature review. EPJ Web of Conferences, 344, 01013. https://doi.org/10.1051/epjconf/202534401013

3.David, O. (2025). Catalytic Converters for Automobile Exhaust Gas Purification.

4.Kritsanaviparkporn, E., Baena-Moreno, F. M., & Reina, T. R. (2021). Catalytic Converters for Vehicle Exhaust: Fundamental Aspects and Technology Overview for Newcomers to the Field. In Chemistry (Switzerland) (Vol. 3, Issue 2, pp. 630–646). MDPI. https://doi.org/10.3390/chemistry3020044

5. Sundar, N. B. B., Shreyaa, V. P., & Ravi, M. (2025). Cold Start Emission Reduction: A Simulation Study of with and without Electric Heater in a Catalytic Converter. https://doi.org/10.21203/rs.3.rs-7273272/v1

6. Patel, K. D., Subedar, D., & Patel, F. (2022). Design and development of automotive catalytic converter using non-nobel catalyst for the reduction of exhaust emission: A review. Materials Today: Proceedings, 57, 2465–2472. https://doi.org/10.1016/j.matpr.2022.03.350

7.Sengolerayan, A., Chakraborty, P., & Mandal, D. K. (2019). Design and fabrication of three-way catalytic converter by using Al2O3 and SiO2 coating as a catalyst and access of emission characteristics in C.I. engine. International Journal of Innovative Technology and Exploring Engineering, 8(12), 1136–1143. https://doi.org/10.35940/ijitee.L3887.1081219

8.Akbar Majidi-Jirandehi, A., Soleymani, M. M., & Dehghani, H. (2021). Determine the Useful Life of Catalytic Converter and Standard Revision of Technical Inspection Centers. Automotive Science and Engineering, 11(3), 3614–3619. https://doi.org/10.22068/ijae.11.3.3614

9.Wagino, W., Purwanto, W., Saputra, H. D., Putra, D. S., Indrawan, E., Rahim, B., & Koto, R. D. (2024). Eco-Friendly Motorcycle Technology: Examining the Impact of Banana Peel-Based Catalytic Converters on CO Emissions with Biogasoline Fuel. E3S Web of Conferences, 500. https://doi.org/10.1051/e3sconf/202450003030

10.Suresh Kumar, P., Bhatnagar, A., & Sahoo, P. K. (2013). Reduction 0f NOx Emissions with Three-Way Catalytic Converter For IDI Engine Fuelled With Diesel, JSVO and Their Blends. International Journal of Engineering Research & Technology (IJERT), 2(2). www.ijert.org

11.Ariyanto, S. R., Warju, W., Arifianti, L. S. Y., Komarudin, K., & Nugraha, A. S. (2025). Evaluating the Impact of Alternative Material-Based Catalytic Converters on Automotive Exhaust Emissions. Journal of Mechanical Engineering, Science, and Innovation, 5(1), 21–30. https://doi.org/10.31284/j.jmesi.2025.v5i1.7287

12.Suresh Kumar1, P., Donga2, R. K., & Sahoo3, P. K. (n.d.). Experimental Investigation on Combined Effect of EGR and Three-way Catalytic Converter for IDI Diesel Engine. International Journal of Engineering Science and Technology.

13.McAtee, C., McCullough, G., & Douglas, R. (2012). Performance and characteristics of platinum, palladium/rhodium and palladium automotive catalysts when subjected to ethanol, acetaldehyde and a synthetic E85 exhaust gas mixture. Proceedings of the Institution of Mechanical Engineers, Part D: Journal of Automobile Engineering, 226(11), 1536–1546. https://doi.org/10.1177/0954407012446911


14.Warju, W., Ariyanto, S. R., Nugraha, A. S., & Pratama, M. Y. (2021). The Effectiveness of the Brass Based Catalytic Converter to Reduce Exhaust Gas Emissions from Four-stroke Motorcycle Engines.

15. Jena, S., & Padhy, M. (2025). The Environment and Catalytic Converter-A Review. 7(1), 7. https://doi.org/10.33263/Materials71.007

16.Pontikakis, G. N., Konstantas, G. S., & Stamatelos, A. M. (2004). Three-way catalytic converter modeling as a modern engineering design tool. Journal of Engineering for Gas Turbines and Power, 126(4), 906–923. https://doi.org/10.1115/1.1787506


17.Templis, C. C., & Papayannakos, N. G. (2019). Mass and heat transfer coefficients in automotive exhaust catalytic converter channels. Catalysts, 9(6). https://doi.org/10.3390/catal9060507

18. Kašpar, J., Fornasiero, P., & Hickey, N. (2003). Automotive catalytic converters: current status and some perspectives. In Catalysis Today (Vol. 77).
Shen, H., Shamim, T., & Sengupta, S. (1999). An Investigation of Catalytic Converter Performances During Cold Starts.

19.Adebayo, Y. (2025). Catalytic Converters for Automobile Exhaust Gas Purification

20. Kumar, K., Kumar, N., & Singh, H. (2017). Comprehensive Review of Three-way Catalytic Converter (Vol. 3). www.ijariie.com1197


21.Akbar Majidi-Jirandehi, A., Soleymani, M. M., & Dehghani, H. (2021). Determine the Useful Life of Catalytic Converter and Standard Revision of Technical Inspection Centers. Automotive Science and Engineering, 11(3), 3614–3619. https://doi.org/10.22068/ijae.11.3.3614


22.Misra, S., David, S., & Devi, S. (2025). Optimizing Air Quality and Pollution Control in Diesel Engines: A Mathematical Perspective. In Int J Auto AI Mach Learn (Vol. 5, Issue 1).

23. Kanchan, S., Singh, M., & Singh, M. (2016). Performance enhancement of three-way catalytic converter using external heating source: An experimental approach. International Journal of Vehicle Structures and Systems, 8(3), 140–145. https://doi.org/10.4273/ijvss.8.3.04

24.Saeed A., Gholamhassan N., Barat G., Ali Z., Mohammad N.,(2019). Comparison of Aged and fresh Automotive Three-Way Catalyst in Driving Cycle. (n.d.). Proceedings of the 2nd National Conference on Internal Combustion Engines,Babol Noshiravni University of Technology, Babol, Iran.


25.Patel, K. D., Subedar, D., & Patel, F. (2022). Design and development of automotive catalytic converter using non-noble catalyst for the reduction of exhaust emission: A review. Materials Today: Proceedings, 57, 2465–2472. https://doi.org/10.1016/j.matpr.2022.03.350

26.Desantes, J. M., Molina, S., Novella, R., & Lopez-Juarez, M. (2020). Comparative global warming impact and NOX emissions of conventional and hydrogen automotive propulsion systems. Energy Conversion and Management, 221. https://doi.org/10.1016/j.enconman.2020.113137

27.Willner, J., Kaduková, J., Fornalczyk, A., Mrážiková, A., Marcinčáková, R., & Velgosová, O. (2015). Possibilities of metals extraction from spent metallic automotive catalytic converters by using biometallurgical method. Archives of Metallurgy and Materials, 60(3A), 1877–1880. https://doi.org/10.1515/amm-2015-0320







image1.png
Stainless Steel Outer Casing

Inlet / : Outlet
(Exhaust Gas) | : — : =R (Treated Gas)

Temperature
Sensor

S —— e e ey ]

Alternative Catalyst Coating (h;n, Cu, Perovskite)




image2.emf

