# Original Research Article

# OPTIMUM CONTACT TIME AND pH FOR BIOSORPTION OF METALS IONS USING TREATED WATERMELON RIND (WMR) AS BIOSORBENT.

Abstract

This research investigated watermelon rind (WMR) powder and biochar as a sustainable biosorbent for removal of selected heavy metals; Cu, Pb, Cd, Ni, and Zn in produced water. Watermelon rind samples were collected, pretreated and then transformed into biochar by charring, followed modification of their chars with the aim of obtaining a highly effective biosorbent. Samples of produced waters were analyzed using AAS (Atomic Absorption Spectrophotometer) instrument, before and after injection into the column and the influences of various pH as well as contact times were investigated. The outcome revealed that all the analyzed heavy metals gave positive indication at an optimum pH and contact times. The most optimum pH and contact times for most effective removal of (Zn2+, Pb2+ and Cu2+) ions in the produced water is 6.2 and contact time of 30  minutes when modified WMR biochar is used as biosorbent with  >99.0%, >99.0%, and 52.72% efficient removals respectively. Modified WMR biochar at pH of 6.2 and contact time of 60 minutes gave optimum removal of Cd2+ ions (>99.0%). Similarly, modified WMR biochar at pH of 6.2 and contact time of 180 minutes gave optimum removal of Ni2+ ions (73.04%).This research shows the advantage of utilizing modified WMR biochar as biosorbent over unmodified WMR powder owing to the presence of active sorption groups, higher surface area, higher porosities and carbonization. The result obtained suggests that watermelon rind biochar is a low-cost, efficient, ecofriendly and reusable sorbent capable of efficiently removing dissolved metals from produced waters before its safe release to the environment; and could also serve as a means to recycle an agricultural waste to wealth. Further increasing the contact time to higher times could lead to far higher Ni2+ removal from produced water.

Keywords: Biosorbent, WMR Powder, Produced water, Contact time, pH

- Introduction

Water contamination from heavy metals represents a growing environmental issue around the globe, with Nigeria's Rivers State also contributing greatly to the amount of poisonous metals in its surface water owing to lithogenic and anthropogenic activities such as discharging untreated industrial effluent, earthquakes, flooding, oil exploitation, and waste dumped in its water bodies. Elements of major significance are toxic heavy metals like Lead (Pb), Zinc (Zn), Copper (Cu), Cadmium (Cd) and Nickel (Ni) as a result of their toxicity, bioaccumulation and bioamplification potentials within food chains, and accumulation in aquatic ecosystems. Onyango et al., (2025); Iwuoha and Umofia (2017). These toxins, even in small quantities can result to toxic effect on humans and living organisms in water, air and soil environments, including neurological problems, loss of organs, and cancer in humans. World Health Organization, (2017); Iwuoha and Onojake (2016).

Globally, the largest volumes of wastewaters are produced during the oil and gas exploration and producing activities. These wastewaters, often termed produced waters, are unavoidable by-products that are co-produced with oil and gas from underground reservoirs. Produced water comprise of formation water, injected water, hydrocarbons dissolved/dispersed (in both free phase and emulsion form), inorganic salts, suspended solids, produced chemicals, naturally occurring radioactive materials (NORMs), microbes, and trace amounts of heavy metals (Fakhru'l-Razi et al. 2009; Igunnu and Chen 2014).

Produced Water production becomes significantly greater compared to oil production in aging oil reservoirs so produced water management is one of the most important environmental challenges faced by the petroleum sector. Annually in millions of barrels of produced waters have been produced and water/oil ratios generally increase as fields mature (Veil et al. 2004). Discharge of untreated or insufficiently treated produced waters to the environment poses a risk to aquatic life owing to the heterogeneity in its chemical composition. Produced water often contain concentrated loads of heavy metals like Pb2+, Cd2+, Ni2+, Cu2+, Zn2+, combined with several dissolved organics (hydrocarbons and production chemicals) and salinity which could negatively impact environmental and ecological values in aquatic environment, if discharged untreated (Neff et al. 2011; Jimnez et al. 2018). Heavy metals in particular are one of the most threatening contaminants commonly found in produced waters because of their stability, toxicity and inability to break down into non-harmful constituents through biological processes.

Current methods for heavy metal removal such as chemical precipitation, adsorption, membrane filtration, electrochemical processes etc usually require significant capital and labor and hence not very feasible in resource-constrained areas such as Nigeria (Ali et al., 2021). This is why research toward the development of low-cost and environmental friendly adsorbent and biosorbents from agricultural wastes and other environmentally alternatives for efficient removal heavy metals’ ions from aqueous solution are gaining momentum from prominent researchers like, Iwuoha and Nkanga (2024); Nkanga et al., (2024); Onojake et al., (2015); Onojake et al., (2021a); Onojake et al., (2021b); Osu et al., (2021) and Chikwe and Iwuoha (2024). In all, none have used raw or modified watermelon rind powders as biosorbent for removing heavy metals from produce water at optimum conditions.

Watermelon rind (Citrullus lanatus) which is a readily available food waste in Nigeria, particularly in Rivers State, has a high potential of being used as a natural adsorbents, because it is locally available, easily degraded by nature and contain some surface functional groups that are able to bond the contaminants to its surface. In solution, watermelon rind acts as a natural adsorbent based on the adsorption, ion exchange and complexation mechanism (Onyango et al., 2025). Watermelon rind is primarily made up of polysaccharides, cellulose, hemicellulose, pectic substances, also rich in some functional groups (-OH, -COOH, -C=O etc which react to metal ions (Adekemi et al., 2025).

In Rivers State, significant amounts of produced water with high concentrations of heavy metals (exceeding recommended levels) are generated in crude oil production. Untreated produced water represents a significant ecotoxicological risk to downstream and surrounding aquatic environments as well as public health. The use of physico-chemical treatment techniques like membrane filtration and chemical precipitation, in many cases, is impeded by factors such as: lack of sufficient capital to establish, high cost of operations and power inputs and the formation of secondary sludge which necessitates proper disposal (especially when there are issues of waste management in resource limited contexts). On the other hand, large quantity of watermelon rind is wasted due to high seasonal watermelon production, posing a solid waste disposal problem, owing to its low market value and disposal value.

This research aims at investigating into the suitability of untreated and treated watermelon rinds powders as biosorbent for the removal of certain heavy metals ions (Cd2+, Pb2+, Zn2+, Cu2+& Ni2+) from produced water. We examined produced water sample for percentage removal of some selected heavy metals. Study different pH as well as contact time (operating conditions) with known dosage concentration that favors removal of the metals ions. Evaluate and compare effect of pretreated watermelon rind in comparison with non pretreatment in its removal efficiency as well as correlate the results with various regulatory standards for maximum permissible level of heavy metal in produced water and make recommendations.

- Materials And Methods

## 2.1 Reagent and Materials

Recently picked watermelon fruits (Citrullus lanatus) (in season: Aug-Sep). - Distilled Water. - Nitric acid (HNO3) - Sodium hydroxide (NaOH) - Hydrochloric acid (HCl). - What man filter paper. - Burner - tripod - beaker.

Oven (105°C), Grinder and sieve (250 mesh sieving, 250 µm) Analytical balance, pH Meter, Mechanical shaker, Filtration system (14A Atomic absorption spectrophotometer; AAS), Sample collectors, Pilot-scale adsorption column [PVC; 1.5m length, 10 cm diameter], Flow rate controller and peristaltic pump, Polyethylene sample bottles (rinsed with 0.05mol·L⁻¹ HNO3).

2.2 Sample Collection and Map of Study Area

Produced water samples were collected from five (5) different oil drilling installations around the Bodo, Gokona L.G.A., in Rivers state mainly and other Niger Delta area of Nigeria. The samples were collected and stored in a clean glass container, which was furthermore put into a cooler to regulate the temperature, as it was transported for analysis to an analytical laboratory i.e the O.K. Research Laboratory, Cam estate besides Alikor Estate, opposite Choba campus main gate, Uniport. The fresh watermelons were collected in Choba main Market in Portharcourt Rivers State, Nigeria and washed with distilled water to remove residual sediments and Peeled to obtain the watermelon rind (WMR).

Figure 1: Map of study area

2.3 Pre-Analysis Preparation and Sample Analysis Procedure

The produced water was separated using a separating funnel to remove all crude oil in the sample before analysis. The WMR were air dried and ground to powdery form using the crusher. The WMR powder was then sieved to a mesh size of 1.18 mm. The sieved WMR powder were then stored in a plastic container for further use. A separating funnel was mounted on a retort stand and 200ml of the produced water was poured into the separating funnel. 20mls of hexane (an organic solvent) was poured in the separating funnel and the funnel was corked and shook vigorously while intermittently opening the lower end of the funnel to allow the removal of air bubbles. The produced water mixture was shaken and hexane was returned to the retort stand allowing it to settle for two (2) minutes, after which water was removed from the separating funnel leaving behind the hexane. A column was created using layers of glass wool, sodium sulphate anhydrous and silica gel and the separated mixture was then passed through the column into a clean glass beaker.

## 2.4 Chemical Activation

For higher loading 100g of the rind WMR powder, was steeped in 0.1 M NaOH solutions for 24hr and then filtered and washed up to neutral pH. It was oven dried at 800C. The activated WMR powdered biosorbent was kept in the desiccators.

2.5 Analysis for Biosorption Using Watermelon Rind (WMR) Powder on Pilot-Scale Adsorption Column Design

A The adsorption process (fixed bed continuous flow) uses a column to which PVC material with following details has been used for construction: Height of the column is 1.5 meters Inner diameter of the column is 10 cm .Thickness of bed is 40cm, and Flow rate to be adjusted in the range of 2-5 L/h. Contents of the columns used for absorption: Cotton Mesh layer, WMR powder adsorbents. The WMR powder was added to filter in bottom, with fine meshes in between not filter WMR powder. Watermelon powder WMR was placed in bed of 40cm thickness. Bed consists of; Support bed is coarse gravel, after that fine mesh separating water melon rinds, then water melon rind WMR powder. Retaining layer is a mesh on top of watermelon rind.

A setup was put in place where the separating funnel was mounted on a retort stand and below it, glass column chamber was also mounted to the stand, while a clean glass beaker was placed below the column chamber. The column chamber was filled with the WMR powder (biochar) and then the separating funnel was opened and the produced water was allowed to run through the chamber filled with WMR powder into a clean glass beaker below, where the filtrate was collected. This procedure was carried out for the entire produced water sample, and was repeated, varying the pH of the WMR powder chamber. The concentrations of each of the metals in the produced water were noted with AAS before and after injection in the column for the differences in concentrations of the respective metal in the produced water samples.

2.6 Analysis of Heavy Metals in Produced Water

About 100 cm3 of well mixed water samples were poured into a 150 cm3 beaker. 5cm3 of conc. HNO3 was added. The solution was later evaporated to near dryness on hot plate, making sure that the sample did not boil by using low to medium heat. The beaker and contents was allowed to cool to room temperature before adding another 5 cm3 conc. HNO3 into the beaker. The beaker was immediately covered afterwards with a watch glass. The beaker was returned to the hot plate and set a gently reflux action of the solution by increasing the temperature of the hot plate (medium to high heat). We continued heating with the addition of conc. HNO3 as necessary until light-coloured residue is obtained (i.e digestion is completed). 1-2 cm3 conc. HNO3 was added to the residue. Wash with distilled water. The solution was later filtered into 100 cm3 volumetric flask to remove silicate and other insoluble materials and made up to the mark with distilled water in the volumetric flask and  Stored in 125 cm3 polypropylene bottle. Lead (Pb), Cadmium (Cd), Copper (Cu) and Zinc (Zn) and Nickel (Ni). Analysis for the heavy metal is Atomic Absorption Spectrophotometer (AAS) with the following steps:

1. Calibration solutions were prepared. 2 .Blank sample were analyzed.

3. Digested sample into atomic absorption spectrophotometer. 4. Absorbance value was detected. 5. The concentration of metal was calculated using the calibration curves

## Adsorption Performance Evaluation

### Removal Efficiency(%)

Removal Efficiency = Co−Ce x 100%

Co

Where:		Co=Initial concentration(mg/L).	Cₑ = Final concentration (mg/L)

### Adsorption Capacity (qₑ);	qe=(Co−Ce)Vx100 M

Where: V=Volume of solution (mL)	, M = Mass of adsorbent (g)

- Results And Discussion

# Table 1. Effect of pH on the Biosorption of Cd2+ (mg/L) on the WMR after 30minutes of filtration down the column.

| # BIOSORBENT | # Initial Cd conc. # In mg/L | # Cd Conc. at # pH of 2.6 | # Cd Conc. at # pH of 6.2 | # Cd Conc. at # pH of 10.5 |
| --- | --- | --- | --- | --- |
| # WMR # (Unmodified) | # 1.550 | # 0.751 # * (51.55%) | # 0.035 # * (97.74%) | # 0.931 # * (39.94%) |
| # WMR BIOCHAR # (Modified) | # 1.550 | # 0.823 # * (46.90%) | # 0.018 # * (98.84%) | # 0.881 # * (43.16%) |

# *(%) Bioadsorption/Removal of Cd2+ ions by the Biosorbent

# In table 1, (above) at a contact time of 30 minutes, we can observe as following: At pH 2.6 (an acidic medium), the Cd2+ ions was remove from the sample of produced water by 51.55 percent from 1.55 mg/l of its initial concentration to 0.751 mg/L with the unmodified watermelon rind powder as a bio-sorbent. At same pH of 2.6 (an acidic medium) the Cd2+ ions in the produced water was reduced by 46.90 percent,  coming down to 0.823 mg/l from an initial concentration of 1.55 mg/l when the modified WMR (bio-char) was used as biosorbent. At pH value of 6.2, the Cd2+ ions were further reduced by 97.74 percent and 98.84 percent from the produced water when the unmodified WMR powder and modified WMR biochar biosorbents were used respectively. Reducing Cd2+ ions concentration from their initial concentration of 1.84 mg/l to 0.035 mg/l and 0.018 mg/l by the unmodified WMR powder and modified WMR biochar biosorbents respectively.

# At pH value of 10.5 (alkaline medium), the Cd2+ ions were reduced by only 39.94 percent and 43.16 percent from the produced water when the unmodified WMR powder and modified WMR biochar biosorbents were used respectively. Reducing it, from their initial concentration of 1.55 mg/l to 0.931 mg/l and 0.881mg/l by the unmodified WMR powder and modified WMR biochar biosorbents respectively.

Table 2. Effect of pH on the Biosorption of Ni2+ (mg/L) on the WMR after 30minutes of filtration down the column.

| # BIOSORBENT | # Initial Ni conc. # In mg/L | # Ni Conc. at # pH of 2.6 | # Ni Conc. at # pH of 6.2 | # Ni Conc. at # pH of 10.5 |
| --- | --- | --- | --- | --- |
| # WMR # (Unmodified) | # 2.04 | # 1.73 # *(15.20%) | # 1.14 # *(44.12%) | # 1.88 # *(7.84%) |
| # WMR BIOCHAR # (Modified) | # 2.04 | # 1.71 # *(16.17%) | # 0.98 # *(51.96%) | # 1.84 # *(9.80%) |

# *(%) Bioadsorption/Removal of Ni2+ ions by the Biosorbent

# In table 2, (above) at a contact time of 30 minutes, we can observe as following: At pH 2.6 (an acidic medium), the Ni2+ ions was remove from the sample of produced water by 15.20 percent from 2.04 mg/l  of its initial concentration to 1.73 mg/L with the unmodified watermelon rind powder as a bio-sorbent. At same pH of 2.6 (an acidic medium) the Ni2+ ions in the produced water was reduced by 16.17 percent, coming down to 1.71 mg/l from an initial concentration of 2.04 mg/l when the modified WMR (bio-char) was used as biosorbent. At pH value of 6.2, the Ni2+ ions were further reduced by 44.12 percent and 51.96 percent from the produced water when the unmodified WMR powder and modified WMR biochar biosorbents were used respectively. Reducing Ni2+ ions concentration from their initial concentration of 2.04 mg/l to 1.14 mg/l and 0.98 mg/l by the unmodified WMR powder and modified WMR biochar biosorbents respectively.

# At pH value of 10.5 (alkaline medium), the Ni2+ ions were reduced by only 7.84 percent and 9.8 percent from the produced water when the unmodified WMR powder and modified WMR biochar biosorbents were used respectively. Reducing it, from their initial concentration of 2.04 mg/l to 1.88 mg/l and 1.84 mg/l by the unmodified WMR powder and modified WMR biochar biosorbents respectively.

Table 3.  Effect of pH on the Biosorption of Pb2+ (mg/L) on the WMR after 30minutes of filtration down the column.

| # BIOSORBENT | # Initial Pb conc. # In mg/L | # Pb Conc. at # pH of 2.6 | # Pb Conc. at # pH of 6.2 | # Pb Conc. at # pH of 10.5 |
| --- | --- | --- | --- | --- |
| # WMR # (Unmodified) | # 0.036 | # 0.021 # * (41.67%) | # 0.013 # * (63.87%) | # 0.028 # * (22.22%) |
| # WMR BIOCHAR # (Modified) | # 0.036 | # 0.024 # * (33.33%) | # < 0.01 # * (>99.00%) | # 0.024 # * (33.33%) |

# *(%) Bioadsorption/Removal of Pb2+ ions by the Biosorbent

# In table 3, (above) at a contact time of 30 minutes, we can observe as following: At pH 2.6 (an acidic medium), the Pb2+ ions was remove from the sample of produced water by 41.67 percent from 0.036 mg/l of its initial concentration to 0.021 mg/L with the unmodified watermelon rind powder as a bio-sorbent. At same pH of 2.6 (an acidic medium) the Pb2+ ions in the produced water was reduced by 33.33 percent, coming down to 0.024 mg/l from an initial concentration of 0,036 mg/l when the modified WMR (bio-char) was used as biosorbent. At pH value of 6.2, the Pb2+ ions were further reduced by 63.87 percent and > 99.9 percent from the produced water when the unmodified WMR powder and modified WMR biochar biosorbents were used respectively. Reducing Pb2+ ions concentration from their initial concentration of 0.036 mg/l to 0.013 mg/l and <0.01 mg/l by the unmodified WMR powder and modified WMR biochar biosorbents respectively.

# At pH value of 10.5 (alkaline medium), the Pb2+ ions were reduced by only 22.22 percent and 33.33 percent from the produced water when the unmodified WMR powder and modified WMR biochar biosorbents were used respectively. Reducing it, from their initial concentration of 0.036 mg/l to 0.028 mg/l and 0.024 mg/l by the unmodified WMR powder and modified WMR biochar biosorbents respectively.

Table 4.  Effect of pH on the Biosorption of Zn2+ (mg/L) on the WMR after 30minutes of filtration down the column.

| # BIOSORBENT | # Initial Zn conc. # In mg/L | # Zn Conc. at # pH of 2.6 | # Zn Conc. at # pH of 6.2 | # Zn Conc. at # pH of 10.5 |
| --- | --- | --- | --- | --- |
| # WMR # (Unmodified) | # 0.189 | # 0.171 # *(9.52%) | # 0.019 # *(90.00%) | # 0.101 # *(8.80%) |
| # WMR BIOCHAR # (Modified) | # 0.189 | # 0.165 # *(12.70%) | # < 0.01 # *(>99.00%) | # 0.093 # *(50.79%) |

# *(%) Bioadsorption/Removal of Zn2+ ions by the Biosorbent

# In table 4, (above) at a contact time of 30 minutes, we can observe as following: At pH 2.6 (an acidic medium), the Zn2+ ions was remove from the sample of produced water by 9.52 percent from 0.189 mg/l of its initial concentration to 0.171 mg/L with the unmodified watermelon rind powder as a bio-sorbent. At same pH of 2.6 (an acidic medium) the Zn2+ ions in the produced water was reduced by 12.7 percent, coming down to 0.165 mg/l from an initial concentration of 0.189 mg/l when the modified WMR (bio-char) was used as biosorbent. At pH value of 6.2, the Zn2+ ions were further reduced by 90.0 percent and >99.0 percent from the produced water when the unmodified WMR powder and modified WMR biochar biosorbents were used respectively. Reducing Zn2+ ions concentration from their initial concentration of 0.189 mg/l to 0.019mg/l and <0.01 mg/l by the unmodified WMR powder and modified WMR biochar biosorbents respectively.

# At pH value of 10.5 (alkaline medium), the Zn2+ ions were reduced by only 8.80 percent and 50.79 percent from the produced water when the unmodified WMR powder and modified WMR biochar biosorbents were used respectively. Reducing it, from their initial concentration of 0.189 mg/l to 0.101 mg/l and 0.093 mg/l by the unmodified WMR powder and modified WMR biochar biosorbents respectively

Table 5. Effect of pH on the Biosorption of Cu2+ (mg/L) on the WMR after 30minutes of filtration down the column.

| # BIOSORBENT | # Initial Cu conc. # In mg/L | # Cu Conc. at # pH of 2.6 | # Cu Conc. at # pH of 6.2 | # Cu Conc. at # pH of 10.5 |
| --- | --- | --- | --- | --- |
| # WMR # (Unmodified) | # 1.84 | # 1.51 # *(17.90%) | # 0.94 # *(48.91%) | # 1.62 # *(11.96%) |
| # WMR BIOCHAR # (Modified) | # 1.84 | # 1.43 # *(22.28%) | # 0.87 # *(52.72%) | # 1.60 # *(13.04%) |

# *(%) Bioadsorption/Removal of Cu2+ ions by the Biosorbent

# In table 5, (above) at a contact time of 30 minutes, we can observe as following: At pH 2.6 (an acidic medium), the Cu2+ ion was remove from the sample of produced water by 17.9 percent from 1.84 mg/l of its initial concentration to 1.62 mg/L with the unmodified watermelon rind powder as a bio-sorbent. At same pH of 2.6 (an acidic medium) the Cu2+ ion in the produced water was reduced by 22.28 percent, coming down to 1.60 mg/l from an initial concentration of 1.84 mg/l when the modified WMR (bio-char) was used as biosorbent. At pH value of 6.2, the Cu2+ ions were further reduced by 48.91 percent and 52.72 percent from the produced water when the unmodified WMR powder and modified WMR biochar biosorbents were used respectively. Reducing Cu2+ ions concentration from their initial concentration of 1.84 mg/l to 0.94mg/l and 0.87mg/l by the unmodified WMR powder and modified WMR biochar biosorbents respectively.

# At pH value of 10.5 (alkaline medium), the Cu2+ ions were reduced by only 11.96 percent and 13.04 percent from the produced water when the unmodified WMR powder and modified WMR biochar biosorbents were used respectively. Reducing it, from their initial concentration of 1.84 mg/l to 1.62 mg/l and 1.60mg/l by the unmodified WMR powder and modified WMR biochar biosorbents respectively.

# Table 6. The Effect of Contact time (minutes) on the Biosorption of selected heavy metals on the WMR (water melon rind) at a pH of 6.2, after filtration down the column.

| Selected Heavy Metal Ions | BIOSORBENT | INITIAL CONC. mg/L | CONC. mg/L AFTER 30 MINUTES FILTRATION | CONC. mg/L AFTER 60 MINUTES FILTRATION | CONC. mg/L AFTER 180 MINUTES FILTRATION |
| --- | --- | --- | --- | --- | --- |
| Cu2+ | WMR Powder (Unmodified) | 1.84 | 0.94 *(48.10%) | 0.98 *(46.79%) | 1.02 *(44.56%) |
|  | WMR Biochar (Modified) | 1.84 | 0.87 *(52.72%) | 0.89 *(51.63%) | 0.96 *(47.83%) |
| Pb2+ | WMR Powder (Unmodified) | 0.036 | 0.013 *(63.89%) | < 0.01 *(>99.90%) | < 0.01 *(>99.90%) |
|  | WMR Biochar (Modified) | 0.036 | < 0.01 *(>99.90%) | < 0.01 *(>99.90%) | < 0.01 *(>99.90%) |
| Cd2+ | WMR Powder (Unmodified) | 1.55 | 0.035 *(97.74%) | 0.024 *(98.45%) | 0.023 *(98.52%) |
|  | WMR Biochar (Modified) | 1.55 | 0.018 *(98.84%) | <0.01 *(>99.90%) | 0.012 *(99.23%) |
| Ni2+ | WMR Powder (Unmodified) | 2.04 | 1.14 *(44.12%) | 0.87 *(57.35%) | 0.74 *(63.73%) |
|  | WMR Biochar (Modified) | 2.04 | 0.98 *(51.96%) | 0.72 *(64.71%) | 0.55 *(73.04%) |
| Zn2+ | WMR Powder (Unmodified) | 0.189 | 0.019 *(89.95%) | 0.020 *(89.42%) | 0.019 *(89.95%) |
|  | WMR Biochar (Modified) | 0.189 | <0.01 *(>99.90%) | <0.01 *(>99.90%) | <0.01 *(>99.90%) |

# *(%) Biosorption/Removal of Metal ions by the Biosorbent with time

# From the Table 6, above, it could be seen that the optimal conditions of pH of 6.2 and contact of 30 minutes were most effective and efficient for application of both modified and unmodified WMR. Thus, Pb2+, Zn2+ and Cu2+ions require 30 minutes of contact time and at a pH of 6.2 using modified WMR biochar as Biosorbent for most efficient removal from the Produced water . Cadmium (Cd2+), at a pH value of 6.2 has a 60 minutes optimum Contact time for most efficient removal from the produced water using WMR biochar as the biosorbent. For Nickel (Ni2+), the biosorbent’s performance increases as contact time increases, meaning optimum contact time might be higher than 180 minutes at a pH value of 6.2. In all both the unmodified and modified WMR biosorbents were able to effectively and efficiently remove or remediate Pb2+, Zn2+ and Cu2+ions below the maximum permissible levels as prescribed by EGASPIN (2018), see Table 7, required for safe release of produced water to the environment all pH values and contact times used in experiment, but were unable to do so for Ni2+ ions at various pH values and contact times used in the experimental investigations. The optimum pH and contact time for remediation/removal of Cd2+ions in produced below the maximum permissible levels as prescribed by EGASPIN (2018) is 6.2 and 60 minutes respectively.

Table 7. Comparison of EGASPIN (2018), WHO (2017) Guideline Values for Selected Heavy Metals and Environmental implications

| Heavy Metals | EGASPIN (2018) Maximum Permissible Limit (mg/L) | WHO Drinking Water (2017) Guideline (mg/L) | Environmental Significance |
| --- | --- | --- | --- |
| Lead (Pb) | 0.05 | 0.01 | Highly toxic; causes neurological, renal and developmental disorders. |
| Cadmium (Cd) | 0.01 | 0.003 | Highly toxic and carcinogenic; accumulates mainly in the kidneys and bones. |
| Copper (Cu) | 1.5 | 2.0 | Essential micronutrient but toxic at elevated concentrations. |
| Nickel (Ni) | 0.5 | 0.07 | Causes allergic reactions, respiratory disorders and potential carcinogenic effects. |
| Zinc (Zn) | 5.0 | 3.0 | Essential trace element; excessive concentrations impair aquatic life and affect water taste. |

# Discussion

The efficiency of the performances of the unmodified WMR powder and modified WMR biochar in removing metal ions are as follows: Using Unmodified WMR powder at a pH value of 2.6 with contact time of 30 minutes.  For each of the heavy metals, we got; Cu2+: 1.51 mg/L (17.90%); Pb2+: 0.02 mg/L (41.67%); Cd2+: 0.75 mg/L (51.55%); Ni2+: 1.73 mg/L (15.20%) and Zn2+: 0.17 mg/L (9.52%). The following were the results for the modified WMR biochar at the same pH value, which was at 2.6 respectively contact time of 30 minutes: Cu2+: 1.43 mg/L (22.82%); Pb2+: 0.024 mg/L (33.33%); Cd2+: 0.823 mg/L (46.90%); Ni2+: 1.71 mg/L (16.17%) and Zn2+: 0.165 mg/L (12.70%)

When the pH value was adjusted to 6.2 at a constant contact time of 30 minutes, the following heavy metal ions concentrations were obtained using unmodified WMR powder: Cu2+: 0.94 mg/L(48.91%); Pb2+: 0.013 mg/L (63.87%); Cd2+: 0.035 mg/L (97.74%); Ni2+: 1.14mg/L (44.12%) and Zn2+: 0.019 mg/L (90.00%). At the same pH value (pH 6.2), utilizing the modified WMR biochar at a steady contact time of 30 minutes, the values were as follows; Cu2+: 0.87 mg/L (52.22%); Pb2+: <0.01 mg/L (>99.90%); Cd2+: 0.018 mg/L (98.84%); Ni2+: 0.98mg/L (51.96%) and Zn2+: <0.01 mg/L (>99.90%).

When the pH was further adjusted to 10.5 using unmodified WMR powder at a constant contact time of 30 minutes, the following heavy metal ion concentration values were obtained, which also reflected its percent removal: Cu2+: 1.62 mg/L (11.96%); Pb2+: 0.028 mg/L (22.22 %); Cd2+: 0.931 mg/L (39.94%); Ni2+: 1.88mg/L (7.84%) and Zn2+: 0.101 mg/L (8.80%). The following values were also obtained using the modified WMR biochar: Cu²: 1.60 mg/L (13.04%); Pb²: 0.024 mg/L (33.33 %); Cd²: 0.881 mg/L (43.16%); Ni²: 1.84 mg/L (9.80%) and Zn²: 0.093 mg/L (50.79%).

Based on the above values, it was observed that neither unmodified nor modified watermelon rinds performs well in the removal of heavy metals in the produced water at pH 2.6 at 30 minutes contact time because system is highly and strongly protonated (H+). The high concentration of strong H+ in the strong acidic media (pH < 3) leads to competition for the adsorption sites in watermelon rinds with the heavy metal ions. In the case when pH is 6.2 and with contact time of 30min, for the removal of heavy metal ions from the produced water, there were considerable removal of the metal ions and even optimum removal in certain cases like Cu2+, Pb2+ and Zn2+ in the produced water. The metal ions are not in competition with weak H+ for the biosorbent’s sorption site and moreso, the metal ions cannot form insoluble metal hydroxide at this pH.

After adjusting the solution to pH of 10.5, both modified WMR biochar and unmodified WMR powder showed decreased biosortion performance. This has due to precipitation of the heavy metals in the produced water as insoluble metal hydroxide in that alkaline media after 30 minutes of contact time. Also modified WMR biochar showed significant increase in biosorption ability compared to unmodified WMR powder.

In all pH values and contact times, the unmodified and modified WMR biosorbents were able to reduce Cu2+, Pb2+ and Zn2+ ions’ concentrations in the produced water to below the maximum limits set by WHO, 2017, safe drinking water. All above discussions are attributed due to increased number of sites in the surface, increase in the porosity of a modified material, high percentage of Carbon, Absence of oxygen-containing functional group and the higher bio sorption capacity of the biochar.

# Conclusions

This research conclusively proved watermelon rind particularly when modified to biochar as highly efficient, cheap, and environmentally friendly to be employed as biosorbent for the removal of heavy metals in production water. Based on the analysis of the result, optimal operational parameters that result in the highest efficiency in biosorption are: pH of 6.2, while the contact times are 30 minutes for Cu2+, Pb2+ and Zn2+ ions, contact time at 60 minutes for Cd2+  ions, and contact time 180 minutes for Ni2+ ions. The modified watermelon rind biochar was more efficiency when compare with the unmodified WMR powder.

The research solved two main environmental problems with a sustainable approach: cheap removal of heavy metals from the produced water, and value-added waste management of agricultural watermelon rind waste.

Competing interest

The authors hereby declare that there is no competing interest in this work

Declaration of AI Use

This manuscript was prepared through the combined contributions of all author(s), including contributions to the study design, data, content development, results, interpretation, and related scholarly work. The author(s) acknowledge the use of Grammarly and ChatGPT to assist with grammar checking, language refinement, reference formatting. These AI-assisted tools were not used as authors and did not replace the intellectual contributions or scholarly judgment of the author(s). All AI-assisted outputs, including content, references, and interpretations, were carefully reviewed, revised, verified, and approved by the author(s). The author(s) accept full responsibility for the accuracy, integrity, and final content of the manuscript.

References

Adekemi, B., John, M. A., Toyib, O., Omoniyi, O. O., Oluseun, K. I., & Augustine, O. E. (2025). Removal of zinc ion (Zn²⁺) from aqueous solution using watermelon rind (Citrillus lanatus). WebLog Journal of Analytical and Pharmaceutical Chemistry. https://doi.org/10.5281/zenodo.17411485

Ali, I., Asim, M., & Khan, T. A. (2012). Low cost adsorbents for the removal of organic pollutants from wastewater. Journal of Environmental Management, 113, 170–183. https://doi.org/10.1016/j.jenvman.2012.08.028

Chikwe T.N. & Iwuoha G. N. (2024). Physical and chemical treatment of produced water from crude oil to obtain injected water properties suitable for reservoir. Global scientific journals.12 (2): 794-813.

Fakhru'l-Razi, A., Pendashteh, A., Abdullah, L. C., Biak, D. R. A., Madaeni, S. S., & Abidin, Z. Z. (2009). Review of technologies for oil and gas produced water treatment. Journal of Hazardous Materials, 170(23), 530–551. https://doi.org/10.1016/j.jhazmat.2009.05.044

Igunnu, E. T., & Chen, G. Z. (2014). Produced water treatment technologies. International Journal of Low-Carbon Technologies, 9(3), 157–177. https://doi.org/10.1093/ijlct/cts049

Iwuoha, G. N & Onojake, M.C. (2016)  Bioaccumulation of Heavy Metals In Crustaceans From Oron Channel, Osung Area Oron-City, Akwa-Ibom, Nigeria. Journal of the Chemical Society of Nigeria. 41 (1): 94-98

Iwuoha, G.N. & Umofia, E (2017). Distribution of trace metals in parts of stock fish marketed in three markets around port Harcourt, Nigeria. Scientia Africana, 16 (2): 1-9

Iwuoha, G. N & Nkanga, T.S (2024). Effect of pH on the removal of metal ions associated with produced water on pulverized Oyster Shell (OS) as Adsorbent. Scientia Africana 23(5); 293-300 https://dx.doi.org/10.4314/sa.v23i5.23

Jiménez, S., Micó, M. M., Arnaldos, M., Medina, F., & Contreras, S. (2018). State of the art of produced water treatment. Chemosphere, 192, 186–208. https://doi.org/10.1016/j.chemosphere.2017.10.139

Neff, J. M., Lee, K., & DeBlois, E. M. (2011). Produced water: Overview of composition, fates, and effects. In K. Lee & J. M. Neff (Eds.), Produced water: Environmental risks and advances in mitigation technologies (pp. 3–54). Springer.

Nkanga, T.S, Iwuoha, G. N & Onojake, M.C.(2024). Effect of contact time on the sorption of metal ions associated with produced water on pulverized Oyster Shell (OS) as Adsorbent. Journal Global Ecology and Environment 20 (4); 136-145. DOI: 10.56557/jogee/2024/v20i48927

Onajake M.C., Iwuoha G. N & Osakwe J.O (2015) Banana peel as a low cost adsorbent for the removal of Ni2+, Cu2+ and Fe2+ from Industrial effluents Journal of the Chemical Society of Nigeria. 40 (2):  59-62.

Onojake, M. C., Ogbole, S. N., Osakwe, J. O. & Iwuoha G. N. (2021). Use Of Pulverized Oyster And Snail Shells In The Removal Of Heavy Metals From Hydrocarbon Contaminated Soils. Journal of Global Ecology and Environment 12(1): 35-43

Onojake, M.C., Ogbole, S.N. & Iwuoha G. N. (2021) Remediation Of Hydrocarbon Contaminated Soils Using Pulverized Oyster And Snail Shells. Journal of Global Ecology and Environment 12(1): 50-60

Onyango, C., Nyairo, W., Tchieta, G. P., & Shikuku, V. O. (2025). Watermelon rind based adsorbents for the removal of water pollutants: A critical review. Frontiers in Environmental Chemistry. https://doi.org/10.3389/fenvc.2025.1568695

Osu Charles Ikenna, Ugwu Henry Chimezie, & Iwuoha G. N. (2021). Use of novel and environmental friendly natural polymer and its Alumina Nano-composite synthesized from Rhynchophorus phoenicis in waste water treatment. American journal of polymer science and technology, 7(4): 57-63

Veil, J. A., Puder, M. G., Elcock, D., & Redweik, R. J. (2004). A white paper describing produced water from production of crude oil, natural gas, and coal bed methane. Argonne National Laboratory.

World  Health Organization. (2017). Guidelines for drinking-water quality (4th ed.). WHO Press.